Supplementary

NANOSTRUCTURED ZINC CARBONATE HYDROXIDE MICROFLAKES: ASSESSING THE TOXICITY AGAINST ERYTHROCYTES AND L929 CELLS IN VITRO

Volodymyr Prokopiuk1,2, Anatolii Onishchenko2, Yuliia Pazura3, Iryna Bespalova3, Umut Kökbaş4, Liliya Tryfonyuk5, Pavlo Mateychenko6, Kateryna Kot7, Saulesh Kurmangaliyeva8, Yurii Kot7*, Svitlana Yefimova3*, Anton Tkachenko2,9*

1Research Institute of Experimental and Clinical Medicine, Kharkiv National Medical University, 4 Nauky ave, 61022 Kharkiv, Ukraine

2Department of Cryobiochemistry, Institute for Problems of Cryobiology and Cryomedicine of the National Academy of Sciences of Ukraine, 23 Pereyaslavskaya st, 61015 Kharkiv, Ukraine

3Department of Nanostructured Materials, Institute for Scintillation Materials of the National Academy of Sciences of Ukraine, 60 Nauky ave, 61072 Kharkiv, Ukraine

4Medical Biochemistry Department, Nevsehir Haci Bektas Veli University, 2000 Evler Mah. Zübeyde Hanım Cad. 50300 / Nevşehir, Turkey

5Institute of Health, National University of Water and Environmental Engineering, 11 Soborna st, 33028 Rivne, Ukraine

6Institute for Single Crystals, National Academy of Sciences of Ukraine, 60 Nauky ave, 61072 Kharkiv, Ukraine

7Department of Biochemistry, V. N. Karazin Kharkiv National University, 4 Svobody sq, 61022 Kharkiv, Ukraine

8Department of Microbiology, Virology and Immunology, West Kazakhstan Marat Ospanov Medical University, 68 Maresyev st, 030012 Aktobe, Republic of Kazakhstan

9BIOCEV, First Faculty of Medicine, Charles University, Průmyslová 595, 25250 Vestec, Czech Republic

Table S1

The single cell Ca2+-specific fluorescence intensity in L929 cells incubated with ZnCH microflakes

| Concentrations of ZnCH microflakes | Fluorescence intensity, rfu/cell |
| --- | --- |
| 0 mg/L | 75.1 ± 6.2 |
| 2 mg/L | 83.9 ± 6.5 |
| 10 mg/L | 89.3 ± 6.8 |
| 25 mg/L | 127.5 ± 13.9, p < 0.01 |
| 50 mg/L | 168.7 ± 14.2, p < 0.001 |
| 100 mg/L | 215.3 ± 16.9, p < 0.001 |

Note: Kruskal-Wallis and Dunn’s tests, means ± SEM (n = 3); rfu – relative fluorescence units. p values provide comparison with the cells not exposed to ZnCH microflakes

Table S2

The single cell reactive nitrogen species (RNS)-specific fluorescence intensity in L929 cells incubated with ZnCH microflakes

| Concentrations of ZnCH microflakes | Fluorescence intensity, rfu/cell |
| --- | --- |
| 0 mg/L | 45.3 ± 9.7 |
| 2 mg/L | 72.8 ± 14.6 |
| 10 mg/L | 109.5 ± 16.2, p < 0.01 |
| 25 mg/L | 181.3 ± 16.8, p < 0.001 |
| 50 mg/L | 263.7 ± 19.1, p < 0.001 |
| 100 mg/L | 315.1 ± 19.8, p < 0.001 |

Note: Kruskal-Wallis and Dunn’s tests, means ± SEM (n = 3); rfu – relative fluorescence units. p values provide comparison with the cells not exposed to ZnCH microflakes

Table S3

The single cell ratiometric index (the ratio of liquid disordered phase-specific fluorescence intensity Fl red 633 nm to liquid ordered phase-specific fluorescence intensity Fl green 550 nm) in L929 cells treated with ZnCH microflakes

| Concentrations of ZnCH microflakes | Ratiometric index |
| --- | --- |
| 0 mg/L | 0.84 ± 0.12 |
| 2 mg/L | 1.07 ± 0.15 |
| 10 mg/L | 1.24 ± 0.18 |
| 25 mg/L | 2.80 ± 0.15, p < 0.001 |
| 50 mg/L | 3.27 ± 0.18, p < 0.001 |
| 100 mg/L | 3.69 ± 0.15, p < 0.001 |

Note: Kruskal-Wallis and Dunn’s tests, means ± SEM (n = 3); rfu – relative fluorescence units. p values provide comparison with the cells not exposed to ZnCH microflakes

Table S4

The single cell caspase-3-, caspase-8-, and caspase-9-specific fluorescence intensity in L929 cells exposed to ZnCH microflakes

| Concentrations of ZnCH microflakes | Fluorescence intensity, rfu/cell |  |  |
| --- | --- | --- | --- |
|  | Caspase-3 | Caspase-8 | Caspase-9 |
| 0 mg/L | 7.2 ± 5.5 | 9.4 ± 6.8 | 11.7 ± 5.3 |
| 2 mg/L | 8.9 ± 6.7 | 8.5 ± 6.2 | 13.1 ± 6.8 |
| 10 mg/L | 15.5 ± 8.9 | 72.5 ± 17.3, p < 0.01 | 19 ± 10.5 |
| 25 mg/L | 151.8 ± 11.7, p <0.001 | 186.1 ± 16.9, p < 0.001 | 173.5 ± 14.3, p < 0.001 |
| 50 mg/L | 192.6 ± 13, p < 0.001 | 242.5 ± 17.1, p < 0.001 | 239.1 ± 15.7, p < 0.001 |
| 100 mg/L | 237.3 ± 15.8, p < 0.001 | 281.3 ± 16.5, p < 0.001 | 270.9 ± 16.8, p < 0.001 |

Note: Kruskal-Wallis and Dunn’s tests, means ± SEM (n = 3); rfu – relative fluorescence units. p values provide comparison with the cells not exposed to ZnCH microflakes

Table S5

The single cell Ca2+-specific fluorescence intensity in erythrocytes exposed to ZnCH microflakes

| Concentrations of ZnCH microflakes | Fluorescence intensity, rfu/cell |
| --- | --- |
| 0 mg/L | 102.6 ± 7.5 |
| 20 mg/L | 118.3 ± 7.1 |
| 100 mg/L | 141.5 ± 7.3, p < 0.01 |
| 250 mg/L | 179.1 ± 9.5, p < 0.001 |
| 500 mg/L | 221.8 ± 11.3, p < 0.001 |

Note: Kruskal-Wallis and Dunn’s tests, means ± SEM (n = 3); rfu – relative fluorescence units. p values provide comparison with the cells not exposed to ZnCH microflakes

Table S6

The single cell reactive nitrogen species (RNS)-specific fluorescence intensity in erythrocytes treated with ZnCH microflakes

| Concentrations of ZnCH microflakes | Fluorescence intensity, rfu/cell |
| --- | --- |
| 0 mg/L | 28.3 ± 7.1 |
| 20 mg/L | 31.4 ± 12.7 |
| 100 mg/L | 77.9 ± 14.1, p < 0.001 |
| 250 mg/L | 165.2 ± 14.5, p < 0.001 |
| 500 mg/L | 223.5 ± 17.4, p < 0.001 |

Note: Kruskal-Wallis and Dunn’s tests, means ± SEM (n = 3); rfu – relative fluorescence units. p values provide comparison with the cells not exposed to ZnCH microflakes

Table S7

The single cell ratiometric index (the ratio of liquid disordered phase-specific fluorescence intensity Fl red 633 nm to liquid ordered phase-specific fluorescence intensity Fl green 550 nm) in red blood cells incubated with ZnCH microflakes

| Concentrations of ZnCH microflakes | Ratiometric index |
| --- | --- |
| 0 mg/L | 0.75 ± 0.10 |
| 20 mg/L | 1.01 ± 0.12 |
| 100 mg/L | 2.08 ± 0.15, p < 0.001 |
| 250 mg/L | 2.60 ± 0.18, p < 0.001 |
| 500 mg/L | 3.18 ± 0.15, p < 0.001 |

Note: Kruskal-Wallis and Dunn’s tests, means ± SEM (n = 3); rfu – relative fluorescence units. p values provide comparison with the cells not exposed to ZnCH microflakes

Table S8

The single cell caspase-3- and caspase-8-specific fluorescence intensity in erythrocytes incubated with ZnCH microflakes

| Concentrations of ZnCH microflakes | Fluorescence intensity, rfu/cell |  |
| --- | --- | --- |
|  | Caspase 3 | Caspase 8 |
| 0 mg/L | 11.5 ± 6.8 | 14.6 ± 5.3 |
| 20 mg/L | 15.3 ± 6.5 | 17.2 ± 6.9 |
| 100 mg/L | 54.9 ± 10.2, p < 0.001 | 66.8 ± 15.1, p < 0.001 |
| 250 mg/L | 127.1 ± 12.5, p < 0.001 | 131.5 ± 15.7, p < 0.001 |
| 500 mg/L | 175.7 ± 12.7, p < 0.001 | 178.4 ± 16.5, p < 0.001 |

Note: Kruskal-Wallis and Dunn’s tests, means ± SEM (n = 3); rfu – relative fluorescence units. p values provide comparison with the cells not exposed to ZnCH microflakes

Figure S1. ROS generation in L929 cells exposed to ZnCH microflakes. Dichlorofluorescein (DCF) fluorescence was normalized to control samples. Kruskal-Wallis and Dunn’s tests, Me and interquartile range (n = 3).

Figure S2. ROS production in mature erythrocytes treated with ZnCH microflakes. Dichlorofluorescein (DCF) fluorescence was normalized to control samples. Kruskal-Wallis and Dunn’s tests, Me and interquartile range (n = 3).

Figure S3. Percentage of cells with externalized phosphatidylserine (eryptotic cells) in erythrocytes exposed to ZnCH microflakes. Kruskal-Wallis and Dunn’s tests, Me and interquartile range (n = 3).