| Wavelength (nm) | Absorbance value |
| --- | --- |
| 350 | 0.97 |
| 400 | 1.12 |
| 450 | 0.81 |
| 500 | 0.72 |
| 550 | 0.64 |
| 600 | 0.57 |

Table 5.2.1 (b) - Absorbance value

| SI.NO. | 2θ, ° | d, Å |
| --- | --- | --- |
| 1 | 7.991 | 11.17 |
| 2 | 8 | 11 |
| 3 | 28.05 | 3.178 |
| 4 | 37.50 | 2.396 |
| 5 | 43.9 | 2.060 |
| 6 | 49.86 | 1.8275 |
| 7 | 65.457 | 1.4247 |

Table –5.2.2 (b) Peak list of X-Ray diffraction

| S.NO | Wavenumber (nm) | Band Assignment |
| --- | --- | --- |
| 1 | 669 | Al – O - Al |
| 2 | 877 |  |
| 3 | 1039 | C – O Stretching of Sodium Carbonate |
| 4 | 1170 |  |
| 5 | 1444 | O – H bending vibration of solvent water |
| 6 | 3449 | O – H Stretching vibration |

Figure 5.2.3 (b) - Assignment of FT-IR bands of alumina nano powder

| Concentration | Staphylococcus aureus |
| --- | --- |
| Control/standard | 18mm |
| 40µg/ml | 17mm |
| 60 µg/ml | 16mm |
| Control/standard | 34mm |
| 100 µg/ml | 19mm |
| 200 µg/ml | 20mm |

Table 5.3.1 (b) –Zone of inhibition against S. aureus

| Concentration | Klebsiella pneumonia |
| --- | --- |
| Control/standard | 12mm |
| 40µg/ml | 15mm |
| 60 µg/ml | 14mm |
| Control/standard | 12mm |
| 100 µg/ml | 17mm |
| 200 µg/ml | 22mm |

Table 5.3.1 (d) –Zone of inhibition against K. pneumonia

| Concentration | Pseudomonas aeruginosa |
| --- | --- |
| Control/standard | 30mm |
| 40µg/ml | 19mm |
| 60 µg/ml | 18mm |
| Control/standard | 41mm |
| 100 µg/ml | 21mm |
| 200 µg/ml | 24mm |

Table 5.3.1 (f) –Zone of inhibition against P. aeruginosa

| No of Bacteria | Pathogens used | Zone of Inhibition (%) |
| --- | --- | --- |
| 1 | Klebsiella pneumonia | 120mm |
| 2 | Pseudomonas aeruginosa | 130mm |
| 3 | Staphylococcus aureus | 110mm |

Table 5.4.1 (d) – Maximum Zone of inhibition (mm