Supporting Information

# Enhancing Lithium-Ion Battery Performance: Nano Al2O3 Film Deposition on High Mass Loading LiFePO4 Cathode Electrode Using Atomic Layer Deposition Technique

# Pejman Salimi *#, Gloria Gottardi,  William Gomes De Morais,  Ruben Bartali, Nadhira Laidani, and Edoardo Gino Macchi *

# Center for Sustainable Energy, Fondazione Bruno Kessler, via Sommarive 18, 38123.Trento, Italy

# * Corresponding authors

# # Current affiliation: Institute for Materials Research (imo-imomec), Hasselt University, Martelarenlaan 42, Hasselt BE3500, Belgium

Fig. S1. FESEM-EDS analysis on 5nm Al2O3 LFP electrode to find out the uniform distribution of the elements (Al- O).

Fig. S2. Galvanostatic discharge curve of the Li/LFP half cell, employing a different discharge cut-off voltage after fully charging the cell.

Fig S3. Bode plot of the cells with pristine and 5 nm Al2O3-coated LFP electrodes at DOD of 50%.

Fig S4. An equivalent circuit model used to fit and analyze the EIS data.

| Samples | Pristine LFP electrode |  |  |  |  |  | 5nm Al2O3-coated LFP electrode |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| DOD (%) | 17% | 33% | 50% | 67% | 83% | 100% | 17% | 33% | 50% | 67% | 83% | 100% |
| Re (Ω) | 5.2 | 8.9 | 8.3 | 13.8 | 16.8 | 11.4 | 7.8 | 5.3 | 5.4 | 5.6 | 5.7 | 5.8 |
| RCEI (Ω) | 66.2 | 60.5 | 64.1 | 59.8 | 53.2 | 63.1 | 58.6 | 56.6 | 55.8 | 56.9 | 57.9 | 58.5 |
| Rct (Ω) | 43.6 | 60.9 | 74.5 | 96.8 | 125.8 | 141.2 | 38.7 | 78.1 | 115.0 | 109.6 | 107.8 | 128.4 |
| Overall Resistance (Ω) | 115 | 130.3 | 146.9 | 170.4 | 195.8 | 215.7 | 105.1 | 140 | 176.2 | 172.1 | 171.4 | 192.7 |
| CCEI (F) ×10-6 | 0.10 | 0.25 | 0.21 | 0.49 | 0.84 | 0.45 | 4.6 | 2.1 | 2.7 | 2.3 | 2.9 | 2.5 |
| Cdl(F) ×10-3 | 1.4 | 2.0 | 2.6 | 3.0 | 3.1 | 2.9 | 3.2 | 1.7 | 1.7 | 2.7 | 2.4 | 1.9 |
| w (Ohm.s-1/2) | 7.5 | 9.5 | 17.2 | 30.1 | 35.6 | 184.2 | 8 | 10.4 | 19.7 | 31.4 | 53.5 | 195.4 |

Table 1. Numerical value of Resistance and capacitances obtained from the fitting of the EIS spectra at different states of lithiation for Pristine LFP electrode and 5nm Al2O3-coated LFP electrode.

Table S2. Lithium  ions diffusion coefficient obtained from EIS spectra as function of the DoD for both pristine and coated LFP.

| DoD (%) | Pristine LFP (cm2 s-1) | 5nm Al2O3-coated LFP electrode (cm2 s-1) |
| --- | --- | --- |
| 17 | 1.01638×10-11 | 8.93302×10-12 |
| 33 | 7.57681×10-12 | 6.32218×10-12 |
| 50 | 2.31035×10-11 | 1.76117×10-11 |
| 67 | 3.21312×10-11 | 2.95257×10-11 |
| 83 | 1.24364×10-10 | 5.50665×10-11 |
| 100 | 1.01466E×10-10 | 9.01674×10-11 |

Fig. S5. Lithium  ions diffusion coefficient obtained from EIS spectra as function of the DoD for both pristine and coated LFP.