Supplementary material

Bismuth-gold nanohybrid conjugated with a HEX-bound oligonucleotide; a novel nano photosensitizer to combat antimicrobial resistance

Figures of designed nanostructures

#### Supplementary Fig. S 1. the EBPP diagrams (based on concentration) Lin-T2, Lin-C2, and Lin-C1 oligonucleotide sequences, and their corresponding equilibrium concentration histogram; a) the equilibrium concentration histogram of 3 stated oligonucleotide sequences at concentrations of 15, 0.5, 1, 1.5 and 2 μM; b) the EBPP graph of the Lin-T2 at concentrations of 15, 0.5, 1, 1.5 and 2 μM; c) the EBPP diagram of the Lin-C2 at concentrations of 15, 0.5, 1, 1.5 and 2 μM; d) the EBPP diagram of the Lin-C1 at concentrations of 15, 0.5, 1, 1.5 and 2 μM.

a)

b)

c)

d)

#### Supplementary Fig. S 2: EBPP diagram (independent of concentration) of oligonucleotide sequences at temperatures of 25, 37 and 40°C and their free energy values: a), b) and c) EBPP diagram of Lin-T2 sequence and its corresponding free energy at temperatures of 25, 37 and 40°C respectively; d) and e) EBPP diagram of Lin-C2 sequence and its corresponding free energy at temperatures of 25 and 37°C, respectively; f) and g) EBPP diagram of Lin-C1 sequence and its corresponding free energy at temperatures of 25 and 37°C, respectively.

a)

b)

c)

d)

e)

f)

g)

Supplementary Fig. S 3. comparison of excitation and emission spectra of synthesized fluorophores. The vertical axis is the normalized fluorescence/absorbance intensity, based on arbitrary units (a.u.) and the horizontal axis is wavelength in nanometers (nm).

c)

f)

b)

g)

h)

e)

a)

d)

Supplementary Fig. S 4. investigating the effect of light and temperature of 40°C on the growth of untreated bacteria; a) E.coli and S.aureus bacteria under photostimulation and non-photostimulation conditions; b) E.coli and S.aureus bacteria under PTT conditions, non-photostimulation and 37°C temperature. The error bar in the results indicates standard deviation.

a)

b)

Supplementary Fig. S 5. BiAu performance under PDT and non-PDT conditions; a) antibacterial activity of BiAu against E.coli; b) antibacterial activity of BiAu against S.aureus. Error bar in both cases indicates standard deviation.

a)

b)

Supplementary Fig. S 6: concentrations with PDT effect in Lin-T1 and Lin-T2 sequences. E.coli: Lin-T1 sequence at 1.5 μM and Lin-T2 at 3 concentrations of 0.5, 1 and 1.5 μM.

S.aureus: Lin-T1 sequence at 3 concentrations of 0.5, 1 and 1.5 μM and Lin-T2 didn't have PDT effect at any concentration.

.

a)

b)

Supplementary Fig. S 6. antibacterial performance of Lin-T1 and Lin-T2 under PDT and non-PDT conditions; a) antibacterial activity of Lin-T1 against E.coli; b) antibacterial activity of Lin-T1 against S.aureus; c) antibacterial performance of Lin-T2 against E.coli; d) antibacterial performance of Lin-T2 against S.aureus. Error bar indicates standard deviation.

c)

d)

#### Supplementary Fig. S 7 presents the antibacterial performance of NCLin-T1 and NCLin-T2. The both NCs exhibited antibacterial activity against both gram-positive and gram-negative strains in all mentioned concentrations under PDT and non-PDT conditions. In non-PDT conditions, the antibacterial effect against gram-positive strain is more than gram-negative strain. NCLin-T1 has shown considerable PDT effect against E.coli at 1.5 μM.

Supplementary Fig. S 7. antibacterial performance of NCLin-T1 and NCLin-T2 under PDT and non-PDT conditions; a) antibacterial activity of NCLin-T1 against E.coli; b) antibacterial activity of NCLin-T1 against S.aureus; c) antibacterial activity of NCLin-T2 against E.coli; d) antibacterial activity of NCLin-T2 against S.aureus. Error bar indicates standard deviation.

a)

b)

c)

d)

Supplementary Fig. S 8: PDT effective concentrations of NCLin-C1 and NCLin-C2 nanostructures.

E.coli: NCLin-C1 and NCLin-C2 at concentrations of 1.5 and 1 μM, respectively.

S.aureus: NCLin-C1 at 3 concentrations of 1, 1.5 and 2 μM. NCLin-C2 didn't have PDT effect at any concentration.

Supplementary Fig. S 8. Antibacterial performance of NCLin-C1 and NCLin-C2 under PDT and non-PDT conditions; a) antibacterial activity of NCLin-C1 against E.coli; b) antibacterial activity of NCLin-C1 against S.aureus; c) antibacterial activity of NCLin-C2 against E.coli; d) antibacterial activity of NCLin-C2 against S.aureus. Error bar indicates standard deviation.

a)

b)

c)

d)

Supplementary Fig. S 9: PDT effective concentrations of Lin-C1 and Lin-C2 nanostructures.

E.coli: Lin-C1 and Lin-C2 sequences at concentrations of 2 and 1.5 μM, respectively.

S.aureus: Lin-C1 and Lin-C2 sequences at concentration of 2 μM.

Supplementary Fig. S 9. antibacterial performance of Lin-C1 and Lin-C2 under PDT and non-PDT conditions; a) antibacterial activity of Lin-C1 against E.coli; b) antibacterial activity of Lin-C1 against S.aureus; c) antibacterial activity of Lin-C2 against E.coli; d) antibacterial activity of Lin-C2 against S.aureus. Error bar indicates standard deviation.

a)

b)

c)

d)

#### Supplementary Fig. S 10 compares the antibacterial performance of BiAu@Lin-T1 with Lin-T1 and BiAu@Lin-T2 with Lin-T2. In the case of E.coli, the PDT efficacy of BiAu@Lin-T1 and BiAu@Lin-T2 nanostructures has been increased across all concentrations compared to Lin-T1 and Lin-T2, respectively. In S.aureus bacteria, a substantial increase in the antibacterial efficacy of Lin-T1 compared to BiAu@Lin-T1 was observed at all 4 concentrations. While BiAu@LinT2 exhibited enhanced antibacterial activity in the three concentrations of 1, 1.5, and 2 μM compared to Lin-T2.

Supplementary Fig. S 10. antibacterial performance of BiAu@Lin-T1 and BiAu@Lin-T2, as well as their comparison with Lin-T1 and Lin-T2 respectively, under PDT conditions; a) antibacterial performance of BiAu@Lin-T1 and Lin-T1 in E.coli; b) antibacterial performance of BiAu@Lin-T1 and Lin-T1 in S.aureus; c) antibacterial performance of BiAu@ Lin-T2 and Lin-T2 in E.coli; d) antibacterial performance of BiAu@Lin-T2 and Lin-T2 in S.aureus. Error bar indicates standard deviation.

a)

b)

c)

d)

#### Supplementary Fig. S 11 presents a comparison of the antibacterial activity of BiAu@Lin-T1 and BiAu@LinT2 with BiAu. In E.coli, both nanostructures had higher PDT performance than BiAu in all 4 concentrations. In S.aureus, it has been determined that both nanostructures had more antibacterial activity than BiAu in 3 concentrations of 1, 1.5 and 2 μM.

b)

d)

c)

a)

Supplementary Fig. S 11. the antibacterial performance of BiAu@Lin-T1 and BiAu@Lin-T2, as well as the comparison with BiAu, under PDT conditions; a) antibacterial performance of BiAu@Lin-T1 and BiAu in E.coli; b) antibacterial performance of BiAu@Lin-T1 and BiAu in S.aureus; c) antibacterial performance of BiAu@ Lin-T2 and BiAu in E.coli; d) antibacterial performance of BiAu@ Lin-T2 and BiAu on S.aureus. Error bar indicates standard deviation.

The antibacterial efficacy of NCLin-T1 and NCLin-T2 compared to the oligonucleotide sequences of Lin-T1 and Lin-T2, respectively, is presented in (Supplementary Fig. S 12). In E.coli, the NCLin-T1 at concentrations of 1.5 μM compared to Lin-T1 and NCLin-T2 at 3 concentrations of 1, 1.5 and 2 μM compared to Lin-T2 showed a considerable increase in PDT effect. In the S.aureus, the NCLin-T1 showed greater antibacterial activity than Lin-T1 at concentration of 1 μM and NCLin-T2 compared to Lin-T2 at concentrations of 1, 1.5 and 2 μM.

Supplementary Fig. S 12. the antibacterial performance of NCLin-T1 and NCLin-T2 and their comparison with Lin-T1 and Lin-T2 respectively under PDT conditions; a) antibacterial function of NCLin-T1 and Lin-T1 in E.coli; b) antibacterial function of NCLin-T1 and Lin-T1 in S.aureus; c) antibacterial function of NCLin-T2 and Lin-T2 in E.coli; d) antibacterial activity of NCLin-T2 and Lin-T2 in S.aureus. Error bar indicates standard deviation.

a)

b)

c)

d)

Supplementary Fig. S 13 depicts the antibacterial performance of NCLin-C1 and NCLin-C2, as well as their comparison with Lin-C1 and Lin-C2, respectively. In the case of E.coli, NCLin-C1 compared to Lin-C1 at concentration of 1.5 μM and NCLin-C2 compared to Lin-C2 at 3 concentrations of 1, 1.5 and 2 μM exhibited a substantial increase in PDT performance.
 In S.aureus, the NCLin-C2, compared to Lin-C2 at concentrations of 1.5 and 2 μM, exhibited more antibacterial PDT performance. Furthermore, the NCLin-C1 compared to Lin-C1 at concentration of 1.5 μM had more antibacterial PDT performance.

Supplementary Fig. S 13. antibacterial performance of NCLin-C1 and NCLin-C2 and their comparison with Lin-C1 and Lin-C2 respectively under PDT conditions; a) antibacterial activity of NCLin-C2 and Lin-C2 against E.coli; b) antibacterial activity of NCLin-C2 and Lin-C2 in S.aureus; c) antibacterial activity of NCLin-C1 and Lin-C1 against E.coli; d) antibacterial activity of NCLin-C1 and Lin-C1 against S.aureus. Error bar indicates standard deviation.

a)

b)

c)

d)

Antibacterial comparison under non-PDT conditions

#### Supplementary Fig. S 14 displays a comparative analysis of the antibacterial effect of BiAu@NCLin-T1 with BiAu@Lin-T1 and BiAu@NCLin-T2 with BiAu@Lin-T2 under non-PDT conditions.

E.coli: the BiAu@Lin-T1 compared to BiAu@NCLin-T1 at all 4 concentrations and BiAu@Lin-T2 compared to BiAu@NCLin-T2 at 3 concentrations of 0.5, 1.5 and 2 μM showed greater antibacterial effect. S.aureus: the BiAu@NCLin-T1 nanostructure compared to BiAu@Lin-T1 at all 4 concentrations and BiAu@NCLin-T2 nanostructure compared to BiAu@Lin-T2 at a concentration of 1.5 μM showed antibacterial performance.

Supplementary Fig. S 15 demonstrates the antibacterial effect of BiAu@Lin-T1 with Lin-T1 and BiAu@Lin-T2 with Lin-T2 under non-PDT conditions. E.coli: the BiAu@Lin-T1 compared to Lin-T1 illustrated a greater antibacterial activity at concentrations of 1.5 and 2 μM. The BiAu@Lin-T2 showed more antibacterial effect than Lin-T2 at 4 concentrations. S.aureus: the Lin-T1 compared to BiAu@Lin-T1 at 3 concentrations of 1, 1.5 and 2 μM. Lin-T2 showed better antibacterial performance than BiAu@Lin-T2 at all 4 concentrations.

Supplementary Fig.S 16 depicts a comparison of antibacterial activity of BiAu@Lin-T1 and BiAu@LinT2 nanostructures with BiAu in non-PDT mode. Both BiAu@Lin-T1 and BiAu@Lin-T2 demonstrated higher antibacterial performance in both gram-positive and gram-negative strains compared to BiAu.

Supplementary Fig. S17 illustrates the comparison of antibacterial performance of NCLin-T1 and NCLin-T2, respectively, compared to Lin-T1 and Lin-T2 in non-PDT mode. E. coli: the NCLin-T1 and NCLin-T2 showed more antibacterial effect than Lin-T1 and Lin-T2, respectively, at concentrations of 1.5 and 2 μM. While at the concentration of 0.5 μM. the antibacterial effect of Lin-T1 was higher than NCLin-T1. S.aureus: a considerable enhancement in antibacterial activity was sighted in the NCLin-T1 compared to Lin-T1 at concentrations of 0.5 and 1.5 μM. The NCLin-T2 displayed a substantial augmentation in antibacterial effect compared to Lin-T2 at all four concentrations.

Supplementary Fig. S 18 illustrates the antibacterial performance of NCLin-C1 and NCLin-C2 and their comparison with Lin-C1 and Lin-C2 respectively under non-PDT conditions.
 E.coli: it was exhibited that NCLin-C1 had a substantial increase in antibacterial effect compared to Lin-C1 at 3 concentrations of 1, 1.5 and 2 μM. While NCLin-C2 showed a considerable enhanced antibacterial activity compared to Lin-C2 across all four concentrations.
 S.aureus: the antibacterial effect of NCLin-C1 surpassed of Lin-C1 at a concentration of 2 μM. Moreover, NCLin-C2 illustrated improved antibacterial performance compared to Lin-C2 at concentrations of 1, 1.5 and 2 μM. While Lin-C1 compared to NCLin-C1 at 3 concentrations of 0.5, 1, and 1.5 μM has shown a substantial antibacterial increase.

Supplementary Fig. S 14. antibacterial performance of BiAu@NCLin-T1 and BiAu@NCLin-T2, as well as their comparison with BiAu@Lin-T1 and BiAu@Lin-T2 respectively, under non-PDT conditions; a) antibacterial performance of BiAu@NCLin-T1 and BiAu@Lin-T1 against E.coli; b) antibacterial performance of BiAu@NCLin-T1 and BiAu@Lin-T1 against S.aureus; c) antibacterial performance of BiAu@NCLin-T2 and BiAu@Lin-T2 against E.coli; d) antibacterial performance of BiAu@NCLin-T2 and BiAu@Lin-T2 against S.aureus. Error bar indicates standard deviation.

a)

b)

c)

d)

Supplementary Fig. S 15. antibacterial performance of BiAu@Lin-T1 and BiAu@ Lin-T2, as well as their comparison with Lin-T1 and Lin-T2 respectively under non-PDT conditions; a) antibacterial performance of BiAu@Lin-T1 and Lin-T1 against E.coli; b) antibacterial performance of BiAu@Lin-T1 and Lin-T1 against S.aureus; c) antibacterial performance of BiAu@Lin-T2 and Lin-T2 against E.coli; d) antibacterial performance of BiAu@Lin-T2 and Lin-T2 against S.aureus. Error bar indicates standard deviation.

a)

b)

c)

d)

Supplementary Fig. S 16. antibacterial performance of BiAu@Lin-T1 and BiAu@Lin-T2 and their comparison with BiAu under non-PDT conditions; a) antibacterial performance of BiAu@Lin-T1 and BiAu against E.coli; b) antibacterial performance of BiAu@Lin-T1 and BiAu against S.aureus; c) antibacterial performance of BiAu@Lin-T2 and BiAu against E.coli; d) antibacterial performance of BiAu@Lin-T2 and BiAu against S.aureus. Error bar indicates standard deviation.

a)

b)

c)

d)

Supplementary Fig. S 17. antibacterial performance of NCLin-T1 and NCLin-T2 and their comparison with Lin-T1 and Lin-T2 respectively under non-PDT conditions; a) antibacterial activity of NCLin-T1 and Lin-T1 against E.coli; b) antibacterial activity of NCLin-T1 and Lin-T1 against S.aureus; c) antibacterial activity of NCLin-T2 and Lin-T2 against E.coli; d) antibacterial activity of NCLin-T2 and Lin-T2 against S.aureus. Error bar indicates standard deviation.

a)

b)

c)

d)

Supplementary Fig. S 18. antibacterial performance of NCLin-C1 and NCLin-C2 and their comparison with Lin-C1 and Lin-C2 respectively under non-PDT conditions; a) antibacterial activity of NCLin-C2 and Lin-C2 in E.coli; b) antibacterial function of NCLin-C2 and Lin-C2 in S.aureus; c) antibacterial function of NCLin-C1 and Lin-C1 in E.coli; d) antibacterial activity of NCLin-C1 and Lin-C1 in S.aureus. Error bar indicates standard deviation.

a)

b)

c)

d)

Supplementary Fig. S 19 comparison of antibacterial performance of BiAu@NCLin-T2, BiAu and Lin-T2 nanostructures under PTT and PDT conditions; a) antibacterial performance of BiAu@NCLin-T2 against E.coli; b) antibacterial activity of BiAu against E.coli; c) antibacterial activity of Lin-T2 against E.coli; d) antibacterial performance of BiAu@NCLin-T2 against S.aureus; e) antibacterial activity of BiAu against S.aureus; f) antibacterial activity of Lin-T2 against S.aureus. Error bar indicates standard deviation.

e)

a)

b)

c)

d)

f)

The PTT effect of BiAu@NCLin-T2, BiAu, and Lin-T2 was investigated under temperature conditions of 40°C. BiAu@NCLin-T2 and BiAu exhibited increased antibacterial activity at 40°C compared to 37°C against both gram-positive and gram-negative bacterial strains in PDT conditions, (Supplementary Fig. S 19). Lin-T2 exhibited more excellent antibacterial performance against gram-negative bacteria (at all 4 concentrations) and gram-positive bacteria (at the concentration of 2 μM) at 40°C compared to 37°C under PDT states. According to the stability analysis and computational analysis, this sequence maintains its stability with increasing temperature.

Supplementary Fig. S 20. The comparison of the antibacterial performance of BiAu@NCLin-T1 in E.coli and S.aureus, under non-PDT conditions.. The error bar indicates the standard deviation.

The length of Lin-T2

Considering that AgNC is synthesized with 12 C nucleobases, the space between 5ʹHEX and AgNC is filled with 3 T nucleobases. The length of each nucleobase is 0.676 nm (Its reference is mentioned below [Ref]). Consequently, the calculated length of the designed oligonucleotide sequence (Lin-T2) with 24 nucleobases is 16.224 nm. The length of 3 nucleobase T, which is located between 5'HEX and AgNC, measures 2.028 nm, which falls below 10 nm.

[Ref] Roth, E., Glick Azaria, A., Girshevitz, O., Bitler, A. & Garini, Y. Measuring the Conformation and Persistence Length of Single-Stranded DNA Using a DNA Origami Structure. Nano Lett. 18(11):6703-6709. 10.1021/acs.nanolett.8b02093 (2018).