Supplementary Information for

Direct observation of layer skyrmions in twisted WSe2 bilayers

Fan Zhang1†, Nicolás Morales-Durán1†, Yanxing Li1†, Wang Yao2, Jung-Jung Su3, Yu-Chuan Lin4,5, Chengye Dong4, Xiaohui Liu1, Fu-Xiang Rikudo Chen1, Hyunsue Kim1, Kenji Watanabe6, Takashi Taniguchi6, Xiaoqin Li1, Joshua A. Robinson4, Allan H. Macdonald1*, and Chih-Kang Shih1*

1Department of Physics, University of Texas at Austin, Austin, TX, USA

2Department of Physics, The University of Hong Kong, Hong Kong, China

3Department of Electrophysics, National Yang Ming Chiao Tung University, Hsinchu, Taiwan

4Department of Materials Science and Engineering, Pennsylvania State University, University Park, PA, USA

5Department of Materials Science and Engineering, National Yang Ming Chiao Tung University, Hsinchu, Taiwan

6Research Center for Materials Nanoarchitectonics, National Institute for Materials Science, Tsukuba, Japan

†These authors contribute equally to this work.

*Corresponding authors’ email: macdpc@physics.utexas.edu; shih@physics.utexas.edu

Figure S1 | Angle distribution of WSe2 flakes in MOCVD grown WSe2/Graphene sample. a, A typical AFM image of the MOCVD grown WSe2/Graphene sample showing monolayer, bilayer and twisted bilayers WSe2 flakes. b, LEED measurement of the sample. c, Dotted and fitted gaussian profile showing there is angle distribution indicating existence of twisted bilayers.

Figure S2 | Large scale STM images of 5.1-degree twist moiré region. a, Large scale STM image showing the ~5.1-degree twist between R stacked flakes with moiré region indicated. b, Zoom-in STM image showing the moiré pattern with a periodicity of 3.7 nm

Figure S3 | Optical image of 4.2-degree twisted tear-and-stack WSe2 sample. The twisted WSe2 bilayer/graphite/hBN/Si structure is made using the exfoliation and stack method with each individual material flake marked with different colors in the image.

Figure S4 | Gamma valley moiré modulation in a 4.2-degree twisted tear-and-stack WSe2 sample. a, Topography b, Constant-height STS color map along AA-MX-Br-XM-AA. c-f, dI/dV mappings obtained at different bias as labeled in each panel. (I = 100 pA). Scale bar: 5nm.

Figure S5 | Constant height conductivity image of 4.2-degree twisted WSe2 at K valley. a, Constant height dI/dV images at (Vs= −0.85 V, I = −100 pA) b, Filtered dI/dV image by removing the Bragg peak in the FFT of a. Scale bar: 2nm. c, averaged line profile and standard deviation of 5 different lines along the AA-XM-Br-MX-AA symmetric sites. For line profiles with uneven AA site intensities, they were symmetrized by multiplying position dependent linear coefficient and then renormalized with the intensity of AA site set as 1.

Figure S6 | The change of tip-to-sample-distance (∆Z) of 5.1-degree twisted WSe2 at K valley. a, Z–V spectroscopies respectively from sites AA, MX, Br and XM. (Iint = −100 pA) b, The change of tip-to-sample-distance (∆Z) as marked by the colored arrows in a for sites AA, XM, Br, MX are estimated to be 1.08 Å, 0.79 Å, 0.88 Å and 0.92 Å. This ∆Z difference among four sites directly reflect the K valley density of states difference, with highest density of state at AA site and lowest at MX site, which is consistent with the CC-STS measurements at K valley.

Figure S7 | Large-scale CHSTS and ZV spectra at high symmetry sites in the moiré superlattice of 5.1-degree twisted WSe2. a, Large scale constant height STS (Vint = −2.2 V, I = −100 pA and Vamp = 30 mV) and b, Z–V and c, (∂Z/∂V)I spectroscopies respectively from sites AA, MX, Br and XM. (Iint = −100 pA) The red dashed line in b marks the transition from G valley to K valley and the black dashed line marks the transition from K valley to graphene state.

Figure S8 | dI/dV mapping of 5.1-degree twisted WSe2 at the G valley. a-b, Topography and constant height dI/dV images at (Vs= −1 V, I = −40 pA), which is inside the Gamma valley. c, Filtered dI/dV image by removing the Bragg peak in the FFT of b. Scale bar: 1nm.

Figure S9 | Topography and constant current conductivity image of the same region of 5.1-degree twisted WSe2 in Figure 3d-e. a-b, Topography and constant current dI/dV images at (Vs= −0.85 V, I = −40 pA) c, Filtered dI/dV image by removing the Bragg peak in the FFT of b. The relative intensity between different sites agrees well with constant height dI/dV shown in Fig. 3e. Scale bar: 1nm.

Supplementary Note 1

Azimuthal components of the layer pseudospin

For the layer pseudospin, the z-component is a physical observable carrying electrical polarization (therefore measurable using STS).  The azimuthal component, which corresponds to the phase difference between electrons in different layers, is not directly measurable by STS.   In our work, we map the measured LDOS texture to the full-layer pseudospin texture through the parameterized continuum model whose parameters are determined via fitting the experimentally determined LDOS texture.

Note that the layer pseudospin is fundamentally different from the valley pseudospin recently discussed by Liu et al (DOI: 10.1126/science.abm3770) concerning intervalley coherence in graphene at zero Landau Level (ZLL). There, the K-states exist in A-sublattice and K’- states in B-sublattice.  Thus, the inter-valley pseudo-spin is directly reflected by atomic scale contrast in A-B sublattices.  Intervalley coherence means that there is macroscopic coherence between valleys K and -K=K’ that gives rise to an interference pattern that varies in space like Vexp(iφ)expiK-K'∙r. Since K and K’ are on the valley corners this gives rise to a periodicity pattern that varies over a three sublattice unit cell.  The length scale that depicts the spatial variation of the coherence order parameter is much larger, thus it can be measured locally at each point in space.  Unfortunately, such a scenario does not exist for the layer pseudospin discussed in our case.

Figure S10 | The evolution of fitting error function f= Iexpriment-Itheory as a function of iterations and as a function of some of the continuum model parameters (Vm, ψ, ω). a, error evolves as a function of the number of iterations b, f as a function of ψ, ω with a fixed Vm=13.6 meV, c, f as a function of Vm, ψ with a fixed ω = 10.0 meV. The yellow star marks the position in the parameter space where f is minimized.

Figure S11 | Obtaining continuum model parameters from STS of 4.2-degree twisted WSe2. a, Fit of the position-dependence of the layer-weighted LDOS near KVBM. The black solid and purple dashed lines are respectively experiment and theoretical fit. The continuum parameters extracted from the fitting: Vm=7.0 meV, ψ=90.1 degrees, ω=24.4 meV and meff=0.6m0. b, Moiré band-structure calculated with parameters obtained by fitting conductivity profile data along the high symmetry direction AA-XM-Br-MX-AA. The faint blue energy window marked where the theoretical LDOS curve in a is obtained. c, Layer-field Δ with arrows corresponding to the x and y components and color-scale corresponding the z component. Black dots indicate moiré superlattice AA sites.

Figure S12 | Relationship between Chern number of the topmost moiré band and position-dependent LDOS. a, Topological phase diagram of the topmost moiré band. b-c, Position-dependent LDOS profiles (dashed lines) for different values of the continuum model parameter: red dashed line (ψ=49.1 degree, Vm=13.6 meV, ω=10 meV), pink dashed line (ψ=49.1 degree, Vm=13.6 meV, ω=5 meV); green dashed line (ψ=150 degree, Vm=13.6 meV, ω=10 meV), light green dashed line (ψ=150 degree, Vm=13.6 meV, ω=5 meV) as marked by colored stars in a.