Supporting information

Enzymatic modification of cellulose nanofibers to enhance thermal resistance and hydrophobicity

Akihiro Hideno* a, b), Junpei Nouta b), Daiki Yokota b)

aPaper Industry Innovation Center, Ehime University, bCourse of paper industry, Department of Industrial Innovation, Faculty of Collaborative Regional Innovation, Ehime University

E-mail: hideno.akihiro.mx@ehime-u.ac.jp

Figure S1

The amounts of reducing-ends glucose units in commercial CNFs

(a) BiNFi-s AMa; (b) BiNFi-s FMa; (c) BiNFi-s BMa; (d) BiNFi-s Ima;

(e) Rheocrysta

Measurement of reducing-ends glucose unit (Hideno, 2020)

The number of moles of reducing-end glucose residue/g sample was determined with a modified 2,2'-bicinchoninate (BCA) method (Zhang and Lynd 2005) based on the previous report (Hideno, 2020). Each sample of CNFs was mixed with 800 L of pure water and added to 800 L of BCA reagent. The mixture was incubated at 75 °C for 30 min and then centrifuged at approximately 20,000 × g for 1 min. The supernatant was analyzed at 560 nm using a spectrophotometer (U-1900, Hitachi High-Technologies Corporation, Tokyo, Japan). A standard curve was plotted using a glucose as the reference. The absorbance was converted to reducing-end glucose units (mmol/g).

Zhang YHP, and Lynd LR (2005) Determination of the number-average degree of polymerization of cellodextrins and cellulose with application to enzymatic hydrolysis. Biomacromolecules 6: 1510-1515. DOI: 10.1021/bm049235j

Hideno A (2020) Thermogravimetric Analysis-based Characterization of Suitable Biomass for Alkaline Peroxide Treatment to Obtain Cellulose and Fermentable Sugars. BioResources 15: 6217-6229. DOI: 10.15376/biores.15.3.6217-6229