# Supporting information

Formic acid dehydrogenation using Ruthenium-POP pincer complexes in ionic liquids

Alexander Tobias Nikol1, Brenda Rabell1, René Wugt Larsen1 & Martin Nielsen1

1) Department for Chemistry, Technical University of Denmark (DTU), 2800 Kongens Lyngby, Denmark, Email: marnie@kemi.dtu.dk

# General Information

All syntheses, unless otherwise stated, were performed under inert gas conditions using standard Schlenk or glovebox techniques. Ligand precursors were commercially achieved and used without further purification or synthesized according to established protocols[1-3]. Solvents were deoxygenated by argon bubbling and dried from water impurities by the use of an Inert Puresolv solvent purification system or by distillation over sodium/benzophenone followed by three cycles of freeze-pump-thaw. Ionic liquids were commercially acquired and used without further purification.

# Instrumentation

Nuclear Magnetic Resonance spectroscopy (NMR)

NMR spectra were obtained using a Bruker Ascend 400, 600 or 800 MHz spectrometer equipped with BBFO and TCI CryoProbe probes. Chemical shifts are expressed in ppm relative to tetramethylsilane (TMS) for 1H and 13C spectra using residual solvent signal peaks or TMS as internal reference. For 31P spectra, values are expressed in ppm relative to H3PO4. Residual solvent chemical shifts are explained according to literature[4]. Coupling constants, if available, are given in Hz as absolute values. Multiplicities are given as singlets (s), dublets (d), triplets (t), quartets (q) and multiplets (m). Literature-known compounds were analyzed only using 1H-NMR spectroscopy to confirm purity. NMR spectra were analysed using MestReNova software.

Single-Crystal X-ray diffraction (SC-XRD)

All crystals were submerged in polybutene oil (Sigma, > 90%) as protection against oxidation and hydrolysis by air. Suitable crystals were identified using light microscopy and harvested with a MiTeGen cryo loop. They were mounted on a 5-axis goniometer attached to a Rigaku SuperNova dual source CCD-diffractometer. The measurements were conducted at 120 K using either Mo Kα or Cu Kα radiation. Structures were solved using Olex2[5] equipped with SHELXT[6] software using intrinsic phasing and refined to completion using SHELXL employing least square minimizations against F2. Thermal ellipsoids are printed at 70% probability. All depictions follow the following colour code: Hydrogen white, carbon grey, oxygen red, phosphorous purple, chlorine dark green, ruthenium dark blue.

Elemental Analysis (EA)

Elemental Analysis (EA, CHN analysis) was performed by Mikroanalytisches Laboratorium Kolbe in Oberhausen, Germany.

Infrared Spectroscopy (ATR-IR)

Solid-state attenuated total reflectance Fourier transform infrared (ATR-FTIR) spectroscopy was performed employing a VERTEX 80 vacuum Fourier transform spectrometer from Bruker Optics GmbH equipped with a Germanium-coated KBr beam splitter, a LN2-cooled HgCdTe detector and globar radiation source. The solid samples were brought in contact with a Germanium ATR crystal of a single-reflection ATR accessory from PIKE Technologies, Inc., which in contrast to a conventional diamond ATR crystal is highly transparent in the important spectral region of the Ru-H stretching fundamental transitions around 2000 cm-1. Blocks of 300 co-added scans with a spectral resolution of 2 cm-1 were collected both with the sample and of the cleaned ATR crystal before and after sample measurements. Minor traces of residual water vapor absorption were subtracted and gentle corrections for baseline drifts were introduced before the final application of extended ATR corrections compensating for the wavelength-dependent penetration depth of the infrared probe beam into the sample.

Gas chromatography (GC)

GC-TCD measurements were taken on an Agilent Technologies 6890M Network GC system.

# Catalyst synthesis

The metal precursor [RuHCl(PPh3)3]•toluene, the iPr-DBFphos ligand, and Ru-1 were synthesized according to previously established protocols[7-9]. The protocol established for Ru-1 was applied for the synthesis of Ru-2.

[RuHCl(iPr-DBFphos)(PPh3)] Ru-2

In a 50 mL Schlenk flask, iPr-DBFphos (46.2 mg, 0.115 mmol, 1.1 eq.) and [RuHCl(PPh3)3]•toluene (106.4 mg, 0.105 mmol, 1.0 eq.) were dissolved in dry THF (15 mL) and refluxed for four hours. A colour change from dark purple to orange was observed. The mixture was allowed to cool to room temperature and the solvent was removed in vacuo. The crude product was freeze-dried from benzene and obtained as an orange powder. It was washed with hexane (3 times 12 mL), dried in vacuo overnight and obtained as a yellow solid in quantitative yield. Crystals of sufficient quality for XRD can be grown by crystallization from THF/diethyl ether, toluene/diethyl ether or toluene/hexane using the gas diffusion method at -30 °C or from benzene/hexane using the gas diffusion method at room temperature.

1H NMR (400 MHz, C6D6, 298 K, ppm) δ 8.49 (t, J = 9.7 Hz, 6H), 7.47 (d, J = 7.6 Hz, 2H), 7.40 (d, J = 7.5 Hz, 2H), 7.20 (d, J = 7.6 Hz, 6H), 7.07 (t, J = 7.4 Hz, 3H), 7.01 (t, J = 7.6 Hz, 2H), 2.04 – 1.93 (m, 2H), 1.64 – 1.54 (m, 6H), 1.16 – 1.09 (m, 8H), 0.95 – 0.81 (m, 12H), -16.80 (dt, J = 28.6, 22.0 Hz, 1H, RuH).

13C NMR (101 MHz, C6D6, 298 K, ppm) δ 161.20, 141.71 (d, J = 39.9 Hz), 135.80 (d, J = 9.5 Hz), 129.11, 128.89, 127.20 (d, J = 8.9 Hz), 124.59, 123.32, 123.08 (t, J = 3.0 Hz), 120.78 (t, J = 7.5 Hz), 28.41 (t, J = 12.1 Hz), 26.06 (t, J = 6.4 Hz), 22.01, 19.79 (t, J = 2.5 Hz), 19.30, 19.03 (t, J = 4.4 Hz).

31P{1H} NMR (162 MHz, C6D6, 298 K, ppm): δ 73.22 (t, 2JPP = 27.8 Hz, 1P, PPh3), 58.97 (d, 2JPP = 27.4 Hz, 2P, iPr-DBFphos).

IR (ATR, Germanium, cm-1): 3051, 2980, 2956, 2924, 2868, 2054, 1481, 1477, 1468, 1436, 1431, 1417, 1401, 1382, 1238, 1223, 1086, 1029, 884, 836, 769, 753, 750, 739, 701, 682, 648, 629, 618, 549, 546, 541, 532, 515, 506, 485, 459.

EA Calcd. (%) for C42H50ClOP3Ru (800.30) C 63.03, H 6.30, found C 62.91, H 6.35.

Supplementary Figure 1: 400 MHz 1H NMR spectrum of Ru-2 in C6D6 at 25 °C.

Supplementary Figure 2: 101 MHz 13C NMR spectrum of Ru-2 in C6D6 at 25 °C.

Supplementary Figure 3: 162 MHz 31P{1H} NMR spectrum of Ru-2 in C6D6 at 25 °C.

Supplementary Figure 4: ATR-IR spectrum of Ru-2.

Supplementary Table 1: Crystallographic data for Ru-2.

|  | [RuHCl(iPr-dbfphos)(PPh3)] Ru-2 |
| --- | --- |
| Empirical formula | C48H56ClOP3Ru |
| Formula weight | 878.418 |
| Temperature/K | 120.00(16) |
| Crystal system | triclinic |
| Space group | P-1 |
| a/Å | 10.9901(2) |
| b/Å | 11.9981(2) |
| c/Å | 16.9442(2) |
| α/° | 100.981(1) |
| β/° | 91.241(1) |
| γ/° | 97.890(1) |
| Volume/Å3 | 2179.97(6) |
| Z | 2 |
| ρcalcg/cm3 | 1.344 |
| μ/mm-1 | 4.797 |
| F(000) | 921.0 |
| Crystal size/mm3 | 0.225 × 0.062 × 0.062 |
| Radiation | Cu Kα (λ = 1.54184) |
| 2Θ range for data collection/° | 5.32 to 153.06 |
| Index ranges | -13 ≤ h ≤ 13, -15 ≤ k ≤ 14, -21 ≤ l ≤ 20 |
| Reflections collected | 46550 |
| Independent reflections | 9080 [Rint = 0.0397, Rsigma = 0.0286] |
| Data/restraints/parameters | 9080/0/499 |
| Goodness-of-fit on F2 | 1.037 |
| Final R indexes [I>=2σ (I)] | R1 = 0.0253, wR2 = 0.0608 |
| Final R indexes [all data] | R1 = 0.0273, wR2 = 0.0624 |
| Largest diff. peak/hole / e Å-3 | 0.65/-0.76 |

# Catalytic protocols

In an inert gas glovebox, a 50 mL two-neck flask equipped with a stir bar and a nitrogen adapter was charged with the ruthenium complex (13.0 µmol, 0.1 mol%), sealed with a stopper and brought outside. It was connected to an air-cooled reflux condenser and BMIM OAc (1.0 mL, 5.35 mmol, 0.4 eq.) was injected via a syringe through a septum. The mixture was stirred and heated to the desired temperature. Formic acid (FA, 0.50 mL, 13.25 mmol, 1.0 eq.) was injected via syringe through a septum. Immediate gas formation of CO2 and H2 as well as a colour change was observed and the mixture was kept stirring at a constant temperature for 3 h, during which multiple samples for NMR analysis were taken via syringe through the septum.

To calculate conversions, the 1H NMR signal of the methyl group on the BMIM cation (peak e) was integrated to three times the molar amount of BMIM. Then, the formate signal was integrated, and divided by the injected amount of FA. An example of this can be found below with 5.35 mmol BMIM OAc and 13.25 mmol of FA. All NMRs were taken at room temperature on a 400 MHz Bruker Ascend spectrometer using acetonitrile-d3 as solvent.

Supplementary Figure 5: Example 400 MHz 1H NMR of FA dehydrogenation using BMIM OAc in d3-MeCN, showing 30% conversion (9.21 mmol of 13.25 mmol FA remaining).

The turnover frequencies were calculated using the following formula:

TOF=n (FA)Startn (catalyst)×conversion×1t [h]

For the time of TOFmax, the timeframe was chosen in which the conversion per unit time was highest (i.e where the conversion/timeline was the steepest).

Supplementary Table 2: Temperature screening of [RuHCl(PPh3)3]•toluene.

| T [°C] | Conversion [%] |  |  |  |  | TOFoverall [h-1] | TOFmax [h-1] (time interval [min]) |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | 10 min | 30 min | 60 min | 120 min | 180 min |  |  |
| 90 | 56 | 78 | 87 | 94 | 97 | 330 | 3424 (0-10) |
| 80 | 24 | 51 | 72 | 84 | 91 | 309 | 1467 (0-10) |
| 70 | 18 | 43 | 65 | 81 | 88 | 299 | 1101 (0-10) |
| 60 | 6 | 29 | 40 | 59 | 65 | 221 | 703 (10-30) |

Conditions: 0.5 mL (13.25 mmol) FA, 1.0 mL (5.35 mmol) BMIM OAc, 13.2 mg (13 µmol, 0.1 mol%) [RuHCl(PPh3)3]•toluene.

Supplementary Table 3: Arrhenius plot data of FA dehydrogenation using [RuHCl(PPh3)3]•toluene.

| T [°C] | 1/T [K-1] | TOFmax [h-1] | ln (TOFmax) |
| --- | --- | --- | --- |
| 90 | 0.00275 | 3424 | 8.14 |
| 80 | 0.00283 | 1467 | 7.29 |
| 70 | 0.00291 | 1101 | 7.00 |
| 60 | 0.003 | 703 | 6.56 |

Supplementary Figure 6: Arrhenius plot of FA dehydrogenation using [RuHCl(PPh3)3]•toluene

Slope= -6063.17
EA =50.4 kJ mol-1

Supplementary Table 4: Temperature screening of Ru-1.

| T [°C] | Conversion [%] |  |  |  |  |  | TOFoverall [h-1] | TOFmax [h-1] (time interval [min]) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 10 min |  | 30 min | 60 min | 120 min | 180 min |  |  |
| 90 | 74 |  | 90 | 93 | 96 | 98 | 333 | 4525 (0-10) |
| 80 | 14 |  | 79 | 87 | 92 | 96 | 326 | 1988 (10-30) |
| 70 | 23 |  | 73 | 85 | 90 | --- | 458 | 1529 (10-30) |
| 60 | 0 |  | 0 | 12 | 79 | 83 | 281 | 682 (60-120) |

Conditions: 0.5 mL (13.25 mmol) FA, 1.0 mL (5.35 mmol) BMIM OAc, 12.7 mg (13 µmol, 0.1 mol%) Ru-1.

Supplementary Table 5: Arrhenius plot data of FA dehydrogenation using Ru-1.

| T [°C] | 1/T [K-1] | TOFmax [h-1] | ln (TOFmax) |
| --- | --- | --- | --- |
| 90 | 0.00275 | 4525 | 8.42 |
| 80 | 0.00283 | 1988 | 7.59 |
| 70 | 0.00291 | 1529 | 7.33 |
| 60 | 0.003 | 682 | 6.53 |

Supplementary Figure 7: Arrhenius plot of FA dehydrogenation using Ru-1.

Slope= -7181.91
EA = 59.7  kJ mol-1

Supplementary Table 6: Temperature screening of Ru-2.

| T [°C] | Conversion [%] |  |  |  |  |  | TOFoverall [h-1] | TOFmax [h-1] (time interval [min]) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 10 min |  | 30 min | 60 min | 120 min | 180 min |  |  |
| 90 | 60 |  | 89 | 99 | --- | --- | 1009 | 3669 (0-10) |
| 80 | 24 |  | 76 | 83 | 92 | 96 | 326 | 1590 (10-30) |
| 70 | 0 |  | 42 | 80 | 86 | 86 | 292 | 1284 (10-30) |
| 60 | 0 |  | 9 | 31 | 78 | 79 | 268 | 479 (60-120) |

Conditions: 0.5 mL (13.25 mmol) FA, 1.0 mL (5.35 mmol) BMIM OAc, 10.4 mg (13 µmol, 0.1 mol%) Ru-2.

Supplementary Table 7: Arrhenius plot of FA dehydrogenation using Ru-2.

| T [°C] | 1/T [K-1] | TOFmax [h-1] | ln (TOFmax) |
| --- | --- | --- | --- |
| 90 | 0.00275 | 3669 | 8.21 |
| 80 | 0.00283 | 1590 | 7.37 |
| 70 | 0.00291 | 1284 | 7.16 |
| 60 | 0.003 | 479 | 6.17 |

Supplementary Figure 8: Arrhenius plot of FA dehydrogenation using Ru-2.

Slope= -7655.64
EA=63.7  kJ mol-1

# GC-TCD report of inorganic gases

Example: Table 1, Entry 5

Reaction conditions: 13 µmol catalyst, 0.5 mL (13.25 mmol) FA, 1.0 mL (5.35 mmol) BMIM OAc. Reaction temperature and -time varies.

Supplementary Figure 9: GC-TCD chromatogram of FA dehydrogenation.

Bibliography

(1) 	Asensio, G. et al. Osmium(III) Complexes with POP Pincer Ligands: Preparation from Commercially Available OsCl3•3H2O and their X-ray Structures. Inorg. Chem. 49, 8665–8667 (2010).

(2) 	Veits, Y. A., Mutsenek, E. V., Neganova, E. G. & Beletskaya, I. P. Niew bidentate diphosphine ligands on the basis of diphenyl ether. Russ. J. Org. Chem. 37, 1583–1586 (2001).

(3) 	Abdur-Rashid, K. et al. The generation of hydrogen from ammonia borane through catalytic hydrolysis. (2008).

(4) 	Fulmer, G. R. et al. NMR chemical shifts of trace impurities: Common laboratory solvents, organics, and gases in deuterated solvents relevant to the organometallic chemist. Organometallics 29, 2176–2179 (2010).

(5) 	Dolomanov, O. V., Bourhis, L. J., Gildea, R. J., Howard, J. A. K. & Puschmann, H. OLEX2: A complete structure solution, refinement and analysis program. J. Appl. Crystallogr. 42, 339–341 (2009).

(6) 	Sheldrick, G. M. SHELXT - Integrated space-group and crystal-structure determination. Acta Crystallogr. Sect. A Found. Crystallogr. 71, 3–8 (2015).

(7) 	Schunn, R. A., Wonchoba, E. R. & Wilkinson, G. Chlorohydridotris(triphenylphosphine)ruthenium(II). Inorganic Syntheses 131–134 (1972)

(8) 	Ledger, A. E. W. et al. Pincer Phosphine Complexes of Ruthenium: Formation of Ru(P-O-P)(PPh3) HCl(P-O-P=xantphos, DPEphos, (Ph2PCH2CH2)2O) and Ru(dppf)(PPh3)HCl and Characterization of Cationic Dioxygen, Dihydrogen, Dinitrogen, and Arene Coordinated Phosphine Products. Inorg. Chem. 49, 7244–7256 (2010).

(9) 	Ledger, A. E. W. Chelating Phosphine Complexes of Ruthenium for the Coordination and Activation of Small Molecules. (University of Bath, 2011).

NMR data of catalytic dehydrogenation of formic acid

# Structural crystallographic data for Ru-2

Fractional atomic coordinates (x104) and equivalent isotropic displaccement parameters (Å2x103)

Atom		x		y		z	U(eq)

Ru01	3156.68(10)	6170.32(9)	7079.04(6)	9.27(4)

Cl02	981.0(3)	6745.0(3)	7265.5(2)	15.44(8)

P03	3724.8(4)	7574.2(3)	6265.1(2)	11.17(8)

P04	4068.6(3)	7042.9(3)	8268.0(2)	10.18(8)

P05	2589.3(4)	4266.1(3)	7292.5(2)	10.49(8)

O006	2315.3(11)	5345.2(10)	5959.2(6)	13.8(2)

C007	2229.2(15)	5828.0(14)	5294.8(9)	13.0(3)

C008	1215.0(15)	3999.1(14)	4985.2(9)	13.5(3)

C009	4058.4(16)	8613.3(14)	8500.4(9)	13.8(3)

C00A	1718.3(15)	4247.8(13)	5775.0(9)	12.9(3)

C00B	5124.2(16)	9411.2(15)	8577.6(11)	19.3(3)

C00C	1728.0(15)	3550.6(14)	6330.6(9)	13.5(3)

C00D	1555.6(15)	5048.3(14)	4668.4(9)	13.2(3)

C00E	3794.2(15)	3324.0(14)	7313.1(9)	14.2(3)

C00F	2815.0(15)	6918.7(14)	5309.6(9)	13.3(3)

C00G	3878.5(16)	6002.4(15)	9656.8(10)	17.7(3)

C00H	6252.0(16)	7548.2(15)	9263.0(10)	18.2(3)

C00I	5698.1(15)	6982.7(13)	8511.2(9)	13.2(3)

C00J	3303.1(15)	6565.2(13)	9136.4(9)	13.2(3)

C00K	5294.4(15)	7674.2(15)	5876.7(10)	16.1(3)

C00L	6438.4(16)	6425.6(14)	7950.1(10)	16.5(3)

C00M	7686.8(17)	6444.6(16)	8124.7(11)	21.4(3)

C00N	1569.2(15)	3882.6(14)	8093.4(9)	14.7(3)

C00O	2689.2(16)	7269.4(15)	4572.3(10)	16.8(3)

C00P	4602.3(16)	3719.7(15)	8090.3(10)	18.5(3)

C00Q	5633.4(17)	6495.7(16)	5519.7(10)	20.8(3)

C00R	3460.0(16)	9108.2(14)	6488.2(10)	16.2(3)

C00S	2000.0(16)	6537.2(16)	3918.3(10)	18.6(3)

C00T	612.8(16)	2883.7(15)	4719.7(10)	17.3(3)

C00U	1129.5(17)	2435.5(15)	6038.5(10)	18.7(3)

C00V	3225.9(18)	5536.6(16)	10242.0(10)	21.7(4)

C00W	1426.5(15)	5440.4(15)	3948.8(9)	16.6(3)

C00X	281.3(16)	4177.3(16)	7949.4(11)	21.2(3)

C00Y	1407.5(17)	6204.5(17)	9819.4(11)	21.9(4)

C00Z	1476.7(17)	2650.4(16)	8234.6(11)	21.0(3)

C010	1994.0(18)	5635.2(16)	10327.8(10)	21.7(4)

C011	4587.3(17)	3267.6(15)	6579.1(11)	21.5(3)

C012	2921.3(16)	9020.7(15)	8524.5(10)	17.8(3)

C013	7491.7(17)	7555.4(16)	9439.3(11)	22.3(4)

C014	2856.2(17)	10188.5(15)	8657.5(11)	20.4(3)

C015	2051.8(16)	6646.3(15)	9223.9(10)	18.7(3)

C016	3927.8(18)	10972.6(15)	8753.1(10)	20.6(3)

C017	4072(2)		9892.8(16)	5949.5(12)	25.5(4)

C018	8214.6(16)	7010.7(17)	8867.9(12)	23.6(4)

C019	2086.2(17)	9194.2(15)	6512.5(11)	21.9(3)

C01A	585.8(17)	2126.1(15)	5254.1(11)	20.8(3)

C01B	6258.5(17)	8326.1(18)	6525.8(11)	24.8(4)

C01C	5058.5(18)	10583.8(16)	8704.6(12)	24.1(4)

C01D	9375(3)		9507(2)		7876(2)		62.5(10)

C01E	9128(3)		9947(2)		7198(3)		61.1(9)

C01F	8435(3)		11014(3)	8677(3)		79.6(14)

C01G	9045(3)		10030(3)	8611(3)		74.3(11)

C01H	8542(3)		10904(3)	7252(3)		71.3(11)

C01I	8202(3)		11419(3)	7983(3)		75.3(12)

Bond lengths (Å)

Atom	Atom	Length/Å	 	Atom	Atom	Length/Å

Ru01	Cl02	2.5874(4)	 	C00G	C00V	1.393(2)

Ru01	P03	2.4005(4)	 	C00H	C00I	1.406(2)

Ru01	P04	2.2316(4)	 	C00H	C013	1.387(3)

Ru01	P05	2.3818(4)	 	C00I	C00L	1.398(2)

Ru01	O006	2.0958(11)	 	C00J	C015	1.401(2)

P03	C00F	1.8624(16)	 	C00K	C00Q	1.527(2)

P03	C00K	1.8563(17)	 	C00K	C01B	1.529(2)

P03	C00R	1.8713(16)	 	C00L	C00M	1.393(2)

P04	C009	1.8516(16)	 	C00M	C018	1.385(3)

P04	C00I	1.8431(16)	 	C00N	C00X	1.531(2)

P04	C00J	1.8558(16)	 	C00N	C00Z	1.532(2)

P05	C00C	1.8617(16)	 	C00O	C00S	1.408(2)

P05	C00E	1.8591(16)	 	C00R	C017	1.534(2)

P05	C00N	1.8634(16)	 	C00R	C019	1.528(2)

O006	C007	1.3678(18)	 	C00S	C00W	1.390(3)

O006	C00A	1.3635(19)	 	C00T	C01A	1.398(3)

C007	C00D	1.395(2)	 	C00U	C01A	1.406(2)

C007	C00F	1.372(2)	 	C00V	C010	1.384(3)

C008	C00A	1.399(2)	 	C00Y	C010	1.395(3)

C008	C00D	1.466(2)	 	C00Y	C015	1.390(2)

C008	C00T	1.395(2)	 	C012	C014	1.388(2)

C009	C00B	1.394(2)	 	C013	C018	1.389(3)

C009	C012	1.402(2)	 	C014	C016	1.388(3)

C00A	C00C	1.374(2)	 	C016	C01C	1.385(3)

C00B	C01C	1.394(3)	 	C01D	C01E	1.389(5)

C00C	C00U	1.400(2)	 	C01D	C01G	1.364(5)

C00D	C00W	1.399(2)	 	C01E	C01H	1.381(4)

C00E	C00P	1.531(2)	 	C01F	C01G	1.424(5)

C00E	C011	1.530(2)	 	C01F	C01I	1.387(6)

C00F	C00O	1.402(2)	 	C01H	C01I	1.359(6)

C00G	C00J	1.398(2)

Bond angles (°)

Atom	Atom	Atom	Angle/˚	 		Atom	Atom	Atom	Angle/˚

P03	Ru01	Cl02	92.486(13)	 	C00W	C00D	C008	138.77(15)

P04	Ru01	Cl02	100.169(13)	 	C00P	C00E	P05	110.12(11)

P04	Ru01	P03	101.622(14)	 	C011	C00E	P05	112.79(11)

P05	Ru01	Cl02	95.101(13)	 	C011	C00E	C00P	110.38(14)

P05	Ru01	P03	153.937(13)	 	C007	C00F	P03	113.87(11)

P05	Ru01	P04	101.509(14)	 	C00O	C00F	P03	133.08(13)

O006	Ru01	Cl02	80.36(3)	 	C00O	C00F	C007	112.77(14)

O006	Ru01	P03	78.33(3)	 	C00V	C00G	C00J	120.95(16)

O006	Ru01	P04	179.48(3)	 	C013	C00H	C00I	121.05(16)

O006	Ru01	P05	78.43(3)	 	C00H	C00I	P04	120.49(12)

C00F	P03	Ru01	101.45(5)	 	C00L	C00I	P04	121.73(12)

C00K	P03	Ru01	117.84(5)	 	C00L	C00I	C00H	117.72(15)

C00K	P03	C00F	99.42(7)	 	C00G	C00J	P04	122.81(13)

C00R	P03	Ru01	126.23(5)	 	C015	C00J	P04	118.93(12)

C00R	P03	C00F	105.40(7)	 	C015	C00J	C00G	117.82(15)

C00R	P03	C00K	102.59(8)	 	C00Q	C00K	P03	112.05(12)

C009	P04	Ru01	114.10(5)	 	C01B	C00K	P03	111.53(12)

C00I	P04	Ru01	121.69(5)	 	C01B	C00K	C00Q	110.54(15)

C00I	P04	C009	100.38(7)	 	C00M	C00L	C00I	121.17(16)

C00J	P04	Ru01	113.51(5)	 	C018	C00M	C00L	120.15(16)

C00J	P04	C009	102.64(7)	 	C00X	C00N	P05	110.12(11)

C00J	P04	C00I	101.99(7)	 	C00Z	C00N	P05	117.02(12)

C00C	P05	Ru01	102.07(5)	 	C00Z	C00N	C00X	109.88(14)

C00E	P05	Ru01	119.36(5)	 	C00S	C00O	C00F	120.51(16)

C00E	P05	C00C	100.47(7)	 	C017	C00R	P03	116.95(12)

C00N	P05	Ru01	124.27(5)	 	C019	C00R	P03	110.92(11)

C00N	P05	C00C	104.70(7)	 	C019	C00R	C017	109.71(15)

C00N	P05	C00E	102.50(7)	 	C00W	C00S	C00O	123.49(15)

C007	O006	Ru01	125.92(10)	 	C01A	C00T	C008	117.70(15)

C00A	O006	Ru01	125.96(10)	 	C01A	C00U	C00C	120.70(16)

C00A	O006	C007	108.08(12)	 	C010	C00V	C00G	120.60(16)

C00D	C007	O006	110.42(14)	 	C00S	C00W	C00D	117.72(15)

C00F	C007	O006	119.64(14)	 	C015	C00Y	C010	120.12(16)

C00F	C007	C00D	129.87(15)	 	C00Y	C010	C00V	119.25(16)

C00D	C008	C00A	105.31(14)	 	C014	C012	C009	121.03(16)

C00T	C008	C00A	115.74(15)	 	C018	C013	C00H	120.26(16)

C00T	C008	C00D	138.88(15)	 	C016	C014	C012	120.01(17)

C00B	C009	P04	123.16(13)	 	C00Y	C015	C00J	121.23(16)

C012	C009	P04	118.40(13)	 	C01C	C016	C014	119.72(16)

C012	C009	C00B	118.15(15)	 	C013	C018	C00M	119.65(16)

C008	C00A	O006	110.58(14)	 	C00U	C01A	C00T	123.30(16)

C00C	C00A	O006	119.65(14)	 	C016	C01C	C00B	120.26(17)

C00C	C00A	C008	129.69(15)	 	C01G	C01D	C01E	119.8(3)

C01C	C00B	C009	120.76(16)	 	C01H	C01E	C01D	121.2(4)

C00A	C00C	P05	113.50(12)	 	C01I	C01F	C01G	118.3(4)

C00U	C00C	P05	133.59(13)	 	C01F	C01G	C01D	119.8(4)

C00U	C00C	C00A	112.85(14)	 	C01I	C01H	C01E	119.1(4)

C008	C00D	C007	105.60(14)	 	C01H	C01I	C01F	121.8(3)

C00W	C00D	C007	115.60(15)

Torsion angles (°)

A	B	C	D	Angle/˚	 		A	B	C	D	Angle/˚

Ru01	O006	C007	C00D	-176.98(13)	 	C007	C00D	C00W	C00S	1.78(17)

Ru01	O006	C007	C00F	5.67(13)	 	C007	C00F	C00O	C00S	1.08(17)

Ru01	O006	C00A	C008	176.96(13)	 	C008	C00A	C00C	C00U	-0.4(2)

Ru01	O006	C00A	C00C	-5.83(13)	 	C008	C00D	C00W	C00S	-175.8(2)

P03	C00F	C007	O006	2.31(13)	 	C008	C00T	C01A	C00U	0.2(2)

P03	C00F	C007	C00D	-174.45(11)	 	C009	C00B	C01C	C016	-0.2(2)

P03	C00F	C00O	C00S	174.53(16)	 	C009	C012	C014	C016	1.3(2)

P04	C009	C00B	C01C	176.06(14)	 	C00A	C00C	C00U	C01A	-0.57(18)

P04	C009	C012	C014	-176.90(13)	 	C00B	C01C	C016	C014	-1.4(2)

P04	C00I	C00H	C013	-176.90(14)	 	C00C	C00U	C01A	C00T	0.7(2)

P04	C00I	C00L	C00M	176.12(14)	 	C00D	C00W	C00S	C00O	-0.57(19)

P04	C00J	C00G	C00V	-172.24(14)	 	C00F	C00O	C00S	C00W	-1.0(2)

P04	C00J	C015	C00Y	174.02(14)	 	C00G	C00J	C015	C00Y	1.38(19)

P05	C00C	C00A	O006	0.49(13)	 	C00G	C00V	C010	C00Y	0.2(2)

P05	C00C	C00A	C008	177.10(10)	 	C00H	C00I	C00L	C00M	-0.97(19)

P05	C00C	C00U	C01A	-177.37(17)	 	C00H	C013	C018	C00M	-1.0(2)

O006	C007	C00D	C008	-0.45(14)	 	C00I	C00L	C00M	C018	0.7(2)

O006	C007	C00D	C00W	-178.79(13)	 	C00J	C015	C00Y	C010	-2.1(2)

O006	C007	C00F	C00O	177.08(15)	 	C00L	C00M	C018	C013	0.3(2)

O006	C00A	C008	C00D	0.50(14)	 	C00V	C010	C00Y	C015	1.3(2)

O006	C00A	C008	C00T	178.04(13)	 	C012	C014	C016	C01C	0.8(2)

O006	C00A	C00C	C00U	-176.99(15)	 	C01D	C01E	C01H	C01I	-0.1(3)

C007	C00D	C008	C00A	-0.03(14)	 	C01D	C01G	C01F	C01I	-0.5(4)

C007	C00D	C008	C00T	-176.65(13)	 	C01E	C01H	C01I	C01F	0.4(3)

Hydrogen Atom Coordinates (Å×104) and Isotropic Displacement Parameters (Å2×103)

Atom		x		y		z	U(eq)

H00B	5904.3(16)	9153.1(15)	8543.2(11)	23.2(4)

H00E	3371.4(15)	2530.6(14)	7312.4(9)	17.1(4)

H00G	4726.8(16)	5936.4(15)	9610.9(10)	21.2(4)

H00H	5769.5(16)	7931.4(15)	9656.4(10)	21.9(4)

H00K	5302.1(15)	8119.7(15)	5434.1(10)	19.4(4)

H00L	6084.2(16)	6027.0(14)	7440.7(10)	19.8(4)

H00M	8176.9(17)	6068.3(16)	7733.0(11)	25.7(4)

H00N	1913.2(15)	4393.7(14)	8608.9(9)	17.6(4)

H00O	3071.7(16)	8006.7(15)	4513.4(10)	20.1(4)

H00a	5051(11)	4487(6)		8097(4)		27.7(5)

H00c	4084(2)		3745(13)	8554.7(11)	27.7(5)

H00d	5190(9)		3181(7)		8116(5)		27.7(5)

H00f	5680(14)	6053(5)		5946(2)		31.2(5)

H00i	5005(8)		6089(6)		5107(7)		31.2(5)

H00j	6432(7)		6589.6(16)	5276(8)		31.2(5)

H00R	3815.2(16)	9433.3(14)	7046.2(10)	19.4(4)

H00S	1923.2(16)	6807.4(16)	3430.3(10)	22.4(4)

H00T	234.2(16)	2647.1(15)	4194.0(10)	20.7(4)

H00U	1090.2(17)	1881.8(15)	6373.6(10)	22.5(4)

H00V	3630.5(18)	5147.8(16)	10585.1(10)	26.1(4)

H00W	962.5(15)	4972.9(15)	3496.6(9)	19.9(4)

H00p	342(2)		4985(4)		7904(9)		31.8(5)

H00q	-99(6)		3691(9)		7450(5)		31.8(5)

H00x	-224(5)		4045(13)	8401(5)		31.8(5)

H00Y	566.2(17)	6290.4(17)	9880.2(11)	26.2(4)

H00z	1140(13)	2114.3(17)	7744(3)		31.5(5)

H	2297(3)		2490(5)		8374(9)		31.5(5)

Ha	934(11)		2559(4)		8676(6)		31.5(5)

H010	1552.5(18)	5318.8(16)	10728.5(10)	26.0(4)

H01a	4067(3)		2954(13)	6088.9(13)	32.2(5)

H01b	4989(12)	4041(2)		6554(6)		32.2(5)

H01c	5214(10)	2772(11)	6624(5)		32.2(5)

H012	2183.7(16)	8489.4(15)	8448.7(10)	21.4(4)

H013	7847.9(17)	7934.1(16)	9952.8(11)	26.8(4)

H014	2078.3(17)	10451.3(15)	8683.1(11)	24.4(4)

H015	1635.8(16)	7010.0(15)	8869.6(10)	22.5(4)

H016	3885.5(18)	11772.4(15)	8851.3(10)	24.8(4)

H01d	4962(3)		9880(11)	5968(8)		38.3(6)

H01e	3739(11)	9621(9)		5394(2)		38.3(6)

H01f	3906(13)	10678(3)	6142(6)		38.3(6)

H018	9066.4(16)	7026.5(17)	8986.4(12)	28.3(4)

H01g	1714(3)		8990(13)	5964.1(14)	32.8(5)

H01h	1692(3)		8667(10)	6838(8)		32.8(5)

H01i	1971.8(17)	9981(4)		6751(9)		32.8(5)

H01j	179.7(17)	1363.9(15)	5078.6(11)	24.9(4)

H01k	6044(8)		9090(5)		6734(7)		37.2(6)

H01l	6282(11)	7904(7)		6966(5)		37.2(6)

H01m	7068(3)		8402(13)	6294(3)		37.2(6)

H01n	5792.4(18)	11118.1(16)	8758.0(12)	29.0(4)

H01o	9773(3)		8844(2)		7828(2)		75.0(11)

H01p	9366(3)		9583(2)		6689(3)		73.4(11)

H01q	8193(3)		11384(3)	9184(3)		95.5(16)

H01r	9222(3)		9738(3)		9078(3)		89.2(14)

H01s	8378(3)		11198(3)	6784(3)		85.6(13)

H01t	7795(3)		12075(3)	8019(3)		90.4(15)

Hb	4450(30)	5820(20)	6884(16)	35(7)