Supplementary Information

Ultrastable Fe-N4-C6O2 Single Atom Sites for Highly Efficient PMS Activation and Enhanced FeIV=O Reactivity

# Tiantian Chen1, Ganbing Zhang2*, Hongwei Sun1, Yetong Hua1, Shu Yang1, Dandan Zhou1, Haoxin Di1, Yiling Xiong1, Shenghuai Hou1, Hui Xu*1, and Lizhi Zhang3*

# 1National Key Laboratory of Green Pesticide, College of Chemistry, Central China Normal University, Wuhan 430079, P.R. China

# 2College of Chemistry and Chemical Engineering, Hubei University, Wuhan, 430062, P. R. China

# 3School of Environmental Science and Engineering, Shanghai Jiao Tong University, Shanghai, 200240, P. R. China

# E-mail: huixu@ccnu.edu.cn; gbzhang@hubu.edu.cn; zhanglz@mail.ccnu.edu.cn.

Supplementary Texts

Supplementary Text 1. Materials and instruments

Materials

Ferrous chloride tetrahydrate (FeCl2·4H2O, ≥ 99.7%), 1,10-phenanthroline monohydrate (AR), sodium hydroxide (NaOH, AR), hydrochloric acid (HCl, AR), tetramethyl orthosilicate (TMOS), anhydrous sodium acetate (NaAc, AR), acetic acid (HAc, AR), absolute ethanol (C2H4OH, ≥ 99.7%), ammonia (28% NH3·H2O, AR), sodium thiosulfate (Na2S2O3, 99%), formaldehyde aqueous solution (37 wt%), bisphenol A (BPA, AR) and 4-Chlorophenol (4-CP, 99.0%) were all supplied by Sinopharm Chemical Reagent Co., Ltd (Shanghai, China). Sodium tetraborate (Na2B4O7, ≥ 99%), 2,4-dichlorophenol (2,4-DCP, ＞98.0%), phenol (PE), p-nitrophenol (PNP, 98%), methyl phenyl sulfone (PMSO2, ＞97.0%), ferroferric oxide (Fe3O4, 99.5% metals basis, 20 nm spheroidal), benzoic acid (BA, AR), resorcinol (AR), and oxone (2KHSO5·KHSO4·K2SO4, active oxygen ≥ 4.50%) were obtained from Shanghai Aladdin Biochemical Technology Co., Ltd (Shanghai, China). Methyl phenyl sulfoxide (PMSO, 98%), 5,5-dimethyl-1-pyrrolineN-oxide (DMPO), (S,S)-(+)-N,N'-Bis(3,5-di-tert-butylsalicylidene)-1,2-cyclohexanediamin (98%), and perchloric acid (HClO4, AR) were acquired from Shanghai Maclin Biochemical Technology Co., Ltd (Shanghai, China). Methanol (MeOH, HPLC) and acetonitrile (HPLC) were bought from Thermo Fisher Technology Co., Ltd. (USA). 2,2,6,6-tetramethyl-4-piperidinol (TEMP), P-nitrobenzaldehyde (PNBD, AR), fipronil (FP, AR), and p-nitrobenzyl alcohol (PNBA, 98%) and m-dihydroxybenzene were purchased from Shanghai Annaeji Chemical Co., Ltd (Shanghai, China). P-chlorobenzoic acid (pCBA, 98%) was purchased from Shanghai Beade Pharmaceutical Technology Co., Ltd. The arium® pro-Ultrapure Water Systems (Sartorius Stedim Biotech, Gottingen, Germany) was used to obtain ultrapure water in the experiments.

Instruments

Field emission scanning electron microscope (FESEM) images were investigated on a JSM7900F (JEOL, Japan) microscope. Transmission electron microscopy (TEM) and High-resolution TEM images (HRTEM) were recorded on a FEI Talos F200x (Thermo Fisheries, USA) instrument. Powder X-ray diffraction (PXRD) analysis was carried out on a D8 ADVANCE apparatus (Bruker, Germany) with a scanning angle (2θ) of 10°- 80°, operated at 40 kV and 40 mA. The chemical state of the catalysts was characterized by X-ray photoelectron spectroscopy (XPS, Escalab 250 Xi, Thermo Fisheries, USA). The Raman spectra were collected using a DXR laser Raman spectrophotometer (Thermo Fisheries, USA). Avio 200 inductively coupled plasma optical emission spectrometry (ICP-OES, PerkinElmer, USA) was used to determine the Fe ions in the Fe-SACs and dissolved iron ions. The aberration-corrected high angle annular dark field scanning transmission electron microscopy (AC-HAADF STEM) image was obtained by FEI TitanTM Themis 60-300 instrument at an accelerating voltage of 200 kV (FEI, USA). The X-ray absorption spectra (XAS) including X-ray absorption near-edge structure (XANES) and extended X-ray adsorption fine structure (EXAFS) for the Fe K-edge in Fe-SACs were carried out on the sample at 21A X-ray nano diffraction beamline of Taiwan Photon Source (TPS), National Synchrotron Radiation Research Center (NSRRC). This beamline adopted 4-bounce channel-cut Si (111) monochromator for mono-beam X-ray nano diffraction and X-ray absorption spectroscopy. The end station is equipped with three ionization chambers and Lytle/SDD detector after the focusing position of the KB mirror for fluorescence/transmission mode X-ray absorption spectroscopy. The photon flux on the sample is range from 1x1011~3x109 photon/sec for X-ray energy from 6-27 keV. XAS data is processed and analyzed by ATHENA and ARTEMIS applications included in IFEFFIT1. Hama Fortran was used to calculate the wavelet transform of the EXAFS spectrum and to reconstruct the spectra from the wavelet transform2. SO4•–, •OH, electron transfer, and hypervalent iron oxides were detected by electron paramagnetic resonance (EPR, EMX-PLUS, Bruker, Germany) spectroscopy. The total organic carbon (TOC) was determined with the TOC-L series analyzer (Shimadzu, Japan).

57Fe Mössbauer spectroscopy:

In order to characterize the various iron species in Fe-N4-C6O2 and Fe-N4 -C, 57Fe Mössbauer spectroscopy was performed using 57Co (Rh) γ–ray radioactive source maintained at room temperature (298 K). The measurements were made in the transmission mode using a 50 mCi 57Co/Rh-source, and the velocity scale and isomer shift (δIso) were calibrated with respect to α-Fe-Standard (25 μm thick, 99.99% purity). All Mössbauer spectra were plotted as relative absorption against the Doppler velocity (ν). The relative absorption was calculated from the original transmission data using equation S1 (Eq. S1):

| AbsνDoppler =Transmax-TransνDopplerTransmax | (S1) |
| --- | --- |

Where, Transmax and TransνDoppler represent the maximum background transmission that occurs at ν where no absorption is observed and the transmission at a specific ν, respectively. AbsνDoppler is the relative absorption for each ν, and expressed as a percentage.

The δIso describes the shift of the electron cloud density at the iron nucleus of the sample (EA,CFSE) with respect to the α-Fe-Standard source (ES,CFSE), which is used to characterize the electrostatic interaction. Specifically, the δIso refers to the difference in ν between the center of gravity of the Mössbauer singlet, doublet, or multiplet state and the zero velocity of the spectral line, and its value is related to the electric monopole interaction. Chemical information such as chemical bond properties, oxidation state, and coordination information etc. can be obtained from the δIso value. The reference formula for determining δIso is shown in Eq. S2:

| δISO=EA, CFSE-ES, CFSE=23πZe2ρe-,A - ρe-,S×RExcited2 - RGround2=νc∙Eγ | (S2) |
| --- | --- |

Where, Z is the atomic number of Fe-57 and e is the electronic charge of a single electron. The coefficients ρe−,A and ρe−,S represent the s-electron density at the nuclei of the iron species in the sample (Fe-N4-C6O2 or Fe-N4-C10) and the α-Fe source, respectively. RExcited and RGround denote the nuclear radius in the excited state and ground state of Fe-57, respectively. The second coefficient in the Eq. S2 is always negative since RExcited is always less than RGround.

Quadrupole splitting (∆EQ) is used to describe the change in energy caused by the electric quadrupole interaction between the external electric field and the nucleus. When the electric field gradient is not zero, the excited state splits into substates with different energies.

Supplementary Text 2. Synthesis details.

Synthesis of carrier.

Synthesis of silica. First, 10 mL of ultrapure water, 70 mL of absolute ethanol, and 3 mL of ammonia water were stirred together for 10 min at room temperature. Subsequently, 3.5 mL of TMOS was quickly added to the above solution and stirred for 24 h at 25 ℃. Finally, the white SiO2 precipitates were collected by centrifugation after washing with ethanol and water for many times.

Synthesis of silica@resorcinol formaldehyde oligomers nanospheres. Silica@resorcinol formaldehyde oligomers (SiO2@RF) nanospheres with core-shell structures were prepared by a one-pot method using in situ generated silica primary particles as templates and used as precursors for the synthesis of single atoms (Figure S1)3. First, 10 mL of ultrapure water, 70 mL of absolute ethanol, and 3 mL of ammonia water were stirred together for 10 min at room temperature. Subsequently, 3.5 mL of TMOS was quickly added to the above solution and stirred for 15 min. Next, 0.56 mL formaldehyde (37 wt%) and 0.4 g resorcinol were added and stirred for 24 h at 25 °C. Finally, the orange-yellow precipitates collected by centrifugation were washed several times with ethanol and water to obtain SiO2@RF nanospheres.

Synthesis of SiO2@N-C. SiO2@phen was obtained by depositing 2 mmol of 1,10-phenanthroline monohydrate dissolved in anhydrous ethanol onto 3 g SiO2 nanospheres by rotary evaporation. Finally, SiO2@N-C was obtained by carbonization of SiO2@phen at 700° for 2h.

Synthesis of different catalysts.

Synthesis of Fe-N4-C6O2 SAC. FeCl2·4H2O and 10-phenanthroline monohydrate were ultrasonically dispersed in 60 mL absolute ethanol to obtain Fe-N coordination complex (I). Then, SiO2@RF was added to the solution and stirred under reflux at 60 °C for 4h. Next, the pre-prepared complex (I) was deposited on SiO2@RF by reduced pressure evaporation at 50 °C. The dried solid was then heated to 700 °C (calcined for 2 h) at a rate of 2 °C min-1 in an N2 atmosphere. Subsequently, the resulting black solid was dispersed into 100 mL 5 wt % HF and stirred at room temperature for 4 h to remove SiO2. This procedure was repeated three times. Afterward, the solid was washed repeatedly with a large amount of ultrapure water until the filtrate reached neutral pH. Finally, the dried black powder was recorded as Fe-N4-C6O2 SAC.

Synthesis of Fe-N2O2-C10 SAC. The other steps remained unchanged except that 10-phenanthroline monohydrate and SiO2@RF were replaced with (S,S)-(+)-N,N'-Bis(3,5-di-tert-butylsalicylidene)-1,2-cyclohexanediamin and SiO2@N-C, respectively.

Synthesis of Fe-N4-C10. The other steps remained unchanged except for the deposition of complex (I) on SiO2.

Synthesis of Fe-NPs/NC. The other steps remained unchanged except without adding SiO2@RF.

Synthesis of metal-free N\O co-doped carbon materials (N/O-C). The other steps remained unchanged except that no FeCl2·4H2O was added.

Synthesis of N-doped carbon materials (N-C). Compared with N/O-C, N-C can be obtained by replacing the SiO2@RF template with the SiO2 template. Besides, the preparation method for each catalyst is summarized in Table S1.

Supplementary Text 3. Catalytic performances of Fe-SACs/PMS system-based advanced oxidation processes (AOPs).

The catalytic activity and stability of Fe-SACs were investigated by activating PMS to degrade BPA at room temperature under neutral pH conditions. In addition, the effects of PMS dosages (100-500 μM), catalyst dosages (0.01, 0.02, 0.05, 0.1 mg mL-1), pH (pH=2-10) and coexisting ions (Cl−, HCO3−) were also investigated. To investigate pH effects, 10 mM acetate and borate buffers were used for maintaining acidic (pH＜7.0) and alkaline (pH≥7.0) pH, respectively. HAc and NaOH were used to regulate pH in acidic condition, ClO4 and NaOH were used to regulate pH in alkaline condition. If it was not otherwise specified, the experiments were carried out at room temperature at pH=7.0, the amount of catalyst is 0.05 mg mL-1 and the amount of PMS is 400 μM. In a typical experiment, the catalyst stock suspension was introduced into the target pollutants solution and stirred at T ± 1 °C for 10 min to achieve the adsorption-desorption equilibrium. After that, the PMS stock solution (10 mM) was placed in the above solution to initiate the oxidation reaction. The mixture was magnetically stirred at T ± 1 °C with a water bath. At predetermined time intervals, sample aliquots (1 mL) were withdrawn and immediately quenched with 20 μL of Na2S2O3 (0.5 M). Then, it was filtered through a 0.22 μm glass fiber membrane (negligible adsorption for reactants), and injected into a 2 mL glass vial for tests. The batch experiments were conducted in duplicates at least, and the average values with standard deviations were given.

Radical quenching and EPR experiments were performed to investigate the activation mechanism. Among them, the quenching experiment is different from the above experiment in that the quenching agent was added together with the catalyst. To evaluate the contribution of singlet oxygenation (1O2) to organic oxidation, the degradation of pollutants based on Fe-SACs/PMS system-based AOPs and 1O2 was also compared, in which 1O2 was produced by photoexcitation of RB under visible light (400-800nm)4.

Supplementary Text 4. Analytical Methods.

The concentration of target pollutants was analyzed by high-performance liquid chromatograph (HPLC, Shimadzu) equipped with an SPD-M20A diode array detector. Chromatographic separations were performed using an Agilent Eclipse XDB-C18 column (4.6 ×150 mm, i.d., 5 µm, Agilent) at a flow rate of 1 mL min-1. The column was maintained at 35 °C. The detailed chromatographic parameters (the flow rate, wavelength, and mobile phase) for the separation and detection of each organic compound are listed in Table S10.

To comprehensively detect the intermediates produced in the process of BPA degradation, the intermediates were purified and enriched by solid phase extraction (SPE). In addition, lower concentrations of catalyst and shorter catalytic time were selected in this study to prevent BPA from being completely degraded. Finally, these intermediates were identified by liquid chromatography-mass spectrometry (LC-MS) and gas chromatography-mass spectrometry (GC-MS) analysis.

Alliance e2695 separations module (Waters, Manchester, UK) and an Agilent Eclipse XDB-C18 column (4.6 ×150 mm, i.d., 5 µm) were used as the LC system to separate the intermediates. The mobile phase started with 80/20 (v/v) methanol/water at a flow rate of 0.2 mL min−1 and the analysis time was 70 min. The column temperature was 30 °C.  Acquity TQD instrument with electrospray ionization (ESI) was used as the MS system (Waters, Manchester, UK). The mass-charge ratio is set to 30-500 to qualitatively analyze the intermediates. The full scan negative ion mode in the MS system is selected to analyze the intermediates. Some other MS parameters were set as follows, capillary voltage: 3 kV, cone hole voltage 30 V. Besides, ion source temperature: 150 °C, solvent temperature: 400 °C.

The GC-MS analysis was performed on a GC-MS-QP2010 plus (Shimadzu, Japan) equipped with an electron impact ion source (EI). Chromatographic separation was carried out with a DB-5MS capillary column (30 m × 0.25 mm, i.d., 0.25 µm, Agilent, J&W, USA). The analytes were introduced into the column using a splitless mode. Ultra-pure helium was used as the carrier gas at a flow rate of 1.2 mL min-1. The injection temperature was set as 240 °C and the column temperature program was as follows: the initial temperature of the GC column was set at 80 °C (held for 1 min), the temperature was increased to 280 °C at a rate of 5 °C min-1 (held for 9 min). The total running time was 50 min. The full scan mode of m/z 35~500 was used to record the mass spectrum in EI mode at 70 eV potential with an ion source temperature of 200 °C. The detected peaks were identified according to the NIST data library.

Supplementary Text 5. Calculation formula

(1) Pseudo-first-order reaction rate constant

In the kinetic investigation, the degradation of organic pollutants is fitted with the pseudo-first-order kinetic model, and the apparent rate constants (k) was calculated according to the following Eq. S3:

| lnCtC0=- kt | (S3) |
| --- | --- |

Where Ct and C0 denote the real-time concentration and initial concentration of contaminants (mol L-1), respectively. k stands for the apparent rate constants or pseudo-first-order reaction rate constant (min-1). t represents the reaction time (min)

(2) Turnover frequency

The turnover frequency (TOF) of SACs was calculated by Eq. S4 - Eq. S6:

| TOF=C0×(Contaminants Removal)t×CFe | (S4) |
| --- | --- |
| Contaminants Removal=C0-CtC0×100% | (S5) |
| CFe=Ccat.×(Fe content/wt%)MFe | (S6) |

Where C0 denotes the initial concentration of BPA (mol L-1). Ct indicates the concentration of BPA after 5 s of degradation. CFe (mol L-1) and Ccat (g L-1) are the concentration of Fe element and catalyst, respectively. t stands for the reaction time (0.083 min). MFe=56 g mol−1.

(3) Catalyst dose-pollutant concentration normalized kinetic rate constant

The catalyst dose-pollutant concentration normalized kinetic rate constant (k-value) was calculated by Eq. S10.

| k-value=k[C1] / [C2] | (S7) |
| --- | --- |

Where k, [C1] and [C2] represent the pseudo-first-order kinetic reaction rate (s-1), contaminant concentration (μmol L-1), and catalyst dosage (g L-1), respectively.

(4) Total Organic Carbon (TOC) removal

The TOC removal of the BPA solution was determined by Eq. S8.

| TOC Reduction=TOC0-TOCtTOC0×100% | (S8) |
| --- | --- |

where TOC0 and TOCt (2 min) are the initial and final TOC values of BPA, respectively. The TOC reduction shows the mineralization degree of BPA to CO2 and water.

Supplementary Text 6. Construction of Fe-SAC/MCE continuous flow reactor.

The Fe-SAC suspension was deposited on a Mixed Cellulose Esters (MCE) membrane (pore size=0.45 μm, D.25 mm) through filtration and then placed in a filter (i.D. 25 mm). The effective membrane area of the Fe-SAC /MCE composite microfiltration membrane is 1.33 cm2 and the loading capacity of the catalyst is 15.03 mg/cm2. Next, the Fe-SAC /MCE filter and peristaltic pump are used to form a continuous flow reactor to evaluate the long-term stability of Fe-SAC.

Supplementary Text 7. Electrode preparation

Nafion® solution (5.0wt %, 0.1 mL) and Fe-SAC powder (10 mg) were ultrasonically dispersed with ethanol (1 mL) for 30 min to form a suspension. Then, 60 μL suspension was dropped on the carbon paper electrode (1 cm*1 cm) in three portions (20 μL each) and dried under vacuum at 60 °C for 3 h.

Supplementary Text 8. Quantifying the steady-state concentration and contribution of reactive oxygen species (ROS)

(1) The steady-state concentrations of •OH and SO4•-

BA does not react with 1O2, O2•-, and high-valent iron oxo (FeIV=O) species, but exhibits high reactivity towards •OH and SO4•-. Additionally, pCBA is inert towards FeIV=O, but can react with •OH, SO4•-, 1O2, and O2•-. Quenching experiments and EPR tests indicate the presence of a small number of radicals (•OH and SO4•-) and a significant amount of FeIV=O in the Fe-N4-C6O2/PMS and Fe-N4-C10/PMS system, while 1O2 and O2•- are almost absent. The consumption rate of pCBA is simplified to be related to •OH and SO4•- only. Therefore, the steady state concentrations of •OH and SO4•- ([•OH]ss and [SO4•-]ss, M) in the Fe-N4-C6O2/PMS and Fe-N4-C10/PMS system can be obtained by using BA and pCBA as probe compounds. The second-order reaction rate constants (kBA,•OH, kBA,SO4•-, kpCBA,•OH, kpCBA,SO4•-, M−1∙s−1) between probe compounds and ROS were provided in Table S6.

| -d[BA]dt=kBA, •OH[•OH][BA]+kBA, SO4•-[SO4•-][BA] | (S9) |
| --- | --- |
| -d[pCBA]dt=kpCBA, •OH[•OH][pCBA] +kpCBA, SO4•-[SO4•-][pCBA] | (S10) |

Where, [BA] and [pCBA] are the concentrations of BA and pCBA at time (min), respectively. [BA]0 and [pCBA]0 are the initial concentrations of BA and pCBA, respectively.

Rearranging Eqs. S10-11 yields:

| -d[BA][BA]=(kBA, •OH[•OH]+kBA, SO4•-[SO4•-])dt | (S11) |
| --- | --- |
| -d[pCBA][pCBA]=(kpCBA, •OH[•OH] +kpCBA, SO4•-[SO4•-])dt | (S12) |

Integrating Eqs. S12-13 gives

| ln[BA]0[BA]=(kBA, •OH[•OH]ss+kBA, SO4•-[SO4•-]ss)t=kobs, BAt | (S13) |
| --- | --- |
| ln[pCBA]0[pCBA]=(kpCBA, •OH[•OH]ss+kpCBA, SO4•-[SO4•-]ss)t=kobs, pCBAt | (S14) |

The pseudo-first-order reaction rate constants (kobs,BA and kobs, pCBA, min-1) can be obtained from the plots of ln[BA]0[BA] and ln[pCBA]0[pCBA] versus time (min), respectively. Then, [•OH]ss and [SO4•-]ss can be obtained by solving Eqs. S13-14.

(2) The steady-state concentrations of FeIV=O

The second-order reaction rate constants between PMSO and ROS were provided in Table S6. As indicated in Eqs. 16-18, the PMSO can react with •OH (k PMSO, •OH = 3.61 × 109 M–1 s–1), SO4•- (kPMSO, SO4•-= 3.17 × 108 M–1s–1), and FeIV=O (kPMSO, FeIV=O=2.58 × 103 M–1s–1), but it will only be oxidized to PMSO2 by FeIV=O5,6. Therefore, the steady-state concentration of FeIV=O ([FeIV=O]ss) in the Fe-N4-C6O2/PMS and Fe-N4-C10/PMS systems can be determined by the kinetics of PMSO2 formation.

| (PMSO)+ Fe(n+2)+=O OAT (PMSO2)+ Fen+ | (S15) |
| --- | --- |
| + SO4•- or | (S16) |
| + •OH | (S17) |

The kinetics of PMSO2 formation can be represented as:

| d[PMSO2]dt=kPMSO, FeIV=O[FeIV=O][PMSO] | (S18) |
| --- | --- |
| d[PMSO2][PMSO]=kPMSO, FeIV=O[FeIV=O]dt | (S19) |

[PMSO2] and [FeIV=O] are the concentrations of PMSO2 and FeIV=O at time t (s), respectively. [PMSO]0 is the initial concentrations of PMSO.

| ŋ=∆[PMSO2]∆[PMSO]=[PMSO2][PMSO]0-[PMSO] | (S20) |
| --- | --- |
| [PMSO]= [PMSO]0-1ŋ[PMSO2] | (S21) |

ŋ is the conversion rate of PMSO to PMSO2, which represents mole of PMSO2 produced per mole of PMSO oxidized.

Substituting Eq. S21 into Eq. S19 gives

| d[PMSO2][PMSO]0-1ŋ[PMSO2]=kPMSO, FeIV=O[FeIV=O]dt | (S22) |
| --- | --- |

Integrating Eq. S23 gives

| 0[PMSO2]1[PMSO]0-1ŋ[PMSO2] d[PMSO2]=0tkPMSO, FeIV=O[FeIV=O]dt | (S23) |
| --- | --- |
| -ŋ0[PMSO2][ln([PMSO]0-1ŋ[PMSO2])]' d[PMSO2]=0t(kPMSO, FeIV=O[FeIV=O]t)'dt | (S24) |
| -ŋln¦[PMSO]0-1ŋ[PMSO2]¦¦0[PMSO2]=kPMSO, FeIV=O[FeIV=O]sst | (S25) |
| ŋln[PMSO]0[PMSO]0-1ŋ[PMSO2]=kPMSO, FeIV=O[FeIV=O]sst=kobs, PMSOt | (S26) |

Where, the kobs, PMSO can be obtained from plots of ŋln[PMSO]0[PMSO]0- 1ŋ[PMSO2] versus time (Figure S32). The values of kPMSO, FeIV=O are listed in Table S6.

| [FeIV=O]ss=kobs, PMSOkPMSO, FeIV=O | (S27) |
| --- | --- |

(3) The oxidation contributions

The quenching experiments and ESR tests have demonstrated that the degradation of BPA in the Fe-N4-C6O2/PMS and Fe-N4-C10/PMS system is associated with electron transfer process (ETP), radicals (•OH and SO4•-) and FeIV=O oxidation processes. Therefore, the degradation kinetics of BPA can be simply represented by Eq. S29. In this equation, kBPA, ETP (s-1) stands for the observed first-order reaction rate constants for the ETP of BPA. It can be obtained from a plot of ln[BPA]0[BPA] vs. time (s) in the methanol and PMSO co-quenching experiments. kBPA, •OH, kBPA, SO4•-, and kBPA, FeIV=O (M−1∙s−1) represent the second-order reaction rate constants between the reactive species (•OH, SO4•-, and FeIV=O) and BPA.

| -d[BPA]dt=kBPA, ETP [BPA] +kBPA, •OH[•OH][BPA]+kBPA, SO4•-[SO4•-][BPA] +kBPA, FeIV=O[FeIV=O][BPA] | (S28) |
| --- | --- |
| -d[BPA][BPA]=(kBPA, ETP +kBPA, •OH[•OH] +kBPA, SO4•-[SO4•-] +kBPA, FeIV=O[FeIV=O])dt | (S29) |

Integrating Eq. S30 gives

| ln[BPA]0[BPA]=(kBPA, ETP +kBPA, •OH[•OH]ss +kBPA, SO4•-[SO4•-]ss +kBPA, FeIV=O[FeIV=O]ss)t=kobs, BPAt | (S30) |
| --- | --- |

The pseudo-first-order reaction rate constants (kobs, BPA, s-1) can be obtained from the plots of ln[BPA]0[BPA] versus time (s). The observed pseudo-first-order reaction rate constants for the active species can then be obtained from Eqs. S31-33.

| kobs, •OH=kBPA, •OH[•OH]ss | (S31) |
| --- | --- |
| kobs, SO4•-=kBPA, SO4•-[SO4•-]ss | (S32) |
| kobs, FeIV=O=kobs, BPA-kBPA, ETP -kBPA, •OH[•OH]ss-kBPA, SO4•-[SO4•-]ss | (S33) |

The oxidation contributions of each reactive species to BPA degradation can be expressed as Eq. S34.

| Contributions (%)=kobs, ROSkobs, BPA×100% | (S34) |
| --- | --- |

(4) The second-order reaction rate between BPA and FeIV=O

| kBPA, FeIV=O=kobs, FeIV=O[FeIV=O]ss | (S35) |
| --- | --- |

Supplementary Text 9. Theoretical Calculation

The density functional theory (DFT) calculations were carried out by Gaussian 16 program using a cluster model7. First, the cluster C32H18FeN4O2 with the Fe-N4-C6O2 structure, C36H16FeN4 with the Fe-N4 structure, and C34H16FeN4O2 with the Fe-N2O2-C10 structure were constructed for modeling the coordination environment of atomically dispersed Fe active sites in three Fe-SACs. Next, the spin-unrestricted DFT calculation with Perdew-Burke-Ernzerh (PBE) of functional and the basis set of Stuttgart-Dresden-Bonn (SDB) relativistic effective core potential for Fe, and 6-31+G (d, p) for the other nonmetal were used for the full geometric optimization of the model clusters, PMS adsorbed clusters, and various evolution species to minimize the total energies. The frequency calculation was used to verify whether the optimized geometry corresponds to the energy minimum or not, and obtained thermodynamic corrections, where the Grimme’s D3 dispersion correction term, UPBE-D3(BJ) were employed to describe van der Waals interactions. Based on the optimal geometries, energies for all species were calculated by UPBE-D3(BJ) method combined with SMD solvation model taking water as solvent, and the basis set of SDB for Fe and 6-311++G(d,p) for the other nonmetal. Natural population analysis (NPA) was carried out for the calculation of natural charges. In order to be convenient for orbital analysis for unrestricted open-shell wavefunction, biorthogonalization between alpha and beta orbitals have been performed for triplets of Leq-Fe=O species. The Multiwfn 3.8 program 8 was used to calculate partial density of states, PDOS of Fe, N, O and C, d-band center of Fe, and the biorthogonalization process. In addition, highest occupied molecular orbital (HOMO), lowest unoccupied molecular orbital (LUMO), and molecular orbitals were plotted using the Multiwfn 3.8 program.The adsorption energy (Eads) of PMS at Fe-SACs was calculated according to the following formula.

| Eads=Etotal-Ecatal-EPMS | (S36) |
| --- | --- |

Where Etotal stands for the total energy of the adsorbed species, Ecatal and EPMS represent the energy of the catalyst surface and the free PMS molecule, respectively.

The dynamic simulations elucidating the material's dynamic behaviors were conducted through the application of Born−Oppenheimer molecular dynamics (BOMD) simulations, as implemented within the openly accessible CP2K/Quickstep package. The systems were subjected to periodic repetition, and focus was solely directed towards processes occurring on the upper surface of the graphene substrate. In each ab initio molecular dynamics (AIMD) simulation, the initial structural configuration underwent optimization, succeeded by an equilibration phase preceding the production period. Canonical (NVT) ensemble sampling was employed for the simulations, utilizing Nose−Hoover thermostats with a time step of 1.0 fs, while maintaining a finite temperature of 300 K. The core electrons of the atoms were characterized by Goedecker-Teter-Hutter pseudopotentials, and their valence states were represented using the Gaussian-type MOLOPT DZVP-MOLOPT-SR-GTH basis set of double-zeta polarized quality sourced from the CP2K package.

Supplementary Figures

Supplementary Figure 1. (a-b) FESEM and (c) HR-TEM images of the SiO2@RF nanospheres. (d) TEM, (e) HR-TEM, and (f) SAED images of Fe-N2O2-C10. (g) TEM, (h) HR-TEM, and (i) SAED images of Fe-N4-C6O2. (j) TEM, (k) HR-TEM, and (l) SAED images of Fe-N4-C10.

Supplementary Figure 2. (a) Pore size diameter distributions of the Fe-N4-C6O2 analyzed by Horvath-Kawazoe (HK, Micropores) and Barrett-Joyner-Halenda (BJH, Mesopores). (b) Pore size diameter distributions of the Fe-N4-C6O2 analyzed by mercury intrusion porosimetry (MIP, Macropores). (c) Nitrogen adsorption isotherms of the Fe-N4-C6O2.

Supplementary Figure 3. (a) FESEM and (b) EDS mapping images of Fe-N4-C6O2.

Supplementary Figure 4. Fe K-edge EXAFS (line) and the curve fit (circle) analysis for (a) Fe-N2O2-C10 and (b) Fe-N4-C10 in R-space.

Supplementary Figure 5. Atomic structure of Fe-N4 and Fe-N2+2 active sites of Fe-SACs.

Supplementary Figure 6. Raman spectroscopy of Fe-SACs.

Supplementary Figure 7. HR-XPS spectra of (a) C 1s, (b) N 1s, (c) O 1s, and (d) Fe 2p of Fe-N4-C6O2.

Supplementary Figure 8. HR-XPS spectra of (a) C 1s, (b) N 1s, and (c) O 1s of N/O-C.

Supplementary Figure 9. The possible mechanism for the formation of the Fe-N4-C6O2 structure.

Supplementary Figure 10. (a) Schematic diagram of the structure of Fe-N4-C10, PMS and Fe-N4-C6O2. The adsorption of different PMS sites (O1, O2, and O3) on (b) Fe-N4-C10 and (c) Fe-N4-C6O2 calculated by DFT.

Supplementary Figure 11.The structures of reaction intermediates in Fe-SACs/PMS system.

Supplementary Figure 12. (a) The free energy diagram of PMS activation through homolytic cleavage on Fe-SACs. (b) The free energy diagram of PMS activation through single electron transfer on Fe-SACs.

For radical pathway, the generation of SO4•− and •OH via the direct homolytic cleavage of the O-O bond was proved to be thermodynamically unfavorable (1.11 eV) for three Fe-SACs (Figure S12a). Although the formation of radical through the single electron transfer pathway was thermodynamically possible in the three Fe-SACs systems, FeIV=O was more inclined to be formed than radicals due to lower ΔG (Figures 3e, 3g, and S12b).

Supplementary Figure 13. (a) The HPLC spectra of BPA in the Fe-N4-C6O2/PMS at different times. (b) Degradation of BPA in the Fe-SACs/PMS system. (c) Degradation of BPA in the N/O-C/PMS and N-C/PMS system. Reaction conditions: [catalysts]=0.05 g L-1, [PMS]0=400 μM, pH=7.0, [BPA]0=50 μM, [MeOH]/[PMS]=1000 if need.

Supplementary Figure 14. Influence of (a) Fe-N4-C6O2 dosage, (b) PMS dosage, and (c) pH on the degradation of BPA in Fe-N4-C6O2/PMS system. Reaction conditions: (a) [PMS]0=400 μM, pH=7.0 (b) [Fe-N4-C6O2]=0.05 g L-1, pH=7.0. (c) [Fe-N4-C6O2]=0.05 g L-1, [PMS]0=400 μM. In all experiments, [BPA]0=50 μM.

To further achieve optimal reaction conditions and explore the most reactive Fe-N4-C6O2/PMS system, the catalyst dosage, PMS dosage, and pH were systematically investigated (Figure S14). As can be seen from Figure S14a, the degradation of BPA was significantly influenced by the amount of Fe-N4-C6O2 catalyst. Fe-N4-C6O2 with a dose of 0.1 g L-1 can achieve 100% ultra-fast removal of BPA in 30 s. This fact is attributed to the increase in catalyst dosage, more active centers can participate in the advanced oxidation process to accelerate the degradation of BPA. Besides, the contaminant adsorbed on the catalyst increased with the increase of Fe-N4-C6O2 dosage, improving the degradation efficiency. The degradation performance of BPA by the Fe-N4-C6O2/PMS system at varying PMS concentrations was further studied (Figure S14b). In the beginning, the degradation efficiency of BPA increased with the increase of the dosage of PMS, which may be due to the production of more reactive oxygen species (ROS) at higher concentrations of PMS. Subsequently, when the concentration of PMS increased further, the degradation efficiency remained almost unchanged, which shows that the degradation of BPA may be not carried out through the free radical mechanism. As shown in Figure S14c, 100% degradation of BPA was achieved in just 2 min at all pH conditions, indicating that the activity of the Fe-N4-C6O2 catalyst is hardly affected by pH. Considering the organic pollutants removal efficiency and reagent cost, 0.05 g L-1 Fe-N4-C6O2 was chosen to activate 400 μM PMS to degrade 50 μM BPA (pH=7) in Fe-N4-C6O2/PMS system.

Supplementary Figure 15. (a) Removal of BPA during homogeneous catalyst/PMS system and Fe-N4-C6O2 /PMS system. (b) Removal of BPA during other catalysts/PMS systems. Experimental conditions: [BPA]=50 μM, [catalyst]=0.05 g L-1 if need, T=25 °C, pH=7.0, [PMS]0=400 μM.

Supplementary Figure 16. (a) Influence of pH on BPA degradation in the Fe-N4-C6O2/PMS system. (b) Influence of Cl− and HCO3− on BPA degradation in Fe-N4-C6O2/PMS system. (c) Removal of BPA by Fe-N4-C6O2/PMS under complex water conditions. Experimental conditions: [Fe-N4-C6O2]=0.05 g L-1, [BPA]=50 μM, T=25 °C, [Cl−]/[PMS]=25 if need, [HCO3−]/[PMS]=25 if need, pH=7 without special requirements. Other experimental conditions, pH=7.0.

Supplementary Figure 17. Removal of (a) 2,4-DCP, (b) 4-CP, and (c) PE during Fe-N4-C6O2/PMS system. Experimental conditions: [Pollutants]0=20 μM, T=25 °C, pH=7.0, [catalysts]=0.05 g L-1, [PMS]0=400 μM, [MeOH]/[PMS]=1000 if need.

Supplementary Figure 18. The degradation of (a) PNP, (b) FP, (c) PNBD, and (d) PNBA by Fe-N4-C6O2/PMS system at different conditions. Experimental conditions: [contaminants]0=20 μM, [Fe-N4-C6O2]=0.05 g L-1, [PMS]0=400 μM, [MeOH]/[PMS]=1000 if need, [PMSO]/[PMS]=100 if need, T=25 °C, pH=7.0.

Supplementary Figure 19. The degradation of (a) PNP, (b) FP, (c) PNBD, and (d) PNBA by Fe-N4-C6O2/PMS system at different conditions. Experimental conditions: [contaminants]0=20 μM, [Fe-N4-C6O2]=0.05 g L-1, [PMS]0=3 mM, [MeOH]/[PMS]=1000 if need, T=25 °C, pH=7.0.

As illustrated in S17-S19, and Table S4, the FeIV=O generated by the Fe-N4-C6O2/PMS system can also efficiently remove various pollutants with electron-donating groups (EDG), such as 2,4-dichlorophenol (2,4-DCP), p-chlorophenol (4-CP), and phenol (PE), and pollutants with electron-withdrawing groups (EWG), such as p-nitrophenol (PNP), fipronil (FP), p-nitrobenzyl alcohol (PNBA), and p-nitrobenzaldehyde (PNBD). Notably, the removal rates of pollutants containing EWG were significantly lower than those of the substances containing EDG. This is attributed to the high electron density environment of pollutants containing EDG, which provides effective targets for electrophilic attack by FeIV=O9,10.

Supplementary Figure 20. TOF of per metal atom for BPA removal.

Supplementary Figure 21. (a) PXRD pattern of Fe-N2O2-C10-high-metal. (b) Pseudo-first-order rate constant for BPA degradation by Fe-SACs-activated PMS.

Supplementary Figure 22. Schematic diagram of a continuous flow catalytic device. Experimental conditions: [BPA]=40 μM and [PMS]=800 μM, pH=7.0, and T=25 °C, average flow rate 45 L/m2/h.

Supplementary Figure 23. (a) BPA removal performance of Fe-N4-C6O2/MCE/PMS and Fe-N4-C6O2/MCE system. (b) Dissolution of Fe in Fe-N4-C6O2/MCE/PMS system at different times. Experimental conditions: [BPA]=40 μM and [PMS]=800 μM, pH=7.0, and T=25 °C, average flow rate 45 L/m2/h in Fe-N4-C6O2/MCE/PMS system.

As depicted in Figure S22, a continuous flow-through water purification apparatus was designed to test the longevity of Fe-N4-C6O2/MCE composite membrane for BPA removal. The Fe-N4-C6O2/MCE composite membrane alone exhibited limited effectiveness in BPA removal, whereas the Fe-N4-C6O2/MCE/PMS system could completely remove the BPA over the duration of 240 h (Figure S23a). Notably, the leaching of Fe during the continuous flow experiments remained significantly below the recommended limit of 0.3 mg/L in water set by US EPA (Figure S23b)11. The above experiments fully demonstrated that Fe-N4-C6O2 exhibited excellent stability in sustaining PMS activation for pollutant degradation and had immense potential in practical applications.

Supplementary Figure 24. FESEM and energy dispersive X-ray spectroscopy images of Fe-N4-C6O2 after being used for 500 h.

Supplementary Figure 25. PXRD patterns of Fe-N4-C6O2 before and after 500 h of catalysis.

Supplementary Figure 26. (a) ESR spectra for O2•- in the Fe-SACs/PMS/DMPO (MeOH) system. ESR spectra for •OH/SO4•− in the (b) Fe-N4-C6O2/PMS/DMPO (water), (c) Fe-N2O2-C10/PMS/DMPO (water), and (d) Fe-N4-C10/PMS/DMPO (water) system.

Supplementary Figure 27. (a) The amount of PMSO consumption and PMSO2 generation during the Fe-SACs/PMS system. (b)The conversion rate of PMSO2 during the Fe-SACs/PMS system. Experimental conditions: [Fe-SACs]=0.05 g L-1, [PMS]=400 μM, T=25 °C, pH=7.0, [PMSO] =50 μM, t=2 min.

Supplementary Figure 28. ESR spectra recorded in H2O- and D2O-based (a) Fe-N2O2-C10/PMS/TEMP system, (b) Fe-N4-C6O2/PMS/TEMP system, and (b) Fe-N4-C10/PMS/TEMP system.

Previous studies have demonstrated that 1O2 quenching such as azide, L-histidine or furfuryl alcohol consume PMS, resulting in false positive4,12. Therefore, the presence of 1O2 is not directly verified by quenching experiments in this paper.

Supplementary Figure 29. Pseudo-first-order rate constants for phenolic compounds degradation by (a) RB (under visible light irradiation), (b) Fe-N2O2-C10/PMS system, (c) Fe-N4-C6O2/PMS system, and (d) Fe-N4-C10/PMS system under various pH conditions. Experimental conditions: [BPA]=50 μM if need, [2,4-DCP]=20 μM if need, [Catalysts]=0.05 g L-1, [PMS]=400 μM, T=25 °C, pH=7.0, [MeOH/PMS]=1000 and [PMSO/PMS]=100 in Fe-SACs/PMS system.

In 1O2 oxidation (visible-lightirradiated RB solution), the degradation rates of the two pollutants increased significantly with increasing pH. This may be attributed to the fact that with the increase of pH, phenolic compounds are more readily dissociated into phenolate anions which are more easily oxidized by 1O213. However, under the quenching of excess methanol and PMSO, the pH dependence of BPA and 2,4-DCP during the non-radical degradation of Fe-SACs/PMS was completely opposite to that of 1O2 oxidation process. This result also refuted the possibility that the oxidation process is accompanied by the formation of 1O2 and proved that the ETP exists.

Supplementary Figure 30. Open circuit potential in different systems. Calomel electrode and platinum wire electrode were used as reference electrodes and opposite electrodes, respectively. Experimental conditions: V(Na2B2O4, 0.02 M) : V(PMS, 10 mM) : V(BPA, 150 μM)=6 mL : 1 mL : 1 mL, sample interval:0. 1 s, run time: 1800 s.

Supplementary Figure 31. Electron transfer mechanism.

Supplementary Figure 32. The pseudo-first-order kinetic fitting on BA and pCBA in (a) Fe-N4-C10/PMS and (b) Fe-N4-C6O2/PMS system. Experimental conditions: [catalysts]=0.05 g L-1, [PMS]=400 μM, [BPA]=50 μM, [BA or pCBA]=1 μM, T=25 ℃, pH=7.0. (c) The plots of ŋln[PMSO]0[PMSO]0- 1ŋ[PMSO2] versus time in the Fe-N4-C10/PMS and Fe-N4-C6O2/PMS system. Experimental conditions: [Catalysts]=0.05 g L-1, [PMS]=400 μM, [PMSO]=5 μM, [BPA]=50 μM, T=25 ℃, pH=7.0.

Supplementary Figure 33. (a) Schematic representation of bonding information for the Fe=O portion of FeIV=O. (b) Different iron species in Fe-N4-C6O2 and Fe-N4-C10.

Supplementary Figure 34. LC-MS total ion chromatography (TIC) for BPA during the degradation process. Reaction conditions: [Fe-N4-C6O2]=0.02 g L-1, [PMS]0=400 μM, [BPA]0=50 μM, pH=7.0, reaction time=1 min.

Supplementary Figure 35. (a-q) ESI mass spectra of various BPA degradation intermediates. Reaction conditions: [Fe-N4-C6O2]=0.02 g L-1, [PMS]0=400 μM, [BPA]0=50 μM, pH=7.0, reaction time=1 min.

Supplementary Figure 36. GC-MS chromatogram of various BPA degradation intermediates. Reaction conditions: [Fe-N4-C6O2]=0.02 g L-1, [PMS]0=400 μM, [BPA]0=50 μM, pH=7.0, reaction time=1 min.

Supplementary Figure 37. (a-d) EI mass spectra of BPA during the degradation process. Reaction conditions: [Fe-N4-C6O2]=0.02 g L-1, [PMS]0=400 μM, [BPA]0=50 μM, pH=7.0, reaction time=1 min.

Supplementary Figure 38. Proposed pathways for the BPA degradation in the Fe-N4-C6O2/PMS system.

According to the intermediates of BPA degradation identified by LC-MS and GC-MS techniques (Figures S34-S37 and Tables S9-S10), two possible degradation pathways for the BPA degradation in Fe-N4-C6O2/PMS system were proposed (Figure S38). Among them, the molecules marked red (HI1-HI7) and black (I1-I15) are hypothetical intermediates and experimentally detected intermediates, respectively. Substances marked green were presumed transition state species. In these two pathways, BPA was oxidized by FeIV=O through oxygen atom transfer (OAT) reaction, electrophilic addition and H-abstraction/O-rebound mechanism. Among them, the OAT reaction was that the electrons of the pollutants are filled into the low-lying σ* orbitals of Fe/O to form the substrate-O-Fe collinear transition state14. Next, another electron transfer occurred between the substrate and the Fe center in this transition state, which led to the breaking of the Fe-O bond and the transfer of oxygen atoms, resulting in the oxidation of pollutants and the reduction of FeIV=O species. Electrophilic addition refers to the hydroxylation of aromatic ring was promoted by FeIV=O species, which usually consists of two steps15. In the initial step, the carbon with high π electron density on the aromatic ring was electrophilic attacked by FeIV=O to form a radical σ-complex. The intermediate then underwent a ring rearrangement and again triggered the transfer of electrons from the carbon to the metal, thus hydroxylating the aromatic ring. In the H-abstraction/O-rebound mechanism, the cleavage of C-H bond and the formation of C-O-H bond were divided into two successive steps. First, a hydrogen atom from hydrocarbons was extracted by FeIV=O species to form high valent iron hydroxyl (FeIII-OH) and aliphatic radical intermediates16-18. Following hydrogen extraction, the generated radical intermediates rapidly recombined with FeIII-OH species, transferring oxygen atoms to organic substrates through the so-called “oxygen rebound” mechanism to form hydroxylated substances. This step not only completed the oxidation of organic substrates. The iron species were also regenerated into their original state, allowing the catalytic cycle to continue. Overall, at the core of all three oxidation mechanisms was the filling of pollutant electrons into the low σ* orbital of Fe/O in FeIV=O, forming a substrate-O-Fe intermediate.

In pathway P1, the quaternary carbon atom located in the center of the BPA molecule was attacked by FeIV=O due to its high frontier electron density, resulting in the formation of 4-isopropenyl radical (R1) and phenyl (R2) radical through the β-scission19,20. Subsequently, R1 could be oxidized to intermediate I1 by FeIV=O species. The high reactivity between the C=C bond in intermediate I1 and FeIV=O made them easy to form the hypothetical intermediates HI1 and ≡FeII via the OAT pathway. HI1 then undergoes demethylation to form intermediate I2. Following this, intermediate I2 reacted with the FeIV=O species to generate intermediate HI2 and ≡FeII through a H-abstraction/O-rebound mechanism. The generated HI2 reacted with FeIV=O via an electrophilic addition mechanism to form I3 and ≡FeII. Intermediate I3 was subsequently oxidized to form ring-opened products, ultimately degrading into CO2 and H2O. In addition, the carbonyl carbon atom in intermediate HI1 was attacked by FeIV=O, thus forming radical R3 and methyl radicals (•CH3) through an α-scission reaction. The radical R3 could react with FeIV=O to form intermediate HI2, while •CH3 and R1 were further transformed into 4-(tert-butyl) phenol (HI3) via a C-C coupling reaction. On the one hand, the aromatic ring in intermediate HI3 lost an electron via the electron transfer to form a phenolic radical (R4). On the other hand, the C-C bond between the isobutyl and phenyl ring in HI3 was attacked by FeIV=O, leading to the formation of the isobutyl radical (R5) and phenyl radical (R2) through a β-scission reaction. These radicals could be further converted to 2,4-di-tert-butylphenol (I4-2), 2-(tert-butyl)phenol (HI4), and 3-(tert-butyl)phenol (HI5) by reorganization. Similarly, intermediates HI4 and HI5 could form four types of di-tert-butylphenol (I4-1-I4-2) via the electron transfer and radical reorganization reactions. Subsequently, I4-1 and I4-4 could react with FeIV=O via an electrophilic addition mechanism to generate hydroxylated intermediate I5, which was further oxidized and converted into I6. With further oxidation, these compounds were gradually converted into organic acids and eventually fully mineralized.

In pathway P2, on the one hand, the radical R2 could react with FeIV=O to form hydroquinone (HI6) and ≡FeII via electrophilic addition reaction. The resulting HI6 can be readily oxidized by FeIV=O to benzoquinone (HI7), which was further ring-opened to form intermediate I10. The generated intermediate I10 could be further oxidised into CO2 and H2O by FeIV=O. On the other hand, radicals R2 form (1,1'-biphenyl)-4,4'-diphenol (I7) through self-reorganization. Next, I7 was gradually oxidized to ring-opening product I8, which was further oxidized toI9 and ultimately mineralized into CO2 and H2O.

Supplementary Figure 39. The TOC removal efficiency of BPA in Fe-N4-C6O2/PMS system. Experimental conditions: [BPA]0=50 μM, T=25 °C, pH=7.0, [Fe-N4-C6O2]=0.1 g L-1 or 0.05 g L-1, [PMS]0=400 μM, reaction time=2 min.

Supplementary Tables

Supplementary Table 1. Synthetic conditions of different samples.

| Catalysts | synthetic conditions |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | FeCl2·4H2O (mmol) | 1,10-phenanthroline (mmol) | (S,S)-(+)-N,N'-Bis(3,5-di-tert-butylsalicylidene)-1,2-cyclohexanediamine | SiO2 a/SiO2@RF b/ SiO2@N-Cc (g) | Calcination | Etching |
| Fe-N2O2-C10 | 0.5 | / | 1.5 | 3c | 2 °C min-1, 700 °C, 2h | 5 wt % HF, 12h |
| Fe-N2O2-C10-high metal | 0.5 | / | 0.6 | 3c | 2 °C min-1, 700 °C, 2h | 5 wt % HF, 12h |
| Fe-N4-C6O2 | 0.5 | 2 | / | 3b | 2 °C min-1, 700 °C, 2h | 5 wt % HF, 12h |
| Fe-N4-C10 | 0.5 | 2 | / | 3a | 2 °C min-1, 700 °C, 2h | 5 wt % HF, 12h |
| Fe NPs/NC | 0.5 | 2 | / | / | 2 °C min-1, 700 °C, 2h | 5 wt % HF, 12h |
| N/O-C | / | 2 | / | 3b | 2 °C min-1, 700 °C, 2h | 5 wt % HF, 12h |
| N-C | / | 2 | / | 3a | 2 °C min-1, 700 °C, 2h | 5 wt % HF, 12h |

Supplementary Table 2. Curve fit Parameters for Fe K-edge EXAFS for FePC and Fe-SACs.

| Sample | Scattering path | CN | R/Å | σ2/Å2 | ∆E0/eV | R-factor |
| --- | --- | --- | --- | --- | --- | --- |
| FePC | Fe-N | 4.0 | 1.98 ± 0.03 | 0.007 ± 0.002 | 0.5 ± 2.0 | 0.011 |
| Fe-N2O2-C10 | Fe-N | 2.0 | 2.00 ± 0.05 | 0.003 ± 0.002 | -6.4 ± 3.3 | 0.018 |
|  | Fe-O | 2.4 | 2.23 ± 0.08 | 0.008 ± 0.005 |  |  |
| Fe-N4-C6O2 | Fe-N1 | 2.2 | 1.91 ± 0.01 | 0.002 ± 0.001 | -2.0 ± 1.3 | 0.014 |
|  | Fe-N2 | 2.1 | 2.09 ± 0.09 | 0.003 ± 0.004 |  |  |
| Fe-N4-C10 | Fe-N | 4.4 | 1.97 ± 0.01 | 0.009 ± 0.003 | -2.8 ± 1.8 | 0.016 |

Where，σ2 stands for the Debye-Waller factor. ΔE stands for threshold energy correction; R-factor (%) indicates the goodness of the fit.

Supplementary Table 3. Mössbauer parameters and assignment of feature components in the deconvoluted Mössbauer spectra.

| Catalysts | Component | δiso (mm/s) | ∆EQ (mm/s) | Γ(mm/s) | Area (%) a | Assignment b |
| --- | --- | --- | --- | --- | --- | --- |
| Fe-N4-C10 | D1 | 0.22 | 2.30 | 0.98 | 60.6 | FeIIN2+2, MS |
|  | D2 | 0.11 | 0.77 | 0.46 | 33.2 | FeIIIN2+2, MS |
|  | D3 | 1.10 | 2.13 | 0.32 | 6.2 | N-FeIIN2+2, HS |
| Fe-N4-C6O2 | D4 | 0.50 | 2.00 | 0.88 | 2.6 | FeIIIN4/C, LS |
|  | D5 | 0.26 | 1.14 | 0.88 | 71.5 | FeⅡN4/C, LS |
|  | D6 | 0.24 | 2.90 | 0.88 | 22.6 | FeⅡN4/C, MS |
|  | D7 | 0.90 | 3.30 | 0.42 | 3.3 | FeⅡN4/C, HS |

a The relative absorption area of each iron species in Fe-SACs samples. b LS, MS, and HS denote low-spin, medium-spin, and high-spin, respectively.

Supplementary Table 4. The molecular structures of the organic substance used in this study and the HPLC conditions used to analyze them.

| No. | Contaminant | Molecular Structure | Formula | Molar Mass (g mol-1) | Eluent | flow rate (mL min-1) | λ (nm) | Retention time (min) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | BPA |  | C15H16O2 | 228.29 | 30% ultrapure water + 70% methanol | 1 | 276 | 3.489 |
| 2 | 2,4-DCP |  | C6H4Cl2O | 163.00 | 20% ultrapure water + 80% methanol | 1 | 286 | 2.954 |
| 3 | 4-CP |  | C6H5ClO | 128.56 | 30% ultrapure water + 70% methanol | 1 | 281 | 3.004 |
| 4 | PE |  | C₆H₆O | 94.11 | 40% ultrapure water + 60% methanol | 1 | 270 | 2.705 |
| 5 | PMSO |  | C7H8OS | 140.03 | 70% ultrapure water + 30% acetonitrile | 1 | 232 | 2.485 |
| 6 | PMSO2 |  | C7H8O2S | 156.20 | 70% ultrapure water + 30% acetonitrile | 1 | 264 | 3.969 |
| 7 | PNP |  | C6H5NO3 | 139.11 | 40% ultrapure water+ 60% methanol | 1 | 316 | 3.004 |
| 8 | FP |  | C12H4Cl2F6N4OS | 437.15 | 20% ultrapure water + 80% methanol | 1 | 270 | 3.357 |
| 9 | PNBD |  | C7H5NO3 | 151.12 | 40% ultrapure water + 60% methanol | 1 | 266 | 3.145 |
| 10 | PNBA |  | C7H7NO3 | 153.14 | 40% ultrapure water + 60% methanol | 1 | 274 | 2.653 |
| 11 | BA |  | C7H6O2 | 122.04 | 95% 0.02 M ammonium acetate solution + 5% acetonitrile | 1 | 230 | 3.561 |
| 12 | pCBA |  | C7H5ClO2 | 156.00 | 90% ultrapure water + 10% acetonitrile | 1 | 233 | 3.787 |

Supplementary Table 5. Comparison between Fe-N4-C6O2 and the previously reported metal-based catalysts in the catalytic performance.

| Catalysts （Dosage, g/L） | Metal (wt%) | Contaminant (μM) | PMSa/PDSb/PSc (mM) | pH | Removal Efficiency | k (min-1) | k-value (μmol s-1 g-1) | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| nZVI/kaolinite (0.5) | ~80 | BPA (109.5) | 1.00 a | 7.0 | 15 min (~90%) | 0.212 | 0.77 | 21 |
| Mn1.8Fe1.2O4 (0.1) | / | BPA (43.8) | 0.65 a | 7.5 | 30 min (95%) | 0.100 | 0.73 | 22 |
| Fe0.8Co2.2O4 (0.1) | / | BPA (87.6) | 0.65 a | 6.0 | 60 min (95%) | 0.049 | 0.72 | 23 |
| CuFe2O4-Fe2O3 (0.2) | / | BPA (21.9) | 1.17 a | 7.0 | 10 min (100%) | 0.620 | 1.13 | 24 |
| Fe1Mn5Co4-N@C (0.1) | / | BPA (87.6) | 0.65 a | 6.0 | 10 min (100%) | 0.480 | 7.01 | 25 |
| Co3O4-Bi2O3 (0.3) | / | BPA (87.6) | 0.65 a | 7.0 | 30 min (98.5%) | 0.122 | 0.59 | 26 |
| CoMnAl-MMO (0.02) | / | BPA (43.8) | 0.65 a | 3.6 | 90 min (100%) | 0.058 | 2.12 | 27 |
| Fe3Co7@C-650 (0.1) | / | BPA (87.6) | 0.65 a | 6.0 | 30 min (98%) | 0.132 | 1.93 | 28 |
| DPA-hematite (0.5) | / | BPA (65.7) | 6.50 a | 7.0 | 120 min (100%) | 0.039 | 0.09 | 29 |
| Co-doped MIL-53-NH2 (0.25) | / | BPA (219.0) | 0.5 (g L-1) c | 4.0 | 73 min (90%) | ＜0.030 | ＜0.44 | 30 |
| Co-TPML (0.2) | 0.04 | BPA (50.0) | 2.00 a | 3.5 | 5 min (100%) | ＜2.500 | ＜10.42 | 31 |
| SA-Fe-NC (0.05) | 1.12 | BPA (100.7) | 1.96 a | 6.7 | 3 min (100%) | 1.990 | 66.33 | 32 |
| FeCo@NC-1 (0.1) | 0.98 (Fe)/ 0.79 (Co) | BPA (87.6) | 0.65 a | 6.0 | 1 min (100%) | 6.062 | 88.50 | 33 |
| Fe@NC (0.1) | / | BPA (87.6) | 0.65 a | 6.0 | 3 min (100%) | 2.370 | 34.60 | 33 |
| Co@NC (0.1) | / | BPA (87.6) | 0.65 a | 6.0 | 2 min (100%) | 4.367 | 63.76 | 33 |
| CoSA/NHCS (0.1) | 1.78 | BPA (87.6) | 0.33 a | 7.0 | 1 min (98%) 2 min (100%) | / | / | 34 |
| CoSA-N4-C (0.05) | 1.17 | BPA (50.0) | 2.0 b | 6.4 | 5 min (96%) | 0.630 | 10.5 | 35 |
| CoSA-N3-C (0.05) | 1.20 | BPA (50.0) | 2.0 b | 6.4 | 4 min (100%) | 1.280 | 21.33 | 35 |
| FeSA-NC-20 (0.15) | 0.88 | BPA (87.6) | 1.30 a | 6.5 | 30 min (100%) | 0.318 | 3.10 | 36 |
| Fe-N2O2-C10 (0.1) | 0.196 | BPA (50.0) | 0.40 a | 7.0 | 5 s (83.7%) 60 s (100%) | 4.558 | 37.983 | This work |
| Fe-N4-C6O2 (0.1) | 2.14 | BPA (50.0) | 0.40 a | 7.0 | 5 s (85.7%) 30 s (100%) | 13.299 | 110.83 |  |
| Fe-N4-C10 (0.1) | 2.63 | BPA (50.0) | 0.40 a | 7.0 | 5 s (49.5%) 120 s (96.1%) | 1.423 | 11.858 |  |

Note: PS and PDS stand for persulfate and peroxodisulfate, respectively.

Supplementary Table 6. The second-order reaction rate constants between quenchers with various ROS (M-1 s-1).

| Quencher | k•OH | kSO4•- | Ref. |
| --- | --- | --- | --- |
| MeOH | 9.7×108 | 3.2 × 106 | 37-40 |

Supplementary Table 7. The second-order reaction rate constants between probe compounds and BPA with various ROS (M−1 s−1).

| Compounds | k•OH | kSO4•- | k1O2 | kO2•- | kFeIV=O | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| BA | 5.9 × 109 | 1.2 × 109 | / | / | / | 41-44 |
| pCBA | 1.5 × 1010 | 1.3 × 1010 | 1.4 × 107 | 8.6 × 107 | / | 37,45,46 |
| PMSO | 3.61 × 109 | 3.17 × 108 | / | / | 2.58 × 103 | 37,41 |
| BPA | 1.7 × 1010 | 1.37 × 109 | 3.0 × 105 | / | 1.08× 103 a | 39,47,48 |
|  |  |  |  |  | 4.6 × 104 b |  |

“a” and “b” represent data provided by this study.

a The second-order reaction rate constants between BPA and FeIV=O generated from Fe-N4-C10.

b The second-order reaction rate constants between BPA and FeIV=O produced from Fe-N4-C6O2.

Supplementary Table 8. The steady-state concentrations, observed pseudo-first-order reaction rate constants, and oxidation contributions to BPA of different  ROS in Fe-SAC/PMS system.

| Oxidation Pathway | Steady-state concentration ([ROS]ss, mol L-1) |  | Observed pseudo-first-order reaction rate constant (kobs,ROS, min-1) |  | Oxidation contribution (%) |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Fe-N4-C10/PMS | Fe-N4-C6O2/PMS | Fe-N4-C10/PMS | Fe-N4-C6O2/PMS | Fe-N4-C10/PMS | Fe-N4-C6O2/PMS |
| ETP | / | / | 0.5069 | 0.7616 | 60.00 | 13.45 |
| •OH | 2.60 × 10-13 | 2.08 × 10-13 | 0.2652 | 0.2124 | 31.40 | 3.75 |
| SO4•- | 2.51 × 10-14 | 3.92 × 10-14 | 2.06 × 10-3 | 3.22 × 10-3 | 0.24 | 0.06 |
| FeIV=O | 1.09 × 10-6 | 1.71 × 10-6 | 0.0706 | 4.6838 | 8.36 | 82.74 |

Supplementary Table 9. Possible intermediates during BPA degradation. The mass spectrometric data were obtained from LC-MS.

| NO. | Compound name | Structure | Marked | Detected | RT (min) | Pseudo-molecular ion | m/z [M-H]obs- | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | pent-2-enoic acid |  | I11-1 |  | 1.79 | [C5H8O2-H]- | 99.05 | 49 |
| 2 | 4-hydroxybenzaldehyde |  | I2 |  | 1.97 | [C7H6O2-H]- | 121.03 | 50 |
| 3 | fumaric acid |  | I11-2 |  | 2.78 | [C4H4O4-H]- | 115.00 | 51 |
| 4 | 3-(3,4-dihydroxyphenyl)pentanedioic acid |  | I9 |  | 3.35 | [C11H12O6-H]- | 239.06 | / |
| 5 | 2-methylmaleic acid |  | I11-3 |  | 4.12 | [C5H6O4-H]- | 129.02 | / |
| 6 | 4-(prop-1-en-2-yl) phenol |  | I1 |  | 4.12 | [C9H10O-H]- | 133.07 | 20,23,51-55 |
| 7 | 3,4-dihydroxybenzoic acid |  | I3 |  | 5.29 | [C7H6O4-H]- | 153.02 | 50,56 |
| 8 | 4,4'-(propane-2,2-diyl) diphenol (BPA) |  | / |  | 7.49 | [C15H16O2-H]- | 227.11 | / |
| 9 | 2,3-dimethylmaleic acid |  | I11-4 |  | 8.82 | [C6H8O4-H]- | 143.03 | / |
| 10 | 2,4-di-tert-butylphenol |  | I4-2 |  | 10.68 | [C14H22O-H]- | 205.19 | 20,53 |
| 11 | 2,5-di-tert-butylphenol |  | I4-3 |  | 10.68 | [C14H22O-H]- | 205.19 | / |
| 12 | 2,6-di-tert-butylphenol |  | I4-1 |  | 10.68 | [C14H22O-H]- | 205.19 | / |
| 13 | 3,5-di-tert-butylphenol |  | I4-4 |  | 10.68 | [C14H22O-H]- | 205.19 | 23 |
| 14 | (E)-3-methylhex-3-enedioic acid |  | I11-5 |  | 16.65 | [C7H10O4-H]- | 157.05 | / |
| 15 | 2,5-dioxohex-3-enedioic acid |  | I10 |  | 29.94 | [C6H4O6-H]- | 170.99 | / |
| 16 | 3-(3,4-dioxocyclohexa-1,5-dien-1-yl)pent-2-enedioic acid |  | I8 |  | 48.72 | [C11H8O6-H]- | 235.02 | / |
| 17 | (1,1'-biphenyl)-4,4'-diol |  | I7 |  | 54.47 | [C12H10O2-H]- | 185.06 | 57 |
| 18 | 1-(4-hydroxyphenyl)ethan-1-one |  | HI1 | / | / | [C8H8O2-H]- | 135.14 | 19,21 |
| 19 | 4-hydroxybenzoic acid |  | HI2 | / | / | [C7H6O3-H]- | 137.02 | 20 |
| 20 | 4-(tert-butyl)phenol |  | HI3 | / | / | [C10H14O-H]- | 149.10 |  |
| 21 | 2-(tert-butyl)phenol |  | HI4 | / | / | [C10H14O-H]- | 149.10 | / |
| 22 | 3-(tert-butyl)phenol |  | HI5 | / | / | [C10H14O-H]- | 149.10 | / |
| 23 | hydroquinone |  | HI6 | / | / | [C6H6O2-H]- | 109.03 | 19,20,49,52,54 |
| 24 | benzoquinone |  | HI7 | / | / | [C6H4O2-H]- | 107.01 | 19-21,52,58 |

Supplementary Table 10. Possible intermediates during BPA degradation. The mass spectrometric data were obtained from GC-MS.

| NO. | Compound name | Structure | Marked | Detected | RT (min) | Molecular ion | m/z [M.+] | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 2,4-di-tert-butylphenol |  | I4-2 |  | 24.76 | C14H22O┐.+ | 206.10 | 20,53 |
| 2 | 2,5-di-tert-butylphenol |  | I4-3 |  | 24.76 | C14H22O┐.+ | 206.10 | / |
| 3 | 2,6-di-tert-butylphenol |  | I5-1 |  | 24.76 | C14H22O┐.+ | 206.10 | / |
| 4 | 3,5-di-tert-butylphenol |  | I4-4 |  | 24.76 | C14H22O┐.+ | 206.10 | 23 |
| 5 | 2,6-di-tert-butylcyclohexa-2,5-diene-1,4-dione |  | I6 |  | 28.27 | C14H20O2┐.+ | 220.00 | 23 |
| 6 | 2,6-di-tert-butylbenzene-1,4-diol |  | I5 |  | 28.87 | C14H22O2┐.+ | 222.00 | / |
| 7 | BPA |  | / |  | 38.86 | C15H16O2┐.+ | 228.00 | / |

Supplementary References

1	Ravel, B. & Newville, M. ATHENA, ARTEMIS, HEPHAESTUS: data analysis for X-ray absorption spectroscopy using IFEFFIT. J. Synchrotron Radiat. 12, 537-541 (2005).

2	Funke, H., Scheinost, A. C. & Chukalina, M. Wavelet analysis of extended x-ray absorption fine structure data. Phys. Rev. B 71, 094110 (2005).

3	Zhang, H. et al. Surfactant-free assembly of mesoporous carbon hollow spheres with large tunable pore sizes. ACS Nano 10, 4579-4586 (2016).

4	Yun, E. T., Lee, J. H., Kim, J., Park, H. D. & Lee, J. Identifying the nonradical mechanism in the peroxymonosulfate activation process: singlet oxygenation versus mediated electron transfer. Environ. Sci. Technol. 52, 7032-7042 (2018).

5	Wang, Z. et al. Is Sulfate Radical Really Generated from Peroxydisulfate Activated by Iron(II) for Environmental Decontamination? Environ. Sci. Technol. 52, 11276-11284 (2018).

6	Zong, Y. et al. Unraveling the Overlooked Involvement of High-Valent Cobalt-Oxo Species Generated from the Cobalt(II)-Activated Peroxymonosulfate Process. Environ. Sci. Technol. 54, 16231-16239 (2020).

7	M. J. Frisch et al. Gaussian, Inc., Wallingford CT (2016).

8	Lu, T. & Chen, F. Multiwfn: a multifunctional wavefunction analyzer. J. Comput. Chem. 33, 580-592 (2012).

9	Yang, M. et al. Unveiling the origins of selective oxidation in single-atom catalysis via Co-N(4)-C intensified radical and nonradical pathways. Environ. Sci. Technol. 56, 11635-11645 (2022).

10	Chen, Y. et al. Facile fabrication of rGO/PPy/nZVI catalytic microreactor for ultrafast removal of p-nitrophenol from water. Appl. Catal. B Environ. 324 (2023).

11	 Vol. EPA 600-R-12-618   (U.S. Environmental Protection Agency, 2012-09).

12	Yang, Y., Banerjee, G., Brudvig, G. W., Kim, J. H. & Pignatello, J. J. Oxidation of organic compounds in water by unactivated peroxymonosulfate. Environ. Sci. Technol. 52, 5911-5919 (2018).

13	Scully Jr, F. E. & Hoigné, J. Rate constants for reactions of singlet oxygen with phenols and other compounds in water. Chemosphere 16, 681-694 (1987).

14	Larson, V. A., Battistella, B., Ray, K., Lehnert, N. & Nam, W. Iron and manganese oxo complexes, oxo wall and beyond. Nature Reviews Chemistry 4, 404-419 (2020).

15	Wang, Z. et al. Aqueous iron(iv)-oxo complex: an emerging powerful reactive oxidant formed by iron(ii)-based advanced oxidation processes for oxidative water treatment. Environ. Sci. Technol. 56, 1492-1509 (2022).

16	Michel, C. & Baerends, E. J. What singles out the FeO2+ moiety? A density-functional theory study of the methane-to-methanol reaction catalyzed by the first row transition-metal oxide dications MO(H2O)p2+,M ) V-Cu. Inorganic Chemistry 48, 3628-3638 (2009).

17	Groves, J. T. & Van der Puy, M. Stereospecific aliphatic hydroxylation by iron-hydrogen peroxide. Evidence for a stepwise process. Journal of the American Chemical Society 98, 5290-5297 (1976).

18	Groves, J. T. & McClusky, G. A. Aliphatic hydroxylation via oxygen rebound. Oxygen transfer catalyzed by iron. Journal of the American Chemical Society 98, 859-861 (1976).

19	Al-Kahtani, A. A., Alshehri, S. M., Naushad, M., Ruksana & Ahamad, T. Fabrication of highly porous N/S doped carbon embedded with ZnS as highly efficient photocatalyst for degradation of bisphenol. Int. J. Biol. Macromol. 121, 415-423 (2019).

20	Du, J. et al. Efficient activation of peroxymonosulfate by magnetic Mn-MGO for degradation of bisphenol A. J. Hazard. Mater. 320, 150-159 (2016).

21	Li, C. et al. Efficient catalytic degradation of bisphenol A coordinated with peroxymonosulfate via anchoring monodispersed zero-valent iron on natural kaolinite. Chem. Eng. J. 448, 137746 (2022).

22	Huang, G. X., Wang, C. Y., Yang, C. W., Guo, P. C. & Yu, H. Q. Degradation of Bisphenol A by peroxymonosulfate catalytically activated with Mn1.8Fe1.2O4 nanospheres: synergism between Mn and Fe. Environ. Sci. Technol. 51, 12611-12618 (2017).

23	Li, X. et al. FexCo3−xO4 nanocages derived from nanoscale metal–organic frameworks for removal of bisphenol A by activation of peroxymonosulfate. Appl. Catal. B Environ. 181, 788-799 (2016).

24	Oh, W.-D., Donga, Z., Hu, Z.-T. & Lim, T.-T. A novel quasi-cubic CuFe2O4–Fe2O3 prepared at low temperature for enhanced oxidation of bisphenol A via peroxymonosulfate activation. J. Mater. Chem. A 3, 22208-22217 (2015).

25	Li, X. et al. Topotactic transformation of metal-organic frameworks to graphene-encapsulated transition-metal nitrides as efficient Fenton-like catalysts. ACS Nano 10, 11532-11540 (2016).

26	Hu, L. et al. Facile synthesis of novel Co3O4-Bi2O3 catalysts and their catalytic activity on bisphenol A by peroxymonosulfate activation. Chem. Eng. J. 326, 1095-1104 (2017).

27	Li, W. et al. Catalytic degradation of bisphenol A by CoMnAl mixed metal oxides catalyzed peroxymonosulfate: Performance and mechanism. Chem. Eng. J. 279, 93-102 (2015).

28	Li, X., Rykov, A. I., Zhang, B., Zhang, Y. & Wang, J. Graphene encapsulated FexCoy nanocages derived from metal–organic frameworks as efficient activators for peroxymonosulfate. Catal. Sci. Technol. 6, 7486-7494 (2016).

29	Oh, W.-D., Lua, S.-K., Dong, Z. & Lim, T.-T. High surface area DPA-hematite for efficient detoxification of bisphenol A via peroxymonosulfate activation. J. Mater. Chem. A 2, 15836-15845 (2014).

30	Lv, S.-W. et al. A novel cobalt doped MOF-based photocatalyst with great applicability as an efficient mediator of peroxydisulfate activation for enhanced degradation of organic pollutants. New J. Chem. 44, 1245-1252 (2020).

31	Chu, C. et al. Cobalt single atoms on tetrapyridomacrocyclic support for efficient peroxymonosulfate activation. Environ. Sci. Technol. 55, 1242-1250 (2021).

32	Gao, Y. et al. Unraveling the high-activity origin of single-atom iron catalysts for organic pollutant oxidation via peroxymonosulfate activation. Environ. Sci. Technol. 55, 8318-8328 (2021).

33	Yang, J. et al. A highly efficient Fenton-like catalyst based on isolated diatomic Fe-Co anchored on N-doped porous carbon. Chem. Eng. J. 404, 126376 (2021).

34	Xu, Z. et al. Co single-atom confined in N-doped hollow carbon sphere with superb stability for rapid degradation of organic pollutants. Chem. Eng. J. 452, 139229 (2023).

35	Liang, X. et al. Engineering the low-coordinated single cobalt atom to boost persulfate activation for enhanced organic pollutant oxidation. Appl. Catal. B Environ. 303, 120877 (2022).

36	Yang, T., Fan, S., Li, Y. & Zhou, Q. Fe-N/C single-atom catalysts with high density of Fe-Nx sites toward peroxymonosulfate activation for high-efficient oxidation of bisphenol A: Electron-transfer mechanism. Chem. Eng. J. 419, 129590 (2021).

37	Wu, Q. Y., Yang, Z. W., Wang, Z. W. & Wang, W. L. Oxygen doping of cobalt-single-atom coordination enhances peroxymonosulfate activation and high-valent cobalt-oxo species formation. Proc. Nat. Acad. Sci. U.S.A. 120, e2219923120 (2023).

38	Li, X. et al. CoN1O2 single-atom catalyst for efficient peroxymonosulfate activation and selective Cobalt(IV)=O generation. Angew. Chem. Int. Ed. 62, e202303267 (2023).

39	Ren, W. et al. Origins of electron-transfer regime in persulfate-based nonradical oxidation processes. Environ. Sci. Technol. 56, 78-97 (2021).

40	Guan, Y. H., Ma, J., Li, X. C., Fang, J. Y. & Chen, L. W. Influence of pH on the formation of sulfate and hydroxyl radicals in the UV/peroxymonosulfate system. Environ. Sci. Technol. 45, 9308-9314 (2011).

41	Wang, Z. et al. High-valent iron-oxo species mediated cyclic oxidation through single-atom Fe-N6 sites with high peroxymonosulfate utilization rate. Appl. Catal. B Environ. 305, 121049 (2022).

42	Liu, B. et al. Peroxymonosulfate activation by cobalt(II) for degradation of organic contaminants via high-valent cobalt-oxo and radical species. J. Hazard. Mater. 416, 125679 (2021).

43	Cong, J., Wen, G., Huang, T., Deng, L. & Ma, J. Study on enhanced ozonation degradation of para-chlorobenzoic acid by peroxymonosulfate in aqueous solution. Chem. Eng. J. 264, 399-403 (2015).

44	Tian, L. et al. Selective oxidation of diclofenac sodium with different electronegative moieties via coexisting SO·−and ·OH. Sci. Total Environ. 782, 146857 (2021).

45	Guo, Y., Long, J., Huang, J., Yu, G. & Wang, Y. Can the commonly used quenching method really evaluate the role of reactive oxygen species in pollutant abatement during catalytic ozonation? Water Res. 215, 118275 (2022).

46	Gao, L., Guo, Y., Zhan, J., Yu, G. & Wang, Y. Assessment of the validity of the quenching method for evaluating the role of reactive species in pollutant abatement during the persulfate-based process. Water Res. 221, 118730 (2022).

47	Sanchez, P. M., Abdel daiem, M. M., Ocampo, P., R., Rivera, U., J. & Mota, A. J. Comparative study of the photodegradation of bisphenol A by HO(*), SO4(*-) and CO3(*-)/HCO3 radicals in aqueous phase. Sci. Total Environ. 463, 423-431 (2013).

48	Ding, J. et al. Electrochemical activation of persulfate on BDD and DSA anodes: Electrolyte influence, kinetics and mechanisms in the degradation of bisphenol A. J. Hazard. Mater. 388, 121789 (2020).

49	Qian, K. et al. Single-atom Fe catalyst outperforms its homogeneous counterpart for activating peroxymonosulfate to achieve effective degradation of organic contaminants. Environ. Sci. Technol. 55, 7034-7043 (2021).

50	Oh, W.-D., Lok, L.-W., Veksha, A., Giannis, A. & Lim, T.-T. Enhanced photocatalytic degradation of bisphenol A with Ag-decorated S-doped g-C3N4 under solar irradiation: Performance and mechanistic studies. Chem. Eng. J. 333, 739-749 (2018).

51	Jia, Y. et al. Oxygen vacancy rich Bi2O4-Bi4O7-BiO2-x composites for UV-vis-NIR activated high efficient photocatalytic degradation of bisphenol A. J. Hazard. Mater. 382, 121121 (2020).

52	Tan, X. et al. Three-dimensional MnO2 porous hollow microspheres for enhanced activity as ozonation catalysts in degradation of bisphenol A. J. Hazard. Mater. 321, 162-172 (2017).

53	Li, Y. et al. Uniform N-coordinated single-atomic iron sites dispersed in porous carbon framework to activate PMS for efficient BPA degradation via high-valent iron-oxo species. Chem. Eng. J. 389, 124382 (2020).

54	Chang, C., Zhu, L., Fu, Y. & Chu, X. Highly active Bi/BiOI composite synthesized by one-step reaction and its capacity to degrade bisphenol A under simulated solar light irradiation. Chem. Eng. J. 233, 305-314 (2013).

55	Xie, Y. et al. Thermally treated fungal manganese oxides for bisphenol A degradation using sulfate radicals. Chem. Eng. J. 335, 728-736 (2018).

56	Darsinou, B., Frontistis, Z., Antonopoulou, M., Konstantinou, I. & Mantzavinos, D. Sono-activated persulfate oxidation of bisphenol A: Kinetics, pathways and the controversial role of temperature. Chem. Eng. J. 280, 623-633 (2015).

57	Liu, Y. et al. Sandwich-like Co3O4/MXene composite with enhanced catalytic performance for Bisphenol A degradation. Chem. Eng. J. 347, 731-740 (2018).

58	Khan, M. A. N. et al. Metal-organic framework-derived hollow Co3O4/carbon as efficient catalyst for peroxymonosulfate activation. Chem. Eng. J. 363, 234-246 (2019).