Bimetallic Chalcogenides Enable Highly Efficient Polysulfide Capture and Conversion in Lean-Electrolyte Li-S Batteries

Junhua Wang1,5, #, Hao Sun2,5 #, Weiran Zhao3,5 #, Chongxiang Pan4, Rongrong Li4, Yuan Yao4, *, Caiyun Chang5, *

1 Weifang University, Weifang 261061, China.

2Department of Computer Science and Technology, Institute for Artificial Intelligence，Tsinghua University, Beijing 100091, China.

3State Key Laboratory of Fine Chemicals, School of Chemical Engineering, Dalian University of Technology, Dalian 116024, China.

4CAS Center for Excellence in Nanoscience, Beijing Key Laboratory of Micro-Nano Energy and Sensor, Beijing Institute of Nanoenergy and Nanosystems, Chinese Academy of Sciences, Beijing 101400, China

5Faculty of Materials Science and Energy Engineering/Institute of Technology for Carbon Neutrality, Shenzhen Institute of Advanced Technology, Chinese Academy of Sciences, Shenzhen 518055, China.

# These authors contributed equally.

*Corresponding author E-mail: yaoyuancy1017@163.com; cy.chang@siat.ac.cn.

Figure S1. SEM images of (Co, Ni)9S8@CNF.

Figure S2. (a) SEM image and (b) EDS elemental mappings of (Co, Ni)9S8@CNF nanofiber.

Figure S3. (a) The contents of Co, Ni and S in the (Co, Ni)9S8. (b) XRD patterns of CNFs/S, Co9S8@CNFs/S, and (Co, Ni)9S8@CNFs/S. (c) The resistivity and electrical conductivity of the three hosts.

Figure S4. XPS survey spectra of CNFs, Co9S8@CNFs, and (Co, Ni)9S8@CNFs (a) before and (b) after adsorbing test.

Figure S5. (a) S 2p core level of precipitate recovered from (Co, Ni)9S8@CNFs soaking Li2Sx solution. (b) Co 2p core level of the pristine Co9S8@CNFs and precipitate recovered from Co9S8@CNFs/Li2Sx suspension.

Figure S6. The band gap of (a) pure Co9S8 and (b) pure (Co, Ni)9S8. The total density of states (TDOS) for (c) pure Co9S8 and (d) pure (Co, Ni)9S8, and polysulfides on the (311) surfaces.

Figure S7. Optimized configurations for the binding of Li2S4 and Li2S6 on top view and side view of Co9S8, and (Co, Ni)9S8 (311).

Figure S8. CVs of (a) CNFs/S, (b) Co9S8@CNFs/S (c) (Co, Ni)9S8@CNFs/S at various scan rates from 0.1 to 0.8 mV s-1.

Figure S9. CV curves of the Li-S batteries with (a) CNFs/S, (b) Co9S8@CNFs/S, and (c) (Co, Ni)9S8@CNFs/S as cathode at various temperatures. (d) Polarization voltage gaps of anodic peaks c and cathodic peaks b.

Figure S10. The discharge-charge curves of (a) CNFs/S and (b) Co9S8@CNFs/S at current densities ranging from 0.1 C to 5.0 C, and (c) (Co, Ni)9S8@CNFs/80.0S at current densities ranging from 0.1 C to 2.0 C.

Figure S11. TG curves of (Co, Ni)9S8@CNFs with high sulfur loading.

Table S1. The resistances of lithium-sulfur batteries with CNFs/S, Co9S8@CNFs/S, and (Co, Ni)9S8@CNFs/S cathodes after first and after 400th discharge at 0.1 C.

| Fitted Data | CNFs/S |  |  | Co9S8@CNFs /S |  |  | (Co,Ni)9S8@CNFs /S |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Rs | Rct | Rl | Rs | Rct | Rl | Rs | Rct | Rl |
| After first | 4.2 | 16.1 | 42.5 | 4.3 | 47.9 | 92.8 | 3.7 | 68.2 | 34.5 |
| After 400th cycling | 5.9 | 26.2 | 16.8 | 4.5 | 12.9 | 12.0 | 4.1 | 23.1 | 7.4 |

Here, Rs represents the resistance of the electrolyte, Rct is assigned to the resistance of the charge-transfer resistance, Rl is the resistance of the deposition of the insoluble Li2S2/Li2S on the surface.

Table S2 Li-S battery performance based on catalyst-anchored carbon cathodes.

| Cathodes | Sulfur content (wt %) | E/S ratio (μl mg-1) | Initial capacity (mAh g-1) | Cycle number |  | Decay rate per cycle | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Ni-MoS2/rGO | 68.4 | 5 | ~900 | 140 | 0.198% (0.5 C) |  | [1] |
| Ti3C2/C | 53.4 | 28 | 1180 | 200 | 0.165% (0.5 C) |  | [2] |
| Co9S8@CNTs | 68.67 | 15 | 1019 | 30 | 0.543% (0.5 C) |  | [3] |
| Ni3(HITP)2-CNT | 65.5 | 20 | 968 | 300 | 0.116% (1.0 C) |  | [53] |
| NiCo-LDH@rGO | ~75 | 15 | 1336 | 100 | 0.251% (0.1 C) |  | [4] |
| CC@NiCo2O4 | ~70 | - | ~1000 | 200 | 0.170% (0.2 C) |  | [5] |
| Co9S8@NCNHP | - | 20 | 1186 | 200 | 0.135% (0.2 C) |  | [39] |
| (Co, Ni)9S8@CNF | 83.3 | 5 | 890 | 180 | 0.110% (0.1 C) |  | This work |

References

[1] R. Zhang, Y. Dong, M. A. Al-Tahan, Y. Zhang, R. Wei, Y. Ma, C. Yang, J. Zhang. J. Energy Chem. 2021, 60, 85-94.

[2] H. Y. Zhou, Z. Y. Sui, K. Amin, L. W. Lin, H. Y. Wang, B. H. Han. ACS Appl. Mater. Interfaces 2020, 12 (12), 13904-13913.

[3] J. Zhou, X. Liu, J. Zhou, H. Zhao, N. Lin, L. Zhu, Y. Zhu, G. Wang, Y. Qian. Nanoscale Horiz. 2019, 4 (1), 182-189.

[4] D. Cai, M. Lu, Li, J. Cao, D. Chen, H. Tu, J. Li, W. Han. Small 2019, 15 (44), 1902605-1902615.

[5] W. Qiu, G. Li, D. Luo, Y. Zhang, Y. Zhao, G. Zhou, L. Shui, X. Wang, Z. Chen. Adv. Sci. (Weinh) 2021, 8 (7), 2003400-2003410.