Mechanochemical synthesis, characterization and reactivity of a room temperature stable calcium electride

Alex W. J. Bowles,a§ James A. Quirk,b§ Yu Liu,a George H. Morritt,c Marina Freitag,b George F. S. Whitehead,d Adam W. Woodward,d Adam Brookfield,e Conrad A. P. Goodwin,d David Collison,e Floriana Tuna,e* Claire L. McMullin,f* James A. Dawson,b* Erli Lu,g* and Fabrizio Ortua*

aSchool of Chemistry, University of Leicester, University Road, Leicester, LE1 7RH, UK

bChemistry – School of Natural and Environmental Sciences, Newcastle University, Newcastle upon Tyne, NE1 7RU, UK

cSchool of Mathematics, Statistics, and Physics, Newcastle University, Newcastle upon Tyne, NE1 7RU, UK

dDepartment of Chemistry, The University of Manchester, Manchester, M13 9PL, UK

eDepartment of Chemistry and Photon Science Institute, The University of Manchester, Manchester, M13 9PL, UK

fDepartment of Chemistry, University of Bath, Claverton Down, Bath, BA2 7AY, UK

gSchool of Chemistry, University of Birmingham, Edgbaston, Birmingham, B15 2TT, UK

§These authors contributed equally

*email: floriana.tuna@manchester.ac.uk, c.mcmullin@bath.ac.uk, James.Dawson@newcastle.ac.uk, e.lu@birmingham.ac.uk, fabrizio.ortu@leicester.ac.uk

Contents

S1. Additional experimental details	S2

S2. NMR and IR data	S4

S3. Crystallographic data	S9

S4. UV-vis measurements	S16

S5. Electroconductivity measurements	S18

S6. Computational details	S19

S7. EPR and SQUID measurements	S52

S8. References	S60

# S1. Additional experimental details

## Reaction of 2 with pyridine

## A Schlenk flask was charged with a glass-coated magnetic stirrer bar and 2 (0.25 g, 0.3395 mmol) before pyridine (10 mL) was added at room temperature. The reaction mixture was stirred overnight before propan-2-ol (1 mL) was added. All volatile components were removed in vacuo before dichloromethane (25 mL) was used to extract the organic components. Removal of the solvent under reduced pressure yielded an oily residue confirmed to be 4,4′-bipyridine and ligand degradation products by 1H NMR spectroscopy (Figure S5) and mass spectrometry.

## Synthesis of [Ca{N(Mes)(SiMe3)}2{C6H2(NSi(Me)2CH2)(Me)2}] (4)

During the isolation of Ca hydride complex 3, we identified complex [Ca{N(Mes)(SiMe3)}2{C6H2(NSi(Me)2CH2)(Me)2}] (4), which formed as a result of degradation of one of the supporting amide ligands. Control experiments revealed that the formation of 4 is not related to the activation of benzene by 2, but it is associated with the degradation of residual starting material 1 present in the reaction, as confirmed via PXRD characterization (see Section S3). PXRD analysis also revealed that less of the starting material 1 is present in the electride material 2 when prepared using excess potassium metal (2ʹ), and gratifyingly we observed a significant reduction in the formation of 4 when 2ʹ is reacted with benzene. Complex 4 was prepared directly by heating a toluene solution of 1 to 70 °C for 3 hours (Scheme S1); colourless crystals were obtained from storing this solution at −30 °C. Complex 4 was fully characterised by multinuclear NMR spectroscopy, XRD studies, FT-IR spectroscopy and elemental analysis. The 1H NMR spectrum clearly shows activation of one NMes ligand and the consequential loss of symmetry with additional resonances compared to that of 1 (Figure S3). Most telling of this is the formation of two additional singlets at 6.42 ppm and 6.93 ppm each integrating to one H-atom. These resonances correspond to the two aryl-protons of the C–H activated ligand, which are now inequivalent due to loss of symmetry.

Scheme S1: Formation of decomposition product 4.

A Schlenk flask was charged with a magnetic stirrer bar and 1 (0.25 g, 0.358 mmol) before toluene (25 mL) was added at room temperature. The resulting pale yellow solution was heated to 70 °C for 3 hours before the volume of solvent was concentrated under reduced pressure and the solution stored at −30 °C yielding 4 as large colourless crystals (0.178 g, 0.261 mmol, 67.9%).

1H NMR (500 MHz, 298 K, C6D6): δ/ppm = −0.05 (br s, 6H, Si(CH3)2), 0.47 (s, 18H, Si(CH3)3), 1.36 (s, 3H, (CH3)C), 1.77 (br s, 2H, CH2), 2.05 (br s, 6H, para-CH3), 2.26 (s, 3H, (CH3)C), 2.27 (s, 12H, ortho-CH3), 6.42 (s, 1H, CH), 6.63 (br s, 4H, meta-H), 6.93 (s, 1H, CH). 13C{1H} (125 MHz, 298 K, C6D6): δ/ppm = 4.6 (Si(CH3)2), 17.9 ((CH3)C), 19.6 (CH2), 20.7 (para-CH3), 20.8 ((CH3)C), 21.2 (ortho-C(CH3)), 117.7 (C(CH3)), 122.5 (para-C) 128.8 ((CH3)C), 129.2 (meta-C), 129.4 ((CH3)C), 133.1 (C(CH3)), 134.1 (ortho-C(CH3)), 158.5 (N(C)). No observable signals were obtained from 29Si{1H} NMR experiments. Anal. calcd. for C35H56N3KCaSi3: C, 61.61 %; H, 8.27 %; N, 6.16 %. Found: C, 61.23 %; H, 7.98 %; N, 6.08 %.

# S2. NMR and IR data

Figure S1: 1H NMR (C6D6, 298 K, 400 MHz) spectrum of 3.

Figure S2: 13C{1H} NMR (C6D6, 298 K, 100 MHz) spectrum of 3.

Figure S3: 2H{1H} NMR (61 MHz, 298 K, C6D6) spectrum of 3D.

Figure S4: 1H NMR (400 MHz, 298 K, C6D6) spectrum of 3D (crude mixture, no workup).

Figure S5: 1H NMR (500 MHz, 298 K, C6D6) spectrum of 4.

Figure S6: 13C{1H} NMR (125 MHz, 298 K, C6D6) spectrum of 4.

Figure S7: 1H NMR (400 MHz, 298 K, CDCl3) spectrum of crude product obtained from the addition of pyridine to 2 following quenching with propan-2-ol.

Figure S8: Solid state IR spectrum of 3.

Figure S9: Solid state IR spectrum of 4.

# S3. Crystallographic data

Crystallographic method

Single Crystal XRD. The crystal data for all compounds are compiled in Table S1. Crystals of 3A, 3B and 4 were examined using a Bruker D8 Quest diffractometer with a Photon III detector and a microfocus source with Cu-Kα radiation (λ = 1.54178 Å). Intensities were integrated from data recorded on 1° frames by ω or φ rotation. A multi-scan absorption correction method with a beam profile was applied.1 The structures were solved using SHELXS2 or SHELXT;3 the datasets were refined by full-matrix least-squares on reflections with F2≥2σ(F2) values, with anisotropic displacement parameters for all non-hydrogen atoms, and with constrained riding hydrogen geometries;4 Uiso(H) was set at 1.2 (1.5 for methyl groups) times Ueq of the parent atom. The largest features in final difference syntheses were close to heavy atoms and were of no chemical significance. SHELX2,3 was employed through OLEX24 for structure solution and refinement. The structures have been deposited with the Cambridge Crystallographic Data Centre (CCDC 2346544-2346546). This information can be obtained free of charge from www.ccdc.cam.ac.uk/data_request/cif.

Powder XRD. Microcrystalline samples of 2 were mounted on a goniometer head with a micromount using a minimum amount of Fomblin. X-ray diffraction data were collected at 100 K using a Rigaku FR-X rotating anode single crystal X-ray diffractometer with Cu Kα radiation (λ = 1.5418 Å), a Hypix-6000HE detector and an Oxford Cryosystems nitrogen flow gas system. Data were collected between 3-70 °θ, with a detector distance of 150 mm and a beam divergence of 1.5 mRad. CrysAlisPro was used to measure, reduce and integrate XRD data.5 Le Bail method profile fitting was performed using JANA2020 software.6,7 In each case Le Bail method profile fitting was performed using the unit cell parameters for 1 and potassium metal.

|  | Table S1: Crystallographic data for 3A, 3B and 4. |  |  |  |
| --- | --- | --- | --- | --- |
|  |  | 3A | 3B | 4 |
| Formula |  | C102H152Ca2K4N6Si6 | C101H157Ca2K4N6Si6 | C35H56CaKN3Si3 |
| Formula Weight |  | 1867.39 | 1860.42 | 682.27 |
| Crystal Size, mm |  | 0.356×0.266×0.222 | 0.01×0.008×0.008 | 0.346×0.33×0.222 |
| Crystal System |  | monoclinic | monoclinic | monoclinic |
| Space group |  | P21/c | C2/c | P21/c |
| a, Å |  | 20.0459(5) | 20.148(3) | 17.9787(6) |
| b, Å |  | 19.8009(5) | 18.945(3) | 12.2698(4) |
| c, Å |  | 27.7174(7) | 33.091(5) | 19.6594(9) |
| α, ° |  | 90 | 90 | 90 |
| β, ° |  | 97.427(2) | 100.175(9) | 117.1260(10) |
| γ, ° |  | 90 | 90 | 90 |
| V, Å³ |  | 10909.5(5) | 12432(3) | 3859.7(3) |
| Z |  | 4 | 4 | 4 |
| Temperature, K |  | 120(2) | 120(2) | 120(2) |
| ρcalc, g cm3 |  | 1.137 | 0.994 | 1.174 |
| μ, mm1 |  | 3.239 | 2.839 | 3.452 |
| F(000) |  | 4024 | 4020 | 1472 |
| No. of reflections (unique) |  | 104042 (21410) | 111995 (11395) | 102125 (8432) |
| Sa |  | 1.02 | 1.25 | 1.03 |
| R1(wR2) (F2 > 2σ(F2)) |  | 0.0395 (0.1039) | 0.1497 (0.4451) | 0.0331 (0.0912) |
| Rint |  | 0.0531 | 0.430 | 0.0308 |
| Min./max. diff map, Å–3 |  | –0.26, 0.51 | –1.07, 1.54 | –0.35, 0.58 |

aConventional R = Σ||Fo| – |Fc||/Σ|Fo|; Rw = [Σw(Fo2 – Fc2)2/Σw(Fo2)2]1/2; S = [Σw(Fo2 – Fc2)2/no. data – no. params)]1/2 for all data.

Figure S10: Ball and stick representation of the molecular structure of 3B. Toluene molecules, together with mesityl and methyl groups are displayed as wireframe for clarity. Hydrogen atoms have also been omitted for clarity with the exception of hydride ligands. Legend: carbon (black), nitrogen (blue), silicon (orange), potassium (light blue), calcium (aquamarine), hydrogen (white).

Solid state characterisation of 4

In the solid state, complex 4 displays a polymeric arrangement supported by potassium-aryl interactions akin to those exhibited by 1. The Ca‒N bond distances are also comparable to those measured for the parent tris(amide) 1. In contrast to 1, complex 4 features a K–N bond between the potassium cation and the nitrogen atom of the activated ligand. As a result, there is a distortion of the trigonal planar geometry around the calcium centre.

Figure S11: Crystal structure of 4. Ellipsoids are set at 30% probability level. Hydrogen atoms have been omitted for clarity. Legend: carbon (black), nitrogen (blue), silicon (orange), potassium (pink), calcium (aquamarine).

Figure S12: PXRD analysis of 2 obtained using an IKA ULTRA-TURRAX mixer mill within a 25 mL PTFE jar and four 3 mm ball bearings (4000 rpm, 3 hours). Black = measured observed data, Red = fitted profile, Green = expected peak positions tick marks, Blue = Observed - fitted difference, Grey regions are regions of the full pattern excluded from the Le Bail method profile fitting.

Figure S13: PXRD analysis of 2 obtained using a RetschTM MM400 mixer mill within a 25 mL RetschTM stainless steel jar and a 10 mm diameter stainless steel ball (30 Hz, 30 minutes). Black = measured observed data, Red = fitted profile, Green = expected peak positions tick marks, Blue = Observed - fitted difference

Figure S14: PXRD analysis of 2′ obtained using an excess of potassium (1:K 1:1.1). Black = measured observed data, Red = fitted profile, Green = expected peak positions tick marks, Blue = Observed - fitted difference

Figure S15: PXRD analysis of 2 (incomplete conversion). Material was obtained using an IKA ULTRA-TURRAX mixer mill within a 25 mL PTFE jar and four 3 mm ball bearings (4000 rpm, 30 minutes). Red = fitted profile, Green = expected peak positions tick marks, Blue = Observed - fitted difference

Figure S16: Simulation (black) of PXRD pattern of 1, Green = expected peak positions tick marks.

# S4. UV-vis measurements

The solid-state UV–vis absorption spectrum of 2 was run on a powdered sample using an Edinburgh Instruments FP920 Phosphorescence Lifetime Spectrometer equipped with a 450 W steady state Xenon lamp (with single 300 mm focal length excitation and emission monochromators in Czerny Turner configuration), a red sensitive photomultiplier in Peltier housing (Hamamatsu R928P) and fitted with an integrating sphere. The instrument was set to measure the total spectral reflectance of the sample in a protected environment against a blank reference plug. These traces were convoluted within the software to produce an absorption spectrum. For completeness, we also measured the UV-vis spectrum of a solution of ‘[K(18-crown-6)]e–’ in THF (0.1 mM) at room temperature.

Figure S17: Raw reflected light spectrum of 2 (solid sample, r.t.).

Figure S18: UV-vis spectrum of ‘[K(18-crown-6)]e–’in THF (0.1 mM, r.t.).

# S5. Electroconductivity measurements

# A similar protocol to our previous report8 is employed for the electroconductivity measurements herein.

# To record the electrical conductivities, interdigitated ‘finger-pattern’ electrodes were scribed into ITO-coated glass (see Figure S19) using a Lasermark Primary (LaserLines) etcher and washed with isopropanol and acetone. The electrodes were subsequently examined with an optical microscope (Celestron); the inter-electrode distance was 200 µm and the length of the channel 99.8 cm on a ca. 2 cm × 1.5 cm glass slide. After transfer into a N2-filled glovebox, the sample powders were carefully spread onto the electrode and held in place with an additional (non-conductive) glass slide. The interdigitated electrodes were connected by crocodile clamps and wired out of the glovebox and into a Keithley 2450 source meter. Then, current-voltage sweeps were applied to the samples across different potential ranges, depending on the conductivity of the sample, and linear fits were applied to extract the resistance. After removal from the N2 glovebox, the samples were examined with optical microscopy. Owing to poor surface coverage of the powder, only around 5% of the channel between the interdigitated electrodes was found to be actively bridged by sample material, giving an effective channel length of 5 cm. The height of the powder film with a Dektak 3ST (sloan) profilometer was on average around 2 µm. Ultimately, the materials’ conductivity σ was obtained as:

σ=contact distanceresistance •channel length •film thickness

Figure S19. Instrument set-up for the electroconductivity measurements

# S6. Computational details

S6.1 AIRSS Calculations

In order to determine low-energy candidate structures, ab-initio random structure searching (AIRSS) was used.9 The geometry of several hundred random structures were optimized without spin, which was found to be sufficient in previous models of electrides.8 A selection of low-energy structures were then optimized again with spin included. Once it became apparent that hydride geometries were overwhelmingly more favorable, hundreds more structures were produced containing H atoms, which were then pre-optimized using the MACE-MP-0 universal forcefield10 with dispersion corrections, with the best structures being taken forward to be optimized at the same level of theory as the rest of the candidate structures.

Final AIRSS optmizations were carried out in VASP using a plane wave cutoff energy of 500 eV. Projector-augmented wave (PAW) pseudopotentials were employed where the following orbitals were treated as valence: 1s for H; 2s2p for C and N; 3s3p for Si; and 3s3p4s for K and Ca.11 All geometry optimizations were carried out using the r2SCAN+vv10 functional12 (a dispersion-corrected meta generalized gradient approximation) until the forces on atoms were less than 0.05 eV Å1.

As the stable structures included hydride-like geometries with anionic electrons highly localized in space, it was possible to use Gaussian basis sets without the risk of compromising the completeness of the basis so long as ghost atoms were included as floating basis centres. Considering this, detailed analysis of the most stable predicted structure and possible defective dimer complexes was carried out in CP2K,13 which allows for faster calculations than in VASP. All calculations used the r2SCAN0+vv10 dispersion-corrected hybrid functional14 with 25% Fock exchange included. Triple-ζ MOLOPT basis sets with GTH pseudopotentials were employed, the anionic electrons used the same basis as H. Hybrid DFT-calculations were accelerated using the auxiliary density matrix method using FIT11 sets for K and Ca and pFIT3 sets for all other elements. For the calculations of the defective complexes, a wavelet Poisson solver was used without periodic boundary conditions to avoid errors due to the interaction of image charges.

S6.2 DFT Methodology

DFT calculations were run with Gaussian 16 (A.03).15 The Ca, K and Si centres were described with the Stuttgart RECPs and associated basis sets,16 and the 6-31G** basis set was used for all other atoms (BS1).17,18 A polarization function was also added to Si (ζd = 0.284) and K (ζd = 1.000). Initial BP86 optimizations were performed using the ‘grid = ultrafine’ option,19,20 with all stationary points being fully characterized via analytical frequency calculations as minima (all positive eigenvalues). All energies were recomputed with a larger basis set featuring 6-311++G** basis sets on all atoms (BS2). Corrections for the effect of benzene (ε = 2.2706) solvent were run using the polarizable continuum model and BS1.21 Single-point dispersion corrections to the BP86 results employed Grimme’s D3 parameter set with Becke-Johnson damping as implemented in Gaussian.22

The Quantum Theory of Atoms in Molecules (QTAIM, AIMALL program23) and Natural Bonding Orbital (NBO724,25) analyses were performed on the BP86-optmised geometry of the anion of 3. The QTAIM topological analyses used wavefunction files obtained with Gaussian 16 (C.01) at the BP86/6-311++G** level, whilst NBO analyses were carried out with NBO 7 within Gaussian (C.01) at the same methodology level as the QTAIM calculations. Contour plots were generated in the AIMStudio package, using critical point (CP) visualisation threshold values of 0.02 e∙Å−3 (solid line BCP = strong) and 0.005 e∙Å−3 (dashed line BCP = weak). The NBO energies of donor-acceptor interactions (“ΔE(2)”) between the various molecular fragments of the structures were estimated with second-order perturbation theory analysis of the Fock matrix in the NBO basis, as calculated by NBO7, with selected donor-acceptor NBO interactions provided. Wiberg bond indices (WBI) were calculated using NBO v7.0.

S6.3 DFT Electronic Structure Analysis of 3

Natural Bond Orbital Analysis

Wiberg Bond Indices (WBIs), with atom numbering in Figure S20

| Ca1 – Ca3 | 0.0001 |  | H2 – H4 | 0.0027 |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Ca1 – H2 | 0.1369 |  | Ca3 – H4 | 0.1389 |  |  |  |
| Ca1 – H4 | 0.0010 |  | Ca3 – H2 | 0.0027 |  |  |  |
| Ca1 – K5 | 0.0046 |  | Ca1 – K6 | 0.0045 |  | Ca1 – K7 | 0.0046 |
| Ca3 – K5 | 0.0046 |  | Ca3 – K6 | 0.0047 |  | Ca3 – K7 | 0.0047 |
| H2 – K5 | 0.0383 |  | H2 – K6 | 0.0367 |  | H2 – K7 | 0.0374 |
| H4 – K5 | 0.0360 |  | H4 – K6 | 0.0378 |  | H4 – K7 | 0.0359 |
| Ca1 – N14 | 0.0773 |  | Ca1 – N15 | 0.0739 |  | Ca1 – N16 | 0.0730 |
| Ca3 – N17 | 0.0755 |  | Ca3 – N18 | 0.0747 |  | Ca3 – N19 | 0.0757 |

Natural Bonding Orbitals

There were no NBOs calculated to involve bonding between the Ca, H and K atoms, suggesting an electrostatic / ionic interaction within the anion of 3.

(NB. There were core and lone pair orbitals for these atoms, but nothing showing any bonding between Ca, H or K and any other atom.)

Second Order Perturbation Energies

Analysis of the NBO calculated Perturbation Energies (ΔE(2)) showed no donor-acceptor interactions for Ca or K atoms. However, the lone pair of the hydrogen atoms (H2 and H4) were shown to interact with the antibonding lone pair orbitals for their nearest Ca and K atoms. These values are given below, and are in units of kcal/mol.

| Donor NBO | Acceptor NBO | ΔE(2) |  | Donor NBO | Acceptor NBO | ΔE(2) |
| --- | --- | --- | --- | --- | --- | --- |
| 154. LP(1) H2 | 390. LV(1) Ca1 | 13.47 |  | 155. LP(1) H4 | 391. LV(1) Ca3 | 14.09 |
| 154. LP(1) H2 | 392. LV(1) K5 | 3.03 |  | 155. LP(1) H4 | 392. LV(1) K5 | 2.83 |
| 154. LP(1) H2 | 393. LV(1) K6 | 2.95 |  | 155. LP(1) H4 | 393. LV(1) K6 | 2.96 |
| 154. LP(1) H2 | 394. LV(1) K7 | 2.99 |  | 155. LP(1) H4 | 394. LV(1) K7 | 2.77 |

QTAIM Analysis

Figure S20: Bader charges (q, purple) for the core atoms of the anion component of 3 from QTAIM calculations on the BP86-optimised geometry.

Electron density (ρ) Contour Plot

Figure S21: Contour plot of ρ(r) of the DFT-optimized anion of 3.

| Table S2. Selected QTAIM BCP data for anion of 3 |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| BCP | ρ(r) | ∇2ρ(r) | ε | G(r) | V(r) | H(r) |
| H2 - H4 | 0.005034 | +0.007452 | 0.047408 | +0.001613 | -0.001362 | -0.001625 |
| Ca1 - H2 | 0.026262 | +0.055751 | 0.009217 | +0.014892 | -0.015846 | -0.026480 |
| Ca3 - H4 | 0.026234 | +0.055978 | 0.002908 | +0.014928 | -0.015862 | -0.026303 |
| H2 - K5 | 0.010418 | +0.026437 | 0.039656 | +0.005879 | -0.005149 | -0.007588 |
| H4 - K5 | 0.009234 | +0.023365 | 0.048880 | +0.005109 | -0.004377 | -0.006505 |
| H2 - K6 | 0.009121 | +0.022981 | 0.049431 | +0.005022 | -0.004299 | -0.006388 |
| H4 - K6 | 0.010450 | +0.026346 | 0.034138 | +0.005870 | -0.005153 | -0.007578 |
| H2 - K7 | 0.009457 | +0.023881 | 0.040789 | +0.005245 | -0.004519 | -0.006701 |
| H4 - K7 | 0.009623 | +0.024298 | 0.047186 | +0.005348 | -0.004621 | -0.006857 |
| Ca1 - N14 | 0.039786 | +0.151569 | 0.167309 | +0.036897 | -0.035902 | -0.046963 |
| Ca1 - N15 | 0.040371 | +0.156698 | 0.193809 | +0.038071 | -0.036968 | -0.048523 |
| Ca1 - N16 | 0.038637 | +0.148490 | 0.191555 | +0.035853 | -0.034583 | -0.045720 |
| Ca3 - N17 | 0.041160 | +0.159858 | 0.190813 | +0.038966 | -0.037968 | -0.049593 |
| Ca3 - N18 | 0.040500 | +0.157103 | 0.191450 | +0.038194 | -0.037113 | -0.048585 |
| Ca3 - N19 | 0.041090 | +0.159030 | 0.189163 | +0.038791 | -0.037825 | -0.049452 |

| Table S3. Selected QTAIM atomic data for anion of 3 |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Atom | q(A) | L(A) | N(A) | Vol(A) | %Loc(A) |
| Ca1 | +1.525345 | +0.000029 | 18.474655 | 106.761068 | 96.638769 |
| H2 | -0.736425 | -0.000017 | 1.736425 | 133.033326 | 77.797187 |
| Ca3 | +1.521895 | -0.000205 | 18.478105 | 106.411304 | 96.602839 |
| H4 | -0.734756 | +0.000001 | 1.734756 | 129.301951 | 77.501661 |
| K5 | +0.845435 | +0.000014 | 18.154565 | 163.754390 | 98.509111 |
| K6 | +0.846105 | +0.000120 | 18.153895 | 165.073482 | 98.519207 |
| K7 | +0.841805 | +0.000010 | 18.158195 | 163.223954 | 98.472725 |
| Si8 | +2.770185 | -0.000147 | 11.229815 | 37.622704 | 90.520310 |
| Si9 | +2.778051 | +0.000091 | 11.221949 | 37.436193 | 90.553858 |
| Si10 | +2.770760 | -0.000369 | 11.229240 | 37.357207 | 90.521091 |
| Si11 | +2.773156 | -0.000400 | 11.226844 | 37.412212 | 90.533300 |
| Si12 | +2.773932 | -0.000229 | 11.226068 | 37.362159 | 90.536180 |
| Si13 | +2.774417 | -0.000487 | 11.225583 | 37.410256 | 90.538482 |
| N14 | -1.633525 | -0.000472 | 8.633525 | 124.068300 | 83.007471 |
| N15 | -1.639089 | +0.000045 | 8.639089 | 121.278043 | 82.874581 |
| N16 | -1.624130 | -0.000062 | 8.624130 | 118.880823 | 82.810524 |
| N17 | -1.630751 | -0.000083 | 8.630751 | 118.063778 | 82.821953 |
| N18 | -1.631180 | +0.000135 | 8.631180 | 118.224338 | 82.820650 |
| N19 | -1.633376 | -0.000250 | 8.633376 | 117.687379 | 82.810318 |

Laplacian (∇2ρ) Contour Plot

Figure S22: Contour plot of ∇2ρ(r) of the DFT-optimized anion of 3.

S6.3 DFT Mechanistic Studies

Formation of 3 from 1

Ligand Conformations in 1

When −90 < τ < −135 °, the mesityl group could be classed as “up” (u), and when +70 < τ < +110 ° classed as “down” (d), based on the slight pyramidal nature of the trigonal planar Ca centre, with the molecule orientated such that the Ca centre is minimally above the {NNN} ligand plane. Five different conformations were isolated (see Table S4) and are close in free energy, with conformers 1a, 1b and 1c having essentially the same geometry. To further probe the flexibility of the ligand and its ability to adapt to the structural environment, one ligand was rotated about the Ca–N bond in 1a (Scheme 2). As the ligand is rotated, when the Mes and SiMe3 groups need to pass through the {NNN} ligand plane, there is a large increase in energy of ca. 16 kcal mol−1. Naturally as the ligand rotates, the other two ligand’s orientations respond to the structural changes.

Scheme S2: The dihedral angle (τ= Nb–Ca–N–Cipso) describing the orientation of the N(Mes)(SiMe3) mesityl groups relative to the N–Ca–N plane

Table S4 – the Free Energy values (ΔGbnz in kcal mol−1) of different conformers of the anion 1, [Ca{N(Mes)(SiMe3)}3]−, alongside the dihedral (τ, in °) to describe the orientation of all three N(Mes)(SiMe3) ligands.

| Computed Structure | Structural Basis | Conformer | ΔGbnz [kcal mol−1] | τ1 [°] | τ2 [°] | τ3 [°] |
| --- | --- | --- | --- | --- | --- | --- |
| 1a | LILKAW – 2259496a | uuu | 0.0 | −98.3 | −119.4 | −137.7 |
| 1b | Half of 3 crystal structure | uuu | 0.1 | −98.3 | −118.7 | −135.1 |
| 1c | LILLAX – 259504 (1)b | uuu | 0.4 | −98.3 | −118.3 | −134.6 |
| 1d | LILKIE – 2259501c | udd | 2.8 | −59.8 | +90.3 | +105.3 |
| 1e | Manually built | uuu | 6.3 | −82.4 | −93.5 | −48.5 |

aCSD Entry for [Sr{N(Mes)(SiMe3)}3K].

bCSD Entry for [Ca{N(Mes)(SiMe3)}3K] (1).

cCSD Entry for [Mg{N(Mes)(SiMe3)}3K].

Figure S23 – Electronic Relative Energy (E in kcal mol−1) rotation profile for one of the N(Mes)(SiMe3) ligands in 1a. The red data point depicts the original orientation of the ligand (τ = 261.7°).

Association of Benzene to 1

Figure S24: The Free energy addition of benzene to 1 in kcal mol−1 at the BP86-D3BJ(C6H6)/BS2//BP986/BS1 level of theory.

Coordination of benzene to 1 was unsuccessful. In all optimisations, the benzene associated to the K cation present in the computational model instead of the Ca centre, with a free energy of −8.2 kcal mol−1 (see Figure S24). Attempts to model benzene association to only the anionic Ca complex, saw an increase in free energy to +4.9 kcal mol−1, with the benzene far from the Ca centre (I’; Ca∙∙∙Hbnz = 5.96 Å). From the multiple efforts made to try and associate benzene to the Ca centre, it is logical to conclude that there is insufficient space at the Ca for the benzene (or indeed pyridine) to coordinate and is prevented by the mesityl substituents of the ligands. No Wheland intermediate was ever successfully isolated, and therefore we can confidently conclude that the Ca centre does not facilitate the C–H activation of the benzene (or pyridine).

Figure S25: Addition of benzene to 1 in kcal mol−1 at the BP86-D3BJ(C6H6)/BS2//BP986/BS1 level of theory.

Coordination of a hydride or phenyl anion to 1 is energetically favoured by 54.6 and 71.3 kcal mol−1 forming anionic intermediates II and III respectively (see Figure S25). However, neither of these values take into account the corresponding cation of the benzene substrate (i.e. either C6H6+ or a proton) but the equivalent anion. Nor do they incorporate the free energy gain that the formation of biphenyl would provide.

Finally, the formation of 3, [K(η6-C6D6)4][{Ca[N(Mes)(SiMe3)](H)}2K3], and the biphenyl C6H5-C6H5 from 1,  four potassium cations and six benzenes, gives a formation Free energy of −254.9 kcal mol−1.

Formation of 4 from 1

The free energy of formation for 4 + CH4, relative to 1, was computed to be −22.7 kcal mol−1.

Figure S26: Molecular structure of 4

To mechanistically understand this process, a range of structures were optimised, where either a H atom or CH3 group had been removed from 1. This provided a range of cationic and anionic species, as a proton, a hydride, a methyl anion or cation were deleted from 1. Across all the species optimised, there was a clear preference for anion loss to occur from the SiMe3 group (leaving a cationic Ca complex behind) or cation loss from the methyl group on the Mes group (leaving an anionic Ca complex behind). Pathways involving proton, hydride, methyl cation and anion loss were explored from both the SiMe3 group or the methyl group of the Mes substituent, however, only one full reaction process was fully mapped. The pathway shown in Figure S26, starts from the loss of a proton at the methyl position on one of the Mes ligand substituents, IV. The CH2 group then attacks the adjacent SiMe3 group via TS(IV-V) as one of the methyl groups of the attacked SiMe3 substituent then migrates to the Ca centre, with a facile barrier of 4.1 kcal mol−1 to exergonically form intermediate V at −4.1 kcal mol−1. The potassium ion then travels (ΔΔG = 2.0 kcal mol−1) towards the methyl anion in TS(V-VI) to give intermediate VI at −8.4 kcal mol−1. Finally, transfer of the anion to the potassium affords VII (ΔGbnz = −5.9 kcal mol−1).

Figure S27: Addition of benzene to 1 in kcal mol−1 at the BP86-D3BJ(C6H6)/BS2//BP986/BS1 level of theory.

S6.4 DFT Breakdown of Energy Contributions

The following tables detail the evolution of the relative energies as the successive corrections to the initial SCF energy are included. Terms used are:

ΔEBSI			SCF energy computed with the BP86 functional with BS1

ΔHBSI			Enthalpy at 0 K with BS1

ΔGBSI			Free energy at 298.15 K and 1 atm with BS1

ΔGBSI/bnz		Free energy corrected for benzene solvent with BS1

ΔGBSI/bnz+D3BJ		Free energy corrected for benzene and dispersion effects with BS1

ΔEBS2			SCF energy computed with the BP86 functional with BS2

ΔGbnz	Free energy corrected for basis set (BS2), dispersion effects and benzene solvent

In each case the final data used in the main article are highlighted in bold.

Table S5. Relative energies for conformer structures of 1 in kcal mol1. Data in bold are those used in the main text.

|  |  | ΔEBSI | ΔHBSI | ΔGBSI | ΔGBSI/bnz | ΔGBSI/bnz+D3BJ | ΔEBS2 | ΔGbnz |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| [Ca{N(Mes)(SiMe3)}3]− | 1a | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | 1b | 2.8 | 2.3 | 1.2 | 0.8 | 0.1 | 2.8 | 0.1 |
|  | 1c | 2.8 | 2.2 | 1.5 | 1.1 | 0.5 | 2.8 | 0.4 |
|  | 1d | 3.6 | 3.7 | 3.6 | 3.8 | 2.6 | 3.8 | 2.8 |
|  | 1e | 5.7 | 6.1 | 6.3 | 6.7 | 6.2 | 5.8 | 6.3 |

Table S6. Relative energies for computed structures in kcal mol1 to 1a + C6H6. Data in bold are those used in the main text.

|  |  | ΔEBSI | ΔHBSI | ΔGBSI | ΔGBSI/bnz | ΔGBSI/bnz+D3BJ | ΔEBS2 | ΔGbnz |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | I | −21.7 | −19.6 | −6.2 | 3.5 | −13.0 | −16.9 | −8.2 |
|  | I' | 76.8 | 76.6 | 76.1 | 1.9 | 3.8 | 77.9 | 4.9 |
|  | II | 13.2 | 6.7 | 7.8 | −32.7 | −32.4 | −9.0 | −54.6 |
|  | III | 54.6 | 47.9 | 56.5 | −7.1 | −21.4 | 4.7 | −71.3 |

Table S7. Relative energies for computed structures in kcal mol1 to the anionic IV (which is based on 1a with a proton removed from the Mes group). Data in bold are those used in the main text.

|  |  | ΔEBSI | ΔHBSI | ΔGBSI | ΔGBSI/bnz | ΔGBSI/bnz+D3BJ | ΔEBS2 | ΔGbnz |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | IV | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 | 0.0 |
|  | TS(IV-V) | 4.6 | 4.1 | 4.5 | 4.6 | 3.6 | 5.0 | 4.1 |
|  | V | −3.1 | −4.0 | −5.2 | −5.6 | −5.6 | −4.6 | −4.1 |
|  | TS(V-VI) | −2.5 | −3.7 | −4.3 | −4.6 | −4.1 | −0.5 | −2.1 |
|  | VI | −7.9 | −9.2 | −10.2 | −12.2 | −10.0 | −6.2 | −8.4 |
|  | VII | −4.0 | −5.1 | −6.5 | −7.7 | −8.3 | −1.6 | −5.9 |

Cartesian Coordinates and DFT Computed Energies [in Hartrees]

3

SCF (BP86) Energy = -4285.74893374

Enthalpy 0K = -4283.652271

Enthalpy 298K = -4283.490792

Free Energy 298K = -4283.885440

Lowest Frequency = 4.9834 cm-1

Second Frequency = 7.0562 cm-1

SCF (BP86-D3BJ) Energy =

-4286.52154667

SCF (C6H6) Energy = -4285.77618007

SCF (BS2) Energy = -9568.73732437

Ca  4.47680 -2.68582 -0.05402

H   3.06815 -0.85919 -0.01825

Ca -0.35890  3.46052  0.00348

H   1.05517  1.66368 -0.02098

K   1.40053 -0.28994  2.10182

K   3.97694  1.88374 -0.15274

K   1.27680 -0.28160 -2.05855

Si  3.13966 -6.14801  0.82038

Si  5.91887 -3.83516 -3.08835

Si  7.57896 -2.65328  2.10345

Si -0.74242  5.56465  3.04296

Si -4.00503  2.97391 -0.51469

Si -0.07584  6.27891 -2.39163

N   3.13907 -4.39195  1.01503

N   4.62873 -2.83776 -2.44008

N   6.33438 -1.79359  1.19268

N  -0.39306  3.99489  2.32170

N  -2.39331  2.43003 -0.87125

N   0.68086  4.99381 -1.46220

C   2.15277 -3.86676  1.85542

C   2.40331 -3.57589  3.24383

C   1.36365 -3.12594  4.08339

H   1.58360 -2.96704  5.14796

C   0.04241 -2.94207  3.62760

C  -0.19375 -3.17080  2.25595

H  -1.21681 -3.06185  1.86519

C   0.81726 -3.60455  1.37712

C   3.76815 -3.85256  3.82821

H   3.83049 -3.51177  4.87568

H   4.56932 -3.36321  3.24855

H   3.99479 -4.93363  3.80535

C  -1.09030 -2.61846  4.58031

H  -1.67931 -3.52243  4.82819

H  -1.79525 -1.88036  4.15690

H  -0.71372 -2.20862  5.53219

C   0.49185 -3.86473 -0.07308

H   1.20962 -3.35463 -0.74057

H  -0.53260 -3.53289 -0.31766

H   0.57041 -4.93628 -0.32739

C   4.69958 -7.02966  1.49816

H   5.62294 -6.70103  0.99352

H   4.60219 -8.11927  1.33728

H   4.83634 -6.86118  2.57977

C   3.04999 -6.69097 -1.01338

H   3.24400 -7.77483 -1.10597

H   3.80492 -6.16203 -1.61953

H   2.06328 -6.48432 -1.46132

C   1.66639 -6.95803  1.74397

H   1.68671 -8.05229  1.59504

H   0.68801 -6.58732  1.39460

H   1.72250 -6.76594  2.82935

C   3.81093 -2.13317 -3.32773

C   4.11408 -0.77645 -3.71314

C   3.33331 -0.10491 -4.67429

H   3.64543  0.89924 -4.99324

C   2.19820 -0.68935 -5.27341

C   1.84495 -1.97941 -4.83139

H   0.96093 -2.46639 -5.26583

C   2.60657 -2.69838 -3.88630

C   5.30680 -0.07810 -3.10735

H   5.35479 -0.25054 -2.01722

H   5.27857  1.00680 -3.30874

H   6.25894 -0.46818 -3.50363

C   1.43593  0.01123 -6.37958

H   1.88980 -0.18611 -7.36932

H   1.42678  1.10663 -6.24341

H   0.38810 -0.33156 -6.43169

C   2.16913 -4.09019 -3.49471

H   1.08149 -4.22308 -3.63505

H   2.43614 -4.30640 -2.44887

H   2.67332 -4.86182 -4.10280

C   7.24853 -2.88841 -4.09859

H   7.80192 -2.16577 -3.47521

H   6.79607 -2.33824 -4.94241

H   7.98328 -3.59616 -4.52371

C   5.37049 -5.25500 -4.25688

H   4.83612 -4.86305 -5.14010

H   4.71148 -5.98064 -3.75153

H   6.25661 -5.80347 -4.62516

C   6.79724 -4.61706 -1.58718

H   6.13531 -5.29752 -1.02184

H   7.17696 -3.84014 -0.89925

H   7.66634 -5.21340 -1.91588

C   6.42403 -0.39377  1.24599

C   5.72064  0.35811  2.25691

C   5.91239  1.74761  2.39129

H   5.43019  2.26550  3.23237

C   6.74406  2.48396  1.52177

C   7.34265  1.77081  0.46435

H   7.98376  2.31290 -0.24470

C   7.20437  0.37549  0.30818

C   4.79946 -0.35689  3.21673

H   4.11775  0.35375  3.71608

H   5.35386 -0.89353  4.00490

H   4.21418 -1.13251  2.69147

C   7.03406  3.95208  1.75971

H   7.33343  4.46471  0.82978

H   7.86280  4.08430  2.48102

H   6.16062  4.48521  2.17402

C   7.94206 -0.30820 -0.82134

H   7.41313 -1.21988 -1.14160

H   8.95253 -0.62486 -0.50911

H   8.06195  0.36769 -1.68528

C   7.69286 -2.13182  3.95067

H   7.76663 -1.03608  4.06286

H   8.59669 -2.57243  4.40923

H   6.82289 -2.48068  4.53343

C   9.37367 -2.42794  1.45778

H  10.06471 -3.03572  2.07042

H   9.70821 -1.37851  1.52949

H   9.48124 -2.75343  0.40934

C   7.22432 -4.52230  2.07329

H   6.15977 -4.73903  2.25315

H   7.80698 -5.02053  2.86845

H   7.51064 -4.98249  1.11382

C   0.05726  2.99463  3.19666

C   1.45683  2.83680  3.50384

C   1.87737  1.92297  4.49006

H   2.94256  1.89572  4.75832

C   0.97882  1.08220  5.17847

C  -0.37280  1.14474  4.78605

H  -1.09968  0.48580  5.28068

C  -0.84150  2.05830  3.81974

C   2.48798  3.67293  2.78383

H   2.24807  3.75100  1.70823

H   3.49679  3.24192  2.90301

H   2.52360  4.70996  3.15531

C   1.44119  0.20669  6.32501

H   1.51256  0.78457  7.26598

H   2.43943 -0.22614  6.13876

H   0.74146 -0.62562  6.51025

C  -2.31429  2.08259  3.47582

H  -2.82167  1.18919  3.88449

H  -2.46966  2.11730  2.38354

H  -2.81753  2.97432  3.88705

C  -2.22866  5.56158  4.26326

H  -2.37298  6.57170  4.68839

H  -2.05613  4.87170  5.10812

H  -3.17056  5.27123  3.76679

C  -1.15414  6.80424  1.65498

H  -0.45502  6.70336  0.80718

H  -1.07261  7.83678  2.03780

H  -2.18123  6.67038  1.27811

C   0.68623  6.32631  4.07597

H   1.52883  6.65083  3.44190

H   1.07287  5.61752  4.82865

H   0.31835  7.21601  4.61868

C  -2.22657  1.29697 -1.67974

C  -2.05278 -0.00922 -1.09641

C  -1.93440 -1.15558 -1.91046

H  -1.82683 -2.13624 -1.42496

C  -1.95907 -1.08855 -3.31912

C  -2.04577  0.19757 -3.88948

H  -2.02748  0.29390 -4.98357

C  -2.16207  1.37120 -3.11786

C  -1.98245 -0.15341  0.40552

H  -2.95377  0.03373  0.89609

H  -1.28916  0.59440  0.83182

H  -1.64074 -1.16342  0.69238

C  -1.94012 -2.33811 -4.17555

H  -2.95646 -2.75868 -4.30364

H  -1.31578 -3.13274 -3.73191

H  -1.55084 -2.12992 -5.18591

C  -2.20236  2.71118 -3.81463

H  -1.51445  3.42497 -3.33118

H  -3.20257  3.17381 -3.77558

H  -1.91935  2.61077 -4.87580

C  -5.10374  3.54262 -1.98731

H  -4.67003  4.41937 -2.49624

H  -6.10589  3.83569 -1.62101

H  -5.24101  2.74584 -2.73994

C  -5.09901  1.55555  0.25044

H  -6.15813  1.87900  0.25565

H  -4.78501  1.30909  1.27900

H  -4.97157  0.66933 -0.39989

C  -3.95829  4.40421  0.73156

H  -4.92869  4.50705  1.24896

H  -3.75325  5.35760  0.21761

H  -3.17645  4.24660  1.49403

C   2.05431  4.76306 -1.64115

C   2.53063  3.82777 -2.62759

C   3.91096  3.66987 -2.86464

H   4.23062  3.00403 -3.67821

C   4.88899  4.37370 -2.13235

C   4.42641  5.20722 -1.09389

H   5.15982  5.75489 -0.48621

C   3.05597  5.41022 -0.83283

C   1.54427  3.02853 -3.44698

H   0.70598  2.67551 -2.81933

H   2.03640  2.16565 -3.92846

H   1.08007  3.63294 -4.24474

C   6.35863  4.29153 -2.49220

H   6.63543  3.29543 -2.87914

H   7.00450  4.50821 -1.62447

H   6.61864  5.02521 -3.27874

C   2.64901  6.35317  0.27653

H   3.49514  6.55123  0.95644

H   1.80863  5.94467  0.86199

H   2.30454  7.32323 -0.12089

C   0.15068  6.12953 -4.29437

H  -0.22844  7.03985 -4.79344

H  -0.39596  5.26763 -4.71375

H   1.21578  6.02496 -4.56560

C   0.53593  8.05510 -1.99810

H   0.35683  8.32898 -0.94472

H   0.00112  8.78708 -2.63087

H   1.61433  8.16868 -2.20545

C  -1.95212  6.24762 -2.03535

H  -2.18047  6.69730 -1.05504

H  -2.34202  5.21528 -2.04805

H  -2.49483  6.82564 -2.80410

K  -7.13498 -0.81949  0.43411

C  -6.67439 -1.47580  3.78280

H  -7.06257 -0.72008  4.47354

C  -5.36579 -1.35842  3.27800

H  -4.73796 -0.51001  3.56917

C  -4.85227 -2.34783  2.41778

H  -3.82762 -2.26370  2.04247

C  -5.64792 -3.45305  2.06196

H  -5.23699 -4.23596  1.41641

C  -6.95886 -3.56772  2.56237

H  -7.56975 -4.43919  2.30424

C  -7.47142 -2.57950  3.42382

H  -8.48089 -2.68346  3.83514

C  -9.21804  1.64329  1.86584

H  -8.76979  2.29935  2.61908

C  -9.82056  0.43185  2.25313

H  -9.84626  0.14803  3.31025

C  -10.41472 -0.40050  1.28535

H  -10.90434 -1.33447  1.58081

C  -10.41033 -0.01904 -0.06964

H  -10.89406 -0.66245 -0.81210

C  -9.81052  1.19448 -0.45614

H  -9.82394  1.50367 -1.50634

C  -9.21315  2.02476  0.51079

H  -8.76096  2.97586  0.21224

C  -5.55556 -1.13715 -2.64413

H  -4.64865 -0.54722 -2.81779

C  -6.81791 -0.64380 -3.02542

H  -6.89639  0.33985 -3.49995

C  -7.97285 -1.42128 -2.81754

H  -8.95119 -1.04594 -3.13556

C  -7.87102 -2.69624 -2.22739

H  -8.77039 -3.30543 -2.08381

C  -6.60783 -3.19265 -1.84997

H  -6.52184 -4.19584 -1.41850

C  -5.45344 -2.41308 -2.05714

H  -4.46510 -2.79537 -1.78248

C  -12.94248 -2.84912 -0.99188

H  -13.60810 -1.97988 -1.02182

C  -12.32594 -3.30416 -2.17040

H  -12.51027 -2.78923 -3.11929

C  -11.49278 -4.43656 -2.13570

H  -11.03099 -4.80471 -3.05816

C  -11.27357 -5.11137 -0.92176

H  -10.63886 -6.00366 -0.89855

C  -11.88899 -4.65551  0.25707

H  -11.73352 -5.19277  1.19879

C  -12.72423 -3.52550  0.22190

H  -13.22332 -3.18401  1.13529

Anion of 3

SCF (BP86) Energy = -3328.49256715

Enthalpy 0K = -3326.790324

Enthalpy 298K = -3326.658467

Free Energy 298K = -3326.968386

Lowest Frequency = 13.7956 cm-1

Second Frequency = 14.5420 cm-1

SCF (BP86-D3BJ) Energy =

-3329.13925282

SCF (C6H6) Energy = -3328.52230157

SCF (BS2) Energy = -8039.61832111

Ca -3.91351 -0.06947  0.01425

H  -1.61630 -0.01213 -0.01305

Ca  3.90632  0.06044 -0.10917

H   1.61183  0.02585  0.01916

K  -0.07102  1.86214 -1.40175

K   0.03944  0.31730  2.31578

K   0.03841 -2.21971 -0.74246

Si -5.92034  0.16609 -3.22201

Si -5.68231 -2.98994  1.06876

Si -5.85277  2.46771  2.07045

Si  5.78271  3.24516  0.29204

Si  5.56767 -0.98072 -3.24858

Si  6.00501 -1.93772  2.21835

N  -4.53679  0.59298 -2.21629

N  -4.12438 -2.40347  0.52533

N  -4.40619  1.50548  1.78342

N   4.30470  2.41588 -0.17245

N   4.21824 -1.17360 -2.14071

N   4.52800 -1.03809  1.92196

C  -3.53685  1.35771 -2.83584

C  -3.49425  2.79187 -2.72734

C  -2.52004  3.53680 -3.42260

H  -2.55125  4.63291 -3.35111

C  -1.55566  2.93598 -4.25592

C  -1.56154  1.52705 -4.32413

H  -0.83881  1.02299 -4.98130

C  -2.50384  0.74292 -3.63029

C  -4.55898  3.51237 -1.93441

H  -4.35435  4.59572 -1.88550

H  -4.63738  3.12082 -0.90598

H  -5.55595  3.37152 -2.38967

C  -0.62167  3.76021 -5.11917

H  -1.00341  3.84554 -6.15484

H   0.38602  3.31362 -5.18623

H  -0.50975  4.78707 -4.73188

C  -2.47016 -0.76006 -3.76421

H  -2.47912 -1.24787 -2.77251

H  -1.57770 -1.09118 -4.32189

H  -3.36106 -1.14780 -4.28875

C  -7.59075  0.92925 -2.66445

H  -7.88475  0.60446 -1.65266

H  -8.38926  0.61330 -3.36149

H  -7.56383  2.03229 -2.66228

C  -6.26151 -1.71881 -3.25691

H  -7.23756 -1.92976 -3.73060

H  -6.28642 -2.13481 -2.23531

H  -5.48660 -2.26822 -3.81762

C  -5.69006  0.75241 -5.03394

H  -6.57121  0.46940 -5.63723

H  -4.79770  0.31407 -5.51115

H  -5.58406  1.84974 -5.08626

C  -3.04892 -3.29779  0.47501

C  -2.14859 -3.45342  1.58970

C  -1.12457 -4.42038  1.56237

H  -0.50796 -4.55507  2.46199

C  -0.88927 -5.24584  0.44424

C  -1.70681 -5.03083 -0.68279

H  -1.54296 -5.63922 -1.58275

C  -2.75681 -4.08935 -0.69473

C  -2.32233 -2.59531  2.81928

H  -2.51099 -1.54215  2.54456

H  -1.43344 -2.65174  3.47207

H  -3.19689 -2.89992  3.41827

C   0.15623 -6.34192  0.47296

H  -0.26776 -7.29612  0.84060

H   0.99872 -6.08550  1.13820

H   0.56849 -6.53725 -0.53189

C  -3.59922 -3.94364 -1.94026

H  -3.04702 -4.27586 -2.83698

H  -3.92636 -2.90121 -2.07551

H  -4.52298 -4.54581 -1.88111

C  -5.71393 -3.67518  2.86420

H  -5.48740 -2.89071  3.60610

H  -4.98083 -4.49090  2.99360

H  -6.71176 -4.08672  3.10315

C  -6.45926 -4.40489  0.02694

H  -5.80354 -5.29311  0.00605

H  -6.64994 -4.09584 -1.01446

H  -7.42341 -4.71632  0.46941

C  -6.87687 -1.50479  1.01020

H  -7.03543 -1.13989 -0.02029

H  -6.49630 -0.66865  1.62371

H  -7.86655 -1.78515  1.41187

C  -3.34187  1.74576  2.66715

C  -2.32634  2.72163  2.35591

C  -1.33337  3.05614  3.29777

H  -0.63580  3.87045  3.05657

C  -1.23724  2.42335  4.55464

C  -2.16363  1.39553  4.81772

H  -2.11395  0.87083  5.78223

C  -3.19366  1.04695  3.91950

C  -2.35229  3.43448  1.02468

H  -1.39440  3.94782  0.83214

H  -3.15492  4.18870  0.97080

H  -2.55877  2.72595  0.20260

C  -0.18578  2.83070  5.56821

H  -0.52665  2.62959  6.59843

H   0.04403  3.90793  5.49530

H   0.76845  2.28713  5.43029

C  -4.17939 -0.02796  4.32026

H  -4.58652 -0.53471  3.43091

H  -5.04233  0.39520  4.86396

H  -3.70678 -0.77419  4.98184

C  -5.53105  4.36428  2.13013

H  -4.69775  4.61447  2.80972

H  -6.43070  4.88894  2.50069

H  -5.29545  4.77375  1.13271

C  -6.76816  2.12289  3.72725

H  -7.68223  2.74322  3.77925

H  -6.14640  2.37925  4.60266

H  -7.07338  1.06682  3.81916

C  -7.12359  2.15923  0.68819

H  -6.64615  2.14143 -0.30381

H  -7.87517  2.96884  0.68683

H  -7.65926  1.20615  0.82681

C   3.21501  3.21171 -0.55166

C   2.25815  3.68418  0.41727

C   1.23812  4.58077  0.04319

H   0.57992  4.98184  0.82661

C   1.06225  5.01732 -1.28570

C   1.92213  4.46113 -2.25453

H   1.79975  4.75583 -3.30588

C   2.96896  3.57547 -1.92429

C   2.35848  3.23518  1.85569

H   2.57110  2.15259  1.91555

H   1.42669  3.45631  2.40407

H   3.18611  3.72700  2.39264

C   0.04092  6.07943 -1.63800

H   0.45028  7.09676 -1.48627

H  -0.86634  6.00169 -1.01390

H  -0.27016  6.01149 -2.69422

C   3.86114  3.04194 -3.02211

H   3.42902  3.24868 -4.01664

H   4.01595  1.95382 -2.92253

H   4.86584  3.49631 -2.98891

C   6.62956  4.24111 -1.11816

H   7.53377  4.74941 -0.73509

H   5.96003  5.02051 -1.52274

H   6.94034  3.58788 -1.95114

C   7.04668  1.95458  0.90140

H   6.57335  1.21533  1.56997

H   7.85608  2.45226  1.46447

H   7.50801  1.41565  0.05776

C   5.57757  4.54754  1.69355

H   5.35664  4.07759  2.66710

H   4.77001  5.26544  1.46661

H   6.51239  5.12655  1.80777

C   3.21307 -2.08099 -2.50575

C   2.07833 -1.67335 -3.29655

C   1.13165 -2.61802 -3.74264

H   0.31871 -2.27716 -4.39906

C   1.21490 -3.98548 -3.41161

C   2.26130 -4.36599 -2.54845

H   2.34442 -5.41953 -2.24669

C   3.23726 -3.46021 -2.08771

C   1.90577 -0.22024 -3.67303

H   2.51864  0.06362 -4.54573

H   2.24315  0.43087 -2.84739

H   0.85392  0.00253 -3.92437

C   0.26484 -5.00382 -4.00769

H   0.22622 -5.92536 -3.40225

H   0.57973 -5.29934 -5.02709

H  -0.76410 -4.61200 -4.09237

C   4.33737 -3.96026 -1.18066

H   4.48752 -3.28370 -0.32264

H   5.30701 -4.01140 -1.70427

H   4.10417 -4.96919 -0.79890

C   6.59572 -2.57567 -3.55641

H   7.09463 -2.92339 -2.63574

H   7.38061 -2.38354 -4.31107

H   5.96532 -3.39815 -3.93766

C   5.09325 -0.40509 -5.02217

H   5.98984 -0.40094 -5.66901

H   4.67270  0.61486 -5.02751

H   4.35603 -1.08447 -5.48494

C   6.75871  0.32272 -2.53154

H   7.46630  0.66259 -3.30846

H   7.35008 -0.09429 -1.69958

H   6.21181  1.20720 -2.16190

C   3.54605 -1.00924  2.92152

C   2.48825 -1.98724  2.96066

C   1.54649 -1.99255  4.00993

H   0.79704 -2.79650  4.03849

C   1.56435 -1.03748  5.04672

C   2.54263 -0.02632  4.95956

H   2.58226  0.74294  5.74380

C   3.50869  0.01497  3.93503

C   2.39885 -3.03973  1.88123

H   2.62169 -2.60459  0.89090

H   1.39984 -3.50860  1.86470

H   3.14100 -3.84420  2.02172

C   0.62621 -1.13555  6.23277

H  -0.33431 -1.60576  5.95912

H   0.40599 -0.14353  6.66277

H   1.06504 -1.74872  7.04348

C   4.52970  1.12897  3.92741

H   4.23008  1.94295  4.60984

H   4.65696  1.54337  2.91337

H   5.52532  0.77313  4.24244

C   5.73548 -3.78849  2.66934

H   6.69332 -4.25145  2.96987

H   5.33607 -4.36772  1.81965

H   5.03618 -3.89616  3.51722

C   7.09911 -1.28590  3.65958

H   7.44657 -0.25489  3.47645

H   7.99356 -1.92627  3.77262

H   6.55932 -1.30184  4.62276

C   7.08213 -1.87429  0.64543

H   7.59244 -0.90133  0.55265

H   6.48064 -2.04041 -0.26456

H   7.85968 -2.65779  0.68466

1a

SCF (BP86) Energy = -1621.11850981

Enthalpy 0K = -1620.274261

Enthalpy 298K = -1620.212101

Free Energy 298K = -1620.374525

Lowest Frequency = 13.3173 cm-1

Second Frequency = 17.5485 cm-1

SCF (BP86-D3BJ) Energy =

-1621.38388539

SCF (C6H6) Energy = -1621.14948349

SCF (BS2) Energy = -3119.22135675

Si  1.39136  3.28589  1.22469

Si  1.32228 -1.41053 -2.54477

Si -1.34339 -1.51628  2.84563

N   0.11714  2.35464  0.47428

N   1.91273 -0.86700 -0.99783

N  -1.50587 -1.39094  1.11673

C   0.85656  4.38483  2.71351

H   0.08419  5.11749  2.42033

H   1.72343  4.95368  3.09853

H   0.45510  3.78135  3.54583

C   2.28945  4.52252  0.05797

H   2.82814  4.00023 -0.75006

H   3.02521  5.12495  0.62227

H   1.57157  5.22242 -0.40498

C   2.69992  2.07240  1.90480

H   2.30730  1.47952  2.74893

H   3.57027  2.63842  2.28297

H   3.08123  1.37537  1.13778

C  -0.98781  2.96829 -0.15318

C  -2.19791  3.25714  0.56871

C  -3.29931  3.83589 -0.08591

H  -4.20452  4.04637  0.50121

C  -3.28849  4.14052 -1.45871

C  -2.11715  3.83651 -2.17143

H  -2.07605  4.05389 -3.24839

C  -0.98435  3.26620 -1.55997

C  -2.30724  2.92012  2.03843

H  -1.64245  3.54144  2.66161

H  -2.01473  1.87163  2.22348

H  -3.34171  3.06143  2.39630

C  -4.50518  4.72489 -2.14695

H  -5.04389  5.43185 -1.49074

H  -5.23240  3.94252 -2.43971

H  -4.22683  5.26685 -3.06782

C   0.24090  2.99542 -2.40658

H  -0.01548  2.99163 -3.48023

H   0.71511  2.03131 -2.15342

H   1.02399  3.75938 -2.25254

C  -0.54985 -0.97935 -2.56978

H  -1.14258 -1.51266 -1.80266

H  -0.97672 -1.28783 -3.54053

H  -0.74659  0.10872 -2.49777

C   1.50039 -3.29462 -2.86446

H   2.55606 -3.60388 -2.76507

H   1.16846 -3.56081 -3.88470

H   0.90465 -3.88378 -2.14789

C   2.07245 -0.59408 -4.11549

H   1.92880  0.49927 -4.11665

H   1.58844 -1.00235 -5.02217

H   3.15460 -0.79692 -4.19807

C   3.24971 -0.99540 -0.57561

C   3.65471 -2.08426  0.27026

C   4.98241 -2.18571  0.72052

H   5.25500 -3.03913  1.35795

C   5.96745 -1.23988  0.38480

C   5.56831 -0.16367 -0.42441

H   6.30743  0.60442 -0.69390

C   4.25160 -0.01897 -0.90097

C   2.65445 -3.13983  0.68205

H   2.27175 -3.70646 -0.18454

H   1.76325 -2.69850  1.16475

H   3.10681 -3.85744  1.38846

C   7.38309 -1.35185  0.91324

H   7.48930 -0.90224  1.92018

H   8.10276 -0.83559  0.25371

H   7.70326 -2.40578  0.99933

C   3.90442  1.18984 -1.74019

H   4.65526  1.98818 -1.60834

H   2.91113  1.58358 -1.46623

H   3.85736  0.95366 -2.81808

C  -2.83422 -0.86886  3.87030

H  -2.99345  0.21231  3.72006

H  -2.67954 -1.04386  4.95099

H  -3.76272 -1.38973  3.57708

C  -0.99699 -3.26063  3.57498

H  -1.81725 -3.96199  3.34216

H  -0.90877 -3.20624  4.67597

H  -0.06062 -3.68871  3.17948

C   0.17739 -0.43488  3.30119

H   1.12435 -0.84226  2.89729

H   0.30307 -0.40198  4.39781

H   0.06336  0.61550  2.97063

C  -2.52491 -2.07291  0.41591

C  -2.34983 -3.41461 -0.06418

C  -3.37351 -4.05136 -0.79138

H  -3.20089 -5.07766 -1.14614

C  -4.59445 -3.42324 -1.08579

C  -4.75275 -2.09726 -0.64485

H  -5.68480 -1.56327 -0.87862

C  -3.75815 -1.41739  0.07965

C  -1.05157 -4.15192  0.17122

H  -0.18795 -3.48124  0.02934

H  -0.95700 -5.01029 -0.51674

H  -0.96977 -4.54336  1.20086

C  -5.69714 -4.14492 -1.83315

H  -6.27050 -3.45529 -2.47810

H  -6.42552 -4.62007 -1.14629

H  -5.29216 -4.94646 -2.47578

C  -3.99160  0.02039  0.47922

H  -3.93670  0.16051  1.57157

H  -4.98138  0.36754  0.13613

H  -3.23462  0.70130  0.04968

Ca  0.14153  0.03195  0.22104

1b

SCF (BP86) Energy = -1621.11402243

Enthalpy 0K = -1620.270661

Enthalpy 298K = -1620.207916

Free Energy 298K = -1620.372580

Lowest Frequency = 10.4307 cm-1

Second Frequency = 19.5926 cm-1

SCF (BP86-D3BJ) Energy =

-1621.38047266

SCF (C6H6) Energy = -1621.14566723

SCF (BS2) Energy = -3119.21690849

Ca -0.27613  0.23213 -0.55970

Si -3.12975  2.69636 -0.89815

Si  2.07314  1.68051 -2.47161

Si -1.66885 -2.79452 -1.75799

N  -2.27037  1.39971 -0.10057

N   1.73622  1.40834 -0.78640

N  -0.31859 -2.07963 -0.90413

C  -2.64114  0.85166  1.13838

C  -3.82279  0.05100  1.33611

C  -4.08064 -0.54368  2.58186

H  -4.98750 -1.15600  2.68878

C  -3.22791 -0.38903  3.69151

C  -2.09378  0.41825  3.51484

H  -1.42386  0.59340  4.36829

C  -1.79011  1.03720  2.28598

C  -4.80477 -0.16078  0.20666

H  -5.54583 -0.93479  0.47001

H  -4.29288 -0.46620 -0.72064

H  -5.36359  0.76221 -0.03564

C  -3.51592 -1.07638  5.01008

H  -3.00356 -0.57116  5.84742

H  -3.17533 -2.12992  5.01088

H  -4.59743 -1.08999  5.23637

C  -0.60818  1.98398  2.21689

H   0.29099  1.59360  1.69673

H  -0.25988  2.24335  3.23102

H  -0.87746  2.90921  1.68105

C  -4.14393  2.19275 -2.45402

H  -3.50314  1.66830 -3.18488

H  -4.55201  3.09028 -2.95480

H  -4.98717  1.52360 -2.21745

C  -1.87912  3.98408 -1.56594

H  -2.38146  4.74368 -2.19256

H  -1.10095  3.50437 -2.18539

H  -1.36559  4.50489 -0.74053

C  -4.30773  3.62656  0.29575

H  -4.84076  4.44034 -0.22789

H  -3.73784  4.07466  1.12797

H  -5.06284  2.95592  0.73942

C   2.61901  1.81558  0.23846

C   3.53405  0.87975  0.83207

C   4.37755  1.27771  1.88352

H   5.06668  0.53426  2.30870

C   4.36663  2.58230  2.41012

C   3.45553  3.48941  1.84683

H   3.40210  4.51189  2.24813

C   2.59517  3.14134  0.78776

C   3.59230 -0.54758  0.34075

H   2.64312 -1.09052  0.49983

H   4.38185 -1.11256  0.86457

H   3.78902 -0.60203 -0.74282

C   5.30904  2.99249  3.52334

H   6.31647  3.25347  3.14268

H   5.44827  2.18105  4.26020

H   4.93101  3.87670  4.06602

C   1.62946  4.17900  0.26158

H   1.37870  4.91840  1.04253

H   0.70462  3.69965 -0.09641

H   2.04362  4.73897 -0.59707

C   3.68931  0.87415 -3.12304

H   3.64504 -0.22688 -3.07596

H   4.55104  1.20060 -2.51454

H   3.88912  1.16419 -4.17095

C   2.17510  3.49984 -3.08446

H   3.03157  4.02721 -2.62925

H   1.26075  4.06643 -2.84173

H   2.31444  3.52576 -4.18132

C   0.60011  0.88718 -3.42315

H  -0.35939  1.40719 -3.23564

H   0.47758 -0.19070 -3.20132

H   0.77667  0.95990 -4.51083

C   0.64286 -2.91114 -0.28641

C   0.54485 -3.27177  1.10008

C   1.52294 -4.09246  1.69201

H   1.40989 -4.35705  2.75306

C   2.63013 -4.58422  0.97977

C   2.74254 -4.20515 -0.36899

H   3.60780 -4.55222 -0.95172

C   1.79414 -3.38280 -1.00350

C  -0.60601 -2.77466  1.94641

H  -0.51502 -3.14331  2.98266

H  -1.58404 -3.09304  1.55159

H  -0.65503 -1.67086  1.99758

C   3.68308 -5.44330  1.65008

H   4.16612 -6.12794  0.93041

H   3.25022 -6.05773  2.45950

H   4.48907 -4.83484  2.10525

C   2.02825 -2.95612 -2.43436

H   2.02172 -1.85469 -2.51676

H   1.24492 -3.32022 -3.11935

H   3.00198 -3.32601 -2.80019

C  -3.04688 -3.53282 -0.63928

H  -2.67436 -4.41141 -0.08298

H  -3.90949 -3.86665 -1.24593

H  -3.40959 -2.79518  0.09608

C  -1.22354 -4.24019 -2.94741

H  -2.13648 -4.78855 -3.24355

H  -0.54485 -4.96034 -2.45810

H  -0.73288 -3.88435 -3.86967

C  -2.46911 -1.41366 -2.81304

H  -2.67137 -0.50438 -2.21627

H  -3.43762 -1.74662 -3.22714

H  -1.81993 -1.13279 -3.66068

1c

SCF (BP86) Energy = -1621.11408483

Enthalpy 0K = -1620.270692

Enthalpy 298K = -1620.207989

Free Energy 298K = -1620.372126

Lowest Frequency = 9.8094 cm-1

Second Frequency = 19.2929 cm-1

SCF (BP86-D3BJ) Energy =

-1621.38052769

SCF (C6H6) Energy = -1621.14568051

SCF (BS2) Energy = -3119.21696465

Ca  0.27711 -0.23031 -0.56260

N  -1.72686 -1.41996 -0.78968

Si -2.06701 -1.68687 -2.47513

Si  1.64097  2.80813 -1.76357

N   0.29935  2.08226 -0.90530

Si  3.14991 -2.67106 -0.90789

N   2.28003 -1.38389 -0.10652

C  -3.43107 -3.51898  1.83905

H  -3.37302 -4.54312  2.23548

C  -4.35998 -1.31035  1.88915

H  -5.04998 -0.57107  2.32011

C  -1.60716 -4.19487  0.24527

H  -2.02118 -4.75159 -0.61555

H  -1.35239 -4.93757  1.02177

H  -0.68462 -3.71045 -0.11194

C  -5.28087 -3.03587  3.52366

H  -6.28740 -3.30241  3.14443

H  -5.42369 -2.22683  4.26243

H  -4.89627 -3.91886  4.06374

C  -3.58570  0.52460  0.35223

H  -3.79019  0.58334 -0.72974

H  -2.63648  1.06873  0.50683

H  -4.37215  1.08623  0.88413

C  -2.15768 -3.50381 -3.09687

H  -3.01018 -4.03924 -2.64361

H  -1.23930 -4.06552 -2.85798

H  -2.29795 -3.52501 -4.19372

C  -3.69107 -0.88876 -3.11680

H  -4.54797 -1.22318 -2.50582

H  -3.89354 -1.17597 -4.16496

H  -3.65365  0.21232 -3.06543

C  -0.60254 -0.87885 -3.42740

H  -0.48662  0.19866 -3.20027

H  -0.78202 -0.94734 -4.51488

H   0.36096 -1.39337 -3.24541

C  -1.53760  4.07501  1.70905

H  -1.42562  4.32650  2.77335

C  -2.76557  4.19651 -0.34648

H  -3.63860  4.53742 -0.92118

C  -3.65890  5.48631  1.66162

H  -3.74415  5.28275  2.74367

H  -4.66287  5.36533  1.21753

H  -3.38803  6.55576  1.55626

C  -2.06224  2.95125 -2.41781

H  -1.29368  3.32919 -3.11211

H  -3.04614  3.30593 -2.77131

H  -2.03820  1.85023 -2.50151

C   2.45705  1.43121 -2.81141

H   2.66665  0.52614 -2.21075

H   3.42323  1.77201 -3.22452

H   1.81270  1.14106 -3.65962

C   3.00718  3.56933 -0.64590

H   2.61689  4.43577 -0.08281

H   3.86036  3.92572 -1.25298

H   3.38861  2.83558  0.08388

C   1.18043  4.24152 -2.96195

H   0.50136  4.96263 -2.47462

H   0.68572  3.87484 -3.87777

H   2.08870  4.79176 -3.26883

C   2.09265 -0.43330  3.51677

H   1.42535 -0.62333  4.36909

C   4.06698  0.56063  2.59053

H   4.96632  1.18317  2.70194

C   0.62652 -2.00776  2.20718

H  -0.27468 -1.62701  1.68374

H   0.27755 -2.27416  3.21926

H   0.90931 -2.92833  1.67014

C   3.49602  1.06840  5.02260

H   2.99211  0.54937  5.85662

H   3.14009  2.11682  5.03191

H   4.57750  1.09607  5.24775

C   4.79568  0.20232  0.21264

H   5.36525 -0.71276 -0.03480

H   5.52767  0.98332  0.48071

H   4.28042  0.50680 -0.71307

C   1.90959 -3.96363 -1.58560

H   1.39469 -4.48962 -0.76432

H   2.41884 -4.71866 -2.21217

H   1.13197 -3.48606 -2.20744

C   4.33149 -3.59757  0.28519

H   3.76324 -4.05207  1.11506

H   5.08102 -2.92285  0.73220

H   4.87125 -4.40596 -0.23989

C   4.16600 -2.15344 -2.45799

H   3.52449 -1.62997 -3.18888

H   4.58221 -3.04584 -2.96124

H   5.00370 -1.47960 -2.21494

C   3.21648  0.38710  3.69907

C   1.79634 -1.04674  2.28338

C   2.64428 -0.84135  1.13700

C   3.81609 -0.02802  1.34047

C  -1.81717  3.38109 -0.98970

C  -2.64555  4.57319  1.00244

C  -0.55973  3.26044  1.10832

C  -0.66003  2.91105 -0.28077

C  -3.52116 -0.90476  0.83684

C  -2.60514 -1.83495  0.23594

C  -2.57515 -3.16317  0.77898

C  -4.34327 -2.61740  2.40946

C   0.58719  2.74789  1.95080

H   0.61870  1.64344  2.00677

H   1.56811  3.04888  1.54996

H   0.50707  3.12094  2.98637

1d

SCF (BP86) Energy = -1621.11279532

Enthalpy 0K = -1620.268342

Enthalpy 298K = -1620.206352

Free Energy 298K = -1620.368825

Lowest Frequency = 9.1945 cm-1

Second Frequency = 14.6700 cm-1

SCF (BP86-D3BJ) Energy =

-1621.38006573

SCF (C6H6) Energy = -1621.14338739

SCF (BS2) Energy = -3119.21530345

Si  0.93808  2.10263 -2.17302

Si -1.64524 -2.46481 -2.82868

N  -0.12307  2.08041 -0.77389

N  -1.54609 -1.64211 -1.29366

N   1.63922 -1.07388  1.27357

C  -0.65887  3.13970 -0.04099

C  -1.06099  2.90677  1.32603

C  -1.55172  3.93897  2.13964

H  -1.82422  3.69634  3.17669

C  -1.71174  5.25598  1.67832

C  -1.40048  5.47717  0.32753

H  -1.56350  6.47912 -0.09595

C  -0.91061  4.47544 -0.52980

C  -0.98723  1.52037  1.91575

H  -1.29833  1.52407  2.97367

H   0.03820  1.09470  1.90257

H  -1.69448  0.82029  1.41560

C  -2.18925  6.37057  2.58419

H  -2.89714  5.99988  3.34745

H  -2.70134  7.16528  2.01239

H  -1.35645  6.85629  3.13157

C  -0.74898  4.83932 -1.98804

H  -1.33174  4.16158 -2.63650

H   0.29598  4.80191 -2.34359

H  -1.11082  5.86672 -2.16710

C   0.21579  2.39490 -3.93740

H   0.86611  1.89468 -4.67842

H   0.13911  3.45508 -4.22357

H  -0.78819  1.94499 -4.02215

C   2.51451  3.17158 -1.95283

H   3.18282  2.68912 -1.21900

H   2.28410  4.18331 -1.58020

H   3.06931  3.27218 -2.90311

C   1.60374  0.29671 -2.35690

H   2.22212 -0.06814 -1.51394

H   2.28915  0.30645 -3.22222

H   0.82946 -0.45230 -2.61706

C  -2.58683 -1.69223 -0.34973

C  -2.70657 -2.78137  0.58266

C  -3.71750 -2.77368  1.56012

H  -3.78148 -3.62179  2.25646

C  -4.64141 -1.71924  1.67937

C  -4.53151 -0.65751  0.76400

H  -5.25046  0.17195  0.81925

C  -3.54233 -0.62215 -0.23727

C  -1.73984 -3.94175  0.50655

H  -1.87182 -4.52794 -0.42140

H  -1.87334 -4.62593  1.36187

H  -0.69268 -3.59002  0.49267

C  -5.69384 -1.71443  2.76930

H  -6.58247 -1.13100  2.47058

H  -5.31526 -1.26645  3.70860

H  -6.02916 -2.73780  3.01491

C  -3.52027  0.51914 -1.23189

H  -3.64559  0.14613 -2.26456

H  -2.56319  1.07428 -1.22656

H  -4.33094  1.23719 -1.02054

C  -0.12936 -3.60177 -3.12242

H   0.81420 -3.03411 -3.03876

H  -0.15423 -4.05892 -4.12868

H  -0.09072 -4.41428 -2.37708

C  -1.67250 -1.26003 -4.32516

H  -2.58285 -0.63579 -4.31252

H  -1.65303 -1.81225 -5.28325

H  -0.80617 -0.57691 -4.31673

C  -3.23558 -3.52568 -2.99058

H  -3.27756 -4.33340 -2.24056

H  -3.29441 -3.98872 -3.99203

H  -4.13601 -2.90246 -2.85304

C   2.95232 -0.87253  0.79007

C   3.62316 -1.85077 -0.02174

C   4.91685 -1.59967 -0.51810

H   5.39677 -2.36923 -1.13973

C   5.60859 -0.40590 -0.25581

C   4.93922  0.56732  0.50874

H   5.44048  1.52401  0.71347

C   3.64404  0.36834  1.01947

C   2.93618 -3.14685 -0.39222

H   1.86300 -2.98712 -0.59403

H   2.98119 -3.89271  0.42100

H   3.40356 -3.59905 -1.28407

C   7.01850 -0.17949 -0.76180

H   7.78075 -0.44144 -0.00146

H   7.18898  0.87755 -1.03327

H   7.23049 -0.79380 -1.65446

C   2.97014  1.49133  1.77697

H   2.10515  1.89350  1.21585

H   3.67235  2.32571  1.94760

H   2.58243  1.15630  2.75237

Si  1.43131 -1.87793  2.81641

C  -0.37607 -1.67559  3.39811

H  -0.58298 -0.63901  3.71198

H  -0.56182 -2.32874  4.26990

H  -1.11547 -1.95192  2.62611

C   1.79333 -3.76974  2.84752

H   1.20138 -4.31428  2.09260

H   1.54041 -4.18611  3.84069

H   2.86097 -3.98267  2.66349

C   2.55996 -1.17471  4.20652

H   3.60216 -1.07579  3.85626

H   2.56259 -1.84372  5.08641

H   2.22337 -0.17907  4.54366

Ca -0.03671 -0.25281 -0.17386

1e

SCF (BP86) Energy = -1621.10943405

Enthalpy 0K = -1620.264550

Enthalpy 298K = -1620.202785

Free Energy 298K = -1620.364415

Lowest Frequency = 6.0830 cm-1

Second Frequency = 14.9791 cm-1

SCF (BP86-D3BJ) Energy =

-1621.37554214

SCF (C6H6) Energy = -1621.13987939

SCF (BS2) Energy = -3119.21217226

Ca  0.42591 -0.08966 -0.60519

N  -0.30605 -2.30211 -0.68239

Si  0.40388 -3.58320 -1.64087

Si  4.06059  1.11174 -1.02417

N   2.65796  0.55648 -0.13561

Si -0.82129  2.01160 -2.73560

N  -1.25248  1.59608 -1.08940

C  -2.68152 -3.31077  2.06603

H  -2.62523 -3.67473  3.10186

C  -3.96613 -2.60068  0.17039

H  -4.93498 -2.39608 -0.30653

C  -0.16800 -3.21451  2.11775

H   0.50582 -3.92991  1.62028

H  -0.34208 -3.56552  3.14983

H   0.39114 -2.26220  2.17786

C  -5.22135 -3.44855  2.21880

H  -5.57616 -4.47455  1.99626

H  -6.04016 -2.75992  1.94501

H  -5.08269 -3.38665  3.31251

C  -2.90580 -1.67990 -1.91838

H  -2.31294 -2.21143 -2.67911

H  -2.53083 -0.63780 -1.88596

H  -3.95826 -1.64974 -2.25039

C   1.05518 -5.10436 -0.65695

H   0.25259 -5.56639 -0.05597

H   1.87768 -4.83122  0.02620

H   1.43659 -5.87567 -1.35177

C  -0.77406 -4.36391 -2.94759

H  -1.73172 -4.66543 -2.48871

H  -0.31705 -5.26595 -3.39455

H  -1.00128 -3.66145 -3.76830

C   1.90073 -2.86510 -2.58738

H   1.58820 -2.19226 -3.40489

H   2.49244 -3.68000 -3.04165

H   2.57428 -2.30076 -1.92007

C   2.96168 -0.75814  3.37250

H   3.16988 -1.71673  3.86831

C   2.47834  1.59107  3.48603

H   2.28809  2.50103  4.07262

C   2.67311  0.29791  5.67292

H   1.66650  0.02713  6.04687

H   2.93975  1.26327  6.13804

H   3.37275 -0.46582  6.05673

C   2.21787  3.02365  1.42650

H   3.12950  3.42673  0.94770

H   1.87127  3.76605  2.16532

H   1.46278  2.94458  0.62405

C   4.57358 -0.12954 -2.39466

H   4.88605 -1.09565 -1.96242

H   5.41818  0.26776 -2.98763

H   3.74380 -0.33461 -3.09277

C   5.57975  1.33618  0.12341

H   5.37900  2.07139  0.92111

H   6.45779  1.68431 -0.44958

H   5.84833  0.38566  0.61545

C   3.82572  2.77666 -1.96053

H   3.61772  3.61059 -1.26928

H   2.98926  2.72782 -2.67860

H   4.73742  3.03041 -2.53304

C  -2.82522  2.46267  2.19251

H  -2.68391  2.16138  3.23990

C  -3.95861  3.71733  0.51770

H  -4.74155  4.42893  0.21714

C  -1.04894  0.79675  1.67831

H  -1.26604 -0.19212  1.21907

H  -1.12616  0.63126  2.76502

H   0.01020  1.08808  1.51539

C  -4.61694  4.11505  2.95095

H  -4.10480  5.00497  3.36915

H  -4.82513  3.44017  3.80077

H  -5.58823  4.46216  2.55506

C  -3.56766  3.46096 -1.92185

H  -2.75679  3.93585 -2.50134

H  -4.42070  4.16134 -1.93360

H  -3.87407  2.55752 -2.47820

C   0.60030  0.78346 -3.21198

H   1.53332  0.87770 -2.62376

H   0.89457  1.01845 -4.24915

H   0.27218 -0.27509 -3.23189

C  -0.04345  3.74966 -2.97133

H   0.80949  3.87036 -2.28215

H  -0.75334  4.56783 -2.76432

H   0.33047  3.87906 -4.00350

C  -2.03504  1.68450 -4.20005

H  -2.63151  0.77519 -4.01329

H  -1.44715  1.51277 -5.12051

H  -2.73155  2.51324 -4.39867

C  -3.79685  3.42727  1.88083

C  -2.02241  1.85292  1.21694

C  -2.12692  2.19729 -0.18189

C  -3.18417  3.12891 -0.49857

C   2.47486  1.68504  2.08236

C   2.71345  0.38005  4.16060

C   2.96813 -0.71422  1.96637

C   2.71203  0.51950  1.27420

C  -2.79292 -2.31955 -0.55286

C  -1.50386 -2.57564  0.02684

C  -1.47958 -3.04793  1.38297

C  -3.94264 -3.11447  1.47843

C   3.28447 -1.96592  1.17823

H   2.41821 -2.30500  0.58013

H   4.10625 -1.79223  0.46140

H   3.57147 -2.79191  1.85190

I

SCF (BP86) Energy = -1881.67556835

Enthalpy 0K = -1880.729952

Enthalpy 298K = -1880.659957

Free Energy 298K = -1880.838634

Lowest Frequency = 18.1487 cm-1

Second Frequency = 19.8250 cm-1

SCF (BP86-D3BJ) Energy =

-1881.99662751

SCF (C6H6) Energy = -1881.68317833

SCF (BS2) Energy = -3951.47002641

Ca  1.62776  0.91487 -0.08863

H  -2.04181 -3.56145 -0.69589

Si  3.57024 -0.74569 -2.27677

Si  0.62001  3.97020 -1.08365

Si  2.68173  0.95294  3.13848

N   2.25484 -1.05623 -1.15353

N  -0.03176  2.33615 -1.04368

N   1.21153  0.72298  2.20858

C   1.85527 -2.40280 -0.94832

C   2.46432 -3.22633  0.05880

C   2.05638 -4.56157  0.23491

H   2.55136 -5.15878  1.01271

C   1.04713 -5.15462 -0.54249

C   0.42289 -4.33770 -1.50067

H  -0.36979 -4.76573 -2.13125

C   0.79211 -2.99341 -1.70926

C   3.52184 -2.66236  0.97858

H   3.79130 -3.39307  1.75997

H   3.15653 -1.74596  1.47339

H   4.44435 -2.38557  0.44352

C   0.67168 -6.61217 -0.37402

H   1.35290 -7.27751 -0.93795

H  -0.35014 -6.81354 -0.73890

H   0.72168 -6.92640  0.68316

C   0.04340 -2.19069 -2.74802

H  -0.40978 -1.27502 -2.32519

H  -0.76153 -2.79443 -3.20266

H   0.70154 -1.84458 -3.56120

C   5.26573 -1.54109 -1.86658

H   5.69251 -1.15682 -0.92446

H   5.98747 -1.32321 -2.67461

H   5.18629 -2.63858 -1.78299

C   3.86246  1.15581 -2.22985

H   4.61699  1.42252 -2.99052

H   4.28087  1.49588 -1.26292

H   2.96078  1.74809 -2.47470

C   3.25379 -1.23634 -4.10191

H   4.15862 -1.05291 -4.70894

H   2.42340 -0.67007 -4.55473

H   3.01697 -2.31169 -4.18080

C  -1.20216  2.03247 -1.77170

C  -2.52479  2.28428 -1.26066

C  -3.66847  1.90520 -1.99896

H  -4.65965  2.13105 -1.57886

C  -3.58653  1.29516 -3.26011

C  -2.29385  1.06135 -3.76966

H  -2.18699  0.60367 -4.76239

C  -1.12691  1.41457 -3.07213

C  -2.73245  2.98897  0.06656

H  -1.88733  2.82166  0.75377

H  -3.67865  2.67961  0.55116

H  -2.80231  4.08307 -0.05966

C  -4.82420  0.94234 -4.05957

H  -4.90081  1.55189 -4.97887

H  -5.74471  1.11811 -3.47694

H  -4.82457 -0.11454 -4.38339

C   0.21711  1.17639 -3.71662

H   0.10076  0.67616 -4.69262

H   0.86581  0.54413 -3.08480

H   0.75635  2.12451 -3.88046

C  -0.42369  5.38632 -0.32042

H  -0.71671  5.18774  0.72307

H  -1.33843  5.57770 -0.90732

H   0.17137  6.31761 -0.33376

C   1.06545  4.60470 -2.83496

H   0.19549  4.54015 -3.51145

H   1.89025  4.02942 -3.28886

H   1.37665  5.66402 -2.79609

C   2.24834  3.91922 -0.06400

H   3.06139  3.35771 -0.56105

H   2.09997  3.53104  0.96119

H   2.62827  4.94952  0.04941

C  -0.04019  0.49462  2.79616

C  -0.53859 -0.84512  2.99880

C  -1.82149 -1.05789  3.54705

H  -2.15061 -2.09273  3.71400

C  -2.68095  0.00023  3.90755

C  -2.20424  1.30792  3.68870

H  -2.84145  2.15988  3.96338

C  -0.92216  1.57387  3.16578

C   0.30741 -2.03980  2.62630

H  -0.23520 -2.98199  2.81072

H   1.24229 -2.06735  3.20899

H   0.62098 -2.03017  1.56730

C  -4.02473 -0.25473  4.55985

H  -4.74477  0.55363  4.34436

H  -3.93216 -0.31638  5.66048

H  -4.46971 -1.20704  4.22305

C  -0.47556  3.00862  3.01225

H   0.02911  3.16374  2.04417

H   0.25228  3.28850  3.79265

H  -1.32954  3.70251  3.08940

C   3.11712 -0.47076  4.34150

H   2.27824 -0.67045  5.03109

H   3.99290 -0.19866  4.95759

H   3.35436 -1.40831  3.81257

C   2.78454  2.53827  4.21230

H   3.78540  2.60853  4.67612

H   2.04583  2.52443  5.03252

H   2.62345  3.45608  3.62199

C   4.09339  1.11147  1.84410

H   4.12087  0.27377  1.12216

H   5.06479  1.09391  2.36882

H   4.06204  2.07217  1.29735

C  -3.00731 -3.10714 -0.44396

C  -3.64174 -2.24079 -1.35580

C  -3.61650 -3.38615  0.79449

C  -4.87913 -1.65342 -1.02799

H  -3.17159 -2.01958 -2.31958

C  -4.85382 -2.80205  1.12106

H  -3.12895 -4.06786  1.49880

C  -5.48477 -1.93413  0.21079

H  -5.36890 -0.98412 -1.74198

H  -5.33225 -3.03178  2.07893

H  -6.45451 -1.48986  0.46003

K  -2.40692 -0.05381  0.65216

I’

SCF (BP86) Energy = -1853.36027721

Enthalpy 0K = -1852.418262

Enthalpy 298K = -1852.348757

Free Energy 298K = -1852.533957

Lowest Frequency = 7.5040 cm-1

Second Frequency = 12.8154 cm-1

SCF (BP86-D3BJ) Energy =

-1853.65204267

SCF (C6H6) Energy = -1853.39208963

SCF (BS2) Energy = -3351.51972237

Ca  1.57211  0.10208  0.37086

Si  2.42365 -2.74330  2.17661

Si  1.83302  2.90408  2.40282

Si  3.69870  0.43936 -2.36952

N   1.08271 -1.71073  1.75707

N   0.95582  2.25429  1.04163

N   2.20939 -0.29575 -1.83916

C  -0.24576 -2.01994  2.12649

C  -1.12066 -2.71594  1.22309

C  -2.44800 -2.99792  1.59461

H  -3.07943 -3.55407  0.88669

C  -2.98682 -2.60714  2.83471

C  -2.13953 -1.90070  3.70319

H  -2.53204 -1.56121  4.67218

C  -0.80322 -1.59834  3.37896

C  -0.62979 -3.15287 -0.13844

H  -0.31559 -2.30383 -0.77279

H  -1.42095 -3.69064 -0.68776

H   0.25061 -3.81192 -0.06766

C  -4.42705 -2.90577  3.19833

H  -4.68919 -3.96249  3.00437

H  -5.13673 -2.28786  2.61542

H  -4.62034 -2.70517  4.26629

C   0.02261 -0.78731  4.35056

H  -0.60649 -0.39617  5.16891

H   0.50035  0.06504  3.83723

H   0.84027 -1.37314  4.80362

C   2.85021 -2.91233  4.04598

H   3.73711 -3.56026  4.17659

H   2.02027 -3.37154  4.61115

H   3.07589 -1.93506  4.50601

C   3.97928 -1.97095  1.36019

H   3.83807 -1.79006  0.27795

H   4.83952 -2.65679  1.45869

H   4.26917 -1.02289  1.84880

C   2.28043 -4.56237  1.57525

H   2.31649 -4.63526  0.47531

H   1.32811 -5.00880  1.91143

H   3.10197 -5.17901  1.98404

C  -0.13191  2.95942  0.47731

C  -1.48102  2.69228  0.88811

C  -2.55331  3.39947  0.31026

H  -3.57126  3.18499  0.66560

C  -2.36897  4.36795 -0.69148

C  -1.05161  4.59362 -1.12696

H  -0.87073  5.31961 -1.93244

C   0.05190  3.91731 -0.57680

C  -1.77388  1.64286  1.93620

H  -1.29038  1.87251  2.89995

H  -1.40438  0.64129  1.64987

H  -2.85949  1.55282  2.10984

C  -3.53428  5.14642 -1.26703

H  -3.43223  5.28838 -2.35807

H  -3.62093  6.15663 -0.82051

H  -4.49289  4.63051 -1.08412

C   1.42964  4.17781 -1.14043

H   1.92974  3.22880 -1.40031

H   2.09131  4.68844 -0.42064

H   1.37043  4.80307 -2.04820

C   2.84183  4.51569  2.10356

H   3.59935  4.38525  1.31186

H   3.36869  4.81298  3.02953

H   2.18602  5.35502  1.81297

C   0.76674  3.31277  3.94746

H   1.36561  3.84128  4.71178

H   0.35091  2.40280  4.41152

H  -0.07871  3.96760  3.67267

C   3.12020  1.57372  2.90857

H   3.61002  1.86184  3.85573

H   3.92159  1.47111  2.15422

H   2.65491  0.58459  3.07824

C   1.35509 -0.97689 -2.73649

C   0.22901 -0.31083 -3.32938

C  -0.63288 -1.00516 -4.19767

H  -1.48169 -0.46137 -4.63550

C  -0.45060 -2.36162 -4.51806

C   0.62942 -3.02211 -3.90883

H   0.78384 -4.09183 -4.11011

C   1.51872 -2.37131 -3.03386

C  -0.05450  1.14222 -3.02139

H  -0.25906  1.32326 -1.94969

H  -0.93693  1.49679 -3.58041

H   0.79884  1.79233 -3.27471

C  -1.37074 -3.07545 -5.48703

H  -2.40364 -2.68966 -5.42509

H  -1.40525 -4.16077 -5.28649

H  -1.04477 -2.95236 -6.53895

C   2.61478 -3.17420 -2.37169

H   2.46841 -4.25450 -2.54528

H   2.62806 -2.99165 -1.28342

H   3.61948 -2.90773 -2.74161

C   3.51125  1.71012 -3.79782

H   4.49897  2.03361 -4.17450

H   2.95904  2.60941 -3.47729

H   2.96079  1.26119 -4.64324

C   5.09833 -0.73347 -2.97851

H   5.37869 -1.47211 -2.20824

H   6.00179 -0.14666 -3.22947

H   4.80045 -1.28481 -3.88750

C   4.42500  1.35173 -0.84575

H   4.77778  0.64054 -0.07650

H   3.69607  2.04583 -0.38736

H   5.29897  1.95739 -1.14473

C  -7.57270  0.27607 -1.31854

C  -6.41376  1.06908 -1.26763

C  -7.52468 -1.06293 -0.89630

H  -8.51296  0.70129 -1.68804

C  -5.20700  0.52647 -0.79459

H  -6.44963  2.11295 -1.59865

C  -6.31762 -1.60635 -0.42463

H  -8.42741 -1.68332 -0.93617

C  -5.15850 -0.81325 -0.37197

H  -4.30508  1.14666 -0.75314

H  -6.27759 -2.65131 -0.09794

H  -4.21851 -1.23897 -0.00404

II

SCF (BP86) Energy = -1650.05123818

Enthalpy 0K = -1649.201425

Enthalpy 298K = -1649.137043

Free Energy 298K = -1649.302095

Lowest Frequency = 14.8529 cm-1

Second Frequency = 20.3983 cm-1

SCF (BP86-D3BJ) Energy =

-1650.32972328

SCF (C6H6) Energy = -1650.08736532

SCF (BS2) Energy = -3719.80354974

Ca  0.27008 -0.21655 -0.46606

H  -0.08439 -0.02769  1.62471

Si  3.16550 -2.25452 -1.37256

Si -2.42718 -1.93799 -2.44304

Si  0.58571  2.85141 -2.49331

N   2.51237 -1.02200 -0.32642

N  -1.84606 -1.49769 -0.85906

N  -0.12283  2.11400 -1.08240

C   3.31705 -0.55318  0.74171

C   4.19576  0.57183  0.57987

C   5.00174  1.01513  1.64489

H   5.66473  1.87608  1.47588

C   4.98094  0.40509  2.90990

C   4.08189 -0.66081  3.08680

H   4.01031 -1.14078  4.07369

C   3.25531 -1.13808  2.05342

C   4.22613  1.33589 -0.72323

H   4.93413  2.18167 -0.66638

H   3.22614  1.74017 -0.95953

H   4.51280  0.70425 -1.57949

C   5.89429  0.86544  4.02754

H   6.85350  0.30978  4.04184

H   5.42801  0.72103  5.01873

H   6.14713  1.93632  3.92918

C   2.25737 -2.22859  2.36249

H   1.22890 -1.83607  2.24063

H   2.37330 -2.58098  3.40322

H   2.35868 -3.09601  1.69104

C   4.82742 -1.82750 -2.24906

H   4.70313 -1.02089 -2.99229

H   5.22832 -2.71259 -2.77715

H   5.58883 -1.50086 -1.51930

C   1.88693 -2.57990 -2.75745

H   2.18925 -3.44259 -3.37769

H   1.79442 -1.70627 -3.42617

H   0.88949 -2.80870 -2.34156

C   3.52615 -3.95545 -0.54292

H   3.99602 -4.65039 -1.26385

H   2.60303 -4.43061 -0.16878

H   4.21694 -3.84236  0.31090

C  -2.40273 -2.02404  0.31342

C  -3.59322 -1.48968  0.92780

C  -4.04490 -1.97227  2.17650

H  -4.96016 -1.53597  2.60769

C  -3.39384 -3.00642  2.86823

C  -2.25028 -3.55718  2.25490

H  -1.71910 -4.37735  2.75804

C  -1.75568 -3.10175  1.02404

C  -4.36962 -0.37067  0.26429

H  -3.70117  0.27044 -0.33358

H  -4.91586  0.24436  1.00685

H  -5.13143 -0.75082 -0.43843

C  -3.91021 -3.53075  4.19257

H  -4.29627 -4.56499  4.10652

H  -4.73639 -2.90678  4.57666

H  -3.12055 -3.55296  4.96638

C  -0.52910 -3.75483  0.43303

H  -0.19948 -4.60533  1.05435

H   0.32236 -3.05333  0.36000

H  -0.72199 -4.11983 -0.58953

C  -4.29729 -1.65574 -2.82026

H  -4.58220 -0.59331 -2.73976

H  -4.94615 -2.23946 -2.14386

H  -4.51657 -1.98650 -3.85261

C  -2.17224 -3.79274 -2.89330

H  -2.65922 -4.45135 -2.15226

H  -1.10163 -4.05797 -2.92886

H  -2.60926 -4.02421 -3.88256

C  -1.47943 -0.90336 -3.73788

H  -0.41625 -1.19180 -3.79036

H  -1.53515  0.17381 -3.50432

H  -1.91184 -1.05515 -4.74302

C  -0.88027  2.79490 -0.13188

C  -0.29026  3.25606  1.10639

C  -1.08356  3.87117  2.09407

H  -0.59031  4.22236  3.01230

C  -2.47394  4.06826  1.94626

C  -3.05559  3.61136  0.74633

H  -4.13525  3.75229  0.58858

C  -2.30275  3.00258 -0.27927

C   1.18243  3.04804  1.36099

H   1.49917  3.55379  2.28968

H   1.79482  3.42501  0.52701

H   1.41258  1.97097  1.46826

C  -3.28816  4.79999  2.99564

H  -4.34767  4.48648  2.98434

H  -3.27966  5.89569  2.83284

H  -2.89521  4.63040  4.01454

C  -3.00350  2.55515 -1.54109

H  -2.61934  1.57497 -1.87211

H  -2.82359  3.25549 -2.37504

H  -4.09526  2.48935 -1.39151

C   1.78889  4.29858 -2.09372

H   1.29422  5.05383 -1.45729

H   2.11692  4.80578 -3.01998

H   2.69015  3.94921 -1.56270

C  -0.61228  3.62636 -3.79053

H  -0.02995  4.00320 -4.65240

H  -1.17541  4.48168 -3.37677

H  -1.33873  2.88970 -4.17368

C   1.54712  1.49613 -3.43720

H   2.14930  0.86704 -2.75820

H   2.24051  1.95444 -4.16505

H   0.85777  0.84375 -3.99991

K  -2.18713  0.86487  2.25544

III

SCF (BP86) Energy = -1881.09226235

Enthalpy 0K = -1880.160618

Enthalpy 298K = -1880.091023

Free Energy 298K = -1880.267129

Lowest Frequency = 15.6796 cm-1

Second Frequency = 19.3673 cm-1

SCF (BP86-D3BJ) Energy =

-1881.40980284

SCF (C6H6) Energy = -1881.12743619

SCF (BS2) Energy = -3950.90001061

Ca -0.26457  0.21304 -0.52695

Si -3.36955  1.72411 -1.93116

Si  2.23089  2.15978 -2.59629

Si -0.19834 -2.79999 -2.79656

N  -2.58308  0.76089 -0.70175

N   1.51732  1.81210 -1.03373

N   0.41235 -2.10947 -1.30426

C  -3.37639  0.29026  0.37411

C  -4.00261 -1.00220  0.33702

C  -4.78678 -1.45322  1.41579

H  -5.25411 -2.44621  1.34387

C  -4.99046 -0.68338  2.57263

C  -4.34174  0.56248  2.63052

H  -4.44628  1.17721  3.53594

C  -3.54349  1.05280  1.58205

C  -3.80266 -1.91727 -0.84953

H  -4.29466 -2.89145 -0.67983

H  -2.72969 -2.10191 -1.03632

H  -4.20384 -1.48972 -1.78327

C  -5.87969 -1.16581  3.70039

H  -6.91462 -0.77844  3.61307

H  -5.50018 -0.84019  4.68560

H  -5.95056 -2.26798  3.71597

C  -2.81314  2.36117  1.77463

H  -1.72067  2.19160  1.78422

H  -3.09031  2.82499  2.73758

H  -3.01757  3.08325  0.96968

C  -4.79898  0.84441 -2.87873

H  -4.42902 -0.00558 -3.47782

H  -5.30050  1.54900 -3.56817

H  -5.56358  0.46177 -2.17995

C  -2.07206  2.22364 -3.24263

H  -2.46498  3.02938 -3.88833

H  -1.81198  1.37079 -3.89159

H  -1.14673  2.59408 -2.76894

C  -4.19612  3.35605 -1.32457

H  -4.76065  3.82708 -2.15094

H  -3.45144  4.08804 -0.96743

H  -4.90653  3.16559 -0.50134

C   1.90894  2.67002  0.01727

C   3.07133  2.41476  0.82472

C   3.44675  3.29927  1.85488

H   4.34845  3.07018  2.44264

C   2.70621  4.44994  2.16562

C   1.53533  4.67454  1.41676

H   0.91047  5.54737  1.65331

C   1.12480  3.82400  0.37666

C   3.88117  1.15271  0.62375

H   3.23589  0.35250  0.22196

H   4.35657  0.83539  1.57321

H   4.69430  1.27027 -0.11503

C   3.14363  5.40907  3.25342

H   3.60619  6.32643  2.83879

H   3.88906  4.94526  3.92304

H   2.29199  5.73684  3.87664

C  -0.16323  4.12723 -0.35391

H  -0.86501  3.27432 -0.31981

H   0.00891  4.34311 -1.42145

H  -0.66988  4.99885  0.09547

C   4.15373  2.03099 -2.67292

H   4.51050  1.01028 -2.45449

H   4.62842  2.72214 -1.95439

H   4.51211  2.30510 -3.68260

C   1.89265  3.93155 -3.26913

H   2.17494  4.70192 -2.53038

H   0.82758  4.07375 -3.52047

H   2.48165  4.11646 -4.18666

C   1.54534  0.93970 -3.89324

H   0.51125  1.20191 -4.17175

H   1.54929 -0.09556 -3.51382

H   2.15848  0.96873 -4.81172

C   1.29895 -2.85399 -0.53093

C   0.85754 -3.79578  0.47940

C   1.79001 -4.50822  1.26250

H   1.40592 -5.22324  2.00523

C   3.18510 -4.35982  1.11706

C   3.62483 -3.42896  0.15111

H   4.70513 -3.28869 -0.00229

C   2.73419 -2.68947 -0.65397

C  -0.61669 -4.03935  0.70651

H  -0.82925 -4.26778  1.76504

H  -0.98101 -4.89163  0.10534

H  -1.20487 -3.16241  0.39650

C   4.16243 -5.20301  1.91268

H   5.12436 -4.68196  2.06752

H   4.39702 -6.15397  1.39604

H   3.75909 -5.47354  2.90510

C   3.28924 -1.72389 -1.67315

H   2.79057 -0.74094 -1.60918

H   3.11861 -2.08626 -2.70094

H   4.37582 -1.58316 -1.53744

C  -1.20690 -4.42978 -2.60977

H  -0.59503 -5.23663 -2.16908

H  -1.53948 -4.77538 -3.60629

H  -2.10293 -4.29546 -1.98205

C   1.16701 -3.28925 -4.06424

H   0.71542 -3.80787 -4.93033

H   1.90872 -3.97590 -3.61874

H   1.70405 -2.40494 -4.44794

C  -1.32701 -1.52642 -3.65373

H  -1.96311 -0.98940 -2.92842

H  -1.99415 -2.03334 -4.37357

H  -0.73242 -0.78467 -4.21161

C  -0.05949  0.01363  2.04063

C   0.71516  0.84602  2.90981

C  -0.72302 -1.05159  2.72564

C   0.87452  0.60929  4.29476

H   1.23473  1.71887  2.49211

C  -0.57693 -1.31952  4.10491

H  -1.39877 -1.71109  2.16395

C   0.24473 -0.49611  4.89823

H   1.47901  1.29531  4.90517

H  -1.11695 -2.15840  4.56580

H   0.35998 -0.68942  5.97239

K   2.27906 -1.60020  2.27255

IV

SCF (BP86) Energy = -1648.83267281

Enthalpy 0K = -1648.000604

Enthalpy 298K = -1647.937455

Free Energy 298K = -1648.098837

Lowest Frequency = 14.8219 cm-1

Second Frequency = 22.0863 cm-1

SCF (BP86-D3BJ) Energy =

-1649.11158974

SCF (C6H6) Energy = -1648.86656874

SCF (BS2) Energy = -3718.58879882

Ca -0.40188  0.53084  0.34175

K   3.56643 -1.23995  0.59664

Si  0.64570 -1.40343  2.73804

Si -3.48043  2.21433  1.14182

Si  0.83149  3.62081 -1.26924

N   0.69945 -1.47045  0.98978

N  -2.75766  0.84679  0.31670

N   1.21492  2.05705 -0.54765

C   2.26583 -0.95309  3.70469

H   3.05799 -1.71499  3.61669

H   2.02755 -0.82370  4.77767

H   2.66817  0.01517  3.35058

C  -0.38830  0.18708  3.16293

H   0.13632  1.13470  2.92064

H  -0.51204  0.21031  4.26006

H  -1.41066  0.21571  2.73961

C   0.95872 -2.58880  0.13404

C   0.31822 -2.62630 -1.14245

C   0.60142 -3.61842 -2.10746

H   0.06781 -3.59813 -3.06668

C   1.52246 -4.64619 -1.82647

C   2.13801 -4.64529 -0.57383

H   2.85491 -5.44587 -0.33744

C  -0.73040 -1.60045 -1.50905

H  -1.48950 -1.47272 -0.71262

H  -1.29298 -1.90623 -2.40640

H  -0.30184 -0.60562 -1.78373

C   1.78789 -5.75137 -2.83060

H   1.87786 -5.35635 -3.85975

H   0.97227 -6.50145 -2.85037

H   2.72130 -6.29332 -2.59618

C  -3.66097 -0.08865 -0.25619

C  -4.12379 -1.23267  0.47786

C  -5.02864 -2.13899 -0.10465

H  -5.36168 -2.99967  0.49217

C  -5.50398 -1.99271 -1.41854

C  -5.00239 -0.90935 -2.15911

H  -5.31601 -0.78651 -3.20561

C  -4.09785  0.02323 -1.61898

C  -3.58814 -1.52585  1.86031

H  -2.50033 -1.72113  1.82203

H  -4.07304 -2.42037  2.28784

H  -3.73247 -0.68637  2.55867

C  -6.51295 -2.95658 -2.00775

H  -7.55624 -2.64572 -1.80084

H  -6.39292 -3.97277 -1.59261

H  -6.41108 -3.02824 -3.10497

C  -3.54119  1.10152 -2.51971

H  -3.95337  1.01049 -3.53981

H  -2.44069  1.02960 -2.58942

H  -3.75390  2.11771 -2.15172

C  -4.51271  3.40374  0.03635

H  -3.89269  3.90652 -0.72507

H  -4.98822  4.18691  0.65549

H  -5.31768  2.85827 -0.48631

C  -2.07628  3.25887  1.92340

H  -1.65574  2.77309  2.82015

H  -2.47003  4.24334  2.23330

H  -1.25152  3.45478  1.21552

C  -4.69072  1.77566  2.57193

H  -5.46286  1.06362  2.23250

H  -5.20806  2.68363  2.93283

H  -4.16871  1.32321  3.43276

C   2.57686  1.70951 -0.55220

C   3.45239  2.04584  0.54252

C   4.82535  1.73111  0.49154

H   5.46096  2.02117  1.34033

C   5.41280  1.08152 -0.61279

C   4.55055  0.70570 -1.66267

H   4.96907  0.18111 -2.53348

C   3.16804  0.98228 -1.64980

C   2.89996  2.73863  1.76782

H   2.03226  2.19316  2.18035

H   2.53327  3.75278  1.53919

H   3.66685  2.81853  2.55735

C   6.90623  0.83321 -0.68441

H   7.34490  0.69299  0.31917

H   7.43896  1.68369 -1.15247

H   7.14295 -0.06271 -1.28473

C   2.31167  0.47344 -2.78968

H   1.84243 -0.49751 -2.53605

H   2.91607  0.31229 -3.69884

H   1.49405  1.17250 -3.01942

C  -0.94683  3.56943 -1.95065

H  -0.97906  3.01446 -2.90401

H  -1.32991  4.58826 -2.13882

H  -1.64437  3.06686 -1.25885

C   2.00183  4.09088 -2.71611

H   3.05905  4.08115 -2.40071

H   1.76592  5.11029 -3.07170

H   1.90244  3.40423 -3.57332

C   0.93300  5.13962 -0.08759

H   0.37315  4.98444  0.85030

H   0.51015  6.03190 -0.58590

H   1.97879  5.37779  0.17548

C  -0.21213 -2.85109  3.64843

H   0.34704 -3.78585  3.47970

H  -0.27440 -2.66463  4.73599

H  -1.23572 -2.99621  3.26457

C   1.91600 -3.65923  0.44672

C   2.71998 -3.71380  1.64012

H   3.23087 -4.67280  1.80961

H   2.30879 -3.30576  2.56793

TS(IV-V)

SCF (BP86) Energy = -1648.82542721

Enthalpy 0K = -1647.994147

Enthalpy 298K = -1647.931740

Free Energy 298K = -1648.091700

Lowest Frequency = -199.4374 cm-1

Second Frequency = 15.1270 cm-1

SCF (BP86-D3BJ) Energy =

-1649.105961

SCF (C6H6) Energy = -1648.85908093

SCF (BS2) Energy = -3718.58081208

Ca  0.52905 -0.56947  0.35107

K  -3.47320  1.24211  0.62415

Si -0.81527  1.32357  2.71427

Si  3.70254 -2.05401  1.11332

Si -0.69040 -3.60085 -1.29987

N  -0.48389  1.43687  0.96878

N   2.87626 -0.76984  0.25867

N  -1.14430 -2.06999 -0.56024

C  -2.44915  0.68485  3.57667

H  -3.15167  1.51869  3.73157

H  -2.19921  0.22791  4.55503

H  -2.95047 -0.11245  2.99218

C   0.22298 -0.33308  3.08538

H  -0.21249 -1.28105  2.69948

H   0.22587 -0.47066  4.18126

H   1.29213 -0.27885  2.79427

C  -0.88941  2.46721  0.10161

C  -0.49186  2.44827 -1.26952

C  -1.07490  3.32894 -2.21132

H  -0.73447  3.28721 -3.25536

C  -2.06447  4.25409 -1.83677

C  -2.40629  4.32869 -0.47127

H  -3.13045  5.09125 -0.14489

C   0.54519  1.45978 -1.75540

H   1.44160  1.43907 -1.10502

H   0.90552  1.72102 -2.76494

H   0.14362  0.42475 -1.86597

C  -2.66670  5.21070 -2.84751

H  -2.55682  4.83093 -3.87898

H  -2.18544  6.20896 -2.81820

H  -3.74494  5.37669 -2.66487

C   3.67239  0.26809 -0.29189

C   3.95013  1.47088  0.44300

C   4.74991  2.48167 -0.12153

H   4.94444  3.38498  0.47355

C   5.29202  2.38464 -1.41428

C   4.96926  1.23588 -2.15597

H   5.33871  1.14402 -3.18745

C   4.17445  0.19832 -1.63532

C   3.33300  1.70211  1.80368

H   2.23161  1.78537  1.72652

H   3.70705  2.64036  2.24854

H   3.54195  0.87884  2.50523

C   6.18821  3.46710 -1.97978

H   7.25278  3.30699 -1.71675

H   5.91030  4.46478 -1.59641

H   6.13218  3.50376 -3.08211

C   3.79762 -0.95413 -2.53830

H   4.24920 -0.83134 -3.53833

H   2.70162 -1.01562 -2.66393

H   4.10965 -1.93123 -2.13671

C   4.89988 -3.13129  0.05947

H   4.36468 -3.69229 -0.72594

H   5.42431 -3.86463  0.69987

H   5.66795 -2.50840 -0.43118

C   2.38387 -3.24936  1.82018

H   1.73869 -2.75899  2.57003

H   2.87990 -4.09961  2.32179

H   1.74239 -3.67117  1.02748

C   4.78598 -1.48532  2.59746

H   5.49036 -0.69207  2.29242

H   5.38093 -2.32911  2.99295

H   4.17172 -1.09004  3.42485

C  -2.50686 -1.73917 -0.53834

C  -3.35634 -2.08670  0.57717

C  -4.72338 -1.74481  0.58295

H  -5.33194 -2.04095  1.44934

C  -5.34180 -1.07090 -0.49043

C  -4.51577 -0.71472 -1.57461

H  -4.96052 -0.19043 -2.43303

C  -3.13801 -1.01625 -1.61896

C  -2.78655 -2.84315  1.75509

H  -1.91014 -2.32775  2.18326

H  -2.43295 -3.84507  1.46059

H  -3.54080 -2.96230  2.55160

C  -6.83249 -0.79483 -0.50053

H  -7.22408 -0.62135  0.51766

H  -7.40277 -1.64606 -0.92042

H  -7.08064  0.08883 -1.11465

C  -2.34046 -0.54676 -2.81732

H  -2.03803  0.51319 -2.70882

H  -2.93518 -0.62253 -3.74454

H  -1.42120 -1.13917 -2.93003

C   1.07536 -3.43729 -2.00352

H   1.05905 -2.86021 -2.94456

H   1.51031 -4.42852 -2.22412

H   1.76434 -2.91443 -1.31599

C  -1.85360 -4.11792 -2.73636

H  -2.90567 -4.15786 -2.40544

H  -1.57845 -5.12296 -3.10426

H  -1.79737 -3.41927 -3.58772

C  -0.68562 -5.13113 -0.12870

H  -0.14175 -4.93713  0.81148

H  -0.19913 -5.99046 -0.62688

H  -1.71229 -5.44351  0.13271

C   0.08400  2.52583  3.92413

H   0.62999  3.30197  3.36295

H  -0.63400  3.03449  4.59020

H   0.81594  1.98477  4.54979

C  -1.81329  3.51550  0.53275

C  -2.22806  3.52756  1.92880

H  -3.07505  4.21581  2.12468

H  -1.41921  3.79113  2.62316

V

SCF (BP86) Energy = -1648.83760232

Enthalpy 0K = -1648.006922

Enthalpy 298K = -1647.943516

Free Energy 298K = -1648.107163

Lowest Frequency = 11.2106 cm-1

Second Frequency = 15.5760 cm-1

SCF (BP86-D3BJ) Energy =

-1649.11651963

SCF (C6H6) Energy = -1648.87212122

SCF (BS2) Energy = -3718.59136147

Ca  0.62600 -0.53941  0.60643

K  -3.24728  0.48225  0.16947

Si  4.25416 -0.98552  1.04215

Si  0.15601 -4.07782 -0.36568

N  -0.69424  1.27737  1.11690

N   2.91620 -0.21877  0.22252

N  -0.56987 -2.47954 -0.39491

C  -1.88150  3.01385  2.82469

H  -2.81081  3.20245  3.39946

H  -1.11857  3.70015  3.24967

C  -2.81841  0.24777  3.35251

H  -3.69077  0.85502  3.03380

H  -2.90352  0.16572  4.45284

H  -2.91643 -0.78145  2.95812

C   0.00325  1.61032  4.46856

H   0.45183  0.77114  5.02701

H  -0.58618  2.22986  5.16943

H   0.83049  2.24962  4.10676

C  -1.26484  2.40269  0.53546

C  -1.25186  2.64539 -0.87938

C  -2.04562  3.67915 -1.42201

H  -2.01917  3.83860 -2.51039

C  -2.85491  4.51293 -0.62847

C  -2.81694  4.30916  0.77402

H  -3.40463  4.97122  1.42752

C  -0.41009  1.77007 -1.77374

H   0.66330  1.82760 -1.50983

H  -0.50686  2.05271 -2.83623

H  -0.70337  0.70158 -1.70073

C  -3.67850  5.62879 -1.23951

H  -4.71155  5.65054 -0.84288

H  -3.74666  5.52299 -2.33683

H  -3.24566  6.62918 -1.03792

C   3.16146  0.86400 -0.65553

C   3.12893  2.22670 -0.19547

C   3.35607  3.28420 -1.09528

H   3.32514  4.31236 -0.70843

C   3.60119  3.07588 -2.46412

C   3.58286  1.74786 -2.92241

H   3.73633  1.54930 -3.99299

C   3.36477  0.65539 -2.06246

C   2.78620  2.54598  1.24265

H   1.73781  2.26623  1.46649

H   2.89277  3.62714  1.43757

H   3.42116  1.99756  1.95524

C   3.88075  4.23327 -3.40085

H   4.94808  4.53116 -3.38865

H   3.29594  5.12893 -3.12572

H   3.63051  3.97676 -4.44538

C   3.30255 -0.73761 -2.64813

H   3.33233 -0.69990 -3.75129

H   2.38128 -1.26374 -2.34160

H   4.13550 -1.37532 -2.30712

C   5.56975 -1.79643 -0.10662

H   5.14230 -2.63073 -0.68910

H   6.41177 -2.19666  0.48826

H   5.98551 -1.06187 -0.81849

C   3.57571 -2.38553  2.15398

H   2.83539 -2.01411  2.88436

H   4.40174 -2.84320  2.72776

H   3.10257 -3.18728  1.56244

C   5.29461  0.16254  2.18382

H   5.65090  1.05417  1.63915

H   6.18319 -0.37341  2.56620

H   4.71098  0.50963  3.05392

C  -1.87083 -2.29158 -0.84702

C  -3.04327 -2.60997 -0.06113

C  -4.33705 -2.30755 -0.53734

H  -5.20039 -2.57354  0.09086

C  -4.56517 -1.69411 -1.78642

C  -3.42807 -1.42485 -2.57887

H  -3.56759 -0.99725 -3.58204

C  -2.12093 -1.73481 -2.15929

C  -2.89270 -3.28814  1.28093

H  -2.09972 -2.81761  1.88529

H  -2.59962 -4.34761  1.16363

H  -3.83899 -3.26819  1.84881

C  -5.96724 -1.41543 -2.29256

H  -6.69667 -1.37278 -1.46459

H  -6.31668 -2.20389 -2.98713

H  -6.02631 -0.45998 -2.84443

C  -0.96962 -1.57895 -3.12624

H  -0.10120 -1.07348 -2.67547

H  -1.27422 -1.02489 -4.03022

H  -0.60126 -2.57390 -3.43983

C   1.88619 -4.01051 -1.17467

H   1.80181 -3.85963 -2.26482

H   2.45809 -4.93968 -0.99895

H   2.47311 -3.16551 -0.77406

C  -0.89513 -5.34913 -1.34580

H  -1.91097 -5.45579 -0.92803

H  -0.41620 -6.34451 -1.32810

H  -1.00252 -5.04505 -2.40144

C   0.42836 -4.80493  1.39126

H   0.96330 -4.09043  2.04055

H   1.03446 -5.72834  1.34221

H  -0.52423 -5.05123  1.88967

C  -2.03248  3.30850  1.36319

Si -1.09780  1.12054  2.92657

C  -0.14681 -0.83725  3.03638

H  -0.43382 -1.71376  2.40477

H   0.96715 -0.82392  3.11538

H  -0.47354 -1.13774  4.04796

TS(V-VI)

SCF (BP86) Energy = -1648.83663425

Enthalpy 0K = -1648.006454

Enthalpy 298K = -1647.943525

Free Energy 298K = -1648.105610

Lowest Frequency = -108.0536 cm-1

Second Frequency = 11.0544 cm-1

SCF (BP86-D3BJ) Energy =

-1649.11478904

SCF (C6H6) Energy = -1648.87110448

SCF (BS2) Energy = -3718.58958988

Ca  0.55344 -0.62019  0.71158

K  -3.19577  0.68679  0.10566

Si  4.15233 -1.28025  1.02729

Si -0.13950 -4.08655 -0.47655

N  -0.64884  1.33013  1.11071

N   2.86366 -0.41219  0.22982

N  -0.76165 -2.44706 -0.40973

C  -1.74327  3.18240  2.78853

H  -2.71220  3.36193  3.29645

H  -1.01946  3.86809  3.27624

C  -2.69437  0.39630  3.38117

H  -3.58393  1.00319  3.11288

H  -2.73444  0.26847  4.47893

H  -2.78168 -0.61284  2.94496

C   0.19520  1.63799  4.34372

H   0.56020  0.74507  4.87184

H  -0.27843  2.32215  5.07212

H   1.07096  2.16921  3.92879

C  -1.10319  2.50374  0.51277

C  -1.02547  2.73560 -0.90244

C  -1.67821  3.85310 -1.46346

H  -1.60451  4.00413 -2.55060

C  -2.40213  4.78267 -0.69312

C  -2.43614  4.57514  0.70691

H  -2.96673  5.29834  1.34395

C  -0.25296  1.77745 -1.77464

H   0.81708  1.74578 -1.49526

H  -0.31067  2.05720 -2.84044

H  -0.63285  0.73831 -1.69311

C  -3.06229  5.99054 -1.32699

H  -4.06906  6.17980 -0.90941

H  -3.17346  5.86237 -2.41832

H  -2.47770  6.91915 -1.17006

C   3.19203  0.65630 -0.63543

C   3.27315  2.01289 -0.16341

C   3.59186  3.05731 -1.05054

H   3.64748  4.08029 -0.65233

C   3.82310  2.84382 -2.42096

C   3.69005  1.52714 -2.89339

H   3.82664  1.32755 -3.96617

C   3.37644  0.44848 -2.04576

C   2.95144  2.34398  1.27672

H   1.88650  2.13322  1.49488

H   3.13132  3.41388  1.48081

H   3.54415  1.74684  1.98650

C   4.20611  3.98216 -3.34431

H   5.29835  4.17044 -3.34487

H   3.71922  4.92791 -3.04673

H   3.91680  3.77013 -4.38889

C   3.18427 -0.92542 -2.64645

H   3.23322 -0.88185 -3.74885

H   2.20974 -1.35635 -2.35635

H   3.94311 -1.64700 -2.29988

C   5.48631 -2.01634 -0.15093

H   5.07820 -2.83920 -0.76300

H   6.34030 -2.41740  0.42573

H   5.87904 -1.24539 -0.83685

C   3.40898 -2.74848  1.99973

H   2.62565 -2.42495  2.70799

H   4.19954 -3.24639  2.58992

H   2.97319 -3.50491  1.32580

C   5.18509 -0.26774  2.30014

H   5.64098  0.62347  1.83452

H   6.00551 -0.88641  2.70975

H   4.56580  0.07285  3.14808

C  -2.06364 -2.17504 -0.80464

C  -3.21200 -2.40422  0.04716

C  -4.50938 -2.04146 -0.37175

H  -5.35361 -2.24572  0.30379

C  -4.76565 -1.44449 -1.62450

C  -3.65500 -1.24629 -2.47388

H  -3.82052 -0.82644 -3.47670

C  -2.34571 -1.61655 -2.11041

C  -3.01919 -3.05647  1.39589

H  -2.15897 -2.62054  1.93115

H  -2.79677 -4.13409  1.28896

H  -3.92451 -2.96526  2.02093

C  -6.17529 -1.10928 -2.07234

H  -6.85001 -0.95209 -1.21215

H  -6.61709 -1.92324 -2.67954

H  -6.20495 -0.19801 -2.69638

C  -1.23027 -1.51648 -3.12511

H  -0.30293 -1.11859 -2.68421

H  -1.52025 -0.89297 -3.98794

H  -0.96900 -2.52273 -3.50423

C   1.55455 -4.10931 -1.35968

H   1.44055 -3.88810 -2.43491

H   2.05467 -5.08987 -1.26060

H   2.22266 -3.33906 -0.93702

C  -1.32376 -5.24471 -1.44676

H  -2.32170 -5.29524 -0.97789

H  -0.91703 -6.27113 -1.48652

H  -1.46381 -4.89657 -2.48481

C   0.15450 -4.91041  1.23348

H   0.77157 -4.27099  1.88768

H   0.68430 -5.87367  1.11376

H  -0.79167 -5.10861  1.76484

C  -1.79918  3.48460  1.31314

Si -1.03903  1.30476  2.89593

C  -0.01483 -1.00954  3.08899

H  -0.18390 -2.01372  2.61971

H   1.06890 -0.97615  3.35111

H  -0.53518 -1.09306  4.05927

VI

SCF (BP86) Energy = -1648.84517768

Enthalpy 0K = -1648.015235

Enthalpy 298K = -1647.951332

Free Energy 298K = -1648.115112

Lowest Frequency = 11.3977 cm-1

Second Frequency = 16.7515 cm-1

SCF (BP86-D3BJ) Energy =

-1649.12069488

SCF (C6H6) Energy = -1648.88219122

SCF (BS2) Energy = -3718.59874663

Ca  0.32615 -0.89605  0.88029

K  -2.91663  1.46592 -0.06462

Si  3.67028 -2.27379  0.99638

Si -1.21252 -3.86945 -0.79775

N  -0.40070  1.48230  1.21906

N   2.63744 -1.07795  0.24124

N  -1.43958 -2.15817 -0.48163

C  -0.83323  3.86052  2.59389

H  -1.76319  4.33152  2.96561

H   0.00293  4.39636  3.08371

C  -2.40868  1.30503  3.55348

H  -3.26078  1.73345  2.98958

H  -2.56046  1.57990  4.61304

H  -2.45080  0.20633  3.47815

C   0.61630  1.54392  4.19463

H   0.76980  0.45448  4.24568

H   0.32149  1.90834  5.19567

H   1.57162  2.02121  3.92046

C  -0.40902  2.65558  0.45466

C  -0.24003  2.65714 -0.97371

C  -0.41814  3.85356 -1.69732

H  -0.28063  3.81988 -2.78769

C  -0.73796  5.08270 -1.08980

C  -0.87063  5.08832  0.31732

H  -1.10251  6.03194  0.83226

C   0.14805  1.38568 -1.68793

H   1.16962  1.06661 -1.40614

H   0.13948  1.51728 -2.78292

H  -0.52344  0.53227 -1.45963

C  -0.87411  6.35507 -1.90087

H  -1.68485  7.00248 -1.51880

H  -1.09293  6.13661 -2.96094

H   0.05197  6.96341 -1.88347

C   3.25784 -0.08928 -0.55063

C   3.66578  1.17889 -0.00720

C   4.28403  2.14243 -0.82427

H   4.58421  3.09720 -0.36911

C   4.51940  1.93512 -2.19502

C   4.07363  0.71947 -2.74127

H   4.20613  0.53635 -3.81766

C   3.45054 -0.27453 -1.96423

C   3.37849  1.51347  1.43861

H   2.28739  1.53820  1.61986

H   3.78883  2.50489  1.70007

H   3.79376  0.76709  2.13364

C   5.22951  2.97189 -3.04114

H   6.33225  2.87076 -2.99051

H   4.98820  3.99892 -2.71322

H   4.94886  2.88576 -4.10600

C   2.92404 -1.51768 -2.64184

H   3.09462 -1.47514 -3.73229

H   1.84030 -1.63550 -2.46239

H   3.39236 -2.43821 -2.25565

C   5.03832 -2.97939 -0.16216

H   4.62629 -3.70025 -0.88962

H   5.81535 -3.50319  0.42428

H   5.53179 -2.17197 -0.73055

C   2.61097 -3.74338  1.59607

H   1.80058 -3.40450  2.26439

H   3.23622 -4.45578  2.16450

H   2.16060 -4.29197  0.75187

C   4.64351 -1.67619  2.54959

H   5.36408 -0.87706  2.30156

H   5.21558 -2.51297  2.99320

H   3.95708 -1.29003  3.32319

C  -2.67960 -1.58550 -0.70242

C  -3.67489 -1.48053  0.34809

C  -4.91315 -0.84953  0.11193

H  -5.64764 -0.81681  0.93051

C  -5.25737 -0.28751 -1.13849

C  -4.29759 -0.38959 -2.16836

H  -4.54085  0.01269 -3.16319

C  -3.05087 -1.02412 -1.98692

C  -3.38745 -2.09736  1.69633

H  -2.37128 -1.85306  2.05884

H  -3.41373 -3.20081  1.63388

H  -4.13416 -1.78566  2.44755

C  -6.62318  0.32431 -1.38421

H  -7.03375  0.79635 -0.47342

H  -7.36119 -0.43617 -1.70613

H  -6.59188  1.09164 -2.17833

C  -2.10632 -1.16294 -3.15916

H  -1.05757 -1.09636 -2.82905

H  -2.30441 -0.40326 -3.93562

H  -2.21182 -2.15646 -3.63430

C   0.37454 -4.17264 -1.81596

H   0.27767 -3.76242 -2.83590

H   0.60130 -5.25120 -1.89859

H   1.23996 -3.67831 -1.34265

C  -2.69335 -4.62441 -1.76273

H  -3.64500 -4.45482 -1.22960

H  -2.55897 -5.71594 -1.87042

H  -2.79820 -4.19772 -2.77478

C  -1.04345 -4.93362  0.78809

H  -0.29905 -4.50369  1.47801

H  -0.72681 -5.96407  0.54114

H  -2.00093 -4.99579  1.33403

C  -0.70954  3.92555  1.07935

Si -0.72164  1.95996  2.91418

C  -0.05959 -1.76687  3.17125

H  -0.33867 -2.84448  3.11153

H   0.89979 -1.75211  3.74114

H  -0.80831 -1.32629  3.86707

VII

SCF (BP86) Energy = -1648.83904784

Enthalpy 0K = -1648.008750

Enthalpy 298K = -1647.944978

Free Energy 298K = -1648.109218

Lowest Frequency = 13.3713 cm-1

Second Frequency = 17.2411 cm-1

SCF (BP86-D3BJ) Energy =

-1649.11902153

SCF (C6H6) Energy = -1648.87478177

SCF (BS2) Energy = -3718.59135137

Ca -0.20654 -0.68966  0.79710

K  -2.04288  2.04380  1.45028

Si  1.88393 -3.55353  1.23824

Si -3.22668 -2.69321 -0.29949

N   0.66912  1.63245  1.24170

N   1.59015 -2.13463  0.26896

N  -2.44304 -1.12410 -0.38298

C   2.21334  3.57718  2.51016

H   1.91762  4.49610  3.05128

H   3.27683  3.39649  2.76071

C  -0.34637  2.69252  4.02611

H  -0.84558  3.57862  3.58487

H   0.06987  3.03033  4.99281

H  -1.09136  1.90925  4.24772

C   2.02655  0.73677  3.94136

H   1.43202 -0.18711  4.02200

H   2.22662  1.10719  4.96330

H   2.99043  0.48725  3.46961

C   1.25532  2.61795  0.42101

C   1.14282  2.60239 -1.00479

C   1.68880  3.65414 -1.76259

H   1.58073  3.61304 -2.85586

C   2.38158  4.73524 -1.18579

C   2.54742  4.71704  0.21535

H   3.11909  5.52106  0.70124

C   0.48641  1.43145 -1.68589

H   1.06154  0.49697 -1.51920

H   0.42905  1.57528 -2.77753

H  -0.55390  1.26505 -1.34032

C   2.91838  5.87185 -2.03114

H   2.21849  6.73064 -2.08346

H   3.10448  5.54830 -3.07062

H   3.87062  6.26388 -1.62950

C   2.47179 -1.79261 -0.78277

C   3.59659 -0.92172 -0.57372

C   4.45305 -0.59085 -1.63897

H   5.30219  0.07699 -1.43625

C   4.25288 -1.06570 -2.94684

C   3.12618 -1.87575 -3.16434

H   2.91717 -2.24015 -4.18058

C   2.24262 -2.23670 -2.12995

C   3.84095 -0.30389  0.78303

H   2.97261  0.30895  1.08641

H   4.73247  0.34664  0.76189

H   3.98138 -1.06312  1.56957

C   5.21410 -0.72593 -4.06739

H   6.08388 -1.41241 -4.09506

H   5.61809  0.29665 -3.96046

H   4.72269 -0.79075 -5.05428

C   1.02648 -3.06812 -2.46321

H   0.93949 -3.21671 -3.55403

H   0.10068 -2.58812 -2.10203

H   1.05367 -4.06203 -1.98549

C   1.99758 -5.20943  0.26313

H   1.03015 -5.47674 -0.19587

H   2.29651 -6.03996  0.92925

H   2.74802 -5.14191 -0.54403

C   0.43066 -3.73204  2.47025

H   0.28262 -2.82815  3.08756

H   0.62455 -4.57101  3.16275

H  -0.52036 -3.94950  1.95330

C   3.49030 -3.54054  2.30140

H   4.38823 -3.40439  1.67349

H   3.60421 -4.49849  2.84261

H   3.47514 -2.73019  3.05073

C  -3.15370 -0.02464 -0.86131

C  -4.15214  0.68236 -0.09100

C  -4.72440  1.88102 -0.57257

H  -5.47737  2.39073  0.04915

C  -4.40215  2.42127 -1.83007

C  -3.50444  1.68197 -2.62803

H  -3.27694  2.03920 -3.64245

C  -2.90774  0.48892 -2.19082

C  -4.60175  0.13257  1.24809

H  -3.75778 -0.29529  1.81763

H  -5.32513 -0.69391  1.11977

H  -5.11267  0.90522  1.85427

C  -5.00527  3.72253 -2.31797

H  -5.84205  4.04343 -1.67311

H  -5.39578  3.63109 -3.34824

H  -4.26723  4.54791 -2.33365

C  -2.05343 -0.31839 -3.13965

H  -1.06346 -0.55300 -2.71763

H  -1.91447  0.20818 -4.09945

H  -2.52568 -1.29680 -3.34590

C  -2.08594 -4.06416 -0.98733

H  -1.93060 -3.95226 -2.07347

H  -2.51704 -5.06468 -0.80064

H  -1.09225 -4.02761 -0.50900

C  -4.84062 -2.71763 -1.34149

H  -5.56921 -1.96645 -0.99101

H  -5.32386 -3.70965 -1.28608

H  -4.63247 -2.50138 -2.40366

C  -3.70431 -3.33369  1.45108

H  -2.82493 -3.36882  2.11692

H  -4.10751 -4.36100  1.37639

H  -4.46435 -2.70716  1.94602

C   2.01562  3.69192  1.00622

Si  1.10866  2.05766  2.92197

C  -1.40649 -0.51370  3.03383

H  -1.89014 -1.51743  3.01873

H  -0.69688 -0.56697  3.89101

H  -2.22707  0.13947  3.42622

# S7. SQUID Magnetometry and EPR measurements

# S7.1 SQUID Magnetometry measurements

Variable temperature magnetic susceptibility data were collected on powdered samples, under an applied field of 0.5 T.  Field dependent magnetisation data were collected at 2 K by varying the magnetic field from 0 to 7 T.  Data were corrected for the diamagnetism of the samples and sample holders by measuring equivalent quantities of diamagnetic precursor and the sample holder under similar experimental conditions to compound 2. Care was taken to ensure complete thermalisation of the sample before each data point was measured by employing delays at each temperature point and the sample was held at 2 K for 60 minutes before isothermal magnetisation data were recorded to account for slow thermal equilibration of the sample.

Figure S28:  Plot of T vs. T for 2 ( = molar magnetic susceptibility), measured under an applied field of 0.5 T, supporting a singlet ground state, and strong antiferromagnetic coupling between electrons in 2, in agreement with AIRSS data.  The blue dashed line marks the expected T value for the case that the two anionic electrons of 2 did not interact with each other (assuming g = 2), while the red line is a simulation using the Bleaney-Bowers equation,27 and assuming antiferromagnetic exchange coupling of 4409 K (ca. 3064 cm1), equivalent to a single-triplet separation of 0.38 eV.

# S7.2 Electron paramagnetic resonance (EPR) spectroscopy

The electron paramagnetic resonance spectra were recorded under magnetic field modulation of 100 kHz, modulation amplitude of 1 G, and microwave power of either 0.02 (40 dB), 0.2 (30 dB) or 0.6325 mW (25 dB). Field corrections were applied using Bruker strong pitch (g = 2.0028) as a reference. Spectra of an empty quartz tube used as sample holder were measured before recording the sample spectra in order to ensure the purity of the obtained signals. To determine the effective percentage of electron spins of 2 that are detectable in the experimental temperature range (5 – 293 K), a sample of known mass (36.2 mg) of 2 was measured under similar conditions as TEMPO (2,2,6,6-tetramethylpiperidine-1-oxyl) reference samples of known spin concentrations (0.074 – 0.37 mM; 4.5 × 1015 to 2.3 × 1016 spins per sample). Both first harmonic (FH) and second harmonic (SH) signals were baselined with a first or second order polynomial function before integration to extract signal intensities or prior to simulations. Simulations of the FH spectra used the EasySpin 6.0.0 software package implemented within MATLAB.26  Thermal dependence of the EPR signal intensity was modelled using the Bleaney-Bowers equation27 in order to establish the nature and the strength of magnetic exchange that may occur between the unpaired electrons of 2, and to probe the triplet-singlet energy gap. To allow comparison between species, SH signal intensities were extracted as the absolute polygon areas of the spectral feature being monitored.

Figure S29:  X-band EPR spectra for 2 at temperatures between 5 and 280 K, measured at the frequency of 9.36 GHz, with field modulation amplitude of 1 G, and attenuation of 30 dB.

Figure S30:  X-band EPR spectra for 2 at temperatures between 80 and 280 K, emphasizing the presence of unpaired electrons in two different environments (A and B), measured at the frequency of 9.36 GHz, with field modulation amplitude of 1 G, and microwave attenuation of 30 dB.

Figure S31:  Second Harmonic (SH) X-band EPR spectra for 2 at temperatures between 20 and 280 K, emphasizing the presence of unpaired electron spins in two different environments (A and B), measured at the frequency of 9.36 GHz, with field modulation amplitude of 1 G, and microwave attenuation of 25 dB.

Figure S32:  A zoomed image of the Second Harmonic (SH) X-band EPR spectra for 2 presented in Figure S30, for the field region 3333-3349 G, and temperatures from 90 to 280 K, emphasizing the limited change in signal intensity for signal B as a function of temperature. Spectra were measured at a microwave frequency of ca. 9.36 GHz, a field modulation amplitude of 1 G, and microwave attenuation of 25 dB.

Figure S33:  Deconvolution of a measured SH signal for 2 (9.36 GHz, 50 K) into its components (A and B) to establish the ratio between them, using the method of calculated absolute polygon areas (highlighted in grey): 1.3635 (A+B), 1.2907 (A) and 0.0756 (B), nB/nA = 0.0586.

Figure S34:  Temperature dependence of the EPR intensity for 2, at microwave powers of 25 and 30 dB, and their fits to the Bleaney-Bowers equation27 with ES-T = 298  5.8 K. Intensities are deduced by double integration of the recorded EPR signal.

Figure S35:  Temperature dependence of the EPR intensity for data recorded at 100280 K, at microwave powers of 25 and 30 dB, and their fits to the Bleaney-Bowers equation27 providing ES-T = 295  6.7 K (25 dB) and 274.0  6.3 K (30 dB).

Figure S36:  X-band EPR spectrum for 2′ (black) at 240 K and 9.36 GHz, and its simulation (red) considering two species: (A) s = ½, gx,y  = 1.9964; gz =1.9939, and (B) s =1/2, interacting with two K atoms, each containing 39K (93.3%, I = 3/2) and 41K (6.73%, I = 3/2)), with g = 2.0024,  AKx,y = 9.7 MHz, AKz = 19.5 MHz. Linewidth [Gaussian Lorentzian] /weight: [6 13]/ 99.8 (A), [0.49 0] / 0.2 (B).

Figure S37:  X-band EPR spectra Ffirst Harmonic) for 2′ at 280 K, measured at the frequency of 9.36 GHz, with field modulation amplitude of 1 G and attenuation of 1 to 30 dB, highlighting the presence of two species, A and B.

Figure S38:  Second Harmonic (SH) X-band EPR spectra for 2′ at 280 K, measured at 9.36 GHz, 1 G modulation amplitude and microwave field attenuations from 1 to 25 dB, showing the hyperfine splitting from two K ions (as modelled in Figure S37).

# S8. References

(1)	Sheldrick, G. M. Program for Area Detector Absorption Correction, Institute for Inorganic Chemistry, University of Göttingen: Göttingen, Germany, 1996.

(2)	Sheldrick, G. M. A Short History of SHELX. Acta Cryst. A 2008, 64 (1), 112–122. https://doi.org/10.1107/S0108767307043930.

(3)	Sheldrick, G. M. SHELXT – Integrated Space-Group and Crystal-Structure Determination. Acta Cryst. A 2015, 71 (1), 3–8. https://doi.org/10.1107/S2053273314026370.

(4)	Dolomanov, O. V.; Bourhis, L. J.; Gildea, R. J.; Howard, J. A. K.; Puschmann, H. OLEX2: A Complete Structure Solution, Refinement and Analysis Program. J. Appl. Cryst. 2009, 42 (2), 339–341. https://doi.org/10.1107/S0021889808042726.

(5)	CrysAlisPro Software System, Version 1.171.42a, Rigaku Corporation, Wroclaw, Poland, 2024.

(6)	Le Bail, A.; Duroy, H.; Fourquet, J. L. Ab-Initio Structure Determination of LiSbWO6 by X-Ray Powder Diffraction. Mat. Res. Bull. 1988, 23 (3), 447–452. https://doi.org/10.1016/0025-5408(88)90019-0.

(7)	Petříček, V.; Palatinus, L.; Plášil, J.; Dušek, M. Jana2020 – a New Version of the Crystallographic Computing System Jana. Z. Kristallogr. 2023, 238 (7–8), 271–282. https://doi.org/10.1515/zkri-2023-0005.

(8)	Davison, N.; Quirk, J. A.; Tuna, F.; Collison, D.; McMullin, C. L.; Michaels, H.; Morritt, G. H.; Waddell, P. G.; Gould, J. A.; Freitag, M.; Dawson, J. A.; Lu, E. A Room-Temperature-Stable Electride and Its Reactivity: Reductive Benzene/Pyridine Couplings and Solvent-Free Birch Reductions. Chem 2023, 9, 576–591. https://doi.org/10.1016/j.chempr.2022.11.006.

(9)	Pickard, C. J.; Needs, R. J. Ab Initio Random Structure Searching. J. Phys. Condens. Matter 2011, 23 (5), 053201. https://doi.org/10.1088/0953-8984/23/5/053201.

(10)	Batatia, I.; Benner, P.; Chiang, Y.; Elena, A. M.; Kovács, D. P.; Riebesell, J.; Advincula, X. R.; Asta, M.; Avaylon, M.; Baldwin, W. J.; Berger, F.; Bernstein, N.; Bhowmik, A.; Blau, S. M.; Cărare, V.; Darby, J. P.; De, S.; Della Pia, F.; Deringer, V. L.; Elijošius, R.; El-Machachi, Z.; Falcioni, F.; Fako, E.; Ferrari, A. C.; Genreith-Schriever, A.; George, J.; Goodall, R. E. A.; Grey, C. P.; Grigorev, P.; Han, S.; Handley, W.; Heenen, H. H.; Hermansson, K.; Holm, C.; Jaafar, J.; Hofmann, S.; Jakob, K. S.; Jung, H.; Kapil, V.; Kaplan, A. D.; Karimitari, N.; Kermode, J. R.; Kroupa, N.; Kullgren, J.; Kuner, M. C.; Kuryla, D.; Liepuoniute, G.; Margraf, J. T.; Magdău, I.-B.; Michaelides, A.; Moore, J. H.; Naik, A. A.; Niblett, S. P.; Norwood, S. W.; O’Neill, N.; Ortner, C.; Persson, K. A.; Reuter, K.; Rosen, A. S.; Schaaf, L. L.; Schran, C.; Shi, B. X.; Sivonxay, E.; Stenczel, T. K.; Svahn, V.; Sutton, C.; Swinburne, T. D.; Tilly, J.; van der Oord, C.; Varga-Umbrich, E.; Vegge, T.; Vondrák, M.; Wang, Y.; Witt, W. C.; Zills, F.; Csányi, G. A Foundation Model for Atomistic Materials Chemistry. arXiv March 1, 2024. https://doi.org/10.48550/arXiv.2401.00096.

(11)	Kresse, G.; Joubert, D. From Ultrasoft Pseudopotentials to the Projector Augmented-Wave Method. Phys. Rev. B 1999, 59 (3), 1758–1775. https://doi.org/10.1103/PhysRevB.59.1758.

(12)	Krukau, A. V.; Vydrov, O. A.; Izmaylov, A. F.; Scuseria, G. E. Influence of the Exchange Screening Parameter on the Performance of Screened Hybrid Functionals. J. Chem. Phys. 2006, 125 (22), 224106. https://doi.org/10.1063/1.2404663.

(13)	Kühne, T. D.; Iannuzzi, M.; Del Ben, M.; Rybkin, V. V.; Seewald, P.; Stein, F.; Laino, T.; Khaliullin, R. Z.; Schütt, O.; Schiffmann, F.; Golze, D.; Wilhelm, J.; Chulkov, S.; Bani-Hashemian, M. H.; Weber, V.; Borštnik, U.; Taillefumier, M.; Jakobovits, A. S.; Lazzaro, A.; Pabst, H.; Müller, T.; Schade, R.; Guidon, M.; Andermatt, S.; Holmberg, N.; Schenter, G. K.; Hehn, A.; Bussy, A.; Belleflamme, F.; Tabacchi, G.; Glöß, A.; Lass, M.; Bethune, I.; Mundy, C. J.; Plessl, C.; Watkins, M.; VandeVondele, J.; Krack, M.; Hutter, J. CP2K: An Electronic Structure and Molecular Dynamics Software Package - Quickstep: Efficient and Accurate Electronic Structure Calculations. J. Chem. Phys. 2020, 152 (19), 194103. https://doi.org/10.1063/5.0007045.

(14)	Bursch, M.; Neugebauer, H.; Ehlert, S.; Grimme, S. Dispersion Corrected r2SCAN Based Global Hybrid Functionals: r2SCANh, r2SCAN0, and r2SCAN50. J. Chem. Phys. 2022, 156 (13), 134105. https://doi.org/10.1063/5.0086040.

(15)	Frisch, M. J.; Trucks, G. W.; Schlegel, H. B.; Scuseria, G. E.; Robb, M. A.; Cheeseman, J. R.; Scalmani, G.; Barone, V.; Petersson, G. A.; Nakatsuji, H.; Li, X.; Caricato, M.; Marenich, A. V.; Bloino, J.; Janesko, B. G.; Gomperts, R.; Mennucci, B.; Hratchian, H. P.; Ortiz, J. V.; Izmaylov, A. F.; Sonnenberg, J. L.; Williams; Ding, F.; Lipparini, F.; Egidi, F.; Goings, J.; Peng, B.; Petrone, A.; Henderson, T.; Ranasinghe, D.; Zakrzewski, V. G.; Gao, J.; Rega, N.; Zheng, G.; Liang, W.; Hada, M.; Ehara, M.; Toyota, K.; Fukuda, R.; Hasegawa, J.; Ishida, M.; Nakajima, T.; Honda, Y.; Kitao, O.; Nakai, H.; Vreven, T.; Throssell, K.; Montgomery Jr., J. A.; Peralta, J. E.; Ogliaro, F.; Bearpark, M. J.; Heyd, J. J.; Brothers, E. N.; Kudin, K. N.; Staroverov, V. N.; Keith, T. A.; Kobayashi, R.; Normand, J.; Raghavachari, K.; Rendell, A. P.; Burant, J. C.; Iyengar, S. S.; Tomasi, J.; Cossi, M.; Millam, J. M.; Klene, M.; Adamo, C.; Cammi, R.; Ochterski, J. W.; Martin, R. L.; Morokuma, K.; Farkas, O.; Foresman, J. B.; Fox, D. J. Gaussian 16 Rev. C.01, 2016.

(16)	Andrae, D.; Häußermann, U.; Dolg, M.; Stoll, H.; Preuß, H. Energy-Adjustedab Initio Pseudopotentials for the Second and Third Row Transition Elements. Theoret. Chim. Acta 1990, 77 (2), 123–141. https://doi.org/10.1007/BF01114537.

(17)	Hariharan, P. C.; Pople, J. A. The Influence of Polarization Functions on Molecular Orbital Hydrogenation Energies. Theoret. Chim. Acta 1973, 28 (3), 213–222. https://doi.org/10.1007/BF00533485.

(18)	Hehre, W. J.; Ditchfield, R.; Pople, J. A. Self—Consistent Molecular Orbital Methods. XII. Further Extensions of Gaussian—Type Basis Sets for Use in Molecular Orbital Studies of Organic Molecules. J. Chem. Phys. 1972, 56, 2257–2261. https://doi.org/10.1063/1.1677527.

(19)	Becke, A. D. Density-Functional Exchange-Energy Approximation with Correct Asymptotic Behavior. Phys. Rev. A 1988, 38 (6), 3098–3100. https://doi.org/10.1103/PhysRevA.38.3098.

(20)	Perdew, J. P. Density-Functional Approximation for the Correlation Energy of the Inhomogeneous Electron Gas. Phys. Rev. B 1986, 33 (12), 8822–8824. https://doi.org/10.1103/PhysRevB.33.8822.

(21)	Tomasi, J.; Mennucci, B.; Cammi, R. Quantum Mechanical Continuum Solvation Models. Chem. Rev. 2005, 105 (8), 2999–3094. https://doi.org/10.1021/cr9904009.

(22)	Grimme, S.; Ehrlich, S.; Goerigk, L. Effect of the Damping Function in Dispersion Corrected Density Functional Theory. J. Comp. Chem. 2011, 32 (7), 1456–1465. https://doi.org/10.1002/jcc.21759.

(23)	Keith, T. A. AIMA11, Version 19.10.12, TK Gristmill Software, Overland Park KS, USA, 2019.

(24)	Gledening, E. D.; Reed, A. E.; Carpenter, J. E.; Weinhold, F. NBO 3.1, Theoretical Chemistry Institute, University of Wisconsin, Madison, USA, 2003.

(25)	Gledening, E. D.; Badenhoop, J. K.; Reed, A. E.; Carpenter, J. E.; Bohmann, J. A.; Morales, C. M.; Karafiloglou, P.; Weinhold, F. NBO 7.0, Theoretical Chemistry Institute, University of Wisconsin, Madison, USA, 2018.

(26)	Stoll, S.; Schweiger, A. EasySpin, a Comprehensive Software Package for Spectral Simulation and Analysis in EPR. J. Magn. Res. 2006, 178 (1), 42–55. https://doi.org/10.1016/j.jmr.2005.08.013.

(27)	Bleaney, B.; Bowers, K. D. Anomalous Paramagnetism of Copper Acetate. Proc. R. Soc. London, Ser. A 1997, 214 (1119), 451–465. https://doi.org/10.1098/rspa.1952.0181.