Supplementary Information

for

Local Electrostatic Screening Enabled Ultrafast Bipolar Homojunction Photodiode Towards High Dynamic Range In-Sensor Image Processing

Shaofeng Wen, Shuren Zhou, Yimin Gong, Rui Zhang, Xinyu Jia, Linkang Kong, Haodong Fan, Yi Yin, Changyong Lan*, Chun Li*, Yong Liu

State Key Laboratory of Electronic Thin Films and Integrated Devices, School of Optoelectronic Science and Engineering, University of Electronic Science and Technology of China, 611731, Chengdu, P. R. China

*Corresponding authors: cylan@uestc.edu.cn; lichun@uestc.edu.cn

Table of Contents

Supporting Figures ...................................................................................................... 1

Supp. Fig. 1. Illuminance levels for daily life and DR of human eye......................... 1

Supp. Fig. 2. Schematic of in-sensor and off-sensor image processing...................... 2

Supp. Fig. 3. Raman characterization of the WSe2/PdSe2/h-BN stacks...................... 3

Supp. Fig. 4. HRTEM and EDS mapping of the WSe2/PdSe2/h-BN stacks................ 4

Suppl. Fig. 5. Electrical properties of the WSe2 in-plane homojunction……………. 5

Suppl. Fig. 6. Output and transfer curves of multilayer WSe2 & PdSe2...................... 6

Suppl. Fig. 7. UPS and band structure of WSe2........................................................... 7

Suppl. Fig. 8. AFM and KPFM measurements of thick WSe2 & PdSe2...................... 8

Suppl. Fig. 9. Band alignment of WSe2 at different gate voltages.............................. 9

Suppl. Fig. 10. Device reproducibility....................................................................... 10

Suppl. Fig. 11. Photocurrent mapping at zero gate voltage....................................... 11

Suppl. Fig. 12. Spectral responsivity and polarization sensitivity............................. 12

Suppl. Fig. 13. Local electrostatic screening enabled bipolar photoresponse of the WSe2/thick graphite device............................................................... 13

Suppl. Fig. 14. Photocurrent mapping and response time of the WSe2/thick graphite device................................................................................................ 14

Suppl. Fig. 15. Local electrostatic screening enabled bipolar photoresponse of the WSe2/Au device................................................................................ 15

Suppl. Fig. 16. Photocurrent mapping and response time of the WSe2/Au device.............................................................................................. 16

Suppl. Fig. 17. Local electrostatic screening enabled bipolar photoresponse of the WSe2/thin graphite device. ………………………………...……… 17

Suppl. Fig. 18. Photocurrent mapping and response time of the WSe2/thin graphite device................................................................................................ 18

Suppl. Fig. 19. Measurements of noise current and NEP.......................................... 19

Suppl. Fig. 20. More typical image processing functions using different in-sensor filters.................................................................................................. 21

Supporting Tables ..................................................................................................... 22

Supplementary Table 1. Performance comparison of reported 2D-based reconfigurable photodetectors.......................................................... 22

Supporting References .............................................................................................. 23

Supplementary Fig. 1 Illuminance levels for daily life and DR of human eye. (a) Illuminance (E) levels for daily life (from left to right: starlight, full moon, dusk, dark clouds, cloudy daylight and sunny noon). E is also converted with light intensity (Ф) using the peak wavelength of 555 nm according to eye-sensitive luminosity function1. (b) The photoreceptors in human eyes have a limited dynamic range (~40 dB)2, but their adaptation characteristics (adjustment of retinal cells and pupil diameters) allow us to perceive and recognize various objects under different levels of illumination, from pretty dim to high brightness (~140 dB)1,3. However, this process of photopic/scotopic vision adaptation takes a long time (~1 min/30 min)1.

Supplementary Fig. 2 Schematic of in-sensor and off-sensor processing. (a) Schematic of in-sensor processing for our WSe2 bipolar photodiode. The image projected on the sensor is partitioned into pixels, with each pixel further divided into subpixels. The light intensity incident on each subpixel is denoted as Pj. The output photocurrent (Iph) from each pixel is described as Iph = ∑PjRj, where Rj represents the photoresponsivity of the subpixel sensor (also considered as the weight of the kernel matrix), which can be tuned by a gate voltage. (b) Schematic of off-sensor processing for traditional image sensor4,5. The separation of sensor and processor extends data output time and leads to higher power consumption.

Supplementary Fig. 3 Raman characterization of the WSe2/PdSe2/h-BN stacks. (a-c) Raman spectrum of the (a) WSe2, (b) PdSe2, and (c) h-BN. Two characteristic peaks at 249.6 and 257.1 cm−1 in (a), corresponding to the E2g1 and A1g Raman modes of WSe2, respectively6,7. Four characteristic peaks at 145.1, 207.3, 223.7, and 259.1 cm−1 in (b), corresponding to the Ag1–B1g1, Ag2, B1g2 and Ag3 Raman modes of multilayer PdSe2, respectively8–10. And a characteristic peaks at 1364.1 cm−1 in (c) corresponds to the E2g Raman modes of h-BN6,11.

Supplementary Fig. 4 High-resolution transmission electron microscopy (HRTEM) characterizations and corresponding energy-dispersive spectrometry (EDS) mapping on the cross-section of the WSe2/PdSe2/h-BN heterostructure. (a) The scanning transmission electron microscope characterization and the EDS of the WSe2/PdSe2/h-BN heterostructure, which clearly shows the thickness in each layer and reveals the element mapping in each layer. (b, c) HRTEM of WSe2/PdSe2(b) and PdSe2/h-BN (c), which confirms the clean interface between these 2D materials.

Supplementary Fig. 5 Electrical properties of the WSe2 in-plane homojunction. (a) Logarithmic scale transfer curves (Ids–Vg) at Vds = −1 V (green) and 1 V (orange). (b) Rr with a function of Vg at Vds = ±1 V. (c) Logarithmic scale Ids–Vds curves of WSe2 in-plane homojunction at Vg = −80 V and 80 V.

Supplementary Fig. 6 Output and transfer characteristics for multilayer WSe2-FET and multilayer PdSe2-FET. (a) Output characteristics of multilayer WSe2 between the electrodes (1) and (2). (b) Output characteristics of multilayer PdSe2 between the electrodes (3) and (4). (c) Transfer characteristics of multilayer WSe2 on linear scale (blue solid line) and logarithmic scale (red solid line). (d) Transfer characteristics of multilayer PdSe2.

Supplementary Fig. 7 Ultraviolet photoelectron spectra (UPS) and band structure of WSe2. (a, b) UPS of WSe2 for work function and valence band edge. (c) The band structure of WSe2. The work function (WF) of WSe2 was determined to be 4.69 eV, by subtracting the second electron cutoff energy from the photo energy of He I light source (21.21 eV)12. The valence band edge of WSe2 was 0.66 eV, lower than their Fermi level (EF) (binding energy equals to 0 eV). Therefore, the band structure of WSe2 was suggested in (c) by combining the bandgap of multilayer WSe2 (~1.38 eV)13,14.

Supplementary Fig. 8 AFM and KPFM measurements of thick WSe2 and thick PdSe2 samples transferred on Au substrate. (a, c) The height profile of WSe2 (a) and PdSe2 (c), showing the thickness of ~32 nm and ~100 nm, respectively. (b, d) The work functions of the thick WSe2 (b) and thick PdSe2 (d) are ~4.63 eV (similar to the UPS data in Supplementary Fig. 7) and ~4.85 eV, respectively. These results indicate a small Schottky barrier of 0.22 eV between the WSe2 and PdSe2.

Supplementary Fig. 9 Band alignment of WSe2 in-plane homojunction at different gate voltages. (a) Vg = −80 V. (b) Vg = 80 V.

Supplementary Fig. 10 Device reproducibility test of the positive and negative photovoltaic photoresponse. (a, d) Optical microscopy image of two new WSe2 in-plane homojunction photodetector, where the red and gray dashed regions indicate the WSe2 and PdSe2 nanosheets, respectively. (b, e) AFM images of the black dashed area in (a) and (d). The inset shows the height profile of the WSe2/PdSe2/ stacks along the red solid line in (b) and (e). (c, f) Positive and negative photovoltaic current–time curves under illumination at 520 nm with a power density of 434 mW/cm2. The different Isc in different devices can be attributed to differences in the area of the photosensitive region or the thickness of the material15.

Supplementary Fig. 11 Scanning photocurrent mapping of the device under 520 nm at Vg = 0 V. The photocurrents of the Au/WSe2 Schottky barrier and WSe2/PdSe2 heterojunction are significantly weaker, and more than an order of magnitude smaller compared to WSe2 in-plane homojunction.

Supplementary Fig. 12 Spectral responsivity and polarization sensitivity of the WSe2 in-plane homojunction device at different Vg. (a) Spectral responsivity of WSe2 in-plane homojunction device at 80 V (blue) and −80 V (red) gate voltage closely corresponding to the light absorption spectrum of WSe216,17. (b, c) Polarization-free sensitivity of photocurrent in WSe2 in-plane homojunction device. (520 nm incident laser, 227 mW/cm2)

Supplementary Fig. 13 Local electrostatic screening enabled bipolar photoresponse of the WSe2/thick graphite structure. (a, b) Schematic (a) and optical microscopy image (b) of the WSe2/thick graphite stack, where the thick graphite as the screening layer. (c) AFM image of the WSe2/thick graphite stack. The inset shows the height profile of the WSe2/thick graphite stack along the green/red solid line in (c). (d) Gate-tunable positive and negative photovoltaic response of the device.

Supplementary Fig. 14 Photocurrent mapping and response time of the WSe2/thick graphite device. (a, c) The scanning photocurrent mapping of the device under 520 nm at (c) Vg = −80 V and (d) 80 V, respectively. The scanning photocurrent mapping of the device illustrate that the formation of WSe2 in-plane homojunction. (b, d) Rise and fall times for positive (b) and negative (d) photovoltaic effects at 405 nm nanosecond pulsed laser.

Supplementary Fig. 15 Local electrostatic screening enabled bipolar photoresponse of the WSe2/Au device. (a, b) Schematic (a) and optical microscopy image (b) of the WSe2/Au stack, where the Au (Source) as the screening layer. (c) AFM image of the WSe2/Au stack. The inset shows the height profile of the WSe2 along the red solid line in (c). Gate-tunable positive and negative photovoltaic response of the device.

Supplementary Fig. 16 Photocurrent mapping and response time of WSe2/Au device. (a, c) The scanning photocurrent mapping of the device under 520 nm at (c) Vg = −80 V and (d) 80 V, respectively. The scanning photocurrent mapping of the device illustrate that the formation of WSe2 in-plane homojunction. (b, d) Rise and fall times for positive (b) and negative (d) photovoltaic effects at 405 nm nanosecond pulsed laser.

Supplementary Fig. 17 Local electrostatic screening enabled bipolar photoresponse of the WSe2/thin graphite device. (a, b) Schematic (a) and optical microscopy image (b) of the WSe2/thin graphite stack, where the thin graphite as the screening layer. (c) AFM image of the WSe2/thin graphite stack. The inset shows the height profile of the WSe2/thin graphite stack along the red solid line in (c). (d) Gate-tunable positive and negative photovoltaic response of the device.

Supplementary Fig. 18 Photocurrent mapping and response time of the WSe2/thin graphite device. (a, c) The scanning photocurrent mapping of the device under 520 nm at (c) Vg = −80 V and (d) 80 V, respectively. The scanning photocurrent mapping of the device illustrate that the formation of WSe2 in-plane homojunction. (b, d) Rise and fall times for positive (b) and negative (d) photovoltaic effects at 405 nm nanosecond pulsed laser.

Supplementary Fig. 19 Noise current measurements and calculation of NEP for WSe2 in-plane homojunction device at different Vg. (a) Schematic diagram of noise current measurement. (b) Noise current measurements of device at Vg = 80 V, Vds = 0 V. (c) Noise current measurements of device at Vg = −80 V, Vds = 0 V. The sampling time interval is 10 ms.

The noise current (In, i) can be calculated by these formulas:

(1)

(2)

(3)

where (ti, Ii) is a set of current data measured in the experiment, N is the total number of data points, I0 is the background current which can be obtained by averaging Ii (equation 1). In, i is the noise current, Δt is the sampling time interval, and T is the total sampling time. As shown in Supplementary Figs. 19a, the measuring current (ti, Ii) makes irregular undulations around background current (I0) due to the presence of noise current (In, i). Therefore, the In, i can be obtained by subtracting the I0 from the Ii (equation 2). The value of noise current (In) cannot be obtained by averaging In, i, but it can be obtained by taking the root mean square of the In, i.

As shown in Supplementary Figs. 19b, c, we measured the time-current curves before (green) and after (brown) the WSe2 homojunction device was connected to the instrument at the same voltage. By taking the root of the difference between two noise powers (), we can obtain the noise current of the WSe2 homojunction device (In, device). Then, the equivalent noise power (PNEP) of WSe2 homojunction device can be calculated by dividing In, device by the responsivity (R) (equation 4).

(4)

Supplementary Fig. 20 More typical image processing functions using different in-sensor filters. (a-c) Different Sobel edge enhancement operators for HDR in-sensor image processing, where (a) is the Sobel operator along the x direction, (b) is the Sobel operator along the y direction, and (c) is a combination of (a) and (b). (d) Edge blurring operators for HDR in-sensor image processing.

Table S1. The performance comparison (R, response speed and LDR) of 2D material-based reconfigurable photodetectors.4–6,8,18–25

Reference

1.	Azimipour, M. et al. Optoretinogram: optical measurement of human cone and rod photoreceptor responses to light. Opt. Lett. 45, 4658 (2020).

2.	Liao, F. et al. Bioinspired in-sensor visual adaptation for accurate perception. Nat. Electron. 5, 84–91 (2022).

3.	Sony Group Portal. https://www.sony.com/en/SonyInfo/vision-s/safety.html.

4.	Zhou, Y. et al. Computational event-driven vision sensors for in-sensor spiking neural networks. Nat. Electron. 6, 870–878 (2023).

5.	Yang, J. et al. A reconfigurable bipolar image sensor for high-efficiency dynamic vision recognition. Nano Lett. 24, 5862–5869 (2024).

6.	Wang, Y. et al. Van der Waals contacted WSe2 ambipolar transistor for in-sensor computing. Nano Res. 16, 12713–12719 (2023).

7.	Del Corro, E. et al. Excited excitonic states in 1L, 2L, 3L, and bulk WSe2 observed by resonant Raman spectroscopy. ACS Nano 8, 9629–9635 (2014).

8.	Jiang, J. et al. Polarization-resolved near-infrared PdSe2 p-i-n homojunction photodetector. Nano Lett. 23, 9522-9528 (2023).

9.	Lu, L.-S. et al. Layer-dependent and in-plane anisotropic properties of low-temperature synthesized few-layer PdSe2 single crystals. ACS Nano 14, 4963–4972 (2020).

10.	Oyedele, A. D. et al. PdSe2: pentagonal two-dimensional layers with high air stability for electronics. J. Am. Chem. Soc. 139, 14090–14097 (2017).

11.	Gorbachev, R. V. et al. Hunting for monolayer boron nitride: optical and Raman signatures. Small 7, 465–468 (2011).

12.	Luo, P. et al. Self‐driven WSe2/Bi2O2Se van der Waals heterostructure photodetectors with high light on/off ratio and fast response. Adv. Funct. Mater. 31, 2008351 (2021).

13.	You, C. et al. Enhanced photodetection performance in graphene-assisted tunneling photodetector. IEEE Trans. Electron Devices 68, 1702–1709 (2021).

14.	Zhang, L. et al. High-performance multilayer WSe2 p-type field effect transistors with Pd contacts for circuit applications. J. Mater. Sci.: Mater. Electron. 32, 17427–17435 (2021).

15.	Li, H. et al. Preparation and applications of mechanically exfoliated single-layer and multilayer MoS2 and WSe2 nanosheets. Acc. Chem. Res. 47, 1067–1075 (2014).

16.	Dong, N. et al. Optical limiting and theoretical modelling of layered transition metal dichalcogenide nanosheets. Sci. Rep. 5, 14646 (2015).

17.	Ansari, N. et al. Light absorption optimization in two-dimensional transition metal dichalcogenide van der Waals heterostructures. J. Opt. Soc. Am. B 35, 1179 (2018).

18.	Pi, L. et al. Broadband convolutional processing using band-alignment-tunable heterostructures. Nat. Electron. 5, 248–254 (2022).

19.	Wang, H. et al. Polarization‐ and gate‐tunable optoelectronic reverse in 2D semimetal/semiconductor photovoltaic heterostructure. Adv. Mater. 36, 2309371 (2024).

20.	Huang, J. et al. Reconfigurable WSe2 Schottky heterojunctions for logic rectifiers and ultrafast photodetectors. Sci. China Mater. 66, 4711–4722 (2023).

21.	Jang, H. et al. In-sensor optoelectronic computing using electrostatically doped silicon. Nat. Electron. 5, 519–525 (2022).

22.	Zhang, Y. et al. Self-powered bidirectional photoresponse in high-detectivity WSe2 phototransistor with asymmetrical van der Waals stacking for retinal neurons emulation. ACS Nano 16, 20937–20945 (2022).

23.	Zhang, Y. et al. An ultrafast WSe2 photodiode based on a lateral p-i-n homojunction. ACS Nano 15, 4405–4415 (2021).

24.	Zhang, Y. et al. High-speed transition-metal dichalcogenides based Schottky photodiodes for visible and infrared light communication. ACS Nano 16, 19187–19198 (2022).

25.	Liu, F. et al. Self-powered programmable van der Waals photodetectors with nonvolatile semifloating gate. Nano Lett. 23, 11645–11654 (2023).