Role of size, surface charge, and PEGylated lipids of lipid nanoparticles (LNPs) on intramuscular delivery of mRNA

Weiwen Konga, Yuning Weia, Zirong Donga, Wenjuan Liua, Jiaxin Zhaoa, Yan Huangb,c, Jinlong Yanga, Wei Wua, Haisheng Hea*, Jianping Qia*

a Key Laboratory of Smart Drug Delivery of MOE, School of Pharmacy, Fudan University, Shanghai 201203, China

b Department of Oncology, Shanghai Medical College of Fudan University, 270 Dong-an Road, Shanghai, 200032, China

c Department of Gynecologic Oncology, Fudan University Shanghai Cancer Center, 270 Dong-an Road, Shanghai, 200032, China

*Corresponding author: Haisheng He, he_haisheng@fudan.edu.cn; Jianping Qi, qijianping@fudan.edu.cn

Supplementary Table

Tab. S1. Flow ratio and total flow rate of LNP-S, LNP-M and LNP-L

|  | Flow ratio (lipid:mRNA) | Total flow rate (mL/min) |
| --- | --- | --- |
| LNP-S | 1:3 | 12 |
| LNP-M | 2:3 | 8 |
| LNP-L | 2:3 | 4 |

Tab. S2. Ratio of SM102 and DOTAP or DSPG, particle size, PDI, zeta potential and encapsulation efficiency (EE) of LNPs with different charge.

|  | Ratio (SM102: DOTAP or DSPG) | Particle size (nm) | PDI | Zeta potential (mV) | EE (%) |
| --- | --- | --- | --- | --- | --- |
| LNP | 50:0 | 91.66±1.08 | 0.13±0.02 | -3.47±3.03 | 90.5±0.1 |
| 15% DSPG | 42.5:7.5 | 81.59±0.43 | 0.24±0.02 | -25.3±3.02 | 94.8±0.2 |
| 25% DSPG | 25:25 | 86.98±1.76 | 0.27±0.02 | -25.9±1.39 | 95.1±0.1 |
| 15% DOTAP | 42.5:7.5 | 109.83±0.64 | 0.25±0.04 | 12.83±0.67 | 91.4±0.1 |
| 25% DOTAP | 37.5:12.5 | 126.57±1.63 | 0.02±0.01 | 19.03±0.23 | 97.4±0.1 |
| 50% DOTAP | 25:25 | 125.33±3.33 | 0.14±0.01 | 23.37±0.61 | 97.9±0.1 |

Fig. S1. Luminescence images of LNP-S, LNP-M and LNP-L. (A) In vivo luminescence images at 0.5 h-24 h. (B) Ex vivo luciferase distribution of LNPs with various sizes at 4 h after intramuscular injection. Luminescence images were harvested by IVIS. AUC0.5-24 h of muscle (C) and AUC0.5-24 h of liver (D) indicate total luciferase expression during 0.5 h-24 h (n=3), *: p<0.05, compared with LNP-S.

Fig. S2. Luminescence images of LNPs with various charges. (A) In vivo luminescence images of LNPs with different charges at 2 h-24 h. (B) Ex vivo luciferase distribution of LNPs with various charge at 4 h after intramuscular injection. Luminescence images were harvested by IVIS. AUC2-24 h of muscle (C) and AUC2-24 h of liver (D) indicate total luciferase expression during 2 h-24 h (n=3), *: p<0.05, **: p<0.01, ***: p<0.001, compared with LNP.

Fig. S3. Luminescence images of LNPs with varying contents of PEGylated lipids. (A) In vivo luminescence images of LNPs with different DMG-PEG2k contents at 0.5h-24h. (B) Luciferase distribution of LNPs with 0.5 mol%, 1.5 mol% and 3 mol% DMG-PEG2k at 4h after intramuscular injection. Luminescence images were harvested by ivis. AUC0.5-24 h of muscle (C) and AUC0.5-24 h of liver (D) indicate total luciferase expression during 0.5 h-24 h (n=3), *: p<0.05, **: p<0.01, compared with 0.5% DMG-PEG2k.

Fig. S4. Stability of LNPs with different types of PEGylated lipids. Stability on particle size (A), PDI (B), zeta potential (C) and encapsulation efficiency (D) in PBS at 4 °C. Stability on particle size (E), PDI (F), zeta potential (G) and encapsulation efficiency (H) in PBS with 10% FBS at 37 °C.

Fig. S5. Luminescence images of LNPs with different types of PEGylated lipids. (A) In vivo luminescence images of LNPs with different types of PEGylated lipid at 0.5 h-24 h. (B) Luciferase distribution of LNPs with DMG-PEG2k, DSG-PEG2k of DSPE-PEG2k at 24 h after intramuscular injection. Luminescence images were harvested by IVIS. AUC0.5-24 h of muscle (C) and AUC0.5-24 h of liver (D) indicate total luciferase expression during 0.5 h-24 h (n=3), *: p<0.05, **: p<0.01, compared with LNPs with DMG-PEG2k.