SUPPLMENTARY INFORMATION

Figure S1.

S21 mapping was performed using two different frequencies with a healthy ½” thick T700s 2x2 Twill Weave CF panel having [0°/90°] layup inserted between the two coils (Figure S1).

The S21 is very different in the presence of the carbon fiber compared to air. In this experiment, the Rx coil is measuring the magnetic field that penetrates through the entire thickness of the ½” (12.7 mm) CF panel. Using a 100 kHz excitation frequency, the gain (magnitude transmitted) and phase plots in Figure S1 show that the field is warped with higher transmission and a more constant phase shift, observed over a longer distance when aligned in the fiber directions. To ensure this wasn’t an artifact of the measurement, the panel was rotated 45° and scanned again. The same distinct cross pattern was observed to rotate 45° with the panel and maintains higher transmission along the fiber directions. This is clear evidence that the 3D CF structure distorts (i.e. shapes) the magnetic field based on internal electrical difference, and is inductively coupling into the coil.

The well-defined circular area in the center of the image (about -60 dB gain) is indicative of the primary magnetic field (B1) penetrating the entire thickness of the panel. The features that form as a function of the fiber direction and ply layup are therefore characteristic of propagating eddy currents in a 3D (2D spread and layer-by-layer) fashion, through the thickness of the CF laminate.

Figure S2.

When the frequency is raised to 3 MHz, the EMF is predominantly spread along the surface of the panel  (in fact the traditional penetration depth equation calculates the skin depth as << 1 mm in this scenario). Nonetheless, there is still a uniform gain observed across the entire CF laminate that must be transmitted from the surface through-the-thickness of the CF. The primary B1 field is not being transmitted through the ½” thickness of CF at this frequency and is confirmed by the lack of a high gain circle near the center of the image. This may be explained by a combination of two possible effects.

First, the displacement currents (i.e. stray capacitance between fibers NOT in direct contact) generated at this high of a frequency are significant and dramatically increases the conductivity in the through-the-thickness direction. Second, the B1 field is known to interact strongly with each of the ply interfaces (especially orthogonal plies), thus generating high intensity eddy currents at each interface and nodes at overlapping loop paths[10, 11]. These strong eddy currents are known to have their own electromagnetic fields and since each interface (n) will generate eddy currents, there will be (Bn) magnetic fields associated with them. This often leads to the creation of eddy currents loops that are confined to a narrow range in the depth (at each interface), and thus act like a “secondary excitation coil”. This confined eddy current loop will have an associated magnetic field that propagates away from the interface in both directions. These magnetic fields will be denoted as the “interfacial magnetic field” from here on.

Part of this interfacial magnetic field (directed up towards the excitation coil) will destructively interact with the primary B1 field and be measured through changes to the original sensor probe. The other part of this field (directed away from the excitation coil) will interact with the next ply interface in the through-the-thickness direction (and could possible constructively interfere with the B1-field) while also aiding in generating another strong interfacial magnetic field. Thus begins a cascade or propagation of eddy currents and magnetic fields that help to compound each other through-the-thickness of the structure. This “avalanche effect” can help to increase the penetration depth and achieves significantly higher sensitivity to structural changes at depth.

This is in stark contrast to a homogenous conductor; there are no discrete “interfaces” and the total contribution of magnetic fields arising from generated eddy currents are often denoted as (B2). This is because the intensities of the eddy currents are constantly decaying from the surface throughout the depth of the conductor. This constant decay is a result of destructive interferences arising from eddy currents being made at every spatial location in the depth and their equal spread in all dimensions. However, for layered 3D CF structures, this is an oversimplification. These interfacial EMFs do interact with each other and result in a bulk change to the B1 field, albeit in a much more complex way than is understood for homogenous conductors.

#### ½” Thick – Unitape [0°/90°]

To further understand the difference in the spread of the EMF by the carbon-fiber internal structure a Unitape lay-up sample was evaluated with the S21 mapping experiment. All other experimental parameters were kept constant. The 100 kHz data is shown in Figure S3.

Figure S3.

Within the 3D structure for the Unitape, there are no carbon fibers that physically weave in between ply layers and thus the primary direction of the EMF flow (after eddy current generation) is along the 0° and 90° fiber directions, on the same plane as the ply layer. In contrast, the 2x2 Twill Weave has fibers that are interwoven between layers and thus provide an alternate path for the current to flow. This results in a more homogenized EMF response in CF structures that are woven and begins to respond more like the homogenous conductor case. The S21 maps support this theory; a higher S21 gain magnitude (dB) of about -77 dB is observed along the fiber directions (±30 mm from the center) in the Unitape structure (Figure S3) and is reduced to about -81 dB at the same positions in the 2x2 Twill Weave (Figure S1). This 4 dB change in magnitude indicates the EMF power that penetrates through the Unitape sample is about >50% higher than what makes it through the 2x2 Twill Weave and is strong evidence supporting the fact that ply layup plays a pivotal role governing the penetration depth in CF laminate structures.  This may also indicate that the penetration depth is shallower in weaved CF structures due to preventing the formation of the confined eddy current loops at the interfaces and in turn the interfacial magnetic field strengths are reduced.

Figure S4.

To further test this, a 3 MHz excitation frequency was applied to the Unitape panel was with the S21 analysis (Figure S4). The 0°/90° spread is observed along the fiber directions, although the response is inverted from what has been seen previously (i.e. less EMF makes it through at these locations). The gain plots now show a slight reduction in transmission along the fiber directions with low transmission nodes forming along the fiber directions, at this frequency. These locations match well with high intensity current density nodes that form at orthogonal ply interfaces due to the overlap of eddy current loops and have been well documented by Yi et. al. in 2023[11].

Nonetheless, the overall gain magnitude that is transmitted through the rest of the panel is slightly higher at about -87 to -88 dB, than when compared with the 3 MHz 2x2 Twill Weave which has a magnitude of about -90 to -91 dB (Figure S2). One possibility is deeper EMF penetration in the Unitape structures due to the generation of continuous cascading eddy currents throughout the interfaces in depth (when the eddy current loops are localized). As the continuous currents preferentially spread in the 0°/90° directions, while propagating through-the-thickness direction, the eddy currents are no longer spatially confined to the localized loop paths (like in the single ply interface), thus lowering the interfacial magnetic field strength (i.e. lower magnetic flux density) and the penetration depth becomes shallower in these regions.