Supporting Information

Novel NiCo2S4 nanorods arrays grown on carbon nanofibers as high-performance anodes for sodium ion batteries

Xiaowei Yang1 • Tongxiang Cai2 • Zhongran Yao1 • Guojie Chao1

1 School of Automobile and Traffic Engineering, Wuxi Institute of Technology, Wuxi 214121, China.

2 Yadea Technology Group Co., Ltd, Wuxi 214105, China

Corresponding author: Xiaowei Yang

E-mail address: xiaoweiyang215@126.com

Experimental

Materials and Reagents

Polyacrylonitrile (PAN) was purchased from Sigma-Aldrich. Nickel nitrate hexahydrate (Ni(NO3)2·6H2O), cobalt nitrate hexahydrate (Co(NO3)2·6H2O), thiourea, urea and hexamethylenetetramine were purchased from Shanghai Macklin Biochemical Co., Ltd. All reagents were used without further purification.

Preparation of CNF membranes

CNF membranes were synthesized by electrospinning and carbonization process. Typically, 1 g PAN was dissolved in 10 ml DMF with magnetic stirring for 2 h. The electrospinning process was implemented on a vulgaris electrospinning machine. The voltage between the spinneret and the drum-type collector was fixed to 15 kV and the distance was adjusted to 15 cm. After electrospinning, the as-obtained electrospinning membranes were transferred to a tube furnace. These membranes were first pre-oxidized at 200 °C for 2 h in the air atmosphere, then carbonized under the flowing nitrogen atmosphere at 700 °C for 2 h. The CNF membranes were final obtained and marked as CNF.

Figure S1 Morphology of carbon fibers before and after hydrothermal treatment.

Table S1 Elemental analysis results of the NiCo2S4@CNF from XPS measurements.

| Sample | XPS spectra analysis |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | C/ at.% | O/ at.% | S/ at.% | Co/ at.% | Ni/ at.% |
| NiCo2S4@CNF | 38.1 | 24.4 | 19.4 | 7.9 | 10.2 |

Table S2 Comparison of sodium storage performance of NiCo2S4@CNF in this work and other related reports in the literatures.

| Samples | Structure | Capacity (mAh g-1) | Current density (A g-1) | ICE/% | Ref. |
| --- | --- | --- | --- | --- | --- |
| NiCo2S4@CNF | nanorods arrays | 683.6 | 0.1 | 90.4 | This work |
| NiCo2S4@CDs | nanosheets | 568.9 | 0.5 | 81.0 | [1] |
| NiCo2S4@MoS2 | hierarchical | 400 | 0.1 | 66.2 | [2] |
| NiCo2S4@Ni-B | hollow nanospheres | 390.2 | 0.1 | 92 | [3] |
| NCS@GNs@CNTs | 3D framework | 558.1 | 0.1 | 96 | [4] |
| NiCo2S4 | dodecahedron | 600 | 0.1 | 83.7 | [5] |
| Flower-like NiCo2S4 | flower-like | 748 | 0.1 | 94 | [6] |

References

1.	Qin, B., Wang, M., Wu, S., Li, Y., Liu, C., Zhang, Y., Fan, H. (2023) Carbon dots confined nanosheets assembled NiCo2S4@CDs cross-stacked architecture for enhanced sodium ion storage. Chinese Chem. Lett. 35(7): 108921

2.	Liu, B., Kong, D., Wang, Y., Lim, Y. V., Huang, S., Yang, H. Y. (2018) Three-dimensional hierarchical NiCo2S4@MoS2 heterostructure arrays for high performance sodium ion battery. FlatChem. 10:14-21

3.	Li, J., Zhou, J., Zhou, Q., Wang, X., Guo, C., Li, M. (2021) Promoting the Na+-storage of NiCo2S4 hollow nanospheres by surfacing Ni-B nanoflakes. J. Mater. Sci. Technol. 82:114-121

4.	Fan, S., Liu, H., Bi, S., Meng, X., Wang, Q., Zhang, K., Chen, Z., Xie, Y. (2023) NiCo2S4 nanoparticles anchored in the 3d interpenetrating framework composed of GNs and CNTs toward enhanced sodium storage performance. Electrochim. Acta 441:141760

5.	Fan, S., Liu, H., Xie, Y., Bi, S., Meng, X., Zhang, K., Sun, L., Zhang, S., Guo, Z. (2023) Electrolyte engineering on performance enhancement of NiCo2S4 anode for sodium storage. Small 19(26): 2300188

6.	Miao, Y., Zhao, X., Wang, X., Ma, C., Cheng, L., Chen, G., Yue, H., Wang, L., Zhang, D. (2020) Flower-like NiCo2S4 nanosheets with high electrochemical performance for sodium-ion batteries. Nano Res 13(11): 3041-3047