Supplementary information for

Electron transfer mediated contaminant activates periodate to generate 1O2 by charge-confined single-atom catalyst

Qianqian Tang1, Bangxiang Wu1, Xiaowen Huang1, Wei Ren1, Lingling Liu1,2, Lei Tian1, Ying Chen1, Long-Shuai Zhang1,2,*, Qing Sun1,2, Zhibing Kang1, Tianyi Ma3 and Jian-Ping Zou1,2,*

1 Key Laboratory of Jiangxi Province for Persistent Pollutants Prevention Control and Resource Reuse, Nanchang Hangkong University, Nanchang 330063, P. R. China

2 National-Local Joint Engineering Research Center of Heavy Metals Pollutants Control and Resource Utilization, Nanchang Hangkong University, Nanchang 330063, P. R. China

3 School of Science, RMIT University, Melbourne, VIC 3000, Australia.

*Corresponding author: Jian-Ping Zou

Email: zjp_112@126.com

This PDF file includes:

Supplementary text

Supplementary Figure 1 to 21

Supplementary Table 1 to 3

Supplementary References

Supplementary Text

Chemicals. Melamine (MA), cyanuric acid (CA), ferric nitrate nonahydrate (Fe(NO3)3·9H2O), oxalic Acid (OA), furfuryl alcohol (FFA), 4-iodophenol (4-IP), 2-iodophenol (2-IP), sodium iodate (NaIO3), phosphoric acid (H3PO4), Nafon 117 solution (~5% in a mixture of lower aliphatic alcohols and water), potassium dichromate (K2Cr2O7), 4-fluorophenol (4-FP), superoxide dismutase (SOD, ≥1400 units/mg dry weight), and 9,10-dimethyl-anthracene (DMA) were purchased from Aladdin Bio-Chem Technology Co., Ltd. Tert-butanol (TBA), p-chlorophenol (4-CP), 2,4,6-trichlorophenol (2,4,6-TCP), methyl alcohol (MeOH), acetonitrile (C2H3N), methyl phenyl sulfoxide (PMSO), methyl phenyl sulfone (PMSO2), p-bromophenol (4-BP ), and ferrouschloride (FeCl2) were purchased from Shanghai Macklin Biochemical Co., Ltd. Thiourea (CH4N2S), sodium sulfate (Na2SO4), sodium hydroxide (NaOH), solublestarch, and ethanol (EtOH) were purchased from Xilong Chemical Co., Ltd. Sodium periodate (PI, NaIO4) was purchased from Shanghai Yi En Chemical Technology Co., Ltd. Iodine (I2) was purchased from Shanghai Boer Chemical Reagent Co., Ltd. Sulfuric acid (H2SO4) was purchased from Shanghai Xinguang Electronic Technology Co., Ltd. Phenol (Ph) was purchased from Sinopharm Chemical Reagent Co., Ltd. Benzoquinone (p-BQ) was purchased from J&K Scientific Co., Ltd. 2,4-Dichlorophenol (2,4-DCP) was purchased from Beijing Wokai Biotechnology Co., LTD. 2,3,5,6-Tetrachlorophenol (2,3,5,6-TeCP) was purchased from Sigma-Aldrich (Shanghai) Trading Co., LTD.

Analysis methods. The concentrations of contaminants were monitored by a high-pressure liquid chromatographer (HPLC, Ultimate 3000, Thermo) with a TC-C18 reverse-phase column (150 mm × 4.6 mm, 5 μm, Agilent). Specific test conditions for each reactant are detailed in Supplementary Table 3. The total organic carbon (TOC) of the solution was tested on a Shimadzu TOC (TOC-L CSH CN200). The degradation products were analyzed using liquid chromatography model Shimadzu 30A and mass spectrometry model AB SCIEX Triple Tof 5600. The liquid chromatography column used was a waters C18 Column, 120Å, 1.7 µm, 2.1 mm* 100 mm, and the scanning range of the mass spectrum was 40-1000 Da. The concentration of Cl- in solution was determined using an ion chromatograph model ZCS-1100.

DMA probe experiment. The determination of indicative products from the specific reactions between 1O2 and classical chemical probe 9,10-dimethylanthracene (DMA), as they would form the corresponding endoperoxide (DMA-O2). Excitation and emission spectra of DMA in 10 wt% acetonitrile in H2O. The excitation was recorded from 280-420 nm with λem= 425 nm.

Oligomer products detection. In order to detect the oligomeric products attached to the catalyst surface that may be generated during the reaction process, the reacted solution was filtered using a polytetrafluoroethylene (PTFE) filter membrane with a pore size of 0.22 μm to obtain the reacted catalyst material. The reacted catalyst was then eluted using an aqueous methanol solution at a volume ratio of 50% and the filtrate at this point was collected and tested by liquid chromatography-mass spectrometry.

Iodinated byproducts detection. 4-IP and 2-IP were measured to probe the generation of HOI as HOI could readily react with phenol to produce iodinated phenols including 4-IP and 2-IP. In a typical procedure, 5 mL of 10 mM phenol was added into the Fe/SCN+PI system before the initiation of the reaction. The possibly generated iodinated phenols were determined by HPLC with details available in Supplementary Table 3. I2 and I3- were analyzed by a starch colorimetric method (1). The aliquots of the Fe/SCN+PI system or I2 authentic sample were mixed with the newly-prepared starch stock solution, and the blue color would indicate the existence of I2. To prepare starch stock solution, soluble starch (3 g) was mixed with 10 mL ultrapure water and then the mixture was poured into 90 mL of boiling water under vigorously stirring. After stirring for 3 min, the mixture was then cooled down to room temperature for subsequent use.

Electrochemical measurement. Electrochemical measurements were performed in a standard three-electrode system (CHI 660D, Shanghai Chenhua, China) comprising an activator-coated fluorine-tin oxide (FTO) glass electrode as the working electrode, a carbon rod as the counter electrode, and Ag/AgCl as the reference electrode. 5 mg of catalyst was dispersed in a mixture of 140 μL of ethanol and 10 μL of naphthol solution and then sonicated for 30 min to obtain the ink solution. The working electrode was obtained by drying at room temperature after dropping 50 μL of ink solution on a 1*1 cm2 FTO glass. Chronoamperometry i-t curves were obtained at an applied voltage of 0.8 V (relative to Ag/AgCl) using 150 mL of 0.5 M Na2SO4 solution as the electrolyte. After an applied voltage of 228 s, 1.5 mL of 0.25 M PI was added, followed by 1.5 mL of 10 mM 4-CP solution at 315 s. The open circuit potential of the Fe/SCN loaded-FTO was monitored by chronopotentiometry analysis using an Ag/AgCl as the reference electrode. The system can also measure the potential variations at the electrode with the addition of PI and 4-CP.

A RRDE electrode with a glassy carbon electrode (0.247 cm2) and a platinum ring electrode (0.186 cm2) was used as the working electrode. Prior to the measurements, the electrode was polished with 0.3 and 0.05 μm alumina suspensions on a polishing cloth and rinsed with ethanol for several times. The electron transfer number (n) on the RRDE were calculated using the following equations (2,3):

n = 4×Id/(Id+Ir/Nc)

Where Ir and Id were the ring current and the disk current, respectively, and Nc was the collection efficiency of the ring electrode (0.33).

- coli culture experiments. Luria-Battani (LB) solid media were prepared for E. coli culture experiments using 20mL of 5 mM 4-CP solution before and after the reaction. Appropriately diluted 10 μL of E. coli bacterial solution was dropped on the prepared LB solid media, evenly coated and then inverted into a constant temperature incubator, and incubated at 35℃ for 48 h.

- Preparation of the Fe/SCN-sodium alginate gel apheres. Sodium alginate (3.0 g) was slowly added to 150 mL of ultrapure water and stirred until the solubilized solution was clarified and free of solid particles. The Fe/SCN (1.0 g) was added into sodium alginate solution. Then, sonicated and stirred until the sample was well dispersed. Subsequently, the Fe/SCN-sodium alginate gel spheres were obtained by dropping the prepared sol solution into ultrapure water.

- DFT calculations. All the calculations are performed in the framework of the density functional theory with the projector augmented plane-wave method, as implemented in the Vienna ab initio simulation package (4). The generalized gradient approximation proposed by Perdew, Burke, and Ernzerhof is selected for the exchange-correlation potential (5). The long-range van der Waals interaction is described by the DFT-D3 approach (6). The cut-off energy for plane wave is set to 450 eV. The energy criterion is set to 10−5 eV in iterative solution of the Kohn-Sham equation. A vacuum layer of 15 Å is added perpendicular to the sheet to avoid artificial interaction between periodic images. The Brillouin zone for energies calculation of the Fe/SCN surfaces was sampled with a Gamma-centered k-mesh of 2×3×1. All the structures are relaxed until the residual forces on the atoms have declined to less than 0.02 eV/Å.

Supplementary Figures

Supplementary Fig. 1 a,b, XRD patterns (a) and FT-IR spectra (b) of the CN, SCN, Fe/CN, and Fe/SCN.

Supplementary Fig. 2 a,b, Nitrogen adsorption-desorption isotherms (a) and corresponding pore size distributions curves (b) of the CN, SCN, Fe/CN, and Fe/SCN.

Supplementary Fig. 3 WT-EXAFS plots of Fe foil, FeO, Fe2O3, FeS, FePc, and the Fe/SCN.

Supplementary Fig. 4 a,b, XPS spectra of N 1s (a) and S 2p (b) for the Fe/SCN.

Supplementary Fig. 5 4-CP degradation by Fe2+, Fe3+, Fe2++CN, and Fe3++CN activated PI systems.

Supplementary Fig. 6 Degradation rate of 4-CP by catalysts prepared with different thiourea additions.

Supplementary Fig. 7 a,b, Degradation curves of 4-CP by the Fe/SCN+PI system with different catalyst additions (a) and different PI additions (b).

Supplementary Fig. 8 Degradation curves of 4-CP with different concentrations by the Fe/SCN+PI system.

Supplementary Fig. 9 The pseudo-first order kinetics for different catalytic systems.

Supplementary Fig. 10 EPR signals of ·OH, ·O2-, 1O2 in the Fe/CN+PI system.

Supplementary Fig. 11 Degradation curves of PMSO and corresponding PMSO2 generation for different catalyst activated PI systems.

Supplementary Fig. 12 PI consumption curves of the Fe/SCN+PI system with/without degradation of 4-CP.

Supplementary Fig. 13 EPR spectra of ·O2- for the Fe/SCN+PI system under different conditions.

Supplementary Fig. 14 a-d, The high-resolution I 3d XPS spectra of CN (a), SCN (b), Fe/CN (c) and Fe/SCN (d) after 30 minutes adsorption of PI.

Supplementary Fig. 15 a-e, Mass spectra of C6H6O2 (a), C6H4O2 (b), C4H4O4 (c), C3H4O2 (d) and C2H4O3 (e) product in the reaction solution at different time intervals.

Supplementary Fig. 16 The degradation curve of 4-CP and variation profile of TOC in the Fe/SCN+PI system.

Supplementary Fig. 17 a,b, XRD patterns (a) and FT-IR patterns (b) of the Fe/SCN before and after reaction.

Supplementary Fig. 18 Fe ions leaching with reaction in the Fe/CN+PI system and the Fe/SCN+PI system.

Supplementary Fig. 19 a-c, Detection of HOI using phenol as the trapping agent (a), IO4- and IO3- concentration curves (b) and detection of I2 and I3- in the Fe/SCN+PI system (c).

Supplementary Fig. 20 a-c, Diagram of the effect of culturing E. coli using different solutions the blank control group not smeared with bacterial solution (a), the contaminant solution before the reaction (b), and the reacted solution obtained by filtration after the reaction (c).

Supplementary Fig. 21 Photo of the catalytic column equipment.

Supplementary Tables

Table 1. Specific surface area and pore volume of each catalyst.

| Samples | Surface Area (m2 g-1) | Pore Volume (cm3 g-1) |
| --- | --- | --- |
| CN | 57.131 | 0.4403 |
| SCN | 70.175 | 0.6033 |
| Fe/CN | 71.920 | 0.5886 |
| Fe/SCN | 76.194 | 0.5504 |

Table 2. EXAFS fitting parameters at the Fe K-edge for Fe foil and the Fe/SCN.

| Sample | Shell | CNa | R(Å)b | σ2(Å2)c | ΔE0(eV)d | S02 | R factor |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Fe foil | Fe-Fe | 8 (set) | 2.47 | 0.006 | 5.1±0.4 | 0.7755 | 0.008 |
|  | Fe-Fe2 | 6 (set) | 2.84 | 0.006 |  |  |  |
| Fe/SCN | Fe-N | 3.3±0.5 | 1.97 | 0.005 | -9.2±1.0 | 0.7755(set) | 0.018 |
|  | Fe-S | 0.9±0.3 | 2.26 | 0.006 |  |  |  |

Table 3. The HPLC analysis conditions for different substrates.

| Substrates | Mobile phase | Ratio (v:v) | Wavelength (nm) | Flow (mL min-1) | Column temperature (℃) |
| --- | --- | --- | --- | --- | --- |
| 4-CP | A1/B1 | 50/50 | 228 | 1.0 | 35 |
| 2,4,6-TCP | A2/B1 | 70/30 | 290 | 1.0 | 35 |
| PMSO | A1/B2 | 20/80 | 230 | 1.0 | 35 |
| PMSO2 | A1/B2 | 20/80 | 215 | 1.0 | 35 |
| IO4-/IO3- | A1/B3 | 20/80 | 214 | 1.0 | 35 |
| 2,4-DCP | A2/B1 | 70/30 | 200 | 0.8 | 40 |
| 2,3,5,6-TeCP | A2/B2 | 70/30 | 210 | 0.8 | 40 |
| 4-FP | A1/B1 | 60/40 | 280 | 1.0 | 35 |
| 4-BP | A1/B1 | 70/30 | 280 | 1.0 | 35 |
| 4-IP/2-IP | A2/B3 | 60/40 | 286 | 1.0 | 35 |

A1: acetonitrile; A2: methanol; B1: ultrapure water; B2: ultrapure water containing 0.1% acetic acid; B3: ultrapure water with 0.1% phosphoric acid.

Supplementary  References

- Sun, H., He, F. & Choi, W. Y. Production of reactive oxygen species by the reaction of periodate and hydroxylamine for rapid removal of organic pollutants and waterborne bacteria. Environ. Sci. Technol. 54, 6427-6437 (2020).

- Wang, J. B., Li, S. Z., Qin, Q. Y. & Peng, C. Sustainable and feasible reagent-free electro-Fenton via sequential dual-cathode electrocatalysis. Proc. Natl. Acad. Sci. U.S.A. 118, e2108573118 (2021).

- Xu, H. et al. Atomically dispersed iron regulating electronic structure of iron atom clusters for electrocatalytic H2O2 production and biomass upgrading. Angew. Chem. Int. Ed. 62, e202314414 (2023).

- Kresse, G. & Joubert, D. From ultrasoft pseudopotentials to the projector augmented-wave method. Phys. Rev. B 59, 1758-177 (1999).

- Perdew, J. P., Burke, K. & Ernzerhof, M. Generalized gradient approximation made simple. Phys. Rev. Lett. 77, 3865-3868 (1996).

- Grimme, S., Antony, J., Ehrlich, S. & Krieg, H. A consistent and accurate ab initio parametrization of density functional dispersion correction (DFT-D) for the 94 elements H-Pu. J. Chem. Phys. 132, 154104 (2010).