Supplementary Information

Grain Boundary Cracks Patching and Defect Dual Passivation with Ammonium Formate for High-Efficiency Triple-Cation Perovskite Solar Cells

Yang Ding,1,2,† Yefan Wu, 1,2,† Xiangxiang Feng,1,2 Hengyue Li,1,2 Erming Feng,1,2 Jianhui Chang,1,2 Caoyu Long,1,2 Yuanji Gao,1,2 Junliang Yang1,2,3,*

1 Hunan Key Laboratory for Super-microstructure and Ultrafast Process, School of Physics, Central South University, Changsha, 410083, China

2 Hunan Key Laboratory of Nanophotonics and Devices, School of Physics, Central South University, Changsha, China

3 State Key Laboratory of Powder Metallurgy, Central South University, Changsha, Hunan 410083, China

† These authors contributed equally to this work.

* Corresponding authors: junliang.yang@csu.edu.cn, +86-731-88660256 (J.L. Yang)

Figure S1. XRD pattern of the NH4HCO2-3 treated film and the prepared NH4HCO2-PbI2 complex.

Figure S2. EDS Mapping of NH4HCO2-modified perovskite surface.

Figure S3. AFM spectrum of perovskite films (a) without and (b) with NH4HCO2 modified.

Figure S4. Chlorobenzene (CB) contact angles of perovskite films (a) without and (b) with NH4HCO2 modified.

Figure S5. Top-view SEM images of perovskite films modified with different concentrations of NH4HCO2 (0, 1, 3, 5 mg/ml, respectively).

Figure S6. (a-b) FTIR spectra of control (NH4HCO2) and target samples (NH4HCO2 + perovskite film).

Figure S7. The schematic structure of PSCs with NH4HCO2 modification.

Table S1. The fitting parameters of TRPL spectra for control and target (NH4HCO2-3) samples.

| Samples | A1 | τ1 (ns) | A2 | τ2 (ns) |
| --- | --- | --- | --- | --- |
| Control | 183 | 32 | 180 | 785 |
| NH4HCO2-3 | 152 | 26 | 243 | 1613 |

Table S2. Key photovoltaic parameters of PSCs with different NH4HCO2 modification.

| Devices | Jsc (mA cm-2) | Voc (V) | FF (%) | PCE (%) |
| --- | --- | --- | --- | --- |
| Control | 24.41 | 1.12 | 80.11 | 21.84 |
| NH4HCO2-1 | 24.59 | 1.12 | 82.80 | 22.80 |
| NH4HCO2-3 | 24.67 | 1.14 | 83.47 | 23.38 |
| NH4HCO2-5 | 24.18 | 1.10 | 80.15 | 21.31 |

Note S1:

In order to study the carrier dynamics behavior inside the device, the relationship of Jsc and Voc as a function of light intensity was fitted using the following formula 1,2: Jsc∝Iα(α≤1) and Voc= nkTln(I)/q+constant, where α is a factor related to bimolecular recombination, it can be ignored under a complete ideal situation and the α should be infinitely close to 1. The parameter n is a factor associated with monomolecular recombination, similarly, a smaller n can be obtained when nonradiative recombination is suppressed. k and q are the Boltzmann constant and elementary charge, respectively.

References

1 C. Xu, L. Cheng, Z. Li, X. Zheng, S. Shan, T. Chen, W. Fu, Y. Yang, L. Zuo, H. Chen, Adv. Energy Mater. 13(17), 2300168 (2023).

2 X. Jiang, B. Zhang, G. Yang, Z. Zhou, X. Guo, F. Zhang, S. Yu, S. Liu, S. Pang, Angew. Chem. Int. Ed. 62(22), e202302462 (2023).