Uncooled ultra-broadband infrared photodetectors based on core/shell/shell colloidal quantum dots

Chengye Yu1#, Jiaqi Zhu2#, Yufeng Shan2,3*, Shaowen Xu2, He Zhu2, Dingyue Sun1, Jingshan Hou1, Yongzheng Fang1*, Huizhen Wu4, Ning Dai2,3* and Yufeng Liu1,3*

Affiliations

1 School of Materials Science and Engineering, Shanghai Institute of Technology, Shanghai 201418, China;

2 School of Physics and Optoelectronic Engineering, Hangzhou Institute for Advanced Study, University of Chinese Academy of Sciences, Hangzhou, Zhejiang, 310024 China

3 State Key Labratory of Infrared Physics, Shanghai Institute of Technical Physics, Chinese Academy of Sciences, Shanghai 200083, China

4 Zhejiang Province Key Laboratory of Quantum Technology and Devices and Department of Physics, State Key Laboratory for Silicon Materials, Zhejiang University, Hangzhou, 310027 P. R. China

*Correspondence authors: yfliu@mail.sitp.ac.cn; shanyf07@foxmail.com; fangyongzheng@gmail.com; ndai@mail.sitp.ac.cn

Chengye Yu# and Jiaqi Zhu# contributed equally to this work.

This file includes：

1. Growth of the HgSe/PbSe/MAPbI3 CSS system

2. AFM measurement of the CSS CQD film

3. Size statistics of CQDs

4. UPS characterization and analysis for the CSS system

5. SEM images of the CSS CQD photodetector

6. Hall effect measurement of the CSS CQD film

7. Cyclical impulse responses of the CQD photodetector

8. Photocurrent origin of VIS response

9. Blackbody detection system

10. Measurement system for relative response spectra

11. Discussion on the G factor

12. Discussion on the 1/f noise

13. Performance comparison of our device with other uncooled VIS or IR CQD photodetectors

14. Performance comparison of our device with other MWIR CQD photodetectors working at uncooled or cryogenic conditions

15. Performance comparison of our device with uncooled state-of-the-art IR detectors

16. References

Supplementary Fig. S1-11, and Table S1-3.

1. Growth of the HgSe/PbSe/MAPbI3 CSS system

Computational methods: First-principles calculations were performed in Quantum Espresso1. Exchange and correlations were treated within the generalized gradient approximation (GGA) proposed by Perdew-Burke-Ernzerhof (PBE)[6]. Pb 5d¹⁰6p², Hg 5d¹⁰ 6s², Se 4s²4p⁴, C 2s22p2, N 2s22p3, H 1s1 and I 5s²5p⁵ were treated as valence states and projector-augmented wave pseudopotentials were adopted to describe the effects of their ionic cores. For geometry optimization, we fully relaxed the systems until the Hellmann-Feynman forces were less than 7.3510-5 Ry/Å. After optimizing the bulk systems, the (0 0 1) surface was cleaved, followed by the construction of a more than 25 Å vacuum layer added to the unit cell of the layers to simulate periodic boundary conditions. The cut-off energy was chosen to be 44 Ry. The convergence criterion of energy in relaxation was set to be 7.3510-8 Ry. The k-grids were adopted 6  6  6, 6  6  6, 4  4  4 and 1  1  1 for HgSe, PbSe, MAPbI3 bulk and [001] HgSe/PbSe/MAPbI3 heterostructure, respectively. The formation energy of PbSe is Ef=EPbSe−EPb−ESe and that of MAPbI3 (CH3NH3PbI3) is Ef=(EMAPbI3−EPb−3EI−EC−EN−6EH)/12, where EMAPbI3, EPbSe, EPb, ESe, EN, EC, EH and EI are total energies of MAPbI3 and PbSe system, the isolate Pb, Se, N, C, H and I in the same slab, respectively. The calculated lattice mismatch of HgSe (cubic, a = 6.085 Å) and PbSe (cubic, a = 6.106 Å) is 0.4%, enabling the heteroepitaxy between PbSe and HgSe. The lower formation energy of PbSe than MAPbI3 (PbSe: -0.57 eV; MAPbI3: -0.47 eV) allows preferential growth of PbSe. In addition, PbSe and MAPbI3 (cubic, a = 8.647 Å) are also well matched by a 45° in-plane rotation of the MAPbI3 with respect to the PbSe. In this case, the HgSe/PbSe intersection is with {001} HgSe and {001} PbSe planes, while the PbSe/MAPbI3 intersection is described by PbSe (001) || MAPbI3 (001); [110] PbSe || [100] MAPbI3; [-110] PbSe || [010] MAPbI3. The corresponding lattice calculated constant mismatch between them is 2.5%, enabling the heteroepitaxy between MAPbI3 and PbSe as well.

Fig. S1: TEM and EDS characterization of the OAm-capped HgSe CQDs. a, TEM image of pristine HgSe CQDs. b, c, EDS results for Hg (b) and Se (c).

2. AFM measurement of the CSS CQD film

Fig. S2: AFM image of CSS CQD film. The achieved root-mean-square (RMS) surface roughness is 0.63 nm, less than the diameter of a CQD.

3. Size statistics of CQDs

Fig. S3: Histograms of CQD sizes derived from TEM results. a, b, c, CQD diameter histograms of pristine HgSe (a), HgSe/PbSe (b), and HgSe/PbSe/MAPbI3 CSS (c). The statistical means are 4.5 nm, 5.1 nm, and 7.1 nm, respectively.

4. UPS characterization and analysis for CSS system

The UPS spectra are used to confirm the valence band and work function of OAm-capped and CSS CQD film. The work functions of OAm-capped and CSS CQD film were estimated to be 2.3 and 4.24 eV, according to the equation W=ℎν−Ecut, where ℎν=21.2 eV is the photon energy of He I light source. Their Fermi levels are 2.81 and 0.41 eV above the valence bands for OAm-capped and CSS CQD films, respectively.

Fig. S4: UPS spectra of OAm-capped and CSS CQD films. a, b, Valence band spectrum, and second electron cutoffs of the OAm-capped HgSe CQD film. c, d, Valence band spectrum, and second electron cutoffs of the CSS CQD film.

5. SEM images of CSS CQD photodetector

Fig. S5: SEM images of our device. a, b, Top and cross-sectional views of our device. The drain and source electrodes have an interdigital structure with 9 electrical channels of 20 μm length and 400 μm width. The CSS film thickness is ~120 nm.

6. Hall effect measurement of the CSS CQD film

Fig. S6: Schematic diagram of Hall effect measurement.

We applied the van der Pauw method to measure the Hall effect of the CSS CQD film, as shown in Fig. 6. The four electrodes are located at the corner edges of the square film, whose sizes are much smaller than that of the film.

(1) Resistivity

First, a constant current IAB is applied between A and B, and then a voltage VCD can be obtained between C and D. Thus, a resistance can be defined as:

|  | RAB,CD=VCDIAB | (S1) |
| --- | --- | --- |

Next, a constant current IBC is applied between B and C, and similarly, another voltage VDA can be obtained between D and A. Another resistance can be defined as:

|  | RBC,DA=VDAIBC | (S2) |
| --- | --- | --- |

The resistivity ρ and the above two resistances follow the equation:

|  | exp−πdρRAB,CD+exp−πdρRBC,DA=1 | (S3) |
| --- | --- | --- |

where d is the film thickness. We can solve this equation via introducing a symmetry factor f:

|  | ρ=πln2dRAB,CD+RBC,DA2f | (S4) |
| --- | --- | --- |

where f can be acquired using an interpolation method:

|  | coshln2f∙RAB,CDRBC,DA−1RAB,CDRBC,DA+1=12expln2f | (S5) |
| --- | --- | --- |

If the four electrodes are perfectly symmetrical, i.e. the two resistances are equal, we can obtain that f = 1.

(2) Hall coefficient

First, a constant magnetic field with an intensity of H is applied vertically across the film. Next, a constant current IAC is applied between A and C, and then a voltage VBD can be obtained between B and D. A Hall coefficient RH1 is defined as:

|  | RH1=VBDdIACH. | (S6) |
| --- | --- | --- |

Similarly, a constant current IBD is applied between B and D, and then a voltage VAC can be obtained between A and C. Another Hall coefficient RH2 is also defined as:

|  | RH2=VACdIBDH. | (S7) |
| --- | --- | --- |

If the film is with a good uniformity, the difference between the two coefficients should be within 10%. In this case, the true Hall coefficient is:

|  | RH=RH1+RH22. | (S8) |
| --- | --- | --- |

By continuously changing H within a certain range, a curve of Vd/I-H is obtained. According to Eqs. S6 and S7, Vd/I-H exhibits a linear trend with a slope of RH. Hence, RH can be obtained. When the slope is positive, the electrical conduction of the film is p-type, otherwise it is n-type.

(3) Carrier concentration

The majority carrier concentration n can be obtained by:

|  | n=1RHq. | (S9) |
| --- | --- | --- |

(4) Carrier mobility

When no magnetic field is applied, a resistivity ρ0 is obtained. Then the mobility can be obtained by:

|  | μ=RHρ0. | (S10) |
| --- | --- | --- |

7. Photoelectric signal irradiated by the square-wave modulated lasers

Figs. S7: a-c, Time-traced photocurrents of the CSS CQD photodetector irradiated by square-wave modulated lasers with different wavelengths and light power densities under different bias voltages (Vds).

8. Cyclical impulse responses of the CQD photodetector

Fig. S8: The cyclic pulse photoresponse irradiated by fs-pulse laser (with a pulse width of ~220 fs). a, irradiated by 400-800 nm fs-pulse laser; b, irradiated by 900-1800 nm fs-pulse laser.

9. Blackbody detection system

The blackbody response was measured using a cavity blackbody source (Infrared System, IR564/301) equipped with chopped modulation, a lock-in amplifier (SRS SR830), and a low-noise current pre-amplifier (SRS SR570). In this system, the bias voltage of the photodetector is applied by the SR570. The schematic of this measurement setup is shown below. Infrared radiation was emitted from the blackbody source with a chopped frequency of 1 kHz, and then incident on the photodetector. The photocurrent generated during the photoelectric conversion process was amplified successively by the SR570 and the SR830. The result obtained was finally read out from the SR830.

Fig. S9: The schematic image of blackbody detection system.

10. Measurement system for relative response spectra

The blackbody response was measured using a cavity blackbody source (Infrared System, IR564/301) equipped with chopped modulation, a lock-in amplifier (SRS SR830), and a low-noise current preamplifier (SRS SR570). In this system, the bias voltage of the photodetector is applied by the SR570. The schematic of this measurement setup is shown in Fig. S10. Infrared radiation was exited from the blackbody source with a chopped frequency of 1 kHz, and then irradiated onto the photodetector. Through a photoelectric conversion process, photocurrent was produced, and it was amplified by the SR570 and the SR830 successively. The obtained result was read out with the SR830 finally.

Fig. S10: The schematic image of relative response spectra system.

11. Discussion on the G factor

The G factor is defined as the ratio of the peak and blackbody responsivities. It can be expressed as:

|  | G=RλpRbb=0∞ϕ(λ)dλ0∞R(λ)ϕ(λ)dλ, | (S11) |
| --- | --- | --- |

where ϕ(λ) is the irradiation power spectrum of blackbody, R (λ) is the measured relative response spectrum.

12. Discussion on the 1/f noise

The low-frequency 1/f noise, also called flicker noise, is still not clearly understood in a photoconductors till nowadays. It is revealed that on spectral density of excess 1/f noise SI is decribed by empirical expression:

SI=BIαfβ

where B, I, ,  and f are the constant value, the DC bias current value, the coefficient ranged from 1.5 to 4.0, and another coefficient ranged from 0.8 to 1.5.

There are assumptions that 1/f noise in photoconductor devices is related to the fluctuation phenomena occurring at contact metal-semiconductor or at interface dielectric film

Fig. S11: The 1/f noise current under different biased voltages.

13. Performance comparison of our device with other uncooled VIS or IR CQD photodetectors

Table S1 Performance list for uncooled CQD photodetectors

| CQD Material | Type | Response range (μm) | D*p (cm∙Hz1/2/W) | tR (μs) | tP-R (μs) | Year/Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| HgTe | PV | 1.0-2.1 | 5.0 × 1010 | - | 0.3 | 2022/[2] |
| PbS | PV | 0.4-1.3 | 2.1 × 1012 | 1.1 | - | 2022/[3] |
| InAs | PV | 0.5-1.05 | 1.0 × 1011 | 0.001 | 0.002 | 2022/[4] |
| HgTe | PC | 0.8-2.5 | 1.5 × 1010 | 1 | - | 2022/[5] |
| HgTe | PC | 0.9-2.1 | 3.0 × 109 | - | - | 2023/[6] |
| PbS | PC | 0.55-1.0 | 4.7 × 109 | 1.1× 105 | - | 2023/[7] |
| HgTe | PT | 1.2-1.8 | 1.0 × 1010 | 0.74 | 2.2 | 2023/[8] |
| PbS | PT | 0.53-1.55 | 4.7 × 1010 | > 103 | - | 2023/[9] |
| InAs | PV | 0.5-1.1 | 1.9 × 1011 | 1.4 | - | 2023/[10] |
| HgTe | PV | 1.7-4.0 | 7.6 × 109 | - | - | 2023/[11] |
| Core-shell HgSe-MAPbI3 | PC | 0.33-0.85 | 2.8 × 1011 | 1.3 | 0.8 / 13.9 | This work |
|  |  | 0.85-2.5 | 8.4 × 1010 |  | 0.8 / 1.8 |  |
|  |  | 2.5-5.3 | 2.6 × 1010 |  |  |  |

PV, photovoltaic; PC, photoconductive; PT, phototransistor. All the listed D*p are characterized using uniformly-distributed large-spot light source.

14. Performance comparison of our device with other MWIR CQD photodetectors working at uncooled or cryogenic conditions

Table S2 Performance list for MWIR CQD photodetectors

| CQD Material | Type | Top (K) | λp / λcut-off (μm) | D*p (cm∙Hz1/2/W) | tR (μs) | NETD (mK) | Year/Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Core-shell HgSe-HgTe | PV | 80 | 2 / 5 | 1.5 × 109 | 0.5 | 40 | 2019/[12] |
| HgTe | PV | 85 | 4.4 / 5.5 | 2 × 1010 | 1.6 | - | 2019/[13] |
|  |  | 295 | 2.4 / 4.1 | 1 × 107 |  |  |  |
| HgTe | PC | 80 | 2.2 / 4 | 7 × 1010 | 0.07 | - | 2022/[14] |
| HgTe | PC | 80 | 2.6 / 4 | 2 × 1010 | 11 | - | 2022/[15] |
| HgTe | PV | 80 | 2.6 / 3.3 | 1 × 1011 | 6.4 | 26.7 | 2022/[16] |
| HgTe | PV | 80 | 3.3 / 5 | 8 × 1010 | 0.2 | 36 | 2022/[17] |
| HgSe/HgTe | PC | 80 | 4.3 / 5 | 5.2 × 108 | 0.17 | - | 2022/[18] |
| HgSe | PC | 80 | 4 / 5.5 | 1.7 × 109 | 2 | - | 2022/[18] |
| HgTe | PV | 80 | 3.6 / 5 | 2.7 × 1011 | - | - | 2023/[19] |
| Core-shell HgSe-MAPbI3 | PC | 300 | 3.3 / 5.3 | 2.6 × 1010 | 1.3 | 39.1 | This work |

Top, operating temperature; λp, peak wavelength; λcut-off, cut-off wavelength.

15. Performance comparison of our device with uncooled state-of the art IR detectors

Table S3 Performance list for uncooled state-of-the-art IR detectors

| Company | Material | Type | λp (μm) | D*p (cm∙Hz1/2/W)/ NEP (W/Hz1/2) | tR (μs) | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| HAMAMATSU | InAs | PV | 3.35 | 4.5 × 109 | 0.7 | [20] |
|  | InAsSb | PV | 4.1 | 1.0 × 109 | 0.1 |  |
|  | Thermopile | Thermal | 3-5 | 1.3 × 108 | 2 × 104 |  |
| VIGO | InAs | PV | 2.9 | 5.0 × 109 | 0.04 | [21] |
|  | InAsSb | PV | 4.5 | 5.0 × 109 | 0.02 |  |
|  | HgCdTe | PC | 4.7 | 1.5 × 109 | 5 |  |
|  | HgCdTe | PV | 4.2 | 3.0 × 1010 | 0.15 |  |
| Thorlabs | Ge | PV | 1.55 | 2.6 × 10-12 | 0.6 | [22] |
|  | InGaAs | PV | 2.3 | 1.0 × 10-12 | 0.025 |  |
|  | HgCdTe | PV | 4.7 | 1.5 × 1010 | 0.12 |  |
| Opto Diode | PbS | PC | 2.4 | 1.0 × 1011 | 200 | [23] |
|  | PbSe | PC | 3.8 | 1.5 × 1010 | 2 |  |
| - | Core-shell HgSe-MAPbI3 | PC | 1.6 | 8.4 × 1010 / 3.2 × 10-13 | 1.3 | This work |
|  |  |  | 3.3 | 2.6 × 1010 |  |  |

NEP, noise equivalent power, expressed by NEP = Ad1/2/D*. For the Ge and InGaAs PV (SWIR) detectors produced by Thorlabs, NEP is used to evaluate their sensitivity performance. As listed in Table S3, our device is superior to them on NEP.

16. References

1	Giannozzi, P. et al. QUANTUM ESPRESSO: a modular and open-source software project for quantum simulations of materials. J. Phys.-Condens. Mat. 21, 395502 (2009).

2	Gréboval, C. et al. HgTe nanocrystal-based photodiode for extended short-wave infrared sensing with optimized electron extraction and injection. ACS Appl. Nano Mater. 5, 8602-8611 (2022).

3	Liu, J. et al. A near-infrared colloidal quantum dot imager with monolithically integrated readout circuitry. Nat. Electron. 5, 443-451 (2022).

4	Sun, B. et al. Fast near-infrared photodetection using III–V colloidal quantum dots. Adv. Mater. 34, 2203039 (2022).

5	Zhang, S. et al. Direct optical lithography enabled multispectral colloidal quantum-dot imagers from ultraviolet to short-wave infrared. ACS Nano 16, 18822-18829 (2022).

6	Grotevent, M. J. et al. Integrated photodetectors for compact Fourier-transform waveguide spectrometers. Nat. Photonics 17, 59-64 (2023).

7	Wu, D. et al. Flexible microcomb printed PbS quantum dot film enables scalable fabrication of near infrared photodetector. Adv. Optical Mater. 11, 2300945 (2023).

8	Sergeeva, K. A. et al. Obviating ligand exchange preserves the intact surface of HgTe colloidal quantum dots and enhances performance of short wavelength infrared photodetectors. Adv. Mater. 36, 2306518 (2024).

9	Kim, S.-H. et al. Sulfurized colloidal quantum dot/tungsten disulfide multi-dimensional heterojunction for an efficient self-powered visible-to-sWIR photodetector. Adv. Funct. Mater. 33, 2303778 (2023).

10	Xia, P. et al. Sequential Co-passivation in InAs colloidal quantum dot solids enables efficient near-Infrared photodetectors. Adv. Mater. 35, 2301842 (2023).

11	Xue, X. et al. High-operating-temperature mid-infrared photodetectors via quantum dot gradient homojunction. Light Sci. Appl. 12, 2 (2023).

12	Livache, C. et al. A colloidal quantum dot infrared photodetector and its use for intraband detection. Nat. Commun. 10, 2125 (2019).

13	Tang, X., Ackerman, M. M., Chen, M. & Guyot-Sionnest, P. Dual-band infrared imaging using stacked colloidal quantum dot photodiodes. Nat. Photonics 13, 277-282 (2019).

14	Dang, T. H. et al. Nanocrystal-based active photonics device through spatial design of light-matter coupling. ACS Photonics 9, 2528-2535 (2022).

15	Dang, T. H. et al. Broadband enhancement of mid-wave infrared absorption in a multi-resonant nanocrystal-based device. Adv. Optical Mater. 10, 2200297 (2022).

16	Zhang, S. et al. Spray-stencil lithography enabled large-scale fabrication of multispectral colloidal quantum-dot infrared detectors. Adv. Mater. Technol. 7, 2101132 (2022).

17	Zhang, S. et al. Single-/fused-band dual-mode mid-infrared imaging with colloidal quantum-dot triple-junctions. Photonics Res. 10, 1987-1995 (2022).

18	Khalili, A. et al. Guided-mode resonator coupled with nanocrystal intraband absorption. ACS Photonics 9, 985-993 (2022).

19	Chen, M., Hao, Q., Luo, Y. & Tang, X. Mid-infrared intraband photodetector via high carrier mobility HgSe colloidal quantum dots. ACS Nano 16, 11027-11035 (2022).

20	Hamamatsu photonics. http://www.hamamatsu.com.cn. (2024)

21	VIGO photonics. https://vigophotonics.com/. (2024)

22	Thorlabs, Inc. http://thorlabs.com. (2024)

23	Opto Diode, Corp. https://optodiode.com. (2024)