[Supplementary Materials]

Superconductivity in bcc-selenium under megabar pressure

Zhongyan Wu1, Timofey Fedotenko2, Nico Giordano2, Jaeyong Kim1

1Department of Physics, Institute for High Pressure, Hanyang University, Seoul 04763, Korea

2Deutsches Elektronen-Synchrotron DESY, Notkestr. 85, Hamburg 22607, Germany

Table S1. Lattice parameters at different pressures. The atomic volume of each phase decreases monotonically with pressure (negative linear compressibility).

| P (GPa) | a (Å) | b (Å) | c (Å) | α (°) | β (°) | γ (°) | V (Å3) | q | V/atom (Å3) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Se(I), trigonal, P3121 |  |  |  |  |  |  |  |  |  |
| 5.4 | 3.91553 |  | 5.06546 |  |  |  | 67.256 |  | 22.41867 |
| 7.4 | 3.8663 |  | 5.0333 |  |  |  | 65.159 |  | 21.71967 |
| 10.9 | 3.74659 |  | 5.01689 |  |  |  | 60.987 |  | 20.329 |
| Se (II), triclinic, P-1 |  |  |  |  |  |  |  |  |  |
| 10.9 | 2.79533 | 3.70778 | 6.29443 | 102.558 | 92.705 | 112.169 | 58.364 |  | 19.45467 |
| (H2Se)2H2, tetragonal, I4/mcm |  |  |  |  |  |  |  |  |  |
| 10.9 | 6.868 |  | 5.801 |  |  |  | 273.643 |  | 34.20537 |
| 19.4 | 6.666 |  | 5.70234 |  |  |  | 253.387 |  | 31.67338 |
| Se (III), triclinic, P-1 |  |  |  |  |  |  |  |  |  |
| 19.4 | 2.68027 | 3.58732 | 6.23503 | 103.981 | 89.556 | 112.909 | 53.335 |  | 17.77833 |
| 21.4 | 2.67216 | 3.5062 | 6.24964 | 102.379 | 93.706 | 111.97 | 52.357 |  | 17.45233 |
| 25.9 | 2.62348 | 3.42615 | 6.27639 | 102.258 | 93.741 | 111.996 | 50.459 |  | 16.81967 |
| Se (IV), body-centered modulated monoclinic, I'2/m(0q0)s0 |  |  |  |  |  |  |  |  |  |
| 30.4 | 3.3675 | 4.01664 | 2.60019 |  | 112.597 |  | 32.47 | 0.3062 | 16.235 |
| 35.4 | 3.30912 | 4.01401 | 2.59121 |  | 112.778 |  | 31.734 | 0.306 | 15.867 |
| 40.9 | 3.24871 | 4.0134 | 2.56893 |  | 112.851 |  | 30.866 | 0.3075 | 15.433 |
| 45.4 | 3.20822 | 3.9949 | 2.55242 |  | 113.041 |  | 30.104 | 0.308 | 15.052 |
| 50.6 | 3.16453 | 3.99519 | 2.52996 |  | 113.125 |  | 29.338 | 0.3078 | 14.669 |
| 53.9 | 3.14491 | 3.99004 | 2.52984 |  | 113.576 |  | 29.095 | 0.3131 | 14.5475 |
| 57.9 | 3.12804 | 3.97168 | 2.53407 |  | 114.209 |  | 28.714 | 0.2969 | 14.357 |
| 63.4 | 3.10793 | 3.98139 | 2.50832 |  | 113.741 |  | 28.411 | 0.2969 | 14.2055 |
| 67.9 | 3.09446 | 3.95003 | 2.49776 |  | 113.298 |  | 28.041 | 0.2941 | 14.0205 |
| 71.9 | 3.08576 | 3.94048 | 2.48895 |  | 113.507 |  | 27.752 | 0.2927 | 13.876 |
| Se (V), primitive rhombohedral, R-3m |  |  |  |  |  |  |  |  |  |
| 67.9 | 3.96012 |  | 3.06799 |  |  |  | 41.668 |  | 13.88933 |
| 71.9 | 3.95053 |  | 3.04518 |  |  |  | 41.158 |  | 13.71933 |
| 77.4 | 3.93682 |  | 3.02237 |  |  |  | 40.567 |  | 13.52233 |
| 79.4 | 3.9275 |  | 3.0092 |  |  |  | 40.199 |  | 13.39967 |
| 80.4 | 3.92308 |  | 3.00226 |  |  |  | 40.016 |  | 13.33867 |
| 83.4 | 3.91407 |  | 2.98783 |  |  |  | 39.641 |  | 13.21367 |
| 85.4 | 3.90589 |  | 2.97555 |  |  |  | 39.313 |  | 13.10433 |
| 87.9 | 3.89578 |  | 2.96147 |  |  |  | 38.925 |  | 12.975 |
| 91.9 | 3.89068 |  | 2.95231 |  |  |  | 38.703 |  | 12.901 |
| 96.4 | 3.88124 |  | 2.9384 |  |  |  | 38.334 |  | 12.778 |
| 97.9 | 3.87623 |  | 2.93033 |  |  |  | 38.13 |  | 12.71 |
| 100.4 | 3.87042 |  | 2.92091 |  |  |  | 37.894 |  | 12.63133 |
| 101.9 | 3.86478 |  | 2.91191 |  |  |  | 37.667 |  | 12.55567 |
| 104.4 | 3.85879 |  | 2.90312 |  |  |  | 37.437 |  | 12.479 |
| 107.4 | 3.85113 |  | 2.89004 |  |  |  | 37.12 |  | 12.37333 |
| 110.4 | 3.83971 |  | 2.87136 |  |  |  | 36.662 |  | 12.22067 |
| 114.4 | 3.83451 |  | 2.86036 |  |  |  | 36.423 |  | 12.141 |
| 117.4 | 3.82808 |  | 2.85128 |  |  |  | 36.185 |  | 12.06167 |
| 120.9 | 3.82343 |  | 2.84145 |  |  |  | 35.973 |  | 11.991 |
| 124.9 | 3.82015 |  | 2.83158 |  |  |  | 35.786 |  | 11.92867 |
| 126.8 | 3.81474 |  | 2.82427 |  |  |  | 35.593 |  | 11.86433 |
| 128.9 | 3.81442 |  | 2.81019 |  |  |  | 35.41 |  | 11.80333 |
| 131.4 | 3.81886 |  | 2.78767 |  |  |  | 35.147 |  | 11.71567 |
| 133.9 | 3.82291 |  | 2.76581 |  |  |  | 35.006 |  | 11.66867 |
| 137.4 | 3.82679 |  | 2.73563 |  |  |  | 34.694 |  | 11.56467 |
| 137.9 | 3.83529 |  | 2.72047 |  |  |  | 34.655 |  | 11.55167 |
| 139.4 | 3.83815 |  | 2.70263 |  |  |  | 34.48 |  | 11.49333 |
| 140.9 | 3.84284 |  | 2.6863 |  |  |  | 34.355 |  | 11.45167 |
| 145.4 | 3.84527 |  | 2.66945 |  |  |  | 34.183 |  | 11.39433 |
| 146.4 | 3.84747 |  | 2.65822 |  |  |  | 34.078 |  | 11.35933 |
| 148.4 | 3.84808 |  | 2.64699 |  |  |  | 33.945 |  | 11.315 |
| 150.4 | 3.85224 |  | 2.64001 |  |  |  | 33.928 |  | 11.30933 |
| 154.9 | 3.85026 |  | 2.63165 |  |  |  | 33.786 |  | 11.262 |
| 155.4 | 3.84833 |  | 2.62546 |  |  |  | 33.673 |  | 11.22433 |
| 156.9 | 3.84812 |  | 2.61879 |  |  |  | 33.584 |  | 11.19467 |
| 157.9 | 3.84822 |  | 2.61366 |  |  |  | 33.52 |  | 11.17333 |
| Se (VI), body-centered cubic, Im-3m |  |  |  |  |  |  |  |  |  |
| 133.9 | 2.83953 |  |  |  |  |  | 22.895 |  | 11.4475 |
| 137.4 | 2.83492 |  |  |  |  |  | 22.784 |  | 11.392 |
| 137.9 | 2.83481 |  |  |  |  |  | 22.781 |  | 11.3905 |
| 139.4 | 2.83378 |  |  |  |  |  | 22.756 |  | 11.378 |
| 140.9 | 2.82848 |  |  |  |  |  | 22.629 |  | 11.3145 |
| 145.4 | 2.82502 |  |  |  |  |  | 22.546 |  | 11.273 |
| 146.4 | 2.82357 |  |  |  |  |  | 22.511 |  | 11.2555 |
| 148.4 | 2.82042 |  |  |  |  |  | 22.436 |  | 11.218 |
| 150.4 | 2.81784 |  |  |  |  |  | 22.374 |  | 11.187 |
| 154.9 | 2.81526 |  |  |  |  |  | 22.313 |  | 11.1565 |
| 155.4 | 2.81386 |  |  |  |  |  | 22.28 |  | 11.14 |
| 156.9 | 2.8119 |  |  |  |  |  | 22.233 |  | 11.1165 |
| 157.9 | 2.80904 |  |  |  |  |  | 22.165 |  | 11.0825 |
| 159.4 | 2.80665 |  |  |  |  |  | 22.109 |  | 11.0545 |
| 161.4 | 2.80357 |  |  |  |  |  | 22.036 |  | 11.018 |
| 163.9 | 2.8001 |  |  |  |  |  | 21.954 |  | 10.977 |
| 165.4 | 2.79667 |  |  |  |  |  | 21.874 |  | 10.937 |
| 168.4 | 2.7938 |  |  |  |  |  | 21.806 |  | 10.903 |
| 170.4 | 2.7908 |  |  |  |  |  | 21.736 |  | 10.868 |
| 173.4 | 2.78645 |  |  |  |  |  | 21.635 |  | 10.8175 |
| 175.9 | 2.78252 |  |  |  |  |  | 21.543 |  | 10.7715 |
| 178.9 | 2.78046 |  |  |  |  |  | 21.496 |  | 10.748 |
| 182.4 | 2.77329 |  |  |  |  |  | 21.33 |  | 10.665 |

FIG. S1(a). Sample images as upon compression at low pressure before measurement.

FIG. S1(b). Pressure calibration through the Raman shift of H2 vibron.

FIG. S2. (a)-(f) Pyrometry spectra measured during laser heating, the yellow and orange boxes are ROI for temperature measurement. Only the upstream side was successfully heated from the observation of a single bright stripe. (g) Representative plank fit for temperature estimation (sixth heating, ~3000 K) using T-Rax program. (h) Comparison of XRD patterns before and after laser heating.

FIG. S3. XRD mapping after laser heating at 102 GPa with grid size of 34 × 34 μm (17 × 17, 2 μm step, 2 μm beam size). (a) Microscope photo taken at the beamline; the red dash square indicates the mapping region. (b)-(c) Scanning X-ray diffraction images counting on the main peak of Se (101) and Pt (111), respectively. The peak intensity is indicated by bright (strong) and dark (weak) color. (d) Batch view of total 289 XRD data, the yellow and red lines mark the peaks of β-Po Se and Pt, respectively. The peak shift is due to the pressure gradient across the diamond culet. The pressure difference of sample at different positions is within ~7 GPa according to the equation of states of Pt. (e) Le Bail Refinement at the center position.

FIG. S4(a). Superconductivity under external magnetic field at different pressures. As increasing magnetic field at 132 GPa, the temperature difference of the overlapped Tp and Tc (transition width) increases, thus the bump turns into giant peak again.

FIG. S4(b). Critical magnetic field fitted by parabolic (red curve) μ0HcT=μ0Hc0(1-(TTC)2) and Ginzburg-Landau formula (blue) μ0HcT=μ0Hc0(1-(TTC)2)(1+(TTC)2), respectively.

FIG. S4(c). Estimation of μ0Hc0 by parabolic (square) and Ginzburg-Landau (circle) fitting over the studied pressure range.

FIG. S5. Representative Le Bail refinement for different phases of Se. The black dots, red lines, and blue lines are experimental data, Le Bail refinement, and residues, respectively.