The Anisotropic Self-Assembly Effect of Silica Hairy Nanoparticles:

toward Sustainable Rubber Nanocomposites for Tyre Application

Barbara Di Credico,a,*Laura Tripaldi,a,§ Luciano Tadiello,b Lucia Conzatti,c Massimiliano D’Arienzo,a Luca Giannini,b Silvia Mostoni, a Andrea Causa,b Paola Stagnaro,c and Roberto Scottia

a Dept. of Materials Science, INSTM, University of Milano-Bicocca, Via R. Cozzi, 55, 20125 Milano, Italy. Tel: +39-02-64485189; e-mail: barbara.dicredico@unimib.it

b Pirelli Tyre SpA, Viale Sarca, 222, 20126 Milano, Italy

c Istituto di Scienze e Tecnologie Chimiche (SCITEC) "G. Natta", Consiglio Nazionale delle Ricerche (CNR), Via De Marini 6, 16149 Genova, Italy

§ first author equal contribution

Keywords: silica, hairy nanoparticles, rubber nanocomposites, rolling resistance, green tyre

S1. Synthesis of SiO2 and SiO2-APTES

For the synthesis of the SiO2 core, 62.5 mL of ammonium hydroxide solution (25 wt% in H2O) and 1250 mL of ethanol were added to a 2000 mL two-necked flask equipped with a reflux condenser. The mixture was stirred at 300 revolutions per minutes (rpm) and heated to 60 °C. A mixture of 31.2 mL of TEOS and 35.0 mL of ethanol was added dropwise in about 50 min. After 20 h, the SiO2 NPs (labelled SiO2-ST) were separated by centrifugation, washed with EtOH and redispersed in 125 mL of EtOH. The suspension of SiO2-ST was then heated at reflux under stirring at 300 rpm with 50 µL of 25 wt% of NH4OH and 0.799 mL of APTES. After 24 h, the NPs (labelled SiO2-APTES) were centrifuged and washed with toluene, then redispersed in 120 mL of toluene.

Figure S1. TGA curves of silica fillers showing weight loss between 150 °C and 1000 °C.

Figure S2. TEM images of SiO2-HNP_X samples.

Table S1. Vulcanization properties of V-SiO2-HNP_X/SBR NCs compared with reference materials.

| Sample | ts2 (min) | ML (dNm) | MH (dNm) | DMH-ML (dNm) |
| --- | --- | --- | --- | --- |
| SiO2-ST/SBR | 5 | 2.1 | 9.0 | 6.9 |
| SiO2-APTES/SBR | 4 | 2.2 | 11.5 | 9.3 |
| SiO2-HNP_3/SBR | 5 | 2.4 | 10.8 | 8.4 |
| SiO2-HNP_4/SBR | 5 | 1.8 | 13.6 | 11.8 |
| SiO2-HNP_6/SBR | 5 | 2.0 | 11.8 | 9.8 |

Figure S3. Storage modulus G' vs strain of uncured SiO2-HNP_X/SBR NCs compared with reference materials.