Supporting information

Hybrid polyimide foams with hyperbranched organosilicon for high-temperature sound absorption

Yang Xu1, Luwei Bo1, Yandong Wang1, Haocheng Xu1, Xiaolin Jiang1, Zhaobo Wei1, Kai Xi*,1

Corresponding author: Kai Xi, *E-mail address: xikai@nju.edu.cn

1 MOE Key Laboratory of High-Performance Polymer Materials and Technology School of Chemistry and Chemical Engineering, Nanjing University, Nanjing, Jiangsu 210023, China

Fig S1 the synthesis route of NH2-HBPSi

Table S1 the specific ratios of various PEAS

|  | ODA/mol | NH2-HBPSi/mol | BTDA/mol | CH3OH/mol | THF/mol |
| --- | --- | --- | --- | --- | --- |
| PAES | 0.1 | - | 0.1 | 1 | 0.5 |
| PEASHBPSi-1 | 0.0889 | 0.0111 | 0.1 | 1 | 0.5 |
| PEASHBPSi-2 | 0.0857 | 0.0143 | 0.1 | 1 | 0.5 |
| PEASHBPSi-3 | 0.08 | 0.02 | 0.1 | 1 | 0.5 |
| PEASHBPSi-4 | 0.0667 | 0.0333 | 0.1 | 1 | 0.5 |

Fig S2 (a) FTIR spectra of NH2-HBPSi (b) 1H NMR spectra of NH2-HBPSi (c) the 13C NMR spectra of NH2-HBPSi (d) 29Si NMR spectra of NH2-HBPSi

Fig S3 storage modulus of PAESs with diverse NH2-HBPSi

Fig S4 The average cell diameters of different PIFs (a) PIFHBPSi-1 (b) PIFHBPSi-2 (c) PIFHBPSi-3 (d) PIFHBPSi-4

Fig S5 (a) the plot of strain-stress at a strain of 10% for PIF (b) the plot of strain-stress at a strain of 10% for PIFHBPSi-1 (c) the plot of strain-stress at a strain of 10% for PIFHBPSi-2 (d) the plot of strain-stress at a strain of 10% for PIFHBPSi-3

Table S2 the characteristic thermal analysis data of various PIFs

| Samples | N2 atmosphere |  |  |  | Air atmosphere |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | T5%(℃) | Tmax(℃) | R1000 (%) | T5%(℃) |  | Tmax(℃) | R1000(%) |
| PIF | 553.08 | 577 | 54.65 | 501.16 |  | 606 | 0 |
| PIFHBPSi-1 | 540.1 | 594 | 55.68 | 499.2 |  | 599 | 3.59 |
| PIFHBPSi-2 | 538.2 | 593 | 56.85 | 501.2 |  | 611.2 | 4.72 |
| PIFHBPSi-3 | 537.1 | 595 | 57.10 | 494.1 |  | 597 | 5.61 |
| PIFHBPSi-4 | 521.08 | 591 | 59.42 | 477.2 |  | 613.1 | 12.44 |

Fig S6 The DTG of various PIFs (a) N2 atmosphere (b) air atmosphere

Table S3 LOI and cone calorimetric data for various PIFs

| Sample | LOI (%) | THR (kJ/g) | PHRR (W/g) | TSP (m2) | Residue (%) |
| --- | --- | --- | --- | --- | --- |
| PIF | 39.2 | 12.07 | 50.74 | 0.11 | 0.21 |
| PIFHBPSi-1 | 40.3 | 10.95 | 54.24 | 0.12 | 4.59 |
| PIFHBPSi-2 | 44.1 | 8.60 | 47.5 | 0.14 | 6.21 |
| PIFHBPSi-3 | 44.5 | 7.76 | 46.17 | 0.19 | 6.51 |
| PIFHBPSi-4 | 45.9 | 17.11 | 62.97 | 0.22 | 21.2 |

Fig S7 SEM and EDX images of various PIFs after the cone calorimeter PIF (a) PIF (b) PIFHBPSi-1 (c) PIF HBPSi-2 (d) PIF HBPSi-3 (e) PIF HBPSi-4