Supplementary Information

CRISPR-Cas9 Activated Graphene Biointerfaces for Capture and Real-Time Monitoring of Cell-Free DNA on a Microneedle Patch

Bin Yang, Xueen Fang , Jilie Kong

Department of Chemistry and Institutes of Biomedical Sciences, Fudan University, Shanghai, 200433, PR China

Part A: Supplementary Note

Supplementary Note 1. Theory for the wearable device signal output.

According to the reference,[1] the electrolyte in the solution formed a Debye layer on the surface of the graphene biointerfaces, and it was a well-organized layer that could offset the difference in charge between the surface and the bulk solution. Then, Donnan potential occurred when the ion permeable layer separated two kinds of ions, as depicted in following Nernst formula equation 1,

(1),

where rD referred to Donnan equilibrium constant.

For an as-prepared CRISPR electrode, there were two phases in the system: CRISPR containing dRNP and target DNA on graphene, epidermis microenvironment containing electrolytes. The immobilized compound layer of graphene, proteins, sgRNA, and nucleic acids separated the graphene channel and double-layer from the epidermis microenvironment. The charge that generated a net charge in an immobilized ion-permeable layer required additional accumulation of counter ions to maintain charge neutrality. Thus, the difference between the epidermis microenvironment and the immobilized ion permeation layer produced the Donnan potential, as depicted in following equation 2,

(2),

where Cs, CCRISPR referred to the epidermis microenvironment and immobilized layers, respectively.

Supplementary Note Figure 1 Schematic of Donnan potential in the wearable system.

Part B: Supplementary Figure Ss

Supplementary Figure S1. Verification for the wearable device signal output.

Figure S1 Verification for the wearable device signal output. (a) CV plot for the as-prepared CRISPR micro-electrode without EBV CfDNA, scanning rate of 0.05 V/s, sampling interval of 0.001 V. (b) CV plots for CRISPR micro-electrode under different concentration of EBV CfDNA, scanning rate of 0.05 V/s, sampling interval of 0.001 V. (c) Peak 1 current of CV plots under different conditions. (d) Integration area of CV plots under different conditions. From the data, when the as-prepared CRISPR micro-electrode was dipped in to PBS buffer (0.01 M, pH 7.4), a characteristic peak 1 around -0.1 V was observed. Due to Donnan potential, the peak 1 current increased, as the concentration of EBV CfDNA increased. Additionally, the integration area increased, as the concentration of EBV CfDNA increased, indicating that the immobilized layer had a well-defined capacitance and electrochemical performance. All the data was analyzed by Origin software. Thus, we chose the initial potential of -0.1 V for the subsequence real-time monitoring experiments.

Supplementary Figure S2. Optimization and screening for sgRNA targeting to EBV CfDNA.

Figure S2 Optimization and screening for sgRNA targeting to EBV CfDNA. (a) Schematic for CRISPR-Cas9 gene editing to EBV CfDNA. (b) Comparison of two types of sgRNA. According to reference,[2,3] truncated sgRNA (+40) has a relative low efficiency for gene editing. It was validated by PAGE gel results in this study. We found that a complete sgRNA show high efficiency for EBV CfDNA gene editing. (c) Efficiency for four complete sgRNA. (d) Reproducibility of the CRISPR-Cas9 targeting to EBV CfDNA. (e) PAGE gel of sgRNA/Cas9 targeting to EBV CfDNA by variable amount, 0, 1, 2 referring to 0×, 1×, 2×sgRNA/Cas. (f) Region of interest intensity from the PAGE gel of sgRNA/Cas9 targeting to EBV CfDNA by variable amount, 0, 1, 2 referring to 0×, 1×, 2×sgRNA/Cas9 respectively.

Supplementary Figure S3. Construction for CRISPR microelectrode.

Figure S3 Construction for CRISPR microelectrode. The method was similar to CRISPR microneedles construction other than 1-pyrenebutanoic acid (PBA). PBA was stacked on graphene via π-π aromatic stacking.

Supplementary Figure S4 Validation for CRISPR-powered strategy.

Figure S4 Validation for CRISPR-powered strategy. Curve I and II referring to micro-electrode after modified graphene and PBA, graphene and PBA modified micro-electrode targeting to 2×10-11 M EBV CfDNA, respectively. In order to test if the non-specific adsorption and physical adsorption of DNA exerts impact on the signal output, PBA was modified on the graphene electrode, and incubated in a certain concentration of EBV CfDNA solution at 37°C for 20 min. The interface was washed with distilled water for 5 minutes, and finally CV was scanned using 0.05 M [Fe(CN)6]3–/4–. As shown, the two curves had hardly obvious change in current and peak deviation. This further showed that EBV CfDNA was recognized and captured by the interface through the CRISPR-driven reaction for gene editing.

Supplementary Figure S5 Optimization for end-point CRISPR reaction time on a microelectrode.

Figure S5 Optimization for CRISPR reaction time on a microelectrode. Under the above preliminary conditions, the reaction time of CRISPR-Cas9 was optimized. EBV CfDNA as the target to explore the changes in the electrode interface, using 0.05 M [Fe(CN)6]3–/4– electrochemical probe. As shown, it is found that as the CRISPR reaction proceeded, the resistance of the electrode surface continues to increase, and the current value continued to decrease. This may be due to the fact that the spatial conformation of the dCas9 protein changed with the CRISPR reaction, affecting the electron transfer and conductivity of the electrode interface. It can be seen that the CRISPR reaction became faster from 30 minutes, and after 60 minutes, the current value remained basically stable, so we chose 60 minutes as the optimized end-point reaction time for micro-electrode.

Supplementary Figure S6 End-point CRISPR microelectrode for quantitative detection of EBV CfDNA.

Figure S6 End-point CRISPR microelectrode for quantitative detection of EBV CfDNA. (a) Dynamic curves for different concentration of EBV CfDNA, I to V referring to 0, 1×10-9 M, 1×10-10 M, 1×10-11 M, 1×10-12 M. (b) Calibration curve. A linear relationship was observed between the change in current and EBV CfDNA concentration in the range of 1 nM-1 pM with the equation: ΔI (μA)=0.7107·lgC+1.0488 (R=0.9836), with a detection limit of 1 pM (DL = 3δb/K).

Supplementary Figure S7 EIS for CRISPR microelectrode.

Figure S7 EIS for CRISPR micro-electrode. (a) Real-time EIS curve under reverse iontophoresis, using 0.05 M [Fe(CN)6]3–/4– electrochemical probe, step 1-4 referring to monitoring of 3×10-12 M EBV CfDNA, rinse 1 by TE buffer (37 °C，pH 8.0), monitoring of 3×10-11 M EBV CfDNA, rinse 2 by TE buffer (37 °C，pH 8.0). (b) Simulation of EIS curve for 30-min time point. (c) Simulation results of the CRISPR micro-electrode capacitance performance. The 30-min group had a CPE value of 0.8466 (RSD=0.8364%). Three groups at different time point showed a CPE value over 0.5. These results evidently showed that the CRISPR sensitive membrane on the micro-electrode had a well-defined capacitance.

Supplementary Figure S8 Construction and optimization for conductive microneedles.

Figure S8 Construction and optimization for conductive microneedles. (a) Schematic of the conductive microneedles process. (b) SEM result of the microneedles modification. The optimized concentration of Cr and graphene was 0.5 mg/mL and 0.2 mg/mL respectively. According to the equation d=KIVT, a theoretical thickness of Au spurring was 102 nm under the optimized condition (600 s, 10 mA, argon). (c) Stylus profiler for Cr+Au (I) and Au (II) functionalized membrane, 0.05 mg loading force, 0.1 mm/s scanning speed. (d) Comparison of different shape microneedles in mechanical performance. I to VIII referring to schematic of two types, type A before compression test, type A after compression test (60 N), type B before compression test, type B after compression test (6 N), different loading (20 N, 40 N, 60 N) for type A, 4 N loading for type B. These results showed that shape, height, and base diameter had of microneedles had impact on its rigidity, stiffness, and penetration ability.

Supplementary Figure S9 SEM for graphene/chitosan membrane.

Figure S9 SEM for graphene/chitosan membrane.

Supplementary Figure S10 Mice bearing CNE-Luc cell under real-time monitoring.

Figure S10 Mice bearing CNE-Luc cell under real-time monitoring, left: optical photograph, right: schematic photograph.

Supplementary Figure S11 Results of other three independent methods.

Figure S11 Results of other three independent methods.

Part C: Supplementary Table Ss

Table S1 CRISPR-Cas MNs compared with other MNs method in the field of chem-biosensing.

| Strategy | Analyte | Function | Time | Real-time (Y/N) | Conductive (Y/N) | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| Wearable array | Opioid and organophosphate | Detection | ~200 min | Y | Y | [4] |
| Stainless steel MNs | Caffeine and glucose in ISF | Sampling | ~20 min | N | Y | [5] |
| Gelatin methacryloyl MNs | Glucose and vancomycin in ISF | Sampling | ~10 min | N | N | [6] |
| MNs detection system | Glucose and lactate | Detection | 300 min | Y | Y | [7] |
| Alginate-peptide MNs | MicroRNA | Sampling and detection | 2 min | N | N | [8] |
| PVA MNs | Phytophthora infestans DNA | Sampling | ~1 min | N | N | [9] |
| Photonic crystal-MNs | Inflammatory cytokines in ISF | Sampling and detection | ~40 min | N | N | [10] |
| SERS MNs | pH level in ISF | Detection | NG | N | N | [11] |
| MNs based on near-infrared quantum dots | Vaccine | Detection | 2-5 min | N | N | [12] |
| rGO-assemble MNs | H2O2 | Detection | ~5 min | Y | Y | [13] |
| Potentiometric MNs | K+ | Detection | 1440 min | Y | Y | [14] |
| MNs-based biosensor | Lactate | Detection | 15 min | Y | Y | [15] |
| SERS MNs array | Glucose | Detection | 15 min | N | N | [16] |
| Wearable electrochemical MNs | Levodopa | Detection | 1 min | Y | Y | [17] |
| MNs-based Sensor | β-lactam antibiotic | Detection | ~330 min | Y | Y | [18] |
| Porous MNs array | Glucose | Sampling, detection, and drug delivery | ~60 min | Y | Y | [19] |
| CRISPR-Cas MNs | EBV CfDNA | Sampling and detection | ~30 min | Y | Y | This work |

Table S2 Nucleic acid sequences in the experiments.

|  | Sequence (5’ - 3’) |
| --- | --- |
| RNA 1 | CCCGCCUCCAGGCGCCCUCCGUUUUAGAGCUAGAAAUAGCAAGUUAAAAUAAGGCUAGUCCGUUAUCAACUUGAAAAAGUGGCACCGAGUCGGUGCUUUU |
| RNA 2 | CCCGCCTCCAGGCGCCCUCCGUUUUAGAGCUAGAAAUAGCAAG |
| RNA 3 | UUCAGAGGAACCAGGGACCUGUUUUAGAGCUAGAAAUAGCAAG |
| RNA 4 | GAGAGGGGCAGAACCAACCCGUUUUAGAGCUAGAAAUAGCAAGUUAAAAUAAGGCUAGUCCGUUAUCAACUUGAAAAAGUGGCACCGAGUCGGUGCUUUU |
| RNA 5 | UAAACCCAAAGAAUGUCUGAGUUUUAGAGCUAGAAAUAGCAAGUUAAAAUAAGGCUAGUCCGUUAUCAACUUGAAAAAGUGGCACCGAGUCGGUGCUUUU |
| RNA 6 | AGACAUUCUUUGGGUUUAACGUUUUAGAGCUAGAAAUAGCAAGUUAAAAUAAGGCUAGUCCGUUAUCAACUUGAAAAAGUGGCACCGAGUCGGUGCUUUU |
| EBV plus | TTCCCTCCTTTTGTAAACAATGCATTCATCGACCTTCCAGCCGGGGTTGGTTCTGCCCCTCTCTCTGTCCTTCAGAGGAACCAGGGACCTCGGGCACCCCAGAGCCCCTCGGGCCCGCCTCCAGGCGCCCTCCTGGTCTCCGCTCCCCTCTGAGCCCCGTTAAACCCAAAGAATGTCTGAGGGGAGCCACCCTCGGGGCCCAGGCCCCAGAGTCACACATCCGACACAACAACAGCATTCTCCT |
| PCR F1 for EBV plus | TGTTGTTGTGTCGGATGTGT |
| PCR R1 for EBV plus | TTCCAGCCGGGGTTGGTTCT |
| PCR F2 for EBV plus | GTGTGACTCTGGGGCCTGGGCC |
| PCR R2 for EBV plus | CTCCTTTTGTAAACAATGCATT |
| PCR F3 for EBV plus | GTGTGACTCTGGGGCCTGGGCCCC |
| PCR R3 for EBV plus | CCCTCCTTTTGTAAACAATGCATT |
| PCR F primer for EBV primer | GGTTCTGCCCCTCTCTCTGTCC |
| PCR R primer for EBV | AGGGGAGCGGAGACCAGGAG |

Reference

[1] P. Bergveld, Biosens. Bioelectron. 1991, 6, 55.

[2] F. A. Ran, P. D. Hsu, J. Wright, V. Agarwala, D. A. Scott, F. Zhang, Nat. Protoc. 2013, 8, 2281.

[3] L. Cong, F. A. Ran, D. Cox, S. Lin, R. Barretto, N. Habib, P. D. Hsu, X. Wu, W. Jiang, L. A. Marraffini, F. Zhang, Science 2013, 339,819.

[4] R. K. Mishra, K. Y. Goud, Z. Li, C. Moonla, M. A. Mohamed, F. Tehrani, H. Teymourian, J. Wang, J. Am. Chem. Soc. 2020, 142, 5991.

[5] P. P. Samant, M. M. Niedzwiecki, N. Raviele, V. Tran, J. M. Lapaix, D. I. Walker, E. I. Felner, D. P. Jones, G. W. Miller, M. R. Prausnitz, Sci. Transl. Med. 2020, 12, eaaw0285.

[6] J. Zhu, X. Zhou, H. J. Kim, M. Qu, X. Jiang, K. Lee, L. Ren, Q. Wu, C. Wang, X. Zhu, P. Tebon, S. Zhang, J. Lee, N. Ashammakhi, S. Ahadian, M. R. Dokmeci, Z. Gu, W. Sun, A. Khademhosseini, Small 2020, 16, 1905910.

[7] H. Teymourian, C. Moonla, F. Tehrani, E. Vargas, R. Aghavali, A. Barfidokht, T. Tangkuaram, P. P. Mercier, E. Dassau, J. Wang, Anal. Chem. 2020, 92, 2291.

[8] D. A. Sulaiman, J. Y. H. Chang, N. R. Bennett, H. Topouzi, C. A. Higgins, D. J. Irvine, S. Ladame, ACS nano 2019, 13, 9620.

[9] R. Paul, A. C. Saville, J. C. Hansel, Y. Ye, C. Ball, A. Williams, X. Chang, G. Chen, Z. Gu, J. B. Ristaino, Q. Wei, ACS nano 2019, 13, 6540.

[10] X. Zhang, G. Chen, F. Bian, L. Cai, Y. Zhao, Adv. Mater. 2019, 31, 1902825.

[11] J. E. Park, N. Y. Tanyeri, E. V. Ende, A. I. Henry, B. E. P. White, M. Mrksich, R. P. V. Duyne, Nano Lett. 2019, 19, 6862.

[12] K. J. McHugn, L. Jing, S. Y. Severt, M. Cruz, M. Sarmadi, H. S. N. Jayawardena, C. F. Perkinson, F. Larusson, S. Rose, S. Tomasic, T. Graf, S. Y. Tzeng, J. L. Sugarman, D. Vlasic, M. Peters, N. Peterson, L. Wood, W. Tang, J. Yeom, J. Collins, P. A. Welkhoff, A. Karchin, M. Tse, M. Gao, M. G. Bawendi, R. Langer, A. Jaklenec, Sci. Transl. Med. 2019, 11, eaay7162.

[13] Q. Jin, H. J. Chen, X. Li, X. Huang, Q. Wu, G. He, T. Hang, C. Yang, Z. Jiang, E. Li, A. Zhang, Z. Lin, F. Liu, X. Xie, Small 2019, 15, 1804298.

[14] M. Parrilla, M. Cuartero, S. P. Sánchez, M. Rajabi, N. Roxhed, F. Niklaus, G. A. Crespo, Anal. Chem. 2019, 91, 1578.

[15] P. Bollella, S. Sharma, A. E. G. Cass, R. Antiochia, Biosens. Bioelectron. 2019, 123,152.

[16] J. Ju, C. M. Hsieh, Y. Tian, J. Kang, R. Chia, H. Chang, Y. Bai, C. Xu, X. Wang, Q. Liu, ACS Sens. 2020, 5, 1777.

[17] K. Y. Goud, C. Moonla, R. K. Mishra, C. Yu, R. Narayan, I. Litvan, J. Wang, ACS Sens. 2019, 4, 2196.

[18] S. A. N. Gowers, D. M. E. Freeman, U. M. Rawson, M. L. Rogers, R. C. Wilson, A. H. Holmes, A. E. Cass, D. O’Hare, ACS Sens. 2019, 4, 1072.

[19] S. Kusama, K. Sato, Y. Matsui, N. Kimura, H. Abe, S. Yoshida, M. Nishizawa, Nat. Commun. 2021, 12, 658.

fxech@fudan.edu.cn (X. E. Fang); jlkong@fudan.edu.cn (J. L. Kong);