Supporting Information

Hierarchical carbon nanofiber/NiCo2O4 composites as electrode for high-performance supercapacitors

Qiqi Zhuo, Yalou Lv, Hanzhao Wu, Jintian Jiang, Jijun Tang, Chao Yan*

College of Material Science & Engineering, Jiangsu University of Science and Technology, 2 Meng-Xi Road, Zhenjiang, Jiangsu, 212003, People’s Republic of China;

* Correspondence: chaoyan@just.edu.cn; Tel: +86-511-84408597

Table S1. The contact angle of pure CNFs and modified CNFs at different time.

| Samples | 0 min (°) | 5 min(°) | 10 min(°) | 15 min(°) |
| --- | --- | --- | --- | --- |
| Pure CNFs | 117.9 | 117.2 | 116.4 | 116.3 |
| KOH | 117.3 | 116.3 | 116.2 | 116.1 |
| HNO3 | 52.2 | 33.6 | 30.9 | 0 |
| H2SO4 | 113.1 | 112.6 | 110.8 | 110.2 |
| KMnO4 | 0 | 0 | 0 | 0 |
| H2O2 | 116.5 | 115.8 | 115.8 | 115.6 |

Figure S1. FTIR spectra of CNFs with different solvent treated.

Figure S2 CV curves of the CNFs-NCO electrode at different scan rates (a) CNFs-NCO1; (b) CNFs-NCO 2; (c) CNFs-NCO3; (d) CNFs-NCO5.

Figure S3 Charge/discharge curves of the CNFs-NCO electrode at different current density (a) CNFs-NCO1; (b) CNFs-NCO 2; (c) CNFs-NCO3; (d) CNFs-NCO5.