Supplementary Information

Scale-up synthesis of bioplastics polyglycolic acid from waste plastic polyethylene terephthalate

Yuxiang Wang1,2, Jiu Chen3, Edmund C. M. Tse3, Rui Shi1* & Yong Chen1,2*

Supplementary Scheme 1. Schematic diagram of the synthesis of Pd-CoCr2O4/NF.

Supplementary Figure 1. SEM images of Pd-CoCr2O4 at different resolutions.

Supplementary Figure 2. a) FTIR spectrum and b) Raman spectrum of CoCr2O4.

Supplementary Figure 3. Electron density difference of Pd/CoCr2O4(311). The isosurface is 0.008 e/Å3. Blue and yellow areas represent the electron depletion and electron accumulation, respectively.

Supplementary Figure 4. The Bode plots of the Pd-CoCr2O4/NF samples in 1 M EG and 1 M KOH.

Supplementary Figure 5. CV curves with different scan rates (from 10 mV/s to 90 mv/s) of a) Pd-CoCr2O4/NF, b) Pd/NF, c) Pd-Cr2O3/NF, and d) Pd-Co3O4/NF.

Supplementary Figure 6. The most stable structure of OH* on (a) Pd/Ni(111), (b) Pd/Cr2O3(104), (c) Pd/Co3O4(311), and (d) Pd/CoCr2O4(311).

Supplementary Figure 7. Calculated adsorption energies of OH– on the surfaces of Pd/Ni, Pd-Co3O4, Pd-Cr2O3, and Pd/CoCr2O4.

Supplementary Figure 8. The electrocatalytic stability of Pd/NF, Pd-Cr2O3, Pd-Co3O4, and Pd/CoCr2O4 at different bias in bath electrosynthesis.

Supplementary Figure 9. Raman spectra of Pd-CoCr2O4 before and after long-term electrolysis.

Supplementary Figure 10. Surface valence band photoemission spectra of Pd-CoCr2O4/NF and Pd/NF.

Supplementary Figure 11. 1H NMR spectra of electrolyte at different charge passed. DMSO was added as an internal standard for quantitative calculations.

Supplementary Figure 12. 1H NMR spectra of electrolyte before and after electrooxidation when using Pd/NF as work electrode for bath electrosynthesis in a H-cell system. DMSO was added as an internal standard for quantitative calculations.

Supplementary Figure 13. a) Waste PET awaiting pretreatment. b) Photographs of stirred reactor used in the scale-up synthesis. c) Photographs of electrolyzer stack and control system used in the scale-up synthesis. Illustration is anodic catalyst used in electrolyzer stack. d) Photographs of separation equipment (filter, vacuum distillation, and drying oven) used in the scale-up synthesis.

Scale-up synthesis

The first step of this process involved adding 20 kg of PET bottles and clothes to a 100 L NaOH aqueous solution (5 M), which was then transferred to a stirred-tank reactor and heated to 80℃ for 12 hours. The resulting hydrolysate solid was acidified with H2SO4, and the white powder that formed was filtered to obtain by-product 1 (TPA, > 99%). The remaining by-product 2 (Na2SO4) was precipitated through crystallization at low temperature. The hydrolysate filtrate 1 was adjusted to a fixed concentration (2 M EG, 5 M NaOH) and then transferred to a flow electrolyzer stack using a peristaltic pump at a speed of 50 ml min-1. The resulting anolyte 2 included NaOH and EG remaining from the reaction, along with the main product GA-, by-product C2O42-, CO32-, and HCOO-. Anolyte 2 is then subjected to vacuum distillation to remove water, resulting in the formation of solid 3, which has the same composition as anolyte 2. To recovery EG and NaOH, solid 3 was extracted and filtered using an ethanol solution containing 15% methyl alcohol and 5% acetonitrile. This process yields solid 4 and a liquid solution containing ethanol, methyl alcohol, acetonitrile, EG, and NaOH. The ethanol solution was evaporated through vacuum distillation, allowing for the recovery of EG and NaOH, which was reintroduced into the flow electrolyzer stack. Solid 4 was dissolved in water, yielding solution 5 (containing CO32-, HCOO-, and the main product GA-) and the by-product Na2C2O4, as Na2C2O4 exhibits poor water solubility. By acidifying solution 5 with H2SO4, solution 6, containing GA, Na2SO4, and HCOOH, was obtained. Through vacuum distillation, the by-product 4 (HCOOH) was separated, resulting in solid 7. Solid 7 was then dissolved and extracted using a mixture of acetone solution containing 15% ethyl acetate to obtain solution 8 and the by-product Na2SO4. This method was chosen because the solubility of GA in mixed solution increases with temperature, while Na2SO4 remains insoluble. By cooling solution 8 at -10 ℃ for crystallization, product 1 (GA crystals) with 99% purity can be obtained. Finally, product 2 (PGA) was prepared via solventless polymerization.

Supplementary Figure 14. 1H NMR of by-product 1 (terephthalic acid) with DMSO as internal standard.

a)

b)

Supplementary Figure 15. a) 1H NMR and b) 13C NMR of filtrate 1 with DMSO as internal standard.

a)

b)

Supplementary Figure 16. a) 1H NMR and b) 13C NMR of anolyte 2 with DMSO as internal standard for quantitative calculations.

c)

d)

a)

b)

Supplementary Figure 17. a) 1H NMR and b) 13C NMR of by-product 3 Na2C2O4 with DMSO as internal standard. c) 1H NMR and d) 13C NMR of by-product 4 HCOOH with DMSO as internal standard.

a)

b)

Supplementary Figure 18. a) 1H NMR and b) 13C NMR of solid 4.

a)

b)

Supplementary Figure 19. a) 1H NMR and b) 13C NMR of solution 5.

Supplementary Figure 20. 1H NMR of solution 6 with DMSO as internal standard for quantitate calculation.

Supplementary Figure 21. 1H NMR of solid 7 with DMSO as internal standard for quantitative calculations.

Supplementary Figure 22. 1H NMR of product 1 GA.

Supplementary Figure 23. Photograph of product 2 PGA synthesized from waste PET.

Supplementary Figure 24. The FTIR spectrum of synthesized PGA.

Supplementary Figure 25. The XRD pattern of the synthesized PGA.

Supplementary Figure 26. GPC analysis of synthesized PGA in hexafluoroisopropanol (HFIP).

Supplementary Figure 27. DSC curve of synthesized PGA.

The crystallinity was calculated by comparing the melting enthalpy (ΔHm) results with the corresponding value of 100% PGA (ΔHm0 = 183.2 J g–1).

Supplementary Table 1. ICP-OES results of CoCr2O4/NF.

| Element | Mass concentration | Molar percent |
| --- | --- | --- |
| Co | 3.35 mg/L | 35.5% |
| Cr | 5.39 mg/L | 64.5% |

Supplementary Table 2. The yield of each step in the whole process.

| Process | Product | Yield | Percentage |
| --- | --- | --- | --- |
| Hydrolysis | EG | 103.2 mol | 99% |
| Electrolysis | GA | 96 mol | 93% |
| Purification | Pure GA | 94 mol | 98% |
| Polymerization | PGA | 91.1 mol | 97% |
| Total | - | - | 87% |

Supplementary Table 3. Process parameters for the scale-up synthesis of PGA.

| Plant size (MW) | 3 |
| --- | --- |
| Production capacity (ton) | 10000 |
| Depreciation time (years) | 15 |
| Maintenance cost | =20% depreciation cost |
| Annual working days (days/year) | 350 |
| Catalyst lifetime (years) | 2 |

Supplementary Table 4. Baseline operating conditions used for technoeconomic analysis (TEA) of GA production.

| Operating conditions | Value |
| --- | --- |
| Current density (mA/cm2) | 280 |
| Cell voltage (V) | 1.25 |
| H2 selectivity (%) | 99 |
| GA selectivity (%) | 93 |
| Glycerol concentration (M) | 2 |
| Anolyte (NaOH) concentration (M) | 5 |
| Catholyte (NaOH) concentration (M) | 5 |
| Electrons needed per mole of GA (n) | 4 |

Supplementary Table 5. Mass balance calculated and price for each ton of PGA produced. (Data source: https://en.made-in-china.com/)

| Components | Consumption/Output [t/t (PGA)] | Unit price ($/t) | costs [$/t (PGA)] |
| --- | --- | --- | --- |
| Waste PET required | 3.63 | 400 | 1452 |
| Ethyl alcohol required | 0.3 | 700 | 210 |
| Acetone required | 0.3 | 972 | 291 |
| Water required | 1.2 | 27.8 | 33.36 |
| NaOH required | 2.27 | 450 | 1021.5 |
| H2SO4 required | 2.84 | 120 | 340.8 |
| Raw and auxiliary material total | - | - | 3348.66 |
| Na2SO4 production | 4.03 | -20 | -80.6 |
| PTA production | 3.1 | -782 | -2424.2 |
| H2 production | 69 | -7.3 | -503.7 |
| By-products total | - | - | -3008.5 |

Supplementary Table 6. Cost of process equipment. (Data source: https://en.made-in-china.com/)

| Scale-up synthesis steps | Components | Equipment price ($) | Capital cost [$/t (PGA)] |
| --- | --- | --- | --- |
| Hydrolysis | Stirred-tank reactor (Capacity: 500 m3) | 2,534,000.00 | 20.272 |
| Electrosynthesis | Stack cost of electrolyzer (Power: 3 MW) | 4,783,000.00 | 38.264 |
| Product separation | Stirred-tank reactor (neutralizer) (Capacity: 800 m3) | 1,740,000.00 | 13.92 |
|  | Crystallizer (Capacity: 500 m3 +300 m3 +200 m3) | 3,850,000.00 | 30.8 |
|  | Distillation (Capacity: 1000 m3) | 3,066,000.00 | 24.528 |
|  | Stirring filter (Capacity: 500 m3 +200 m3+600 m3 +400 m3+400 m3) | 2,740,000.00 | 21.92 |
|  | Vacuum distillation (Capacity: 800 m3 +300 m3) | 4,857,000.00 | 38.856 |
|  | Storage tank (300 m3 × 4) | 1,220,000.00 | 9.76 |
|  | Hydrogen processing (VolumeH2 = 20000 Nm3/day) | 1,143,000.00 | 9.144 |
| Polymerization reactor | Vacuum reactor (Capacity: 200 m3) | 8,569,000.00 | 68.552 |
| Total | - | 34,502,000.00 | 276.016 |

Supplementary Table 7. Yearly energy costs for PGA production.

| Type of energy | Power consumption [kwh/t (PGA)] | Unit price | Energy cost [$/t (PGA)] | CO2 emission [kg/t (PGA)] |
| --- | --- | --- | --- | --- |
| Electricity for electrolyzer | 2656 | 0.08 $/kWh | 212.5 | 1596.8 |
| Electricity for separation | 1821 | 0.08 $/kWh | 145.7 | 1094.8 |
| Electricity for polymerization | 518 | 0.08 $/kWh | 41.44 | 311.4 |
| Total | - | - | 399.64 | 3003 |

CO2 emission calculated method: Electricity consumption × CO2 emission factor (Refer to the Ministry of Ecology and Environment's National Bureau of Statistics of the People's Republic of China on the release of 2021 electricity CO2 emission factors in the Middle East region data)

Supplementary Table 8. Process parameters and electrolyser cost.

| Process parameters |  |
| --- | --- |
| Plant size (MW) | 3 |
| Plant lifetime (years) | 20 |
| Depreciation time (years) | 15 |
| Annual working days (days/year) | 350 |
| Electrolyzer cost |  |
| Stack cost of electrolyzer ($/kW) | $ 450.00 |
| Balance of plant (BoP) capital cost includes power electronics ($/kW) | = Stack cost of electrolyser = 450 $/kW |
| Fixed O&M (% of total uninstalled CAPEX) | 3.0% |
| BoP electrical usage (kWh/kg H2) | 5.10 |
| Electrolyser installation (% of total uninstalled CAPEX) | 12.0% |
| Stack replacement factor | 15.0% |
| Stack replacement time (years) | 5 |