| TiO2/SiO2 (3) | TiO2/SiO2 (2) | TiO2/SiO2 (1) | Silica | Main constituents (wt. %) |
| --- | --- | --- | --- | --- |
| 91.02 | 92.5 | 93.3 | 95.0 | SiO2 |
| 5.6 | 4.9 | 2.7 |  | TiO2 |
| 0.85 | 0.94 | 0.95 | 1.02 | MgO |
| 0.22 | 0.23 | 0.021 | 0.003 | Al2O3 |
| 1.12 | 1.18 | 1.09 | 1.2 | Fe2O3 |
| 0.26 | 0.030 | 0.027 | 0.06 | MnO |
| 0.004 | 0.006 | -- | -- | CuO |
| 0.006 | 0.006 | 0.006 | -- | NiO |
| 0.48 | 0.60 | 0.40 | 0.62 | CaO |
| 0.63 | 0.71 | 0.65 | 0.29 | K2O |
| 0.01 | 0.02 | 0.08 | 1.10 | P2O5 |
| 0.36 | 0.37 | 0.25 | 0.044 | SO3 |
| 0.02 | 0.05 | 0.05 | 0.03 | Cl |

Table (1) XRF of silica fume and silica covered with titanium dioxide

Table 2: porosity data for uncovered and covered paper sheets with PLA, PLA-1% TiO2/SiO2 (3), and PLA-2% TiO2/SiO2 (3)

| Sample | Total Area, μm2 | Average Size, μm | Porosity, % | Feret diameter, μm |
| --- | --- | --- | --- | --- |
| Blank | 120746.9 | 168.406 | 17.153 | 29.833 |
| PLA | 57994.36 | 101.923 | 8.215 | 24.779 |
| 1% TiO2/SiO2(3) | 8024.952 | 57.321 | 1.139 | 14.85 |
| 2% TiO2/SiO2(3) | 106041.8 | 171.312 | 15.045 | 27.749 |

Feret's Diameter is the longest distance between any two points along the selection boundary, also known as maximum caliper

Table (3): Thermo-analytical and thermodynamic data of the thermal decomposition for coated paper sheets with PLA-TiO2/SiO2

|  | Phase | To | Tm | WL, % | WLRmax, %∙min/°C | Ea, kJ/mol | A, 1/s | ΔHa, kJ/mol | ΔSa, J/K mol | ΔGa, kJ/mol |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Blank | 1 | 40 | 81.14 | 7.50 | 6.828 | 83.82 | 7.06ꓫ1011 | 80.87 | -19.51 | 87.78 |
|  | 2 | 315.32 | 355.03 | 79.09 |  | 151.52 | 5.65ꓫ1011 | 146.30 | -26.14 | 162.71 |
|  |  |  |  |  |  | ∑235.33 |  | ∑227.17 | ∑-45.65 | ∑250.49 |
| PLA | 1 | 40 | 49.28 | 8.35 | 6.964 | 28.66 | 1.99ꓫ103 | 25.98 | -182.47 | 84.78 |
|  | 2 | 310.5 | 352.96 | 78.02 |  | 143.60 | 1.19ꓫ1011 | 138.40 | -39.05 | 162.84 |
|  |  |  |  |  |  | ∑172.26 |  | ∑164.37 | ∑-221.52 | ∑247.62 |
| 1% TiO2/SiO2(3) | 1 | 40 | 62.41 | 6.09 | 4.497 | 47.14 | 1.14ꓫ106 | 44.35 | -129.95 | 87.94 |
|  | 2 | 306.79 | 358.09 | 77.69 |  | 139.07 | 3.78ꓫ1010 | 133.83 | -48.67 | 164.54 |
|  |  |  |  |  |  | ∑186.21 |  | ∑178.17 | ∑-178.62 | ∑252.48 |
| 2% TiO2/SiO2(3) | 1 | 40 | 95.61 | 5.27 | 4.665 | 60.61 | 3.36ꓫ107 | 57.55 | -102.63 | 95.38 |
|  | 2 | 295.3 | 350.82 | 80.35 |  | 148.57 | 2.88ꓫ1011 | 143.38 | -31.68 | 163.14 |
|  |  |  |  |  |  | ∑209.18 |  | ∑200.93 | ∑-134.30 | ∑258.52 |