# Supplementary Information

Tumor-specific high-valence bismuth(V) nanoplatform potentiates cancer immunotherapy with exogenous excitation-free endogenous H2O2- and O2-independent ROS generation

Yizhang Tang1, Xujiang Yu1*, Liangrui He1, Meng Tang2, Wenji Yue1, Ruitong Chen1, Jie Zhao1, Qi Pan3 and Wanwan Li1*

1 State Key Lab of Metal Matrix Composites

School of Materials Science and Engineering

Zhangjiang Institute for Advanced Study

Shanghai Jiao Tong University

800 Dongchuan Road, Shanghai 200240, P. R. China

# 2 Department of Comprehensive Oncology

National Cancer Center/National Clinical Research Center for Cancer/Cancer Hospital

Chinese Academy of Medical Sciences and Peking Union Medical College

Beijing 100021, China

3 Department of Urology

Shanghai General Hospital, Shanghai Jiao Tong University School of Medicine

# Shanghai 200080, China

Supplementary Fig. 1 | A representative transmission electron microscopy (TEM) image of commercially purchased sodium bismuthate (Macklin).

# Supplementary Fig. 2 | Selected-area electron diffraction pattern of BiIIIOx.

# Supplementary Fig. 3 | HADDF imageand element mapping of BiIIIOx.

# Supplementary Fig. 4 | Selected-area electron diffraction pattern of NaBiVO3.

# Supplementary Fig. 5 | HADDF imageand element mapping of NaBiVO3.

Supplementary Fig. 6 | A photograph of NaBiVO3-PEG prepared by two-step for PEGylation modification.

Supplementary Fig. 7 | Dynamic light scattering (DLS) data of BiIIIOx, NaBiVO3 and NaBiVO3-PEG in the aqueous solution.

Supplementary Fig. 8 | UV–Vis–NIR spectra of BiIIIOx, NaBiVO3 and NaBiVO3-PEG solutions.

Supplementary Fig. 9 | Photographs of NaBiVO3 nanoparticles in PBS and NaBiVO3-PEG nanoparticles in PBS and culture medium.

Supplementary Fig. 10 | Time-dependent TEM images of NaBiVO3-PEG when dispersed in PBS with different pH values.

Supplementary Fig. 11 | XRD pattern of NaBiVO3-PEG and hydrolystate after NaBiVO3-PEG dispersed in PBS for 48 h at pH 5.5.

Supplementary Fig. 12 | High-resolution XPS spectra of Bi 4f of NaBiVO3-PEG and hydrolystates after NaBiVO3-PEG dispersed in SBF(a) and PBS (b) for 48 h at pH 5.5.

Supplementary Fig. 13 | High-resolution XPS spectra of Na 1s of NaBiVO3-PEG and hydrolystates after NaBiVO3-PEG dispersed in SBF(a) and PBS (b) for 48 h at pH 5.5.

Supplementary Fig. 14 | High-resolution XPS spectra of O 1s of NaBiVO3-PEG and hydrolystates after NaBiVO3-PEG dispersed in PBS for 48 h at pH 5.5.

Supplementary Fig. 15 | a, Time-dependent fluorescence intensity of PBS recorded at 525 nm after incubation with APF in buffers at different pH values. b, Time-dependent fluorescence intensity of PBS recorded at 525 nm after incubation with SOSG in buffers at different pH values. Data were shown as mean ± s.d.

Supplementary Fig. 16 | a, Time-dependent fluorescence intensity of BiIIIOx-PEG recorded at 525 nm after incubation with APF in buffers at different pH values. b, Time-dependent fluorescence intensity of BiIIIOx-PEG recorded at 525 nm after incubation with SOSG in buffers at different pH values. Data were shown as mean ± s.d.

Supplementary Fig. 17 | a, A photograph of the mixed solution of NaBiVO3-PEG and Mn2+ before (left) and after (right) dropping two drops of 1 M HNO3. b, UV–Vis–NIR spectra of the mixed solution of NaBiVO3-PEG and Mn2+ before and after dropping two drops of 1 M HNO3.

Supplementary Fig. 18 | a, Time-dependent fluorescence intensity of NaBiVO3-PEG recorded at 525 nm after incubation with APF in buffers at different H2O2 concentration. b, Time-dependent fluorescence intensity of NaBiVO3-PEG recorded at 525 nm after incubation with SOSG in buffers at different H2O2 concentration. Data were shown as mean ± s.d.

Supplementary Fig. 19 | a, Time-dependent fluorescence intensity of PBS recorded at 525 nm after incubation with APF in buffers at different H2O2 concentration. b, Time-dependent fluorescence intensity of PBS recorded at 525 nm after incubation with SOSG in buffers at different H2O2 concentration. Data were shown as mean ± s.d.

Supplementary Fig. 20 | a, Time-dependent fluorescence intensity of BiIIIOx-PEG recorded at 525 nm after incubation with APF in buffers at different H2O2 concentration. b, Time-dependent fluorescence intensity of BiIIIOx-PEG recorded at 525 nm after incubation with SOSG in buffers at different H2O2 concentration. Data were shown as mean ± s.d.

Supplementary Fig. 21 | a, Time-dependent fluorescence intensity of NaBiVO3-PEG recorded at 525 nm after incubation with APF in buffers at different GSH concentration. b, Time-dependent fluorescence intensity of NaBiVO3-PEG recorded at 525 nm after incubation with SOSG in buffers at different GSH concentration. Data were shown as mean ± s.d.

Supplementary Fig. 22 | a, Time-dependent fluorescence spectra of NaBiVO3-PEG after incubation with APF in pH 5.5 PBS under normoxic and hypoxic conditions b, Time-dependent fluorescence spectra of NaBiVO3-PEG after incubation with SOSG in PBS at pH 5.5 under normoxic and hypoxic conditions.

Supplementary Fig. 23 | Cytotoxicity of BIIIOx-PEG and NaBiVO3-PEG on MB49. Data were shown as mean ± s.d. The P values were calculated by one-way ANOVA and Tukey multiple-comparison test. *P < 0.05, **P < 0.01, ***P < 0.001, ****P < 0.0001, and n.s., not significant.

Supplementary Fig. 24 | Apoptosis of 4T1 cells conducted by flow cytometry analysis with different treatments.

Supplementary Fig. 25 | Average weights of primary tumor (a) and distant tumor (b) collected from mice at day 14 after various treatments indicated. Data were shown as mean ± s.d. The P values were calculated by Kruskal-Wallis and Dunn multiple-comparison test. *P < 0.05, **P < 0.01, ***P < 0.001, ****P < 0.0001, and n.s., not significant.

Supplementary Fig. 26 | Representative H&E-stained images of the heart, liver, lung, kidney, and spleen at day 14 under different treatments.

Supplementary Fig. 27 | The body weight of mice after different treatments. Data were shown as mean ± s.d.

Supplementary Fig. 28 | Schematic diagram of cell sorting process for analysis of DCs (CD11c+ CD80+ CD86+) in mouse lymph node.

Supplementary Fig. 29 | Schematic diagram of cell sorting process for analysis of DCs (CD3+ CD4+ CD8+) in mouse distant tumor.

Supplementary Fig. 30 | Survival fractions of 4T1 cells incubated with PBS, and degraded NaBiVO3-PEG under various X-ray doses (100 μg mL-1). Data were shown as mean ± s.d. The P values were calculated by one-way ANOVA and Tukey multiple-comparison test. *P < 0.05, **P < 0.01, ***P < 0.001, ****P < 0.0001, and n.s., not significant.

Supplementary Fig. 31 | Average weights of tumor collected from mice at day 14 after various treatments indicated. Data were shown as mean ± s.d. The P values were calculated by one-way ANOVA and Tukey multiple-comparison test. *P < 0.05, **P < 0.01, ***P < 0.001, ****P < 0.0001, and n.s., not significant.

Supplementary Fig. 32 | Blood routine test of mice evaluated at day 1, 7,and 14 day after intravenous Injection with NaBiVO3-PEG. Data were shown as mean ± s.d.