Supplementary Table 1. The electric parameters of each tissue of the head and the materials of TTFields under frequency of 200kHz.

| Electric parameter |  | Scalp | Skull | CSF | GM | WM | Peritumoral tissue | Tumor core | Gel | Ceramic electrode |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| σ(S/m) | min | 0.10 | 0.010 | 1.40 | 0.20 | 0.10 | 0.20 | 0.50 | - | - |
|  | standard | 0.25 | 0.013 | 1.79 | 0.25 | 0.12 | 0.24 | 1.00 | 0.10 | 0 |
|  | max | 0.70 | 0.080 | 2.60 | 0.80 | 0.80 | 1.60 | 4.00 | - | - |
| εr |  | 5000 | 200 | 110 | 3000 | 2000 | 2000 | 100 | 100 | 10000 |
| σstandard/ωε |  | 4.50 | 5.84 | 1463.21 | 7.49 | 5.40 | 10.79 | 817.44 | 89.92 | 0.00 |

Abbreviation: CSF, cerebrospinal fluid; GM, grey matter; WM, white matter; σ, the electrical conductivity; ε, the permittivity; ω, the angular frequency.

Supplementary Table 2. The parameters of each material used in the validation experiments.

| Material | σ(S/m) | εr | Size(mm) |
| --- | --- | --- | --- |
| Titanium plate | 2.34×106 | / | 60×25×4 |
| PEEK plate | 1×10-15 | 3.2 | 60×25×4 |
| Bovine bone plate | 1.0×10-2 | 200 | 60×10×3.5 |
| Fat tissue of pork | *2.2×10-2 | *5.6 | / |
| Muscle tissue of pork | *1.7×10-1 | *57.1 | / |

*These parameters were measured at 200kHz with ZVL vector network analyzer (R&S Company).

Supplementary Table 3. The alteration in electric intensity with the implantation of bio-compatible materials under the skull drilling of 3×3 array

| Implanted material | Maximum peritumoral EF (Emax, V·m-1) | Average peritumoral EF (Eave, V·m-1) | Average EF enhancement (%) |
| --- | --- | --- | --- |
| Titanium | 936.44 | 508.67 | 96.98 |
| PEEK | 402.15 | 218.41 | -15.42 |
| Connective tissue | 805.78 | 437.50 | 69.42 |
| CSF | 894.89 | 484.98 | 87.81 |
| Skull (reference) | 475.28 | 258.23 | 0 |

Abbreviation: CSF, cerebrospinal fluid; EF, electric field; PEEK, polyether ether ketone