Facile preparation of 3D porous graphene-based composite hydrogels doped with different ratios of MXene for MB adsorption

Yaning Wangb, Xiaoxia Yanb, Yuxi Wangb, Kai Yangb, Fei Lina,*, Jiefen Shenb, Xuming Sunb,c, Zhigang Chena,*, Wenshuai Jianga,b,c,d,*

a The First Affiliated Hospital of Xinxiang Medical University, Xinxiang, Henan 453003, People's Republic of China

b School of Medical Engineering, Xinxiang Medical University, Xinxiang, Henan 453003, People's Republic of China

c Xinxiang Key Laboratory of Neurobiosensor, Xinxiang, Henan 453003, People's Republic of China

d Henan Engineering Technology Research Center of Neural Sensing and Control, Henan 453003, People's Republic of China

Corresponding author. E-mail addresses: linfeixixi@aliyun.com (Fei Lin); 1fy2000129@xxmu.edu.cn (Zhigang Chen); 171024@xxmu.edu.cn (Wenshuai Jiang).

Figure S1- Figure S9

FigureS1.（a）GO;(b)MXene

Figure S2. Digital photographs of 3D graphene@MXene composite hydrogels with different MXene contents

Figure S3. Pure graphene composite hydrogels

Figure S4. MB adsorption based on graphene hydrogels and Graphene@MXene composite hydrogels.

Figure S5. Digital photographs of Calcium ion-regulated graphene@MXene composite hydrogels with different MXene contents

Figure S6. SEM of Ca2+regulated graphene@MXene composite aerogels

Figure S7. Elasticity test results of composite aerogels prepared before and after Ca2+ introduction.

Figure S8. Changes in pore size of composite hydrogels prepared before and after Ca2+introduction

Figure S9. Luminescence spectra of MXene films under microwave irradiation.

Table S1-Table S2

TableS1. Sheet resistance of graphene@MXene composite membranes with different MXene contents. (50℃, heating 3h)

| MXene contents | Sheet resistance |
| --- | --- |
| 0% | 0 |
| 20% | 6.18 ± 1.69 MΩ/□ |
| 40% | 377.8 ± 46.8 KΩ/□ |
| 60% | 131.6 ± 27.6 KΩ/□ |
| 80% | 405.2 ± 95.5Ω/□ |
| 100% | 2.60 ± 0.6Ω/□ |

Table S2. Sheet resistance measurements of graphene@MXene aerogels with different MXene contents.

| MXene contents | Sheet resistance |
| --- | --- |
| 20% | ~321.6 KΩ/□ |
| 40% | ~ 28.7K Ω/□ |
| 60% | ~578.2 Ω/□ |
| 80% | ~54.9 Ω/□ |