Appendix A. Supplementary Data

Rational Development of Fingolimod Nano-embedded Microparticles as Nose-to-Brain Neuroprotective Therapy for Ischemic Stroke

Xinyue Zhang a,b, Guangpu Su c, Zitong Shao a,b, Ho Wan Chan a, Si Li a,b, Stephanie Chow a, Chi Kwan Tsang c, Shing Fung Chow a,b,*

a Department of Pharmacology and Pharmacy, Li Ka Shing Faculty of Medicine, The University of Hong Kong, Pokfulam, Hong Kong SAR, China

b Advanced Biomedical Instrumentation Centre, Hong Kong Science Park, Shatin, Hong Kong SAR, China

c Clinical Neuroscience Institute and Department of Neurology, The First Affiliated Hospital of Jinan University, Guangzhou, Guangdong Province, China

* Corresponding author

Table S1

The gradient mode of FIN and CUR in HPLC.

| Time (min) | Mobile phase A (% v/v) | Mobile phase B (% v/v) |
| --- | --- | --- |
| 0 | 23 | 77 |
| 10 | 15 | 85 |
| 11 | 15 | 85 |
| 12 | 23 | 77 |
| 17 | 23 | 77 |

Table S2

A 3-factor, 2-level full factorial design for the preparation of FIN nanosuspension

| Factors: Formulation Parameters |  | Levels |  |  |
| --- | --- | --- | --- | --- |
|  |  | -1 | 0 | +1 |
| A: Initial FIN concentration (mg/ml) B: CLT: FIN (w/w) C: Concentration of PVP solution (% w/v) |  | 5 0.5 0.25 | 7.5 1 0.625 | 10 1.5 1 |
| Responses (Y) | Goals | Requirements |  |  |
| Y1: Particle Size of nanoparticle (nm) Y2: PDI Y3: Physical Stability (hours) Y4: Encapsulation Efficiency of FIN (%) | In range Minimize Maximize Maximize | 0-200 nm < 0.3 > 24 hours > 90 % |  |  |

Table S3

A 3-factor, 2-level full factorial design for the fabrication of FIN dry powder.

| Factors: Formulation Parameters |  | Levels |  |  |
| --- | --- | --- | --- | --- |
|  |  | -1 | 0 | +1 |
| A: Mannitol: nano (w/w) B: Atomization gas flow rate (L/h) C: Feed rate (ml/min) |  | 4 357 1.5 | 7 473 3 | 10 601 4.5 |
| Responses (Y) | Goals | Requirements |  |  |
| Z1: Redispersibility Z2: PDI Z3: Volumetric particle size of dry powder | In range Minimize Target | 0.8 - 1.2 < 0.3 10 µm |  |  |

Table S4

Initial trials on FIN nanosuspension fabrication by FNP (initial FIN concentration = 5 mg/mL; n = 3).

| Trial | Stabilizer | Co-stabilizer | Particle size (nm) | Physical stability |
| --- | --- | --- | --- | --- |
| 1 | PVP [0.5% (w/v)] | / | 1290.5±20.7 | 5 minutes |
| 2 | TPGS [FIN-CUR-TPGS ratio = 1:1:1 (w/w)] | / | NA* | NA^ |
| 3 | TPGS [FIN-CUR-TPGS ratio = 1:1:1 (w/w)] | CLT [FIN -CLT ratio = 5:1 (w/w)] | NA* | NA^ |
| 4 | PVP [0.5% (w/v)] | CLT [FIN-CUR-CLT ratio = 2:1:2 (w/w)] | 228.0±10.3 | 1 h |
| 5 | TPGS [FIN-TPGS ratio = 1:1 (w/w)] | CLT [FIN -CLT ratio = 5:1 (w/w)] | NA* | NA^ |

NA*: The particle size of nanoparticle was not detected under the detection by dynamic light scattering.

NA^: The physical stability of nanoparticle was not available due to the missing particle size data.

Table S5

Coded regression equations for probing the relationship between formulation parameters and CQAs of FIN nanosuspensions with ANOVA and multiple reliability test (R2) results.

| Response | Regression equation | F value | p value | R2 | Adjusted R2 |
| --- | --- | --- | --- | --- | --- |
| Particle Size (nm) (Y1) | =147.68+17.48A+6.28B+3.26C-1.92AB+8.4AC+7.78BC-1.72 ABC | 148.33 | < 0.0001 | 0.983 | 0.976 |
| PDI (Y2) | =0.2244-0.0377A-0.0252 B+0.0321C+0.0222AB-0.0218 AC-0.0127BC | 14.41 | < 0.0001 | 0.849 | 0.790 |
| Physical Stability (hours) (Y3) | =18.00-10.17A+17.50B-1.67C-10.33AB+6.50AC-1.83BC+6.00ABC | 95.23 | < 0.0001 | 0.974 | 0.964 |
| EE of FIN (%) (Y4) | =83.22+6.10A+1.75B-9.36C-0.6796AB+3.29AC+1.13BC-0.4029ABC | 497.62 | < 0.0001 | 0.995 | 0.993 |

Table S6

Volumetric particle size distribution of FIN dry powder formulations. The powders were dispersed using the nasal powder device at 15 L/min and the particle size distribution was measured by laser diffraction (n=3).

| Powder Formulation (PF) | D10 (µm) | D50 (µm) | D90 (µm) | Span |
| --- | --- | --- | --- | --- |
| PF1 | 2.27 ± 0.34 | 8.69 ± 0.21 | 17.76 ± 0.12 | 1.78 ± 0.03 |
| PF2 | 2.97 ± 0.11 | 9.91 ± 0.28 | 19.53 ± 0.88 | 1.67 ± 0.05 |
| PF3 | 1.51 ± 0.18 | 5.16 ± 0.62 | 12.43 ± 2.17 | 2.10 ± 0.14 |
| PF4 | 1.49 ± 0.25 | 4.58 ± 0.57 | 10.67 ± 2.15 | 1.99 ± 0.19 |
| PF5 | 2.27 ± 0.04 | 8.95 ± 1.14 | 19.02 ± 2.36 | 1.87 ± 0.03 |
| PF6 | 3.20 ± 0.11 | 10.84 ± 0.47 | 24.44 ± 3.61 | 1.95 ± 0.25 |
| PF7 | 2.72 ± 0.17 | 8.34 ± 0.28 | 17.04 ± 0.23 | 1.72 ± 0.06 |
| PF8 | 2.29 ± 0.30 | 7.44 ± 0.49 | 15.47 ± 1.38 | 1.77 ± 0.04 |
| PF9 | 2.39 ± 0.07 | 8.38 ± 0.53 | 16.87 ± 0.98 | 1.73 ± 0.03 |

Table S7

Coded regression equations for probing the relationship between formulation and process parameters and CQAs of FIN powder with ANOVA and multiple reliability test (R2) results.

| Response | Regression equation | F value | p value | R2 | Adjusted R2 |
| --- | --- | --- | --- | --- | --- |
| Redispersibility (Z1) | =1.26+0.1150A+0.1850B+0.0475C+0.1558AB+0.0000AC+0.0717BC-0.0092ABC | 115.11 | < 0.0001 | 0.978 | 0.970 |
| PDI (Z2) | =0.3100+0.0135A-0.0005B+0.0039C+0.0010AB+0.0013AC-0.0057BC-0.0131ABC | 0.6429 | 0.7154 | 0.200 | -0.111 |
| Volumetric Particle Size of dry powder (µm) (Z3) | =7.99-0.9046A-1.61B+0.2029C-0.6063AB-0.0438AC-0.5738BC+0.1246ABC | 43.39 | < 0.0001 | 0.944 | 0.922 |

Fig. S1. (a) The intensity-weighted size distribution of the optimized FIN nanoparticle. (b) TEM figure of optimized FIN nanoparticle at 19,500 magnification, scale bar = 200 nm.

Fig. S2. (a) DSC profiles, (b) PXRD patterns, (c) TGA profiles, and (d) FTIR profiles of the raw materials, physical mixture, and the optimized FIN powder.

Fig. S3. The in vitro drug release of (a) FIN and (b) CUR from the optimized FIN dry powder and its physical mixture in an 80:20 v/v solution of simulated nasal fluid (SNF) and ethanol (EtOH).

Fig. S4. The deposition fraction of the olfactory region at inspiratory flow rates (0, 7.5 and 15 L/min) using 3D-printed nasal cast and AINI nasal model.