Table1 The main components of HTPB propellant

| Components | Function | Proportion | Form |
| --- | --- | --- | --- |
| HTPB | Adhesive | 11.3% | Liquid |
| Ammonium perchlorate | Solid oxidizer | 68% | Solid |
| Aluminum powder | Solid oxidizer | 17% | Solid |
| 2, 4-toluene diisocyanate | Curing agent | 0.5% | Liquid |
| Plasticizer, stabilizer, combustion plasticizer, etc | Other | 3.2% | Solid\Liquid |

Table 2. Parameters in fatigue failure

|  | ε0 | A | B | R2 |
| --- | --- | --- | --- | --- |
| C1 | 0.04627 | 0.25281 | -0.20678 | 0.93 |
| C2 | 0.0754 | 0.15512 | -3.34528 | 0.94 |
| C3 | 0.05032 | 0.04094 | -3.05407 | 0.96 |
| S | 0.02097 | 0.30928 | -8.76631 | 0.99 |

Table3 Parameters related to fatigue damage

| Specimen | ε1 | ∆Ts1/℃ | n | ε2 | ∆Ts2/℃ | Predicted life | Actual life | Correlation |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 0.25 | 20 | 153345 | 0.2 | 32.6 | 34566 | 33985 | 98.3% |
| 2 | 0.25 | 19.8 | 103543 | 0.2 | 33.9 | 41169 | 39985 | 97.0% |
| 3 | 0.25 | 19.7 | 99765 | 0.2 | 34.0 | 68954 | 62859 | 90.3% |
| 4 | 0.25 | 20 | 86259 | 0.2 | 34.6 | 75945 | 70695 | 92.6% |
| 5 | 0.25 | 20 | 96845 | 0.2 | 32.8 | 85249 | 87595 | 97.3% |

Note: ε1 is the maximum strain of the first stage, ∆Ts1 is the initial temperature, n is the number of fatigue load cycles, ε2 is the maximum strain of the second stage, and ∆Ts2 is the temperature rise after cycling.