Supplementary Material

Stable pH-responsive superhydrophobic fabric based on AgNPs/copolymer composites for controllable oil-water separation

Xuanjun Li, Xiaojing Su*, Pingping Deng, Shengye Chen, Zhuohan Chen, Kunquan Li, Wenjian Wu*

School of Materials Science and Engineering, Dongguan University of Technology, Dongguan 523808, China

*Corresponding authors.

E-mail addresses: suxj@dgut.edu.cn, wuwj@dgut.edu.cn.

| DMAEMA (g) | VMDMO (g) | MATE (g) | Solvent (mL) | AIBN (g) | Reaction temperature (oC) | Reaction time (h) | Response time (s) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2 | 0.5 | 1 | ethanol (30) | 0.04 | 70 | 8 | >300 |
| 2 | 1 | 1 | ethanol (30) | 0.04 | 70 | 8 | >300 |
| 2 | 1.5 | 1 | ethanol (30) | 0.04 | 70 | 8 | none |
| 2 | 0.5 | 0.5 | ethanol (30) | 0.04 | 70 | 8 | >300 |
| 2 | 0.5 | 1.5 | ethanol (30) | 0.04 | 70 | 8 | none |
| 3 | 0.5 | 1 | ethanol (30) | 0.04 | 70 | 8 | none |
| 4 | 0.5 | 1 | ethanol (30) | 0.04 | 70 | 8 | none |
| 1 | 0.5 | 1 | ethanol (30) | 0.04 | 70 | 8 | 189 |
| 1 | 0.5 | 1 | ethanol (30) | 0.04 | 60 | 8 | 226 |
| 1 | 0.5 | 1 | ethanol (30) | 0.04 | 80 | 8 | >300 |
| 1 | 0.5 | 1 | DMF (30) | 0.04 | 70 | 8 | none |
| 1 | 0.5 | 1 | toluene (30) | 0.04 | 70 | 8 | none |
| 1 | 0.5 | 1 | toluene (20) | 0.04 | 65 | 8 | >300 |
| 1 | 0.5 | 1 | toluene (20) | 0.04 | 65 | 6 | 273 |
| 1 | 0.5 | 1 | toluene (20) | 0.04 | 65 | 4 | 150 |

Table. S1 Response time of the Ag-S@DVM fabric with different preparation conditions of DVM

Fig. S1 SEM images of the Ag-S@DVM fabric after pH response

Fig. S2 Wettability of the (a) original fabric, (b) Ag-fabric, (c) Ag-S fabric, and (d) Ag-S@DVM fabric

Fig. S3 Water pressure tolerance test of the Ag-S@DVM fabric

Fig. S4 (a) Separation flux and separation efficiency of the oil in heavy oil-salty water mixture under different NaCl solubility of the Ag-S@DVM fabric before pH response. (b) Separation flux and separation efficiency of the water in light oil-salty water mixture under different NaCl solubility of the Ag-S@DVM fabric after pH response

Fig. S5 Oil-absorption processes of the (a) original fabric, and (b) Ag-S@DVM fabric

Fig. S6 Absorption capacity of the Ag-S@DVM fabric to various oils

Fig. S7 Superhydrophobicity and adhesion resistance of the Ag-S@DVM fabric