Supplementary Information for

Effectiveness of strain and dopants on breaking the activity-stability trade-off of RuO2 acidic oxygen evolution electrocatalysts

Yang Liu1,2#, Yixuan Wang2#, Hao Li2#, Min Gyu Kim5, Mingbo Wu6, Hyoyoung Lee2,3,4*

1Shandong Provincial Key Laboratory for Science of Material Creation and Energy Conversion, Institute of Frontier Chemistry, School of Chemistry and Chemical Engineering, Shandong University, Qingdao, 266237 P. R. China

2Department of Chemistry, Sungkyunkwan University, Seobu-Ro 2066, Suwon, 16419, Republic of Korea

3Creative Research Institute, Sungkyunkwan University, Seobu-Ro 2066, Suwon, 16419, Republic of Korea

4Institute of Quantum Biophysics, Sungkyunkwan University, Seobu-Ro 2066, Suwon, 16419, Republic of Korea

5Beamline Research Division, Pohang Accelerator Laboratory, Pohang University of Science and Technology, Pohang, 37673, Republic of Korea

6State Key Laboratory of Heavy Oil Processing, College of Chemical Engineering, College of New Energy, China University of Petroleum (East China), Qingdao 266580, China

#These authors contributed equally to this work.

*e-mail: hyoyoung@skku.edu

Experimental Section

Materials

RuCl3·xH2O, NH4OH (25-30 wt%), H2SO4 (98wt%), NaNO3, NaCl, TaCl5, Sr(NO3)2, ethanol, citric acid, commercial RuO2 (c-RuO2), and Naﬁon (5 wt%) were purchased from Sigma-Aldrich. Carbon paper (CP GDL) and Platinized Ti foam (Pt/Ti GDL) were purchased from the Fuel Cell Store. All chemicals were used as received without further puriﬁcation. The water used in all experiments was puriﬁed using a Millipore system.

Synthesis of tensile strained and Sr/Ta doped RuO2-x electrocatalysts

The preparation of precursors for the synthesis of RuO2-x nanocatalysts was based on the sol-gel method. Specifically for the synthesis process of TS-Sr0.1Ta0.1Ru0.8O2-x, the mixed solution was prepared with water (30 mL) and ethanol (50 mL) containing citric acid (0.125 mmol) and 5 g (92wt% NaNO3 + 8 wt %NaCl) under sonication 1 h. 0.24 mmol of RuCl3·H2O, 0.03 mmol of TaCl5, and 0.03 mmol of Sr(NO3)2 were added into the above solution under vigorous stirring in an ice bath. After stirring for 2 h, ammonia solution was added dropwise into the reaction solution within 1 h to adjust the pH to around 6. After ball milling for 4 h, the reaction solution bottle was quickly frozen using liquid N2 and freezing dried.

A pot-type quartz crucible was used to anneal precursor in the muffle furnace under 400 ℃ (10 ℃/min) for 2 hours and then was quickly take out the quartz crucible and pour mixture into enough water (1 L water) at room temperature (with vigorous stirring) to obtain the TS-Sr0.1Ta0.1Ru0.8O2-x nanocatalysts.

The other ratios in feed (0.28 mmol of RuCl3·H2O, 0.01 mmol of TaCl5, and 0.01 mmol of Sr(NO3)2) and (0.2 mmol of RuCl3·H2O, 0.05 mmol of TaCl5, and 0.05 mmol of Sr(NO3)2) were also prepared and performance was investigated. A similar process was conducted but with only Sr or Ta salt to obtain TS-Sr0.1Ru0.9O2-x and TS-Ta0.1Ru0.9O2-x nanocatalysts. Substituting the quenching with the natural cooling process gave the Sr0.1Ta0.1Ru0.8O2-x samples.

Material characterizations.

The morphology of the samples was investigated by using a JSM 7401F (JEOL Ltd., Tokyo, Japan) scanning electron microscope (SEM) operated at 3.0 kV. High-resolution TEM (HRTEM) images and scanning transmission electron microscopy (STEM) images were collected on a JEOL ARM-200F ﬁeld-emission transmission electron microscope operating at a 200 kV accelerating voltage. X-ray photoelectron spectroscopy (XPS) was performed using a VG Microtech ESCA 2000 equipped with a monochromic Al X-ray source (97.9 W, 93.9 eV). X-ray diffraction (XRD) patterns were acquired using a Rigaku Ultima IV, using the substrates directly. ICP-OES was measured on 5110 ICP-OES (Varian, US) for samples after diluent 100 μL electrolytes using 0.5 M H2SO4 (5 mL total) at regular intervals when measuring in the cell as shown in Fig. S15 at a current density of 10 mA cm-2.

The X-ray absorption spectroscopy (XAS) measurements were performed at the BL10C beamline of the Pohang Light Source (PLS-II, Korea) under an operation mode of 3.0 G eV with a ring current of 250 mA. The acquired XAFS data were analyzed by Athena and Artemis software according to the standard process. The spectra were calibrated, averaged, pre-edge background subtracted, and post-edge normalized using the Athena program in the IFEFFIT software package. The Fourier transformation of EXAFS oscillations from k space to R space was achieved to obtain a radial distribution function. All data fitting was completed in the Artemis program. The in-situ attenuated total reﬂection surface-enhanced infrared absorption spectroscopy (ATR-SEIRAS) was conducted using a Bruker INVENIO-R spectrometer equipped with a mercury cadmium telluride (MCT) detector, a Veemax III ATR accessory (Kromatek), and an electrochemical reaction cell equipped with a CaF2 bottom. The electrochemical tests were performed on a CHI 760E workstation in a typical three-electrode configuration with a Pt wire and Ag/AgCl (saturated KCl electrolyte) electrode as the counter and reference electrodes, respectively. Our electrodes were directly stuck on the working electrode (Pt coin surface) surface using conductive adhesive tape. The Ar inlet was connected and flowed the electrolyte for 30 min with 20 ccm on two sides.

Electrochemical measurements

To prepare all RuO2-x electrodes, the catalyst ink was prepared by suspending 5 mg of catalyst powder in a 1 mL solution consisting of 500 μL of 5 wt% Nafion® (117 solutions, Aldrich), 250 μL of ethanol, and 710 μL of distilled water. 200 μL ink was carefully distributed dropwise on the surface of CP(1cm2) and dried in the vacuum oven at 40℃.

Electrochemical measurements were performed in a standard three-electrode system (CHI 660E, USA) consisting of a RuO2-x catalyst working electrode, a Pt mesh counter electrode, and a Hg/Hg2SO4 reference electrode. All potentials reported in our work are referenced to a reversible hydrogen electrode (RHE) via the Nernst equation (Eqn(1)), and the Hg/Hg2SO4 reference electrode was calibrated in a hydrogen-saturated 0.5 M H2SO4 (Figure S7). The linear sweep voltammetry curves were recorded at a scan rate of 2 mV s−1 in 0.5 M H2SO4 (PH=0).

ERHE=EHg/Hg2SO4+0.059pH+ E0Hg/Hg2SO4                   (1)

where ERHE is the converted potential vs. RHE, EHg/Hg2SO4 is the experimentally measured potential against the Hg/Hg2SO4 reference electrode, and E0Hg/Hg2SO4 is the standard potential of Hg/Hg2SO4 at 25oC (0.65 V). All the potentials were automatically iR-corrected for the ohmic resistance of the solution unless specified.

The tests of the two-electrodes electrolyzer were conducted after coating the TS-Sr0.1Ta0.1Ru0.8O2-x or c-RuO2 for the anode and Pt/C for the cathode, respectively. LSV curves were recorded in a certain region of 1~1.8 V with a scan of 2 mV s-1. The chronoamperometry measurements were carried out at the current densities of 10 mA cm−2 and 50 mA cm−2 during the long term.

Before recording the electroactivity in 0.5 M H2SO4, the catalysts were activated by 10 cycles of CV scans in a certain region (0.3~0.9 V vs. Hg/Hg2SO4). To study the OER electrocatalytic activity in acid conditions, the polarization curves were created from 0.2 to 0.9 V (vs. Hg/Hg2SO4) at a negative scan (scan rate of 2 mV/s) to avoid the non-faradaic capacitance/current contribution. And chronopotentiometric (V-t) measurements were carried out on CP or Pt/Ti GDL at a constant current density in the 0.5 M H2SO4 solution.

In-situ electrochemical impedance spectroscopy (EIS) was carried out on a Bio-Logic workstation in a frequency range from 100 kHz to 0.01 Hz and a potential range from 1.0 to 1.5 V (vs. RHE). Then simulation and analysis of EIS data were carried out using ZSimpWin software1, 2.

The electrochemical double-layer capacitance (Cdl) of every electrocatalyst was assessed using cyclic voltammetry in a non-Faradaic region (0 ~ 0.1 V vs. Hg/Hg2SO4) at scan rates of 20, 40, 60, 80, and 100 mV s−1. Based on a plot of the difference between anodic and cathodic current densities at the mid-potential (0.05 V vs. Hg/Hg2SO4) vs. the scan rate, the resulting linear slope was twice the value of Cdl.

18O isotope-labelled experiments

The 18O isotope-labeled experiments were conducted in two sealed compart electrolyzers with proton exchange membrane separated (Fig. S15)3, 4. A Hg/Hg2SO4 electrode and a Pt mesh were used as reference electrode and counter electrode, respectively. The working electrodes were prepared by coating our nanocatalyst powder on CP and dried in a vacuum oven. Firstly, the catalysts on the working electrode (anode) were activated by performing 10 CV cycles at 2 mV s-1 in an 18O-labelled H2SO4 electrolyte in a potential window of 0.3~0.9 V vs. Hg/Hg2SO4, resulting in the 18O-labelled surface oxygen. The working electrodes were carefully and thoroughly washed using 16O-H2O and dried in a vacuum oven. Then blow the Ar gas for 20 min to eliminate the pollution gas and the electrolyzer was tightly sealed. After that, an oxygen gas sample (100μL) produced at the anode cell was collected using a syringe needle when conducting the chronoamperometry experiments at 5 mA cm-2. Injecting in the gas chromatograph mass spectrometer (GC-MS) system (YL 6900, YL instrument CO., LTD. Korea) to determine the composition of gas products and the relative ratio of 34O2 (18O16O), 36O2 (18O18O), and 32O2 (16O16O) signals, which can reflect the LOM level during the OER on our catalysts.

Calculation methods

The spin-polarized DFT calculations were performed to investigate the structural properties of the catalysts in the Vienna ab initio simulation package (VASP)5. The generalized gradient approximation (GGA) along with the revised Perdew-Burke-Ernzerhof (RPBE) function was used to account for electron exchange and correction, and the cut of the plane-wave kinetic energy was 450 eV. The DFT + D3 correction was employed to describe the van der Waals interaction. A vacuum layer of around 15 Å was employed to avoid interactions between periodic slab images. A periodic slab model of the RuO2 (110) surface was constructed using 2*3 surface supercells with four metal-oxide layers, resulting in a chemical composition of Ru48O96. Corresponding tensile strain (5 %) is applied by changing the lattice constant. Then a series of models were established in this work, including undoped RuO2 (110), TS-RuO2 (110), Sr/Ta co-doped RuO2 (110), and Sr/Ta co-doped TS-RuO2 (110) surfaces. The k-point grid was set to 3*2*1 for geometry optimization and electronic properties calculations. Energy and force convergence were set to 10-5 eV and -0.05 eV/Å, respectively. In the electrocatalytic simulation process, the lattice strain was fixed in these slab models. All simulation processes adopt the same optimization parameters and keep the lattice constant.

To investigate the activity of AEM (adsorbate evolution mechanism) and LOM (a lattice-oxygen-mediate mechanism), the Gibbs free energy changes (ΔG) were calculated using the computational hydrogen electrode (CHE) 6 model:

ΔG = ΔE + ΔZPE + ∫CpdT - TΔS

where ΔE is the difference of electron energies obtained from DFT calculations. ΔZPE, ∫CpdT, and ΔS are the change in zero-point energy, enthalpic temperature correction, and the entropy difference, respectively.

Fig. S1| Schematic diagram of synthesizing the RuO2-x with tensile strain and electronic modifications via a molten salt assistant quench process. This strategy presents attractive advantages for the formation of uniform high-crystal and small-sized nanocatalysts.

Fig. S2| HRTEM images (a,b) and HAADF-STEM with corresponding EDS mapping images (c) of RuO2-x. d Rendered HRTEM image, inset is selected area electron diffraction (SEAD) patterns (110 facet), below is intensity profiles along white line and (e) GPA contour map of the strain components εxx, εxy, and εyy relative to the RuO2-x reference values on the surface of RuO2-x.

Fig. S3| HRTEM images (a,b) and HAADF-STEM with corresponding EDS mapping images (c) of TS-RuO2-x. d Rendered HRTEM image, inset is selected area electron diffraction (SEAD) patterns (110 facet), below is intensity profiles along white line and (e) GPA contour map of the strain components εxx, εxy, and εyy relative to the RuO2-x reference values on the surface of TS-RuO2-x. The lattice of (110)  is expanded to 0.328 nm,  combined with GPA confirms the tensile strain of about 5 %.

Fig. S4| HRTEM images (a,b) and HAADF-STEM with corresponding EDS mapping images (c) of TS-Sr0.1Ru0.9O2-x. d Rendered HRTEM image, inset is selected area electron diffraction (SEAD) patterns (110 facet), below is intensity profiles along white line and (e) GPA contour map of the strain components εxx, εxy, and εyy relative to the RuO2-x reference values on the surface of TS-Sr0.1Ru0.9O2-x.

Fig. S5| HRTEM images (a,b) and HAADF-STEM with corresponding EDS mapping images (c) of TS-Ta0.1Ru0.9O2-x. d Rendered HRTEM image, inset is selected area electron diffraction (SEAD) patterns (110 facet), below is intensity profiles along white line and (e) GPA contour map of the strain components εxx, εxy, and εyy relative to the RuO2-x reference values on the surface of TS-Ta0.1Ru0.9O2-x.

Fig. S6| HRTEM images (a,b) and HAADF-STEM with corresponding EDS mapping images (c) of Sr0.1Ta0.1Ru0.8O2-x. d Rendered HRTEM image, inset is selected area electron diffraction (SEAD) patterns (110 facet), below is intensity profiles along white line and (e) GPA contour map of the strain components εxx, εxy, and εyy relative to the RuO2-x reference values on the surface of Sr0.1Ta0.1Ru0.8O2-x.

Fig. S7| XRD patterns with local magnificent (110) peak of all strained catalysts.

Fig. S8| a,b O 1s and Ru 3d XPS spectra of all strained catalysts. c,d Sr 3d XPS spectra of all Sr doped samples, e,f Ta 4f XPS spectra of all Ta doped samples. The tensile strain has less effect on the peaks shifting, whereas co-doped Sr and Ta redistribute the local electrons among Sr-Ru-Ta groups since more electrons are transferred to nearby O and Ru.

Fig. S9| a,b Corresponding EXAFS fitting curve of all catalysts in k spaces, respectively. c,d The Ru K-edge XANES and EXAFS spectra of TS-RuO2-x, TS-Sr0.1Ru0.9O2-x, TS-Ta0.1Ru0.9O2-x, and TS-Sr0.1Ta0.1Ru0.8O2-x catalysts with those of r-Ru, r-RuCl3, and, r-RuO2 references, showing the vibration of Ru valence states on doped samples and elongated Ru-O and Ru-O-M bonding in strained samples. In addition, the case of Sr and Ta co-doping induces the suitable modulation of the valence state of Ru.

Fig. S10| The Sr K-edge XANES (a,b) and EXAFS spectra (e,f) of all Sr-doped catalysts. The Ta K-edge XANES (c,d) and EXAFS spectra (g,h) of all Ta-doped catalysts. Sr and Ta co-dopants interplay on electronic and bonding structure.

Fig. S11|  The CV curves (scan rate of 2 mV/s) of the Pt electrode in a hydrogen-saturated 0.5 M H2SO4 with Pt counter and Hg/Hg2SO4 reference electrode.

Fig. S12| a,b Tafel plots of all prepared RuO2-x catalysts obtained from the geometry-normalized LSV curves. c,d Mass-normalized (Ru mass) LSV curves of all prepared RuO2-x catalysts, which indicates that compared to the tensile strain, Sr and Ta co-doping induce more favorable electronic modulations, resulting in superior mass activity.

Fig. S13| CV curves (0-0.1 V vs. Hg/Hg2SO4) of all as-synthesized RuO2-x catalysts were obtained at various scan rates in 0.5 M H2SO4 electrolyte, and corresponding double-layer capacitance (Cdl) obtained based on the scan rate and current density gap at a 0.05 V vs. Hg/Hg2SO4.

Fig. S14| a,c,e,g Geometry-normalized LSV curves of Sr0.1Ta0.1Ru0.8O2-x, TS-Sr0.1Ru0.9O2-x, TS-Ta0.1Ru0.9O2-x, and TS-Sr0.1Ta0.1Ru0.8O2-x electrodes in various pH-H2SO4 electrolytes, b,d,f,h Corresponding curves of overpotentials-dependent pH values at 5, 10, 20 mA cm-2, respectively. Those suggest tensile strained samples show the almost no-pH dependent relation, mainly lowering the possibility of the LOM pathway.

Fig. S15| a Schematic diagram and (b) sealed electrolyzer photo of the isotopic oxygen (18O) labeling experiments process for detecting the LOM portion and related O2 composition.

Fig. S16| a,b The GC and MS spectra measured from GC-MS equipment of standard gas. The GC and MS spectra measured when injecting gas collected on (c,d) c-RuO2, (e,f) RuO2-x, and (g,h) Sr0.1Ta0.1Ru0.8O2-x electrodes, showing the different intensity of 34O2 (18O16O) and 36O2 (18O18O) but similar 32O2 (16O16O) signals.

Fig. S17| The GC and MS spectra measured when injecting gas collected on (a,b) TS-RuO2-x, (c,d) TS-Sr0.1Ru0.9O2-x, (e,f) TS-Ta0.1Ru0.9O2-x, and (g,h) TS-Sr0.1Ta0.1Ru0.8O2-x electrodes, showing the different intensity of 34O2 (18O16O) and 36O2 (18O18O) but similar 32O2 (16O16O) signals and further suggesting the reduced LOM possibility on strained catalysts.

Fig. S18| a In-situ ATR-SEIRAS spectra measured on TS-Sr0.1Ta0.1Ru0.8O2-x electrode in D2O based electrolyte from open circuit potential to 1.6 V (vs. RHE). b In-situ ATR-SEIRAS absorption intensity comparison of *OOD intermediates on RuO2-x, TS-RuO2-x, and TS-Sr0.1Ta0.1Ru0.8O2-x electrodes in H2O-based electrolyte, which illustrates that the higher AEM catalysts ability on TS-Sr0.1Ta0.1Ru0.8O2-x electrodes. In-situ ATR-SEIRAS spectra were measured in H2O and D2O, along with the comparison among every signal at 1.6 V on (c,d,e) RuO2-x and (f,g,h) TS-RuO2-x.

Fig. S19| a ICP-OES measured dissolved concentration curves of Ru from RuO2-x with and without strain working electrodes, demonstrating the stability improvement induced by the lattice expansion. b Standard curves of O2 gas measured on GC equipment. c,d,e Collected O2 gas and theoretical gas amount at 10 mA cm-2 on TS-RuO2-x, Sr0.1Ta0.1Ru0.8O2-x, and TS-Sr0.1Ta0.1Ru0.8O2-x electrodes, which shows the selectivity as high as 100 % on our electrodes.

Fig. S20| a,b O 1s and Ru 3d XPS spectra on RuO2-x and TS-RuO2-x samples before and after OER reaction. c,d Ta 4f and Sr 3d XPS spectra on strained or without strained samples before and after reaction. The higher proportion of OH and Vo on post-reaction samples reflects the O sites are active for deprotonation, and slightly riched Ru>4+ species suggest the improved stability on strained catalysts.

Fig. S21| a,c,e The Ru K-edge, Sr K-edge, and Ta K-edge XANES and (b,d,f ) EXAFS spectra of TS-Sr0.1Ta0.1Ru0.8O2-x before and after reaction, showing the reasonable increase of Ru valence states induced by the OER reaction and almost unchanged Ru-O bonding.

Fig. S22| HRTEM images (a,b) and HAADF-STEM with corresponding EDS mapping images (c) of post-TS-Sr0.1Ta0.1Ru0.8O2-x. d Rendered HRTEM image, inset is selected area electron diffraction (SEAD) patterns (110 facet), below is intensity profiles along white line and (e) GPA contour map of the strain components εxx, εxy, and εyy relative to the RuO2-x reference values on the surface of post-TS-Sr0.1Ta0.1Ru0.8O2-x. The lattice of (110) remains at 0.324 nm, combined with GPA confirms the tensile strain is well preserved.

Fig. S23| a,c,e In-situ EIS spectra and (b,d,f) corresponded bode plots on c-RuO2, RuO2-x, and TS-RuO2-x electrodes measured from 1.0 to 1.5 V (vs. RHE) with 50 mV amplitude in 0.5 M H2SO4. No evidence supporting the promotion of strain on activity can be found due to that compared to RuO2-x the even higher phase angle is achieved on TS-RuO2-x.

Fig. S24| a,c,e,g In-situ EIS spectra and (b,d,f,h) corresponded bode plots on Sr0.1Ta0.1Ru0.8O2-x, TS-Sr0.1Ru0.9O2-x, TS-Ta0.1Ru0.9O2-x, and TS-Sr0.1Ta0.1Ru0.8O2-x, electrodes measured from 1.0 to 1.5 V (vs. RHE) with 50 mV amplitude in 0.5 M H2SO4.

Fig. S25| a,b Simulated Q1R1 values on c-RuO2, RuO2-x, TS-RuO2-x, Sr0.1Ta0.1Ru0.8O2-x, and TS-Sr0.1Ta0.1Ru0.8O2-x catalysts. Simulated (c,d) Q1R1 and (e,f) Q2R2 values of doped catalysts. Those comparisons evidence that the enhanced OER activity mainly originated from the co-doping of Sr and Ta, in terms of lower R1 and R2, as well as much higher Q2.

Fig. S26| a,b,c,d The built configurations with oxygen vacancy (VO) on RuO2-x, TS-RuO2-x, Sr0.1Ta0.1Ru0.8O2-x, and TS-Sr0.1Ta0.1Ru0.8O2-x catalysts surface. e Corresponded VO formation energy. It suggests the strain significantly increases the VO formation energy, even though the co-doping also does, similar to the experimental investigations.

Fig. S27| a,b Calculated AEM mechanism energy barrier diagrams on Sr0.1Ta0.1Ru0.8O2-x (g) and TS-RuO2-x (f) configurations. This higher overpotential of LOM on TS-RuO2-x reflects a suppressed LOM pathway due to the presence of tensile strain.

Fig. S28| The theoretical configurations during calculating AEM pathway energy barrier diagrams on RuO2-x catalyst.

Fig. S29| The theoretical configurations during calculating LOM pathway energy barrier diagrams on RuO2-x catalyst.

Fig. S30| The theoretical configurations during calculating AEM pathway energy barrier diagrams on TS-RuO2-x catalyst.

Fig. S31| The theoretical configurations during calculating LOM pathway energy barrier diagrams on TS-RuO2-x catalyst.

Fig. S32| The theoretical configurations during calculating AEM pathway energy barrier diagrams on Sr0.1Ta0.1Ru0.8O2-x catalyst.

Fig. S33| The theoretical configurations during calculating LOM pathway energy barrier diagrams on Sr0.1Ta0.1Ru0.8O2-x catalyst.

Fig. S34| The theoretical configurations during calculating AEM pathway energy barrier diagrams on TS-Sr0.1Ta0.1Ru0.8O2-x catalyst.

Fig. S35| The theoretical configurations during calculating LOM pathway energy barrier diagrams on TS-Sr0.1Ta0.1Ru0.8O2-x catalyst.

Table S1 Performance summary of recently reported representative OER catalysts in the acidic electrolyte (η10: the overpotential at 10 mAcm-2).

| Catalysts | Electrolyte | η10 (mV) | Tafel Slope (mV/dec) | Stability (Voltage-Time) | Reference |
| --- | --- | --- | --- | --- | --- |
| RuO2-x | 0.5M H2SO4 | 243 | 154.5 | 300 h @ 10 mA cm-2 | This work |
| TS-RuO2-x | 0.5M H2SO4 | 210 | 57.5 | 1000 h @ 10 mA cm-2 | This work |
| Ta0.1Sr0.1Ru0.8O2-x | 0.5M H2SO4 | 183 | 67.9 | 300 h @ 10 mA cm-2 | This work |
| TS-Ta0.1Sr0.1Ru0.8O2-x | 0.5M H2SO4 | 166 | 56.6 | 1000 h @ 10 mA cm-2 | This work |
| Li0.52RuO2 | 0.5M H2SO4 | 156 | 83.3 | 70 h @ 10 mA cm-2 | Nat. Commun, 2022, 13(1): 3784. |
| Ru5W1Ox | 0.5M H2SO4 | 227 | 42 | 550 h @ 10 mA cm-2 | Nat. Commun, 2022, 13(1): 4871. |
| Ni-RuO2 | 0.1 M HClO4 | 214 | 42.6 | 200 h @ 10 mA cm-2 | Nat. Mater., 2023, 22(1): 100-108. |
| W0.2Er0.1Ru0.7 O2−δ | 0.5M H2SO4 | 168 | 66.8 | 500 h @ 10 mA cm-2 | Nat. Commun, 2020, 11(1): 5368. |
| PtCo–RuO2/C | 0.1 M HClO4 | 212.6 | 48.5 | 20 h @ 10 mA cm-2 | Energy Environ. Sci., 2022, 15(3): 1119-1130. |
| TaxTmyIr1−x−y O2−δ | 0.5M H2SO4 | 198 | 64 | 500 h @ 10 mA cm-2 | Nat. Nano., 2021, 16(12): 1371-1377. |
| SS Pt­RuO2 | 0.5M H2SO4 | 228 | 51.0 | 100 h @ 10 mA cm-2 | Sci. Adv., 2022, 8(9): eabl9271. |
| 3R-IrO2 | 0.1 M HClO4 | 188 | 52 | 500 h @ 10 mA cm-2 | Joule, 2021, 5(12): 3221-3234. |
| RuO2 NSs | 0.5M H2SO4 | 199 | 38.2 | 6 h @ 10 mA cm-2 | Energy Environ. Sci., 2020, 13(12): 5143-5151 |
| Ru/MnO2 | 0.1 M HClO4 | 161 | 29.4 | 200 h @ 10 mA cm-2 | Nat. Catal, 2021, 4(12): 1012-1023. |
| Re0.06Ru0.94O2 | 0.1 M HClO4 | 190 | 45.5 | 200 h @ 10 mA cm-2 | Nat. Commun, 2023, 14(1): 1-11. |
| Rh-RuO2/G | 0.5M H2SO4 | 161 | 45.8 | 700 h @ 50 mA cm-2 | Nat. Commun, 2023, 14(1): 1412. |
| Ru/RuS2-2 | 0.5M H2SO4 | 201 | 47.2 | 24 h @ 50 mA cm-2 | Angew. Chem. Int. Ed., 2021, 133(22): 12436-12442. |
| Ir-MnO2 | 0.5M H2SO4 | 181 | 87.4 | 180 h @ 10 mA cm-2 | Adv. Sci., 2023: 2205920. |
| Ir–MnO2 | 0.5M H2SO4 | 218 | 59.61 | 700 h @ 10 mA cm-2 | Joule, 2021, 5(8): 2164-2176. |
| Ir/Nb2O5−x | 0.5M H2SO4 | 218 | 52.3 | 105 h @ 10 mA cm-2 | Angew. Chem. Int. Ed., 2022: e202212341. |
| Ir1-Co3O4-NS-350 | 0.5M H2SO4 | 226 | 74.4 | 500 h @ 10 mA cm-2 | ACS Catal, 2023, 13: 3757-3767. |
| Nd0.1RuOx | 0.5M H2SO4 | 211 | 50 | 25 h @ 10 mA cm-2 | Adv. Funct. Mater., 2023: 2213304. |
| IrO2@TaB2 | 0.1 M HClO4 | 288 | 42.6 | 120 h @ 10 mA cm-2 | Nat. Commun, 2023, 14(1): 5119. |
| Ba0.3(SO4)δW0.2Ru0.5O2−δ | 0.5M H2SO4 | 206 | 43.3 | 1000 h @ 10 mA cm-2 | Nat. Commun., 2023, 14(1): 8093. |
| py-RuO2:Zn | 0.5M H2SO4 | 173 | 41.2 | 1000 h @ 10 mA cm-2 | Nat. Commun, 2023, 14(1): 2517. |
| (Ru–W)Ox | 0.5M H2SO4 | 170 | 46.2 | 300 h @ 10 mA cm-2 | Adv. Mater., 2023: 2305939 |
| Al-doped RuOx | 0.5M H2SO4 | 192 | 48 | 300 h @ 10 mA cm-2 | Chem, 2023, 9(12): 3600-3612. |
| BixEr2-xRu2O7 | 0.1 M HClO4 | 180 | 51.3 | 100 h @ 10 mA cm-2 | Nat. Commun, 2022, 13(1): 4106. |
| Ru/Se-RuO2 | 0.5M H2SO4 | 190 | 43.7 | 24 h @ 10 mA cm-2 | Adv. Funct. Mater., 2023: 2211102. |

Table S2 Elemental composition analysis measured by the HAADF-STEM EDS and XPS.

|  | HAADF-STEM-EDS (at %) |  |  |  | XPS (at %) |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Elements Samples | Sr | Ta | Ru | O | Sr | Ta | Ru | O |
| Sr0.1Ta0.1Ru0.8O2-x | 2.86 | 2.62 | 34.65 | 59.87 | 1.33 | 1.216 | 25.989 | 71.465 |
| TS-Sr0.1Ta0.1Ru0.8O2-x | 3.02 | 2.51 | 36.1 | 58.37 | 1.48 | 1.247 | 26.43 | 70.843 |
| TS-Sr0.1Ru0.9O2-x | 3.43 |  | 32.67 | 63.9 | 1.632 |  | 26.347 | 72.021 |
| TS-Ta0.1Ru0.9O2-x |  | 2.53 | 36.63 | 60.84 |  | 1.229 | 27.191 | 71.58 |
| Post-TS-Sr0.1Ta0.1Ru0.8O2-x | 2.8 | 2.45 | 35.02 | 59.73 | 1.196 | 1.153 | 26.52 | 71.131 |

Table S3 The fitted parameters of the in-situ EIS data of c-RuO2 catalyst for OER in 0.5 M H2SO4.

| Potential (vs. RHE) | Rs(Ω) | Q1(F) | Q1-n | R1(Ω) | Q2 (F) | Q2-n | R2(Ω) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1.00 | 2.074 | 0.0021 | 0.8923 | 86310 | 0.0037 | 0.5840 | 64.90 |
| 1.05 | 2.095 | 0.0021 | 0.8960 | 70560 | 0.0039 | 0.8000 | 63.59 |
| 1.10 | 2.093 | 0.0030 | 0.9051 | 52130 | 0.0042 | 0.5183 | 62.88 |
| 1.15 | 2.098 | 0.0026 | 0.9072 | 36980 | 0.0047 | 0.5714 | 61.41 |
| 1.20 | 2.101 | 0.0053 | 0.6013 | 30250 | 0.0029 | 0.9029 | 61.10 |
| 1.25 | 2.103 | 0.0030 | 0.9098 | 25800 | 0.0053 | 0.5711 | 60.96 |
| 1.30 | 2.101 | 0.0030 | 0.9103 | 18390 | 0.0053 | 0.5729 | 60.61 |
| 1.35 | 2.103 | 0.0033 | 0.9142 | 5894 | 0.0058 | 0.5704 | 60.48 |
| 1.40 | 2.104 | 0.0040 | 0.8884 | 891 | 0.0075 | 0.8838 | 60.14 |
| 1.45 | 2.055 | 0.0046 | 0.4142 | 343 | 0.0079 | 0.6771 | 59.25 |
| 1.50 | 2.061 | 0.0047 | 0.4298 | 65.5 | 0.0088 | 0.7000 | 58.94 |

Table S4 The fitted parameters of the in-situ EIS data of RuO2-x catalyst for OER in 0.5 M H2SO4.

| Potential (vs. RHE) | Rs(Ω) | Q1(F) | Q1-n | R1(Ω) | Q2 (F) | Q2-n | R2(Ω) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1.00 | 2.403 | 0.0216 | 0.8983 | 62210 | 0.0668 | 0.4759 | 43.23 |
| 1.05 | 2.429 | 0.0276 | 0.9087 | 53425 | 0.0782 | 0.4992 | 40.21 |
| 1.10 | 2.451 | 0.0288 | 0.8852 | 49820 | 0.0895 | 0.4753 | 39.09 |
| 1.15 | 2.528 | 0.0345 | 0.8799 | 35460 | 0.1063 | 0.4709 | 35.19 |
| 1.20 | 2.574 | 0.0457 | 0.4550 | 24610 | 0.1279 | 0.8791 | 29.5 |
| 1.25 | 2.582 | 0.0679 | 0.8673 | 15840 | 0.1387 | 0.4492 | 28.21 |
| 1.30 | 2.588 | 0.0707 | 0.8818 | 2678 | 0.1557 | 0.4643 | 27.73 |
| 1.35 | 2.591 | 0.1103 | 0.8981 | 354 | 0.1676 | 0.4674 | 26.41 |
| 1.40 | 2.588 | 0.1557 | 0.4466 | 25.14 | 0.1884 | 0.8237 | 25.02 |
| 1.45 | 2.596 | 0.1574 | 0.8000 | 8.831 | 0.1976 | 0.8025 | 8.94 |
| 1.50 | 2.618 | 0.1673 | 0.8352 | 2.828 | 0.1972 | 0.8000 | 7.33 |

Table S5 The fitted parameters of the in-situ EIS data of TS-RuO2-x catalyst for OER in 0.5 M H2SO4.

| Potential (vs. RHE) | Rs(Ω) | Q1(F) | Q1-n | R1(Ω) | Q2 (F) | Q2-n | R2(Ω) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1.00 | 2.190 | 0.0207 | 0.9159 | 14140 | 0.0641 | 0.5083 | 31.56 |
| 1.05 | 2.186 | 0.0620 | 0.8000 | 11033 | 0.0727 | 0.8000 | 26.83 |
| 1.10 | 2.179 | 0.0745 | 0.9158 | 9413 | 0.0864 | 0.5224 | 24.2 |
| 1.15 | 2.167 | 0.1057 | 0.5006 | 6793 | 0.1051 | 0.9048 | 23.8 |
| 1.20 | 2.183 | 0.1328 | 0.7270 | 4565 | 0.1354 | 0.8542 | 22.1 |
| 1.25 | 2.171 | 0.1475 | 0.9185 | 1284 | 0.1634 | 0.8000 | 20.15 |
| 1.30 | 2.138 | 0.1760 | 0.8899 | 845 | 0.1769 | 0.4221 | 13.54 |
| 1.35 | 2.163 | 0.1776 | 0.5178 | 68.4 | 0.1884 | 0.9265 | 9.16 |
| 1.40 | 2.143 | 0.2007 | 0.8539 | 18.18 | 0.1915 | 0.8000 | 1.74 |
| 1.45 | 2.143 | 0.1905 | 0.8718 | 6.227 | 0.2003 | 0.9505 | 0.62 |
| 1.50 | 2.150 | 0.1925 | 0.9031 | 2.34 | 0.2032 | 0.4878 | 0.50 |

Table S6 The fitted parameters of the in-situ EIS data of TS-Ta0.1Ru0.9O2-x catalyst for OER in 0.5 M H2SO4.

| Potential (vs. RHE) | Rs(Ω) | Q1(F) | Q1-n | R1(Ω) | Q2 (F) | Q2-n | R2(Ω) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1.00 | 2.022 | 0.0109 | 0.6367 | 81540 | 0.0050 | 0.9333 | 43.9 |
| 1.05 | 1.998 | 0.0420 | 0.8723 | 65320 | 0.0290 | 0.8000 | 42.94 |
| 1.10 | 1.995 | 0.0490 | 0.8796 | 51540 | 0.0295 | 0.8585 | 32.98 |
| 1.15 | 1.982 | 0.0560 | 0.8683 | 38565 | 0.0484 | 0.5537 | 27.64 |
| 1.20 | 1.968 | 0.0605 | 0.8547 | 30254 | 0.0751 | 0.9000 | 18.37 |
| 1.25 | 1.937 | 0.0622 | 0.8752 | 21940 | 0.0729 | 0.5681 | 17.64 |
| 1.30 | 1.956 | 0.0670 | 0.5229 | 8540 | 0.0748 | 0.8651 | 16.56 |
| 1.35 | 1.970 | 0.0740 | 0.8927 | 2010 | 0.0827 | 0.5866 | 14.89 |
| 1.40 | 1.907 | 0.0971 | 0.8367 | 154.8 | 0.1225 | 0.4254 | 10.56 |
| 1.45 | 1.957 | 0.1069 | 0.9667 | 12.55 | 0.1430 | 0.5689 | 7.49 |
| 1.50 | 1.913 | 0.1240 | 0.6947 | 4.779 | 0.1520 | 0.9457 | 5.314 |

Table S7 The fitted parameters of the in-situ EIS data of TS-Sr0.1Ru0.9O2-x catalyst for OER in 0.5 M H2SO4.

| Potential (vs. RHE) | Rs(Ω) | Q1(F) | Q1-n | R1(Ω) | Q2 (F) | Q2-n | R2(Ω) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1.00 | 3.177 | 0.0361 | 0.4583 | 6127 | 0.0299 | 0.9107 | 46.21 |
| 1.05 | 3.178 | 0.0516 | 0.8461 | 4812 | 0.0330 | 0.9103 | 38.6 |
| 1.10 | 3.168 | 0.0906 | 0.4480 | 3307 | 0.0363 | 0.9038 | 25.79 |
| 1.15 | 3.142 | 0.1253 | 0.8124 | 2540 | 0.0494 | 0.8981 | 21.05 |
| 1.20 | 3.137 | 0.1714 | 0.8970 | 1834 | 0.1545 | 0.3843 | 18.13 |
| 1.25 | 3.133 | 0.2015 | 0.9007 | 778 | 0.2561 | 0.8000 | 16.14 |
| 1.30 | 3.143 | 0.2264 | 0.9089 | 552 | 0.2985 | 0.4067 | 14.38 |
| 1.35 | 3.144 | 0.2334 | 0.4143 | 19.18 | 0.3019 | 0.9052 | 13.1 |
| 1.40 | 3.252 | 0.2438 | 0.9001 | 11.30 | 0.3661 | 0.6896 | 5.54 |
| 1.45 | 3.149 | 0.2593 | 0.4546 | 1.58 | 0.4247 | 0.8505 | 3.075 |
| 1.50 | 3.163 | 0.2545 | 0.4196 | 0.82 | 0.4257 | 0.9419 | 1.119 |

Table S8 The fitted parameters of the in-situ EIS data of TS-Sr0.1Ta0.1Ru0.8O2-x catalyst for OER in 0.5 M H2SO4.

| Potential (vs. RHE) | Rs(Ω) | Q1(F) | Q1-n | R1(Ω) | Q2 (F) | Q2-n | R2(Ω) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1.00 | 3.030 | 0.0273 | 0.8672 | 3290 | 0.0989 | 0.5502 | 16.48 |
| 1.05 | 3.047 | 0.0605 | 0.8700 | 1683 | 0.1059 | 0.5445 | 13.62 |
| 1.10 | 3.056 | 0.0807 | 0.5854 | 945.8 | 0.1244 | 0.8986 | 12.5 |
| 1.15 | 3.056 | 0.1252 | 0.5646 | 565.5 | 0.1801 | 0.8759 | 8.36 |
| 1.20 | 3.057 | 0.1768 | 0.8423 | 321.4 | 0.2036 | 0.5071 | 5.42 |
| 1.25 | 3.052 | 0.2045 | 0.7429 | 165.3 | 0.2964 | 0.6415 | 3.54 |
| 1.30 | 3.067 | 0.2426 | 0.9161 | 111.7 | 0.3847 | 0.5775 | 2.67 |
| 1.35 | 3.062 | 0.2558 | 0.5904 | 22.62 | 0.4621 | 0.9161 | 1.72 |
| 1.40 | 3.053 | 0.3054 | 0.4946 | 3.39 | 0.4835 | 0.8560 | 1.47 |
| 1.45 | 3.020 | 0.3369 | 0.8618 | 1.26 | 0.4606 | 0.3807 | 1.13 |
| 1.50 | 3.045 | 0.3417 | 0.8892 | 0.47 | 0.4711 | 0.3858 | 0.64 |

Table S9 The fitted parameters of the in-situ EIS data of Sr0.1Ta0.1Ru0.8O2-x catalyst for OER in 0.5 M H2SO4.

| Potential (vs. RHE) | Rs(Ω) | Q1(F) | Q1-n | R1(Ω) | Q2 (F) | Q2-n | R2(Ω) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1.00 | 2.445 | 0.0326 | 0.8675 | 4535 | 0.0483 | 0.8000 | 20.69 |
| 1.05 | 2.484 | 0.0366 | 0.8725 | 2678 | 0.0700 | 0.8001 | 18.61 |
| 1.10 | 2.489 | 0.0418 | 0.8721 | 1955 | 0.0925 | 0.8073 | 16.16 |
| 1.15 | 2.486 | 0.0549 | 0.8740 | 1294 | 0.1359 | 0.8954 | 14.44 |
| 1.20 | 2.490 | 0.0843 | 0.9515 | 993 | 0.2582 | 0.8765 | 13.54 |
| 1.25 | 2.480 | 0.1015 | 0.8766 | 675 | 0.3408 | 0.5805 | 11.50 |
| 1.30 | 2.451 | 0.1542 | 0.6463 | 423.5 | 0.3605 | 0.8689 | 7.77 |
| 1.35 | 2.452 | 0.1643 | 0.8793 | 300.6 | 0.4554 | 0.8492 | 5.50 |
| 1.40 | 2.468 | 0.1960 | 0.8550 | 19.38 | 0.4668 | 0.5846 | 3.81 |
| 1.45 | 2.480 | 0.2236 | 0.7704 | 2.1 | 0.4784 | 0.8735 | 2.20 |
| 1.50 | 2.540 | 0.2350 | 0.8676 | 1.51 | 0.5050 | 0.7714 | 0.68 |

Reference

1.	Gu K, et al. Defect-Rich High-Entropy Oxide Nanosheets for Efficient 5-Hydroxymethylfurfural Electrooxidation. Angew Chem Int Ed Engl 60, 20253-20258 (2021).

2.	Liu Y, et al. Unveiling the Protonation Kinetics-Dependent Selectivity in Nitrogen Electroreduction: Achieving 75.05 % Selectivity. Angew Chem Int Ed Engl 61, e202209555 (2022).

3.	Zhang N, et al. Lattice oxygen activation enabled by high-valence metal sites for enhanced water oxidation. Nat Commun 11, 4066 (2020).

4.	Wen Y, et al. Stabilizing Highly Active Ru Sites by Suppressing Lattice Oxygen Participation in Acidic Water Oxidation. J Am Chem Soc 143, 6482-6490 (2021).

5.	Kresse G, Furthmuller J. Efficient iterative schemes for ab initio total-energy calculations using a plane-wave basis set. Phys Rev B 54, 11169-11186 (1996).

6.	Norskov JK, et al. Origin of the overpotential for oxygen reduction at a fuel-cell cathode. J Phys Chem B 108, 17886-17892 (2004).