Activation Behavior of 4-AcNH-TEMPO by ClO2 for Selective Oxidation of Cellulose in DMAc/LiCl System

Yao Zhao a, Xueping Wang a, Tian Si a, Xin Gao a, b, *, Lincai Peng a, *, Heng Zhang a, *

a Faculty of Chemical Engineering, Kunming University of Science and Technology, Kunming 650500, Yunnan, China

b CAS Key Laboratory of Magnetic Materials and Devices, Ningbo Institute of Materials Technology and Engineering, Chinese Academy of Sciences, Ningbo 315201, Zhejiang, People’s Republic of China.

E-mail: drgaoxin@sina.com, penglincai@kust.edu.cn, zhangheng0625@sina.com

Table S1. Reaction Conditions for the 4-AcNH-TEMPO/ClO2 Homogeneous Selective Oxidation of Cellulose were Investigated with Varying Amounts of Chlorine Dioxide.

| Amount of ClO2 (mmol/g) (OC) | Amount of 4-AcNH-TEMPO (mmol/g) | Concentration of cellulose (%) | Oxidation temperature (℃) | Oxidation time (h) |
| --- | --- | --- | --- | --- |
| 2 | 0.3 | 0.2 | 25 | 72 |
| 4 |  |  |  |  |
| 6 |  |  |  |  |
| 8 |  |  |  |  |
| 10 |  |  |  |  |

Table S2. Reaction Conditions for the 4-AcNH-TEMPO/ClO2 Homogeneous Selective Oxidation of Cellulose were Investigated with Varying Amounts of 4-AcNH-TEMPO.

| Amount of ClO2 (mmol/g) | Amount of 4-AcNH-TEMPO (mmol/g) (TEMPO) | Concentration of cellulose (%) | Oxidation temperature (℃) | Oxidation time (h) |
| --- | --- | --- | --- | --- |
| 10 | 0 | 0.2 | 25 | 72 |
|  | 0.05 |  |  |  |
|  | 0.1 |  |  |  |
|  | 0.2 |  |  |  |
|  | 0.3 |  |  |  |
|  | 0.4 |  |  |  |

Table S3. Reaction Conditions for the 4-AcNH-TEMPO/ClO2 Homogeneous Selective Oxidation of Cellulose were Investigated with Varying Concentration of Cellulose.

| Amount of ClO2 (mmol/g) | Amount of 4-AcNH-TEMPO (mmol/g) | Concentration of cellulose (%) (C) | Oxidation temperature (℃) | Oxidation time (h) |
| --- | --- | --- | --- | --- |
| 10 | 0.3 | 0.1 | 25 | 72 |
|  |  | 0.2 |  |  |
|  |  | 0.3 |  |  |
|  |  | 0.4 |  |  |
|  |  | 0.5 |  |  |
|  |  | 0.6 |  |  |

Table S4. Reaction Conditions for the 4-AcNH-TEMPO/ClO2 Homogeneous Selective Oxidation of Cellulose were Investigated with Varying Oxidation Temperature.

| Amount of ClO2 (mmol/g) | Amount of 4-AcNH-TEMPO (mmol/g) | Concentration of cellulose (%) | Oxidation temperature (℃) (T) | Oxidation time (h) |
| --- | --- | --- | --- | --- |
| 10 | 0.3 | 0.2 | 15 | 72 |
|  |  |  | 20 |  |
|  |  |  | 25 |  |
|  |  |  | 30 |  |
|  |  |  | 35 |  |
|  |  |  | 40 |  |

Table S5. Reaction Conditions for the 4-AcNH-TEMPO/ClO2 Homogeneous Selective Oxidation of Cellulose were Investigated with Varying Oxidation Temperature.

| Amount of ClO2 (mmol/g) | Amount of 4-AcNH-TEMPO (mmol/g) | Concentration of cellulose (%) | Oxidation temperature (℃) | Oxidation time (h) (Time) |
| --- | --- | --- | --- | --- |
| 10 | 0.3 | 0.2 | 25 | 12 |
|  |  |  |  | 24 |
|  |  |  |  | 36 |
|  |  |  |  | 48 |
|  |  |  |  | 60 |
|  |  |  |  | 72 |
|  |  |  |  | 96 |
|  |  |  |  | 120 |