Highly active Fenton-like catalyst derived from solid waste-iron tailings using wheat straw pyrolysis

Lihui Gao1; Lizhang Wang1; Shulei Li2*; Yijun Cao2,3*

- School of Environment and Spatial Informatics, China University of Mining and Technology, Xuzhou 221116, China

- National Engineering Research Center of Coal Preparation and Purification, China University of Mining and Technology, Xuzhou 221116, China

- School of Chemical Engineering and Technology, Zhengzhou University, Zhengzhou 450001, China

Table S1 Characteristics of wheat straw and iron tailings

| Proximate analysis | Wheat straw (Raw biomass) Average wt% |  |
| --- | --- | --- |
| Volatile matter | 86.09 |  |
| Fixed carbon | 9.27 |  |
| Ash | 4.64 |  |
| XRF analysis | Wheat straw （Raw biomass） | Iron tailings |
|  | Average wt% |  |
| SiO2 | 4.35 | 41.21 |
| Fe2O3 | 0.264 | 29.25 |
| Al2O3 | 0.337 | 9.47 |
| CaO | 0.443 | 7.105 |
| MgO | 0.235 | 5.31 |
| Ba | - | 3.62 |
| K2O | 2.369 | 1.73 |
| Cl | 0.905 | - |
| S | 0.181 | 1.23 |
| Mn | 0.0502 | 0.41 |
| TiO2 | 0.024 | 0.35 |
| Na2O | 0.072 | 0.15 |
| Sr | - | 0.0762 |
| P | 0.0721 | 0.057 |

Table S2 The metal ion concentration in leaching test

| Metals | Concentration (ppb) |  |  |
| --- | --- | --- | --- |
|  | 1st | 2nd | 3rd |
| Li | 7.07 | 1.77 | 3.67 |
| Na | 1051.94 | 468.46 | 1592.07 |
| Mg | 393.97 | 257.27 | 474.06 |
| Al | 84.62 | 34.04 | 86.94 |
| K | 1131.30 | 569.80 | 2299.87 |
| Ca | 4706.97 | 2423.60 | 2993.95 |
| V | 2.07 | 1.13 | 1.29 |
| Cr | 1.10 | 0.40 | 0.82 |
| Mn | 25.50 | 19.29 | 29.91 |
| Fe | 88.78 | 85.07 | 92.67 |
| Ni | 0.82 | 0.24 | 2.05 |
| Cu | 3.27 | 1.29 | 4.17 |
| Zn | 1.27 | 0.28 | 3.47 |
| Ga | 0.08 | 0.10 | 0.15 |
| As | 0.59 | 0.32 | 0.33 |
| Rb | 3.99 | 1.39 | 2.87 |
| Sr | 60.76 | 49.57 | 86.80 |
| Ag | 0.02 | 0.03 | 0.03 |
| Cd | 0.04 | 0.14 | 0.14 |
| Cs | 1.93 | 0.88 | 1.04 |
| Ba | 331.78 | 239.93 | 422.94 |
| Pb | 0.23 | 0.57 | 1.00 |

Figure S1 The SEM image of synthesized RT-900-60, scale bar=10 μm (a) and I/W(3:1)-900-60, scale bar=10 um, insert image scale bar=3 um (b)

Figure S2 Characterization of the prepared catalysts by N2 adsorption-desorption: (a) Pore size distribution; (b) adsorption-desorption isotherm

Figure S3 Stability and reusability of I/W(3:1)-900-60 for the degradation of MB

Figure S4 (a) XRD patterns of fresh and used I/W(3:1)-900-60; (b) SEM image of used I/W(3:1)-900-60 ([MB]=60 mg/L, [catalyst]=0.3 g/L, [H2O2]=16 mmol/L)