Supporting Information

A preprogrammed force field generated in a confined space enables external-module-free anisotropic

vat-photopolymerization 3D printing

Satoshi Honda*

Department of Basic Science, Graduate School of Arts and Sciences, The University of Tokyo, 3-8-1 Komaba, Meguro-ku, Tokyo 153–8902, Japan.

| Table 1. Size characteristics of mica flakes. |  |  |  |
| --- | --- | --- | --- |
| Mica | Size (m)a | Aspect ratiob | d (g mL-1)c |
| A-11 | 3 | N/A | 0.11 |
| A-21S | 23 | 70 | 0.13 |
| AB-25S | 24 | 80 | 0.17 |
| J-31M | 35 | 75 | 0.20 |
| Y-1800 | 10 | 70 | 0.15 |
| Y-2300X | 19 | 60 | 0.16 |
| Y-3000 | 23 | 80 | 0.25 |
| aAveraged particle size, determined based on laser diffraction particle size analysis, provided from the manufacturer. bAspect ratio, provided from the manufacturer. cBulk density, provided from the manufacturer. |  |  |  |

Figure S1. SEM image of (a, b) CPMCAB-25S, (c, d) CPMCA-21S, and (e, f) CPMCY-3000 fabricated with the thickness of each layer to be cured during 3DP as 25 m. The images were taken to observe the distribution of mica flakes in the (a, c, e) xy-plane and (b, d, f) yz-plane.

Figure S2. SEM image of (a, b) CPMCY-2300, (c, d) CPMCY-1800 fabricated with the thickness of each layer to be cured during 3DP as 25 m. The images were taken to observe the distribution of mica flakes in the (a, c) xy-plane and (b, d) yz-plane.

Figure S3. SEM image of CPMCA-11 fabricated with the thickness of each layer to be cured during 3DP as 10 m. The images were taken to observe the distribution of mica flakes in the (a) xy-plane and (b) yz-plane.

Figure S4. Stress–strain curves of (a) BT, (b) CPMCA-11, (c) CPMCA-21S, (d) CPMCAB-25S, (e) CPMCJ-31M, (f) CPMCY-1800, (g) CPMCY-2300X, (h) CPMCY-3000 measured in three different (L, T, and P) directions.