Supplementary Information for

Direct bonding and debonding of 2D semiconductors

Jieying Liu1,2†, Jiaojiao Zhao1,2,3†, Lu Li2,3, Zheng Wei2, Jiawei Li2, Qinqin Wang2, Hua Yu1, Lanying Zhou1, Tong Li1, Fanfan Wu2,3, Mingtong Zhu2, Huacong Sun2, Yutong Chen1, Yun Li1, Songge Zhang1, Jinpeng Tian2, Xuedong Bai2, Nianpeng Lu2, Zexian Cao2, Shenghuang Lin1, Shuopei Wang1, Luojun Du2,3, Wei Yang2,3, Dongxia Shi2,3, Na Li1 & Guangyu Zhang1,2,3*

1 Songshan Lake Materials Laboratory; Dongguan, Guangdong 523808, China.

2 Beijing National Laboratory for Condensed Matter Physics and Institute of Physics, Chinese Academy of Sciences; Beijing 100190, China.

3 School of Physical Sciences, University of Chinese Academy of Sciences; Beijing 100190, China.

†These authors contributed equally to this work

*Corresponding author. Email: gyzhang@iphy.ac.cn OR gyzhang@sslab.org.cn

Supplementary Note 1. Pick-up of epitaxial MoS2 assisted by PMMA

The dry transfer method assisted by PMMA18 requires a lower adhesion between 2D materials and substrate than that between 2D materials and PMMA. When we apply this method on epitaxially grown MoS2 on sapphire with strong adhesion, the transfer is failed and as-obtained films is fragmented as shown in Fig. S1.

Figure S1 PMMA-assisted pick-up of epitaxial MoS2 grown on sapphire. a, Optical micrograph of MoS2/sapphire after PMMA-assisted peeling, vast bright area is MoS2 films left behind after peeling. b, Optical micrograph of MoS2/PMMA after PMMA-assisted peeling, bright area is fragmented MoS2 films transferred onto PMMA.

Supplementary Note 2. Debonding process

During debonding, the stress exerted on films is affected by critical energy release rate (Gc) of the cracked interface. In interface fracture mechanics, Gc is influenced by mode-mixity, debonding loading rate, and temperature. Mode-mixity phase angle is: ψ =tan-1(σsσn), where σn (σs) is the normal (shear) component of traction. ψ = 0° and 90° corresponds to pure mode-I (σs = 0) and mode-Ⅱ (σn = 0) fracture, respectively. During crack propagation, Gc increases monotonously with the growth of mode-mix phase angle28–30. The double cantilever beam (DCB) mode I fracture applied in our debonding process (Movie S1), which have been used for the large area dry transfer of graphene and bismuth films24,25, can effectively reduce Gc and shear stress during delamination.

In DCB fracture, the fracture toughness is influenced by displacement loading rate, low loading rate (~2 μm/s) leads to smaller strain energy release rate G, which ensures a stable crack propagation and a lower level of shear stress31,32. In contrast, the wafer delaminated under rapid exfoliation shows countless cracks caused by unstable crack propagation and high shear stress (Fig. S2). The exfoliating temperature also dramatically influences Gc. Debonding under low temperature (room temperature) increases Gc, leading to higher G, causing unstable crack propagation. As shown in Fig. S3, bilayer MoS2 wafer obtained by exfoliating under room temperature shows many cracks (crack kinks occurred during unstable crack propagation), while bilayer MoS2 wafer obtained by debonding under 90 ℃ doesn’t (Fig. 1e, right). This is probably because higher temperature induces thermal strain and thermal ripple effect42–44 which in turn leads to reduction of fadhesion.

Figure S2 Optical micrographs of bilayer MoS2 wafer obtained by bonding and debonding, in which debonding is performed under 90 ℃ with high displacement loading rate (~ 50 μm/s).

Figure S3 Photograph of bilayer MoS2 wafer obtained by bonding and debonding, in which debonding is performed with low loading rate but under room temperature.

Supplementary Note 3. Homo-bonding and debonding

For the bonding-debonding of 2D materials with identical adhesion force to their substrates, we add a spherical epoxy gasket between the top pressure plate and graphite gasket (Extended Data Fig. 3a) to form a slightly domed indenter. With the aid of spherical gasket, a warpage is induced in bonded samples (Extended Data Fig. 3b) and sustains until after debonding.

Consider a small fraction of bilayer MoS2 film between the delaminated area and bonded area, it is subjected to tractions from film in delaminated area (σd) and bonded area (σb), and tangential tractions from top sapphire (τtop) and bottom sapphire (τbottom). During delamination, the MoS2 in delaminated area (strain released area, εd) and bonded area (tensile strain area, εb) have different strain, namely εd<εb thus σd<σb. Before delamination of this area, balanced force requires τtop>τbottom, which means the shear stress in the interface between bilayer MoS2 and top sapphire is larger than that between bilayer MoS2 and bottom sapphire, hence the top interface is delaminated first. Thus, the employ of a domed top indenter facilitates unidirectional transfer of MoS2 from top sapphire to bottom MoS2/sapphire.

The bonding-debonding results of bilayer MoS2/sapphire with and without spherical epoxy gasket is shown in Extended Data Fig. 3c, which verifies the importance of domed indenter in bonding-debonding transfer of 2D materials with identical adhesion force to their substrates.

Supplementary Note 4. SHG determination of twist angles in tBLMs

Consider a tBLMs film with twisted angle of β and laser electric field polarization direction of α, the generated SH electric field is E1(2ω) and E2(2ω) from the first layer and second layer. By superposition, the total SH electric field Et(2ω) can then be obtained: Et(2ω) = E1(2ω) + E2(2ω). The SH intensity of first layer (|E1(2ω)|2) and bilayer |Et(2ω)|2 can be calculated

|E1(2ω)|2 = |E1(2ω)|2cos2 (3α)

|Et(2ω)|2 = |E1(2ω)|2(cos2 (3α) +cos2(3α+3β) +2cos(3α)cos(3α+3β).

As shown in Fig. S4 the simulated SHG pattern, 30° tBLMs SHG petals rotated 15° compared to monolayer SHG petals.

Figure S4 Calculated SHG patterns of monolayer MoS2 and 30° tBLMs.

References from Supplementary Information

42.	Chang, Z., Yang, R. & Wei, Y. The linear-dependence of adhesion strength and adhesion range on temperature in soft membranes. J. Mech. Phys. Solids 132, 103697 (2019).

43.	Costamagna, S., Neek-Amal, M., Los, J. H. & Peeters, F. M. Thermal rippling behavior of graphane. Phys. Rev. B 86, 041408 (2012).

44.	Meyer, J. C. et al. The structure of suspended graphene sheets. Nature 446, 60–63 (2007).