Supplementary Information for

Direct bonding and debonding of 2D semiconductors

Jieying Liu1,2†, Jiaojiao Zhao1,2,3†, Lu Li2,3, Zheng Wei2, Jiawei Li2, Qinqin Wang2, Hua Yu1, Lanying Zhou1, Tong Li1, Fanfan Wu2,3, Mingtong Zhu2, Huacong Sun2, Yutong Chen1, Yun Li1, Songge Zhang1, Jinpeng Tian2, Xuedong Bai2, Nianpeng Lu2, Zexian Cao2, Shenghuang Lin1, Shuopei Wang1, Luojun Du2,3, Wei Yang2,3, Dongxia Shi2,3, Na Li1 & Guangyu Zhang1,2,3*

1 Songshan Lake Materials Laboratory; Dongguan, Guangdong 523808, China.

2 Beijing National Laboratory for Condensed Matter Physics and Institute of Physics, Chinese Academy of Sciences; Beijing 100190, China.

3 School of Physical Sciences, University of Chinese Academy of Sciences; Beijing 100190, China.

†These authors contributed equally to this work

*Corresponding author. Email: gyzhang@iphy.ac.cn OR gyzhang@sslab.org.cn

Table of Contents

Supplementary Notes

Supplementary Note 1. 	Pick-up epitaxial MoS2 assisted by PMMA ....................  3

Supplementary Note 2. 	Debonding process...........................................................  3

Supplementary Note 3. 	Homo-bonding and debonding.........................................  4

Supplementary Note 4. 	SHG determination of twist angles in tBLMs..................  5

Supplementary Figures

Supplementary Figure 1.	PMMA-assisted pick-up of epitaxial MoS2 grown

on sapphire........................................................................  3

Supplementary Figure 2.	Optical micrographs of bilayer MoS2 wafer obtained by bonding and debonding....................................................  4

Supplementary Figure 3.	Photograph of bilayer MoS2 wafer obtained by bonding        and debonding..................................................................  4

Supplementary Figure 4.	Calculated SHG patterns of monolayer MoS2 and 30° tBLMs..............................................................................  5

Supplementary Movie 1 Double cantilever beam debonding process

References