Supplementary Information

Oscillatory mechanoluminescence of SrZnOS: Mn2+ in dynamic response to rapid compression

Hao Wang1, Tingting Zhao1, Mei Li1, Junlong Li1, Ke Liu1, Shang Peng1, Xuqiang Liu1, Bohao Zhao1, Yanlong Chen1, Jiao An1, Xiaohui Chen2, Sheng Jiang3, and Chuanlong Lin1, Wenge Yang1

1Center for High Pressure Science and Technology Advanced Research, Beijing 100093, China

2Institute of Fluid Physics, China Academy of Engineering Physics, Mianyang 621900, China

3Shanghai Institute of Applied Physics, Chinese Academy of Sciences, Shanghai 201203, China

*Email: chuanlong.lin@hpstar.ac.cn

Supplementary Figure 1 | Characterization of the structure, morphology and elements of SrZnOS: Mn2+. a, Powder XRD patterns of pure SrZnOS, SrZnOS:1%Mn2+ and refinement of the XRD pattern. b, Schematic diagram of the crystal structure of hexagonal SrZnOS. c, The morphology and elemental analysis of the synthesized samples.

Supplementary Figure 2 | PL spectra of Mn-doped and undoped SrZnOS. The emission peak of the undoped sample lies at 525 nm that comes from the oxygen or Zn vacancies, whereas the emission peak of the Mn-doped sample is located at 608 nm (λex=375 nm).

Supplementary Figure 3 | Rate-dependent ML behavior. ML spectra of Mn-doped SrZnOS as a function of pressure (or time) at different compression rates at room temperature, presenting temporal characteristics. The PL peaks around 695 nm (marked by “*”) come from ruby.

Supplementary Figure 4 | Rate dependent total ML intensity. Total ML intensities at different compression rate. a, 0.28-1.04 GPa/s; b, 1.25-3.82 GPa/s at room temperature.

Supplementary Figure 5 | Temperature dependent ML of SrZnOS: Mn2+. ML of SrZnOS: Mn2+ during continuous compression process at different compression rates and temperatures.

Supplementary Figure 6 | In-situ high-pressure Raman spectra. a, High-pressure Raman spectra of SrZnOS with 532 nm laser. b, The Raman peaks as a function of pressure.

Supplementary Figure 7 | Pressure-induced PL properties of SrZnOS: Mn2+. a, PL spectra and b, peak position of Mn-doped SrZnOS as a function of pressure.

Supplementary Table 1 | Structural parameters obtained from the refinementr for SrZnOS.

Supplementary Figure 8 | Refinement of the XRD patterns. The refined XRD patterns of SrZnOS at selected pressures of 3.1 GPa, 11.3 GPa and 18.3 GPa.

Supplementary Figure 9 | Bond length of Zn (or Mn)-S/O as a function of pressure.

Supplementary Figure 10 | Decay curve and lifetime of PL for SrZnOS: Mn2+ excited by a 375 nm laser at various pressures.

Supplementary Figure 11 | TL properties of SrZnOS: Mn2+. a, TL intensity at various excitation temperatures and b, the trap-depth distribution in SrZnOS: Mn2+.

Supplementary Figure 12 | Dynamic ML response. a, ML intensity during stepwise compression process and b, ML emission during multi-cyclic compression-decompression processes.

Supplementary Figure 13 | ML emission under compression at different onset pressure.

Supplementary Movies 1−7

Supplementary references

Reference

1.	Liu, W. et al. Synthesis and characterization of sulfide oxide SrZnSO with strongly polar crystal structure. J. Solid State Chem. 246, 225-229 (2017).

2.	Toby, B. H. EXPGUI, a graphical user interface for GSAS. J. Appl. Crystallogr. 34, 210−213 (2001).

3.	Van den Eeckhout, K. et al. Revealing trap depth distributions in persistent phosphors. Phys. Rev. B 87, 045126 (2013).

4.	Xiong, P. & Peng, M. Visible to near-infrared persistent luminescence from Tm3+- doped two-dimensional layered perovskite Sr2SnO4. J. Mater. Chem. C 7, 8303–8309 (2019).