Supplementary information (SI)

Advanced Catalytic Approaches for Synthesizing 1,2-dihydro-1-aryl-3H-naphtho[1,2-e]-[1,3]oxazin-3-one Derivatives through Electrophilic Substitution Reactions using Mono- and Bimetallic Phosphate Catalysts: A Study of Co₃(PO₄)₂ and CoCa₃(HPO₄)(PO₄)₂(OH)

Achraf EL HALLAOUI1 *, Nouhaila FERRAA1, Yousssef MERROUN1, Soukaina CHEHAB2, Said BOUKHRIS1, Mounia Bennani Ziatni1, Hicham HASSOUNE3, Abdelaziz SOUIZI1 and Rachida GHAILANE1

1Organic Chemistry, Catalysis, and Environment Laboratory, University of Ibn Tofail, Faculty of Sciences, Po Box 133, 14000 Kenitra, Morocco

2Higher Institute for Nursing Professions and Health Techniques of Rabat-Annex Kenitra- Ministry of Health and Social Protection, Morocco

3Department of Chemical and Biochemical Sciences (CBS), Mohammed VI Polytechnic University (UM6P), Hay Moulay Rachid Ben Guerir, 43150, Morocco

Email: achraf.el.hallaoui@uit.ac.ma

Figure s1. XRD spectrum of Co3(PO4)2 catalyst

Figure s2. FTIR spectrum of Co3(PO4)2 catalyst

| C K |  |  |  |  |  | 2.9 |  |  |  |  |  |  | 5.8 |  | 4.2 |  |  |  | 34.7 |  |  |  | 0.0057 |  |  | 1.1447 |  |  |  | 0.9213 |  |  |  | 0.1728 |  |  |  |  |  |  | 1.0000 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| O K |  |  |  |  |  | 41.7 |  |  |  |  |  |  | 62.3 |  | 162.5 |  |  |  | 10.2 |  |  |  | 0.1077 |  |  | 1.0987 |  |  |  | 0.9445 |  |  |  | 0.2351 |  |  |  |  |  |  | 1.0000 |  |  |
| P K |  |  |  |  |  | 18.7 |  |  |  |  |  |  | 14.4 |  | 303.5 |  |  |  | 4.8 |  |  |  | 0.1382 |  |  | 0.9648 |  |  |  | 1.0032 |  |  |  | 0.7575 |  |  |  |  |  |  | 1.0105 |  |  |
| CaK |  |  |  |  |  | 13.5 |  |  |  |  |  |  | 8.0 |  | 166.4 |  |  |  | 4.4 |  |  |  | 0.1242 |  |  | 0.9505 |  |  |  | 1.0331 |  |  |  | 0.9383 |  |  |  |  |  |  | 1.0349 |  |  |
| CoK |  |  |  |  |  | 23.2 |  |  |  |  |  |  | 9.4 |  | 118.0 |  |  |  | 4.7 |  |  |  | 0.2014 |  |  | 0.8301 |  |  |  | 1.0599 |  |  |  | 0.9951 |  |  |  |  |  |  | 1.0491 |  |  |

Figure s3. SEM/EDAX analysis of Co3(PO4)2 catalyst

Figure s4. XRD spectrum of CoCa3(HPO4)(PO4)2(OH)

Figure s5. FTIR spectrum of CoCa3(HPO4)(PO4)2(OH)

Table s1. Elemental analysis of the prepared support

| Ref. Ech | P2O5 | Co | CaO |
| --- | --- | --- | --- |
|  | w.t % | w.t % | w.t % |
| Prepared Support | 46.31 | 19.61 | 36.92 |