Supporting Information

Flexible and efficient perovskite quantum dot solar cells via hybrid interfacial architecture

Long Hu,2,3 Qian Zhao,4 Shujuan Huang,3 Jianghui Zheng,5,7 Xinwei Guan,2 Robert Patterson,5 Jiyun Kim,2 Lei Shi,5 Chun-Ho Lin,2 Qi Lei,2 Dewei Chu,2 Wan Tao,2 Soshan Cheong,6 Richard D. Tilley,6 Anita W. Y. Ho-Baillie,5,7 Joseph M. Luther,8 Jianyu Yuan,1,* and Tom Wu2

1Institute of Functional Nano & Soft Materials (FUNSOM), Jiangsu Key Laboratory for Carbon-Based Functional Materials & Devices, Soochow University, Suzhou, Jiangsu 215123, P. R. China.

2School of Materials Science and Engineering, University of New South Wales (UNSW), Sydney, NSW, 2052, Australia.

3School of Engineering, Macquarie University, Sydney, NSW 2109, Australia

4 School of Materials Science and Engineering, Nankai University, Tianjin 300350, China.

5Australian Centre for Advanced Photovoltaics, University of New South Wales, Sydney, Australia

6Electron Microscope Unit, Mark Wainwright Analytical Centre, UNSW, Sydney, NSW, 2052, Australia.

7School of Physics, University of Sydney Nano Institute, The University of Sydney, NSW, 2006, Australia.

8National Renewable Energy Laboratory, Golden, CO 80401, USA.

*To whom correspondence should be addressed. E-mail: jyyuan@suda.edu.cn

Figure S1. The TEM images of CsPbI3 CQDs from (a) control and (b) PCBM/QD hybrid solutions.

Figure S2. Steady state PL spectra of pristine, control and hybrid CsPbI3 QD films

Figure S3. Time-resolved PL spectra of pristine, control and hybrid CsPbI3 QD films

Figure S4. Cross-sectional SEM images of (a) control and (b) target devices.

Figure S5. The J-V curves of target and control device under reverse and forward scanning.

Figure S6. Stability of corresponding CsPbI3 QD solar cells under dark conditions in a dry air atmosphere.

Figure S7. Contact angle of a water drop on the control and the hybrid films.

Figure S8. EIS curves of champion control and target devices (inset: equivalent circuit).

Figure S9. Dark current curves of the control and target devices

Figure S10. Transient photocurrent (a) and photovoltage (b) curves in optimal control and target devices.

Figure S11. (a) Ultraviolet photoelectron spectroscopy (UPS) cutoff edge (b) Valence band spectra of CsPbI3 film, SnO2 film and PCBM film from UPS measurements.

Figure S12. Bandgap of (a) three types of films (b) SnO2 film.

Figure S13. XPS signals of Cs 3d/5.

Figure S14. SEM images of (a) control CsPbI3 QD and (b) PCBM@CsPbI3 QD hybrid films, scale bar: 1 µm

Figure S15. AFM height images of the control and the hybrid films.

Figure S16. Jsc, Voc and FF of flexible CsPbI3 QD (a) and CsPbI2Br bulk film devices as a function of bending cycles.

Figure S17. Image of bending robot and flexible films.

Table S1. Statistics of CsPbI3 QD solar cell performance with varied QD absorber layers based on 24 devices for each condition

| Hybrid:Control | Voc (V) | Jsc (mA∙cm-2) | FF | PCE (%) |
| --- | --- | --- | --- | --- |
| 0:3 | 1.24 (1.21±0.02) | 11.4 (11.0±0.8) | 0.74 (0.72±0.03) | 10.5 (9.6±0.4) |
| 0:4 | 1.23 (1.22±0.02) | 13.6 (13.3±0.7) | 0.74 (0.73±0.02) | 12.4 (11.9±0.4) |
| 0:5 | 1.22 (1.20±0.03) | 13.4 (13.1±0.8) | 0.72 (0.72±0.03) | 11.8 (11.6±0.5) |
| 1:3 | 1.26 (1.24±0.04) | 13.9 (13.5±0.8) | 0.76 (0.74±0.03) | 13.3 (12.4±0.7) |
| 1:4 | 1.26 (1.24±0.03) | 15.2 (14.4±0.9) | 0.78 (0.76±0.03) | 15.1 (14.6±0.6) |
| 1:5 | 1.22 (1.20±0.05) | 14.4 (13.9±1.0) | 0.74 (0.72±0.04) | 13.0 (12.0±0.7) |
| 2:3 | 1.25 (1.23±0.05) | 13.9 (14.1±1.0) | 0.72 (0.73±0.04) | 13.8 (13.1±0.8) |
| 2:4 | 1.23 (1.19±0.05) | 13.8 (13.2±1.1) | 0.71 (0.69±0.04) | 12.1 (10.8±0.9) |

Table S2. Summary of device information, efficiency and stability of CsPbI3-QD solar cells and flexible QD solar cells reported so far.

| Device architecture | QDs | Rigid device PCE | Flexible device PCE | Reference |
| --- | --- | --- | --- | --- |
| FTO/TiO2/QDs/spiro-OMeTAD/MoOx/Al | CsPbI3 | 10.77% | - | Science 354 (2016) 92. |
| FTO/TiO2/QDs/spiro-OMeTAD/MoOx/Al | CsPbI3 | 13.4% | - | Sci. Adv. 3 (2017) eaao4204. |
| FTO/TiO2/QDs/spiro-OMeTAD/MoOx/Al | CsPbI3 | 13.47% | - | ACS Nano 12 (2018) 10327. |
| FTO/TiO2/QDs/PTB7/MoO3/Ag | CsPbI3 | 12.55% | - | Joule 2 (2018) 2450. |
| FTO/TiO2/QDs/PTAA/Au | CsPbI3 | 11.64% | - | Adv. Energy Mater. 8 (2018) 1800007. |
| ITO/TiO2/QDs/spiro-OMeTAD/MoOx/Al | CsPbI3 | 13.67% | - | Nat. Commun. 10 (2019) 2842. |
| FTO/TiO2 /QDs /PTAA /MoOx/Ag | CsPbI3 | 12.30% | - | ACS Energy Lett. 4 (2019) 2571. |
| FTO/TiO2/QDs/spiro-OMeTAD/MoOx/Ag | CsPbI3 | 12.40% | - | Nano Energy 66 (2019) 104130. |
| FTO/TiO2 /QDs /PTAA/MoO3/Ag | CsPbI3 | 14.1% | - | Adv. Energy Mater. 9 (2019) 1900721. |
| FTO/TiO2 /QDs/PTB7 /MoO3/Ag | CsPbI3 | 12.27% | - | J. Mater. Chem. A 7 (2019) 20936. |
| FTO/c-TiO2/QDs/spiro-OMeTAD/Au | CsPbI3 | 11.87% | - | Adv. Funct. Mater. 29 (2019) 1900991. |
| ITO/SnO2/QDs/spiro-OMeTAD/Au | CsPbI3 | 9.6% | - | Nat. Energy 5 (2020) 79. |
| FTO/TiO2/QDs/spiro-OMeTAD/Au | CsPbI3 | 14.32% | - | J. Am. Chem. Soc. 142 (2020) 3775. |
| FTO/TiO2 /QDs/QD:Polymer/PTAA/MoO3/Ag | CsPbI3 | 13.8% | - | J. Mater. Chem. A 8 (2020) 8104. |
| FTO/TiO2 /QDs /PTAA/MoO3/Ag | CsPbI3 | 15.2% |  | Adv. Mater. 32 (2020) 2001906. |
| FTO/TiO2 /QDs /PTAA/MoO3/Ag | CsPbI3 | 14.9% |  | Adv. Mater. 32 (2020) 2000449. |
| PET/ITO/ZnMgO/QDs/PbS-EDT/Au | PbS | - | 9.4% | ACS Nano 8 (2017) 8478. |
| PEN/Ag NWs/AZO/QDs/PbS-EDT/Au | PbS | - | 9.9% | Energy Environmental Sci. 11 (2018) 354. |
| PET/ITO/ZnO/QDs/PbS-EDT/Au | PbS | - | 5.1% | Adv. Energy. Mater. 8 (2018) 1700809. |
| PET/ITO/TiO2/QDs/MoO3/Al | PbS | - | 1.8% | Energy Environmental Sci. 6 (2013) 1565. |
| Glass (PET)/ITO/ SnO2/QD:PCBM/QDs/ PTB7/MoO3/Ag | CsPbI3 | 15.1% | 12.3% | This Work |