Table (1) Chemical analysis and oxides composition of dry Egyptian Ordinary Portland Cement powder

| Oxides | Oxides Concentration, % (mass/mass) | Oxide Compounds | Oxide Compounds Mass Fraction, (%) |
| --- | --- | --- | --- |
| SiO2 | 19.84 | 3CaO − SiO2 (C3S) tricalcium silicate | 53.11 |
| Al2O3 | 4.74 | 2CaO − SiO2 (C2S) dicalcium silicate | 16.89 |
| Fe2O3 | 4.0 | 3CaO − Al2O3 (C3A) tricalcium aluminate | 5.81 |
| CaO | 61.01 | 4CaO − Al2O3− Fe2O3 (C4AF) tetracalcium aluminoferrite | 12.16 |
| MgO | 2.5 |  |  |
| K2O | 0.6 |  |  |
| SO3 | 2.4 |  |  |
| Na2O | 0.5 |  |  |
| Others | 4.41 |  | 12.03 |

Loss on ignition (LOI): ≈3.96 %       Specific gravity (g/cm3) =3.26 g/cm3

Table (2) Impact of F/T weathering on some physical characterization of the GCC	   	final waste forms as function of the freeze/thaw cycles

| F/T, cycles | M, % | A, % | B, g/cm3 | C, % |
| --- | --- | --- | --- | --- |
| 0 | 82.14 | 16.13 | 2.10 | 70.88 |
| 15 | 90.10 | 8.71 | 1.98 | 66.24 |
| 30 | 93.91 | 12.58 | 1.97 | 67.22 |
| 45 | 95.63 | 14.13 | 1.97 | 68.57 |
| 90 | 94.54 | 15.40 | 2.01 | 62.23 |

Table (3) XR-D Peak positions and abbreviations for the most interesting phases of the granite-cement composite after freeze/thaw treatment

| Phases | abbreviation | Peak, 2 θ° |
| --- | --- | --- |
| Portlandite | CH | 17.98-27.86- 33.97-46.964 |
| Calcium silicate hydrate | C-S-H | overlapped with CH ≈ 28 &≈ 34 |
| Calcite | CC | 22.93- 29.36-36.46-43.08-48.39-64.02 |
| Gypsite | GY | 15.75,26.566-44.707 |
| Ettringite | E | Near 9-10 & confused with 49.98 |
| Quartz | Q | 21.836-39.297-59.754 |

Table (4): The portlandite average crystallite size and, the mean distance between   	      the closest neighbouring chains as function of freeze /thaw cycles

| F/T, cycle | D, ηm | <R>, Å |
| --- | --- | --- |
| 15 | 12.93 | 5.1 |
| 30 | 13.35 | 5.2 |
| 45 | 13.12 | 5.1 |
| 90 | 13.33 | 5.2 |

Table (5) Impact of increasing freeze/ thaw cycles on the thermal behavior and mass losses of the granite-cement composite based on thermal analyses

| Freeze-thaw, cycles | Peak array | Temperature of decomposition peak, ° C |  |  | Mass loss at maximum ,% | Total mass loss*, % |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | On -set | Maximum | Off- set |  |  |
| 15 | first | 84.30 | 124.03 | 196.94 | 2.32 | 17.78 |
|  | second | 437.39 | 467.79 | 492.63 | 15.02 |  |
| 30 | first | 72.38 | 138.76 | 168.40 | 6.30 | 19.45 |
|  | second | 482.58 | 491.34 | 507.04 | 16.42 |  |
| 45 | first | 75.18 | 131.92 | 188.59 | 2.93 | 16.64 |
|  | second | 483.49 | 489.00 | 496.75 | 11.36 |  |
| 90 | first | 107.58 | 128.71 | 147.04 | 1.49 | 9.45 |
|  | second | 480.26 | 485.02 | 489.98 | 6.69 |  |

* at ~600 °C.