Table 1

Colloidal properties of rGO and Mg/rGO NCs prepared by both CH and MI methods

| Ζf (mV) | PDI (μ2/Ƭ2)e |  | D(nm) |  | P (W)a | T (°C) | Sample |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | DLSd | SEMc | XRDb |  |  |  |
| +32.1 | 0.377 | 62.19 | 9-11 | 15.73 | - | 35 | rGO |
| -25.5 | 0.444 | 171.9 | 14-18 | 16.86 | - | 90 | Mg/rGO NCs (H) |
| -15.8 | 1.132 | 289.3 | 11-13 | 26.88 | 900 | - | Mg/rGO NCs (M) |

a Power of microwave irradiation.

b Theoretical diameter calculated by Origin software based on Scherrer's equation.

c Particle mean diameter measured by SEM.

d Hydrodynamic diameter measured by DLS in water.

e Polydispersity index based on DLS.

f Zeta potential.

Table 2

The influence of different concentrations of rGO NPs and Mg/rGO NCs on growth parameters of M. longifolia

|  | Length (mm) |  |  |  | Number (per explants) | Treatments (mg/L) |
| --- | --- | --- | --- | --- | --- | --- |
| The tallest root | The smallest shoot | Roots | Shoots | Leaves | Nodes |  |
| 27.95 ± 11.24 a | 4.60 ± 2.40 c | 4.50 ± 0.71 a | 5.00 ± 0.00 a | 33.00 ± 1.41 a | 18.00 ± 1.41 a | Control |
| 20.73 ± 8.37 abc | 9.37 ± 1.45 ab | 4.00 ± 0.00 ab | 4.33 ± 0.58 bc | 21.33 ± 6.11 bcd bcd | 12.33 ± 3.21 bcd bcd | 25 rGO |
| 11.43 ± 3.45 bcd bcd | 6.83 ± 1.45 bc | 3.67 ± 0.58 ab | 4.00 ± 0.00 bc | 18.33 ± 2.08 cd | 11.00 ± 1.00 cd | 50 rGO |
| 9.10 ± 3.14 cd | 7.00 ± 1.32 bc | 3.00 ± 0.00 b | 4.00 ± 0.00 bc | 15.00 ± 1.73 d | 8.67 ± 1.15 d | 100 rGO |
| 7.15 ± 2.62 d | 6.45 ± 2.19 bc | 3.00 ± 0.00 b | 3.50 ± 0.71 c | 14.50 ± 2.12 d | 9.00 ± 1.41 d | 150 rGO |
| 22.63 ± 7.67 ab | 5.20 ± 0.85 c | 4.33 ± 1.15 a | 4.67 ± 0.58 ab | 31.33 ± 5.13 a | 16.67 ± 2.52 a | 25 NCs |
| 22.77 ± 8.14 ab | 5.70 ± 0.52 c | 3.67 ± 0.58 ab | 4.33 ± 0.58 bc | 26.00 ± 5.29 abc | 14.67 ± 2.89 abc | 50 NCs |
| 19.10 ± 5.40 bcd | 7.03 ± 2.26 bc | 3.33 ± 0.58 ab | 5.00 ± 0.00 a | 29.00 ± 0.00 ab | 16.00 ± 0.00 ab | 100 NCs |
| 13.10 ± 0.99 bcd bcd | 10.20 ± 0.14 a | 4.00 ± 0.00 ab | 4.50 ± 0.71 bc | 29.00 ± 0.00 ab | 16.00 ± 0.00 ab | 150 NCs |

Values represent mean ± standard error (SE). Means followed by the same letters within each column are not significantly different (P=0.05) using Duncan’s comparison mean test (n=3).

Table 3

The influence of rGO NPs and Mg/rGO NCs on the production of photosynthetic pigments of the regenerated shoots M. longifolia

| Carotenoids (mg/g fw) |  | Chlorophyll b (mg/g fw) |  | Chlorophyll a (mg/g fw) |  | Treatments (mg/L) |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.10 ± 0.00 d | 0.14 ± 0.01 cd |  | 0.37 ± 0.01 d |  | Control |  |
| 0.07 ± 0.01 e | 0.07 ± 0.02 ef |  | 0.29 ± 0.00 e |  | 25 rGO |  |
| 0.05 ± 0.00 f | 0.08 ± 0.02 f |  | 0.14 ± 0.01 f |  | 50 rGO |  |
| 0.10 ± 0.00 d | 0.12 ± 0.02 d |  | 0.34 ± 0.01 d |  | 100 rGO |  |
| 0.05 ± 0.00 f | 0.05 ± 0.09 f |  | 0.14 ± 0.01 f |  | 150 rGO |  |
| 0.13 ± 0.00 b | 0.20 ± 0.01 a |  | 0.42 ± 0.01 c |  | 25 NCs |  |
| 0.16 ± 0.01 a | 0.15 ± 0.02 bc |  | 0.56 ± 0.04 a |  | 50 NCs |  |
| 0.14 ± 0.00 b | 0.17 ± 0.02 ab |  | 0.50 ± 0.03 b |  | 100 NCs |  |
| 0.12 ± 0.00 c | 0.12 ± 0.00 d |  | 0.36 ± 0.01 d |  | 150 NCs |  |

Values represent mean ± standard error (SE). Means followed by the same letters within each column are not significantly different (P=0.05) using Duncan’s comparison mean test (n=3).

Table 4 Composition of the volatile compounds of the untreated and treated shoot cultures of M. longifolia with rGO and Mg/rGO NCs

| RIb | RIa | RT | Classification |  |  |  |  |  | Percentage of compounds in treatments |  | Constituent | Raw |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Mg/RGO 100 mg/L | Mg/RGO 50 mg/L | Mg/RGO 25 mg/L | RGO 100 mg/L | RGO 50 mg/L | RGO 25 mg/L | Control |  |  |
| 930 | 928 | 6.62 | Hydrocarbon monoterpene | _ | _ | 0.72 | _ | _ | _ | _ | α-Thujene | 1 |
| 939 | 938 | 6.81 | Hydrocarbon monoterpene | _ | _ | 16.48 | _ | _ | _ | _ | α-Pinene | 2 |
| 947 | 939 | 6.86 | Aromatic hydrocarbon | _ | _ | 0.31 | _ | _ | _ | _ | Allyl benzene | 3 |
| 952 | 956 | 7.17 | Hydrocarbon monoterpene | _ | _ | 0.96 | _ | _ | _ | _ | Sabinene | 4 |
| 979 | 982 | 7.71 | Hydrocarbon monoterpene | _ | 0.04 | 5.77 | _ | _ | _ | _ | β-Pinene | 5 |
| 987 | 984 | 7.75 | Hydrocarbon monoterpene | _ | _ | 6.67 | _ | _ | _ | _ | β-Myrcene | 6 |
| 1003 | 989 | 7.80 | Hydrocarbon monoterpene | _ | _ | 0.33 | _ | _ | _ | _ | α-Phellandrene | 7 |
| 1008 | 993 | 7.91 | Hydrocarbon monoterpene | _ | 0.06 | _ | _ | _ | _ | _ | 3-Carene | 8 |
| 1018 | 1004 | 8.13 | Oxygenated monoterpene | _ | 0.30 | _ | _ | _ | _ | _ | α-Terpinene | 9 |
| 1024 | 1006 | 8.15 | Hydrocarbon monoterpene | _ | 0.18 | _ | _ | _ | _ | _ | p-Cymene | 10 |
| 1026 | 1011 | 8.20 | Hydrocarbon monoterpene | _ | _ | 0.56 | _ | _ | _ | _ | m-Cymene | 11 |
| 1028 | 1014 | 8.25 | Hydrocarbon monoterpene | _ | _ | 7.34 | _ | _ | _ | _ | β-Phellandrene | 12 |
| 1030 | 1016 | 8.29 | Oxygenated monoterpene | _ | 0.05 | _ | _ | _ | _ | _ | 1,8-Cineole | 13 |
| 1038 | 1024 | 8.43 | Hydrocarbon monoterpene | _ | _ | 1.65 | _ | _ | _ | _ | cis-Ocimene | 14 |
| 1047 | 1039 | 8.71 | Oxygenated monoterpene | _ | 0.03 | _ | _ | _ | _ | _ | cis-Sabinene hydrate | 15 |
| 1065 | 1046 | 8.80 | Hydrocarbon monoterpene | _ | 0.32 | 0.28 | _ | _ | _ | _ | γ-Terpinene | 16 |
| 1083 | 1078 | 9.36 | Hydrocarbon monoterpene | _ | _ | 0.36 | _ | _ | _ | _ | α-Terpinolene | 17 |
| 1098 | 1086 | 9.50 | Oxygenated monoterpene | _ | 0.12 | 1.19 | _ | _ | _ | _ | Linalool | 18 |
| 1127 | 1115 | 10.03 | Oxygenated monoterpene | _ | _ | 0.2 | _ | _ | _ | _ | α-Campholenal | 19 |
| 1175 | 1167 | 10.97 | Oxygenated monoterpene | _ | _ | 0.36 | _ | _ | _ | _ | (-)-Terpinen-4-ol | 20 |
| 1180 | 1181 | 11.23 | Oxygenated monoterpene | _ | 0.44 | 0.22 | _ | _ | _ | _ | α-Terpineol | 21 |
| 1231 | 1226 | 12.22 | Oxygenated monoterpene | _ | 0.16 | _ | _ | _ | _ | _ | Nerol | 22 |
| 1235 | 1232 | 12.37 | Oxygenated monoterpene | _ | 0.04 | _ | _ | _ | _ | _ | Thymol methyl ether | 23 |
| 1244 | 1233 | 12.39 | Oxygenated monoterpene | _ | _ | _ | 46.40 | 3.15 | _ | _ | L-Carvone | 24 |
| 1250 | 1261 | 13.08 | Oxygenated monoterpene | _ | 0.11 | _ | _ | _ | _ | _ | Geraniol | 25 |
| 1290 | 1297 | 13.96 | Oxygenated monoterpene | 32.36 | 37.01 | 1.00 | 28.05 | 0.80 | _ | 26.72 | Thymol | 26 |
| 1311 | 1307 | 14.19 | Oxygenated monoterpene | 2.55 | 0.25 | 0.16 | 1.22 | 1.31 | _ | 21.60 | Carvacrol | 27 |
| 1332 | 1326 | 14.58 | Oxygenated monoterpene | 32.54 | _ | _ | _ | _ | _ | 9.63 | o-Cymen-5-ol | 28 |
| 1357 | 1360 | 15.31 | Oxygenated monoterpene | _ | _ | _ | 0.76 | _ | _ | _ | Thymyl acetate | 29 |
| 1366 | 1365 | 15.40 | Oxygenated monoterpene | _ | _ | 0.28 | _ | _ | _ | _ | Piperitenone oxide | 30 |
| 1375 | 1370 | 15.51 | Hydrocarbon sesquiterpene | _ | _ | 1.03 | _ | _ | _ | _ | α-Copaene | 31 |
| 1380 | 1375 | 15.62 | Oxygenated monoterpene | 1.53 | 1.84 | _ | _ | _ | _ | _ | Geranyl acetate | 32 |
| 1382 | 1383 | 15.78 | Hydrocarbon sesquiterpene | _ | _ | 0.22 | _ | _ | _ | _ | β-Bourbonene | 33 |
| 1389 | 1388 | 15.89 | Hydrocarbon sesquiterpene | _ | _ | 0.42 | _ | _ | _ | _ | β-Elemene | 34 |
| 1408 | 1400 | 16.14 | Hydrocarbon sesquiterpene | _ | _ | _ | 0.51 | _ | _ | _ | (-)-α-Cedrene | 35 |
| 1418 | 1415 | 16.47 | Hydrocarbon sesquiterpene | _ | 0.29 | 0.36 | _ | _ | _ | _ | trans-Caryophyllene | 36 |
| 1419 | 1424 | 16.67 | Hydrocarbon sesquiterpene | _ | _ | 0.15 | _ | _ | _ | _ | β-Cubebene | 37 |
| 1430 | 1424 | 16.68 | Oxygenated monoterpene | _ | _ | _ | 8.35 | _ | _ | _ | Neryl propanoate | 38 |
| 1440 | 1427 | 16.74 | Hydrocarbon sesquiterpene | _ | _ | 0.46 | _ | _ | _ | _ | trans-α-Bergamotene | 39 |
| 1461 | 1447 | 17.19 | Hydrocarbon sesquiterpene | _ | _ | 1.41 | _ | _ | _ | _ | trans-β-Farnesene | 40 |
| 1480 | 1469 | 17.69 | Hydrocarbon sesquiterpene | _ | 0.16 | 7.54 | _ | _ | _ | _ | Germacrene D | 41 |
| 1513 | 1489 | 18.14 | Hydrocarbon sesquiterpene | _ | _ | 0.93 | _ | _ | _ | _ | γ-Cadinene | 42 |
| 1482 | 1492 | 18.20 | Hydrocarbon sesquiterpene | _ | 0.12 | 0.27 | _ | _ | _ | _ | α-Amorphene | 43 |
| 1494 | 1493 | 18.23 | Hydrocarbon sesquiterpene | _ | _ | 0.35 | _ | _ | _ | _ | Bicyclogermacrene | 44 |
| 1510 | 1500 | 18.40 | Hydrocarbon sesquiterpene | _ | _ | _ | _ | _ | 1.69 | _ | Bicyclo[4.4.0]dec-1-ene, 2-isopropyl-5-methyl-9-methylene | 45 |
| 1514 | 1503 | 18.46 | Hydrocarbon sesquiterpene | _ | 0.27 | 0.49 | _ | _ | _ | _ | β-Bisabolene | 46 |
| 1518 | 1520 | 18.92 | Hydrocarbon sesquiterpene | _ | 0.28 | _ | _ | _ | _ | _ | β -Cadinene | 47 |
| _ | 1521 | 18.93 | Alkaloid | _ | _ | _ | 0.28 | _ | _ | _ | 1,2-Benzisothiazole-3-propanoic acid | 48 |
| 1519 | 1521 | 18.94 | Oxygenated sesquiterpene | _ | _ | _ | _ | _ | 0.53 | _ | Cycloisolongifol-5-ol | 49 |
| 1524 | 1521 | 18.95 | Hydrocarbon sesquiterpene | _ |  | 1.46 | _ | _ | 0.44 | _ | δ-Cadinene | 50 |
| 1532 | 1525 | 19.05 | Hydrocarbon sesquiterpene | _ | 0.22 | _ | _ | _ | _ | _ | γ-Selinene | 51 |
| 1533 | 1526 | 19.07 | Hydrocarbon sesquiterpene | _ | _ | 0.28 | _ | _ | _ | _ | α-Cadinene | 52 |
| 1535 | 1529 | 19.16 | Oxygenated sesquiterpene | _ | 0.14 | _ | _ | _ | _ | _ | Nerolidol | 53 |
| 1566 | 1554 | 19.82 | Fatty acid | _ | _ | _ | _ | _ | 0.61 | _ | Dodecanoic acid;Lauric acid | 54 |
| 1572 | 1574 | 20.34 | Oxygenated sesquiterpene | _ | _ | 0.75 | _ | _ | _ | _ | (-)-Spathulenol | 55 |
| 1578 | 1578 | 20.44 | Oxygenated sesquiterpene | _ | 0.28 | _ | _ | _ | 1.27 | _ | (+)-Spathulenol | 56 |
| 1580 | 1582 | 20.56 | Oxygenated sesquiterpene | _ | 0.47 | _ | _ | _ | _ | _ | (-)-Caryophyllene oxide | 57 |
| 1603 | 1585 | 20.64 | Oxygenated sesquiterpene | _ | _ | 0.62 | _ | _ | 0.62 | _ | Salvial-4(14)-en-1-one | 58 |
| 1605 | 1587 | 20.69 | Oxygenated sesquiterpene | _ | _ | _ | 0.46 | _ | _ | _ | Sesquisabinene hydrate | 59 |
| 1609 | 1591 | 20.80 | Oxygenated sesquiterpene | _ | _ | _ | _ | _ | 0.55 | _ | Veridiflorol | 60 |
| 1611 | 1594 | 20.89 | Oxygenated sesquiterpene | _ | 0.16 | _ | _ | _ | _ | _ | Geranyl isovalerate | 61 |
| _ | 1612 | 21.30 | Oxygenated monoterpene | _ | 0.12 | _ | _ | _ | _ | _ | 1-(5(methyl-2-furanyl)-1-buten-3-one | 62 |
| 1641 | 1636 | 21.83 | Oxygenated sesquiterpene | _ | 0.39 | 0.76 | _ | _ | _ | _ | τ-Muurolol | 63 |
| _ | 1642 | 21.95 | Phenolic compound | _ | _ | _ | 0.65 | _ | _ | _ | Terbutaline derivative | 64 |
| 1650 | 1642 | 21.96 | Oxygenated sesquiterpene | _ | 0.08 | 1.06 | _ | _ | _ | _ | τ-Cadinol | 65 |
| 1653 | 1650 | 22.14 | Oxygenated sesquiterpene | _ | _ | _ | _ | _ | 2.17 | _ | α-Cadinol | 66 |
| 1654 | 1663 | 22.43 | Oxygenated monoterpene | _ | _ | 0.40 | _ | _ | _ | _ | Benzene, 1-(1-formylethyl)-4-(1-buten-3-yl) | 67 |
| 1669 | 1669 | 22.55 | Oxygenated sesquiterpene | _ | _ | 0.60 | _ | _ | 0.30 | _ | Valeranone | 68 |
| 1681 | 1679 | 22.78 | Oxygenated sesquiterpene | _ | _ | _ | _ | _ | 2.59 | _ | α-Bisabolol | 69 |
| 1756 | 1747 | 24.13 | Oxygenated monoterpene | _ | 0.18 | _ | _ | _ | _ | _ | Geranyl hexanoate | 70 |
| 1758 | 1756 | 24.31 | Fatty acid | _ | _ | _ | _ | _ | 2.90 | _ | Tetradecanoic acid | 71 |
| 1800 | 1789 | 24.93 | Aliphatic hydrocarbon | _ | _ | _ | _ | _ | 0.16 | _ | Octadecane | 72 |
| _ | 1821 | 25.50 | Substituted aromatic hydrocarbon | _ | _ | _ | _ | _ | _ | 0.45 | Benzamide, N-(1,1-dimethylethyl)-4-methoxy | 73 |
| 1839 | 1825 | 25.56 | Oxygenated fatty acid | _ | _ | _ | _ | _ | 0.36 | _ | Cyclopentadecanone,2-hydroxy | 74 |
| 1841 | 1830 | 25.64 | Hydrocarbon diterpene | _ | _ | _ | _ | _ | 0.34 | _ | Neophytadiene | 75 |
| 1847 | 1836 | 25.75 | Oxygenated diterpene | _ | _ | _ | _ | _ | 2.26 | _ | 2-Pentadecanone,6,10,14-trimethyl | 76 |
| 1847 | 1839 | 25.79 | Oxygenated sesquiterpene | _ | _ | 0.45 | _ | _ | _ | _ | Hexahydrofarnesyl acetone | 77 |
| 1868 | 1853 | 26.04 | Fatty acid | _ | _ | _ | _ | _ | 0.52 | _ | Pentadecanoic acid | 78 |
| 1871 | 1862 | 26.19 | Phenolic compound | _ | _ | 0.36 | _ | _ | 1.64 | _ | Isobutyl phthalate | 79 |
| 1900 | 1882 | 26.53 | Aliphatic hydrocarbon | _ | _ | _ | _ | _ | 0.44 | _ | Nonadecane | 80 |
| 1906 | 1890 | 26.66 | Oxygenated diterpene | _ | _ | _ | _ | _ | 1.33 | _ | Sclareoloxide | 81 |
| _ | 1901 | 26.84 | Phenolic compound | _ | _ | _ | _ | _ | _ | 0.45 | Phenylacetic acid, 2-(1-adamantyl)ethyl ester | 82 |
| 1955 | 1940 | 27.44 | Substituted aliphatic hydrocarbon | _ | _ | _ | _ | _ | 0.22 | _ | 11,13-Dimethyl-12-tetradecen-1-ol acetate | 83 |
| 1968 | 1945 | 27.52 | Fatty acid | _ | 0.36 | 3.40 | _ | _ | 0.73 | _ | Palmitic acid | 84 |
| _ | 1990 | 28.22 | Substituted fatty acid | _ | 0.29 | _ | _ | _ | _ | _ | 1-Chlorooctadecane | 85 |
| 2000 | 1992 | 28.24 | Aliphatic hydrocarbon | _ | 0.07 | _ | _ | _ | 0.50 | _ | Eicosane | 86 |
| 2002 | 1994 | 28.27 | Heterocyclic compound | _ | _ | _ | _ | _ | 0.85 | _ | epi-13-Manoyl oxide | 87 |
| _ | 2032 | 28.84 | Substituted fatty acid | _ | 0.19 | _ | _ | _ | _ | _ | 1-Adamantyl-1,8-diaza-4-oxanonan-2,5,7-trione | 88 |
| 2100 | 2090 | 29.70 | Aliphatic hydrocarbon | _ | 0.47 | _ | _ | _ | 0.48 | _ | Heneicosane | 89 |
| _ | 2110 | 30.03 | Phenolic compound | _ | 0.62 | _ | _ | _ | _ | _ | 5,8-Dimethoxy-2-methyl-4H-naphtho[2,3-b]pyran-4,6,9-trione | 90 |
| 2144 | 2126 | 30.31 | Fatty acid | _ | _ | _ | _ | _ | 4.79 | _ | Linolic acid | 91 |
| _ | 2128 | 30.35 | Hydrocarbon diterpene | _ | 0.39 | _ | _ | _ | _ | _ | D-Homopregn-17a(20)-ene, (5.alpha.,17aE) | 92 |
| _ | 2152 | 30.77 | Substituted fatty acid | _ | 0.27 | _ | _ | _ | _ | _ | Androst-4-en-9,11-epoxy-3,17-dione | 93 |
| 2148 | 2152 | 30.78 | Oxygenated diterpene | _ | _ | _ | _ | _ | 1.80 | _ | Phytol | 94 |
| 2172 | 2153 | 30.79 | Aliphatic hydrocarbon | _ | _ | _ | 0.22 | _ | _ | _ | Heneicosane,3-methyl | 95 |
| 2178 | 2154 | 30.81 | Fatty acid | _ | _ | _ | _ | _ | 2.14 | _ | Stearic acid | 96 |
| 2200 | 2192 | 31.48 | Aliphatic hydrocarbon | _ | 0.52 | _ | _ | _ | _ | _ | Docosane | 97 |
| _ | 2268 | 32.94 | Oxygenated diterpene | _ | _ | _ | _ | _ | 0.26 | _ | (12R)-13(16),14-Labdadien-8,12-epoxide | 98 |
| 2300 | 2292 | 33.42 | Aliphatic hydrocarbon | _ | 0.12 | _ | _ | _ | _ | _ | Tricosane | 99 |
| _ | 2349 | 34.40 | Heterocyclic compound | _ | _ | _ | 0.11 | _ | _ | _ | Thiophene,2-nonadecyl | 100 |
| 2364 | 2367 | 34.72 | Substituted aliphatic hydrocarbon | _ | 0.07 | _ | _ | _ | _ | _ | 1-Bromoeicosane | 101 |
| _ | 2391 | 35.12 | Phenolic compound | _ | 0.05 | _ | _ | _ | _ | _ | 2-Cyclohexylethyl isobutyl phthalate | 102 |
| 2400 | 2393 | 35.15 | Aliphatic hydrocarbon | _ | _ | _ | _ | _ | 0.22 | _ | Tetracosane | 103 |
| _ | 2399 | 35.26 | Steroid | _ | 0.07 | _ | _ | _ | _ | _ | 14-β-H-Pregna | 104 |
| 2500 | 2495 | 36.71 | Aliphatic hydrocarbon | _ | 0.26 | _ | _ | _ | 2.26 | _ | Pentacosane | 105 |
| 2550 | 2575 | 37.79 | Phenolic compound | 23.47 | 42.0 | 18.31 | _ | 1.29 | 24.79 | 19.97 | Bis-(2-ethylhexyl)phthalate | 106 |
| 2600 | 2597 | 38.10 | Aliphatic hydrocarbon | _ | 0.73 | _ | _ | _ | 0.5 | _ | Hexacosane | 107 |
| _ | 2599 | 38.12 | Aliphatic hydrocarbon | _ | _ | 0.46 | _ | _ | _ | _ | Octadecane, 3-ethyl-5-(2-ethylbutyl) | 108 |
| _ | 2666 | 38.95 | Alkaloid | _ | 0.19 | _ | _ | _ | _ | _ | Kopsinyl alcohol | 109 |
| 2700 | 2704 | 39.43 | Aliphatic hydrocarbon | _ | 0.47 | 3.66 | _ | _ | 10.13 | _ | Heptacosane | 110 |
| 2741 | 2725 | 39.67 | Phenolic compound | _ | _ | _ | _ | 57.92 | 0.44 | _ | Di-n-octyl phthalate | 111 |
| _ | 2726 | 39.68 | Phenolic compound | 0.57 | 0.20 | _ | 5.65 | 1.55 | 0.53 | _ | Diisooctyl phthalate | 112 |
| _ | 2755 | 40.01 | Alkaloid | _ | _ | _ | _ | _ | 0.34 | _ | 7,11b-Diphenylpiperidino[2,1-a]phthalazine | 113 |
| 2858 | 2802 | 40.55 | Oxygenated triterpene | _ | _ | _ | _ | 30.13 | _ | _ | Friedelan-3-one | 114 |
| 2800 | 2812 | 40.66 | Aliphatic hydrocarbon | _ | _ | _ | _ | _ | 1.10 | _ | Octacosane | 115 |
| 2836 | 2845 | 41.02 | Hydrocarbon triterpene | _ | _ | _ | _ | _ | 0.75 | _ | Squalene | 116 |
| 2900 | _ | 41.88 | Aliphatic hydrocarbon | _ | 0.69 | 3.56 | _ | _ | 10.74 | _ | Nonacosane | 117 |
| _ | _ | 45.04 | Phenolic compound | _ | _ | _ | 0.1 | _ | _ | _ | Merochlorophaeic Acid | 118 |
|  |  |  |  | 93.02 | 92.20 | 97.81 | 92.76 | 96.15 | 84.15 | 78.82 | Total Identification |  |

RT Retention time.

RI Retention index.

a Retention indices of each component were collected from the literature for column HP-5MS.

b As identified by GC–MS software; names according to NIST mass spectral library, and by comparing their retention indices.

b As identified by GC–MS software; names according to NIST mass spectral library, and by comparing their retention indices.

Table 5

Classification of the volatile compounds of the shoot cultures of M. longifolia under rGO and Mg/rGO NCs treatments

|  |  |  |  |  |  | Percentage of compounds in treatments | Constituent |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Mg/RGO 100 mg/L | Mg/RGO 50 mg/L | Mg/RGO 25 mg/L | RGO 100 mg/L | RGO 50 mg/L | RGO 25 mg/L | Control |  |
| _ | 0.19 | _ | 0.28 | _ | 0.34 | _ | Alkaloid |
| _ | 3.23 | 8.20 | 0.22 | _ | 24.53 | _ | Aliphatic hydrocarbons |
| _ | 0.07 | _ | _ | _ | 0.22 | _ | Substituted aliphatic hydrocarbon |
| _ | _ | 0.31 | _ | _ | _ | _ | Aromatic hydrocarbons |
| _ | _ | _ | _ | _ | _ | 0.45 | Substituted aromatic hydrocarbons |
| _ | 0.39 | _ | _ | _ | 0.34 | _ | Hydrocarbon diterpenes |
| _ | _ | 0.40 | _ | _ | 5.65 | _ | Oxygenated diterpenes |
| _ | 0.36 | 3.40 | _ | _ | 13.55 | _ | Fatty acids |
| _ | 0.75 | _ | _ | _ | _ | _ | Substituted fatty acids |
| _ | _ | _ | _ | _ | 0.36 | _ | Oxygenated fatty acids |
| _ | _ | _ | 0.11 | _ | 0.85 | _ | Heterocyclic compound |
| _ | 40.28 | _ | _ | _ | _ | _ | Hydrocarbon monoterpenes |
| 68.98 | 1.03 | 47.22 | 84.78 | 5.26 | _ | 57.95 | Oxygenated monoterpenes |
| 24.04 | 42.97 | 18.67 | 6.40 | 60.76 | 27.40 | 20.42 | Phenolic compounds |
| _ | 1.34 | 15.37 | 0.51 | _ | 2.13 | _ | Hydrocarbon sesquiterpenes |
| _ | 1.52 | 4.24 | 0.46 | _ | 8.03 | _ | Oxygenated sesquiterpenes |
| _ | 0.07 | _ | _ | _ | _ | _ | Steroids |
| _ | _ | _ | _ | _ | 0.75 | _ | Hydrocarbon triterpenes |
| _ | _ | _ | _ | 30.13 | _ | _ | Oxygenated triterpenes |
| 93.02 | 92.20 | 97.81 | 92.76 | 96.15 | 84.15 | 78.82 | Total Identification |