Supplementary information for:

Mesh-reinforced Vaseline-assisted graphene transfer compatible with industrial automation operations

Xiaomeng Guo1,2,3, Fangzhu Qing1,2,3*, Wei Liu4, Yaxin Liu3, Yiji Liang5, Runlai Li6, Pingjian Li1,2, Changqing Shen1, Xiaoming Tu1, Chunlin Liu1, Zhancheng Li7, Huaipeng Wang8, Yutong Ran9, Haofei Shi7, Dan Xie8, Hongwei Zhu9, Xiaobin Niu4*, Zejia Zhao5*, Xuesong Li1,2,3*

Correspondence to: lxs@uestc.edu.cn; qingfz@uestc.edu.cn; zhaozejia@szu.edu.cn; xbniu@uestc.edu.cn

This supplementary information includes:

Supplementary Figure 1-8

Supplementary Figure 1. Photographs of the key transfer steps.

Supplementary Figure 2. Contact angle tests on SiO2/Si, Vaseline and Graphene/Vaseline when using different solution. a, Water. b, Diluted ethanol.

Supplementary Figure 3. Differential scanning calorimetry results of Vaseline.

Supplementary Figure 4. Graphene transfer with recycled Vaseline. a-b, OM images of transferred graphene on a SiO2/Si substrate. c, SEM image of transferred graphene. d, Raman spectrum of transferred graphene.

Supplementary Figure 5. Photographs of four 4-inch graphene wafers, indicating the reproducibility of graphene transfer.

Supplementary Figure 6. Photographs of sequential transfer of three layers of graphene.

Supplementary Figure 7. Transfer characteristics of GrFETs with (a) Vaseline-transferred graphene and (b) PMMA-transferred graphene.

Supplementary Figure 8. Photographs of the key steps of PMMA-assisted graphene transfer. a, Etch Cu. b, Fish out the PMMA/graphene after Cu etching. c, Transfer PMMA/graphene to water surface. d-e, Fish out PMMA/graphene with the target substrate. Note: Ideally, robots can replace all manual operations even for the case of PMMA assisted transfer. However, as aforementioned, PMMA is too fragile to be processed. It has to float on liquid surface or lay on a substrate. This makes the process more complicated and not practical for robot. Instead, the mesh reinforced Vaseline layer is self-supporting and can be processed with simple mechanical systems.