SUPPLEMENTARY INFORMATION for

Characterizing G-type Antiferromagnetism Quantitatively with Optical Second Harmonic Generation

Shuai Xu1, Kuijuan Jin1,2,*, Qinghua Zhang1,2, Cheng Ma1,2, Sisi Huang1,2, Yiru Wang1,2, Xu He3, Jiesu Wang4, Donggang Xie1,2, Qiulin Zhang1,2, Er-Jia Guo1,2, Chen Ge1,2, Can Wang1,2, Xiulai Xu5, Lin Gu6, Meng He1, Guozhen Yang1,2

1 Beijing National Laboratory for Condensed Matter Physics, Institute of Physics, Chinese Academy of Sciences, Beijing 100190, China

2 University of Chinese Academy of Sciences, Beijing 100049, China

3Theoretical Materials Physics, Q-MAT, Université de Liège, Liège B-4000, Belgium

4Beijing Academy of Quantum Information Sciences, Beijing 100193, China

5State Key Laboratory for Mesoscopic Physics and Frontiers Science Center for Nano-optoelectronics, School of Physics, Peking University, Beijing 100871, China

6Beijing National Center for Electron Microscopy and Laboratory of Advanced Materials, Department of Materials Science and Engineering, Tsinghua University, 100084, Beijing, China

*Author to whom correspondence should be addressed: kjjin@iphy.ac.cn

CONTENTS

1. RA-SHG measurements of BFO/SAO/STO heterostructures at different temperatures

2. RA-SHG measurements of freestanding BFO films at different temperatures

3. X-ray reflectivity measurements of BFO films grown on different substrates

4. RA-SHG measurements of BFO/LSAT films at different temperatures

5. RA-SHG measurements of BFO/STO films at different temperatures

6. RA-SHG measurements of BFO/DSO films at different temperatures

7. RA-SHG measurements of BFO/GSO films at different temperatures

8. RA-SHG measurements of BFO/KTO films at different temperatures

9. First-principles calculation results of the crystal structures of BFO with different strains

10. 110 plane-view of the BFO crystal structure with different strains

11. Functional forms of electric dipole SHG for crystallographic 4mm and magnetic point-group m

1. RA-SHG measurements of BFO/SAO/STO films at different temperatures

Supplementary Figure 1 | a-f RA-SHG results and analyses of BFO/SAO/STO films below TN (about 596 K for BFO/SAO/STO films), where both the antiferromagnetic order and the ferroelectric order contribute to the SHG signal, leading to the asymmetry of the RA-SHG patterns. g-i RA-SHG results and analyses of BFO/SAO/STO films above TN, where contribution from the antiferromagnetic order disappears and only the ferroelectric order contributes to the SHG signal. The hollow dots are the experimental data, the blue lines represent the contribution from the ferroelectric order, and the gray shadows represent the contribution from the antiferromagnetic order.

2. RA-SHG measurements of freestanding BFO films at different temperatures

Supplementary Figure 2 | a-d RA-SHG results and analyses of freestanding BFO films below TN (about 565 K for freestanding BFO films), where both the antiferromagnetic order and the ferroelectric order contribute to the SHG signal, leading to the asymmetry of the RA-SHG patterns. e-g RA-SHG results and analyses of freestanding BFO films above TN, where contribution from the antiferromagnetic order disappears and only the ferroelectric order contributes to the SHG signal.  The hollow dots are the experimental data, the blue lines represent the contribution from the ferroelectric order, and the gray shadows represent the contribution from the antiferromagnetic order.

3. X-ray reflectivity measurements of BFO films grown on different substrates

Supplementary Figure 3 | X-ray reflectivity measurements of BFO/LSAT, BFO/STO, BFO/DSO, BFO/GSO, and BFO/KTO films, respectively. The lines are the fitting curves to the experimental data (hollow dots). The thickness of all epitaxial BFO films on different substrates is approximately 30 nm.

4. RA-SHG measurements of BFO/LSAT films at different temperatures

Supplementary Figure 4 | a RA-SHG results of BFO/LSAT films at different temperatures. b-f RA-SHG results and analyses of BFO/LSAT films below TN (about 428 K for BFO/LSAT films), where both the antiferromagnetic order and the ferroelectric order contribute to the SHG signal, leading to the asymmetry of the RA-SHG patterns. g-l RA-SHG results and analyses of BFO/LSAT films above TN, where contribution from the antiferromagnetic order disappears and only the ferroelectric order contributes to the SHG signal. The hollow dots are the experimental data, the blue lines represent the contribution from the ferroelectric order, and the gray shadows represent the contribution from the antiferromagnetic order.

5. RA-SHG measurements of BFO/STO films at different temperatures

Supplementary Figure 5 | a RA-SHG results of BFO/STO films at different temperatures. b-g RA-SHG results and analyses of BFO/STO films below TN (about 496 K for BFO/STO films), where both the antiferromagnetic order and the ferroelectric order contribute to the SHG signal, leading to the asymmetry of the RA-SHG patterns. h-l RA-SHG results and analyses of BFO/STO films above TN, where contribution from the antiferromagnetic order disappears and only the ferroelectric order contributes to the SHG signal. The hollow dots are the experimental data, the blue lines represent the contribution from the ferroelectric order, and the gray shadows represent the contribution from the antiferromagnetic order.

6. RA-SHG measurements of BFO/DSO films at different temperatures

Supplementary Figure 6 | a RA-SHG results of BFO/DSO films at different temperatures. b-h RA-SHG results and analyses of BFO/DSO films below TN (about 582 K for BFO/DSO films), where both the antiferromagnetic order and the ferroelectric order contribute to the SHG signal, leading to the asymmetry of the RA-SHG patterns. i-l RA-SHG results and analyses of BFO/DSO films above TN, where contribution from the antiferromagnetic order disappears and only the ferroelectric order contributes to the SHG signal. The hollow dots are the experimental data, the blue lines represent the contribution from the ferroelectric order, and the gray shadows represent the contribution from the antiferromagnetic order.

7. RA-SHG measurements of BFO/GSO films at different temperatures

Supplementary Figure 7 | a RA-SHG results of BFO/GSO films at different temperatures. b-j RA-SHG results and analyses of BFO/GSO films below TN (about 632 K for BFO/GSO films), where both the antiferromagnetic order and the ferroelectric order contribute to the SHG signal, leading to the asymmetry of the RA-SHG patterns. k and l RA-SHG results and analyses of BFO/GSO films above TN, where contribution from the antiferromagnetic order disappears and only the ferroelectric order contributes to the SHG signal. The hollow dots are the experimental data, the blue lines represent the contribution from the ferroelectric order, and the gray shadows represent the contribution from the antiferromagnetic order.

8. RA-SHG measurements of BFO/KTO films at different temperatures

Supplementary Figure 8 | a RA-SHG results of BFO/KTO films at different temperatures, the scattered points are the experimental data at different temperatures. b-i RA-SHG results and analyses of BFO/KTO films below TN (about 646 K for BFO/KTO films), where both the antiferromagnetic order and the ferroelectric order contribute to the SHG signal, leading to the asymmetry of the RA-SHG patterns. j-l RA-SHG results and analyses of BFO/KTO films above TN, where contribution from the antiferromagnetic order disappears and only the ferroelectric order contributes to the SHG signal. The hollow dots are the experimental data, the blue lines represent the contribution from the ferroelectric order, and the gray shadows represent the contribution from the antiferromagnetic order.

9. First-principles calculation results of the crystal structures of BFO with different strains

Supplementary Figure 9 | a-i Crystal structures of BFO with strains of -4%, -3%, -2%, -1%, 0%, +1%, +2%, +3%, and +4%, respectively.

10. 110 plane-view of the BFO crystal structure with different strains

Supplementary Figure 10 | a-i 110 plane- view of the BFO crystal structure with strains of -4%, -3%, -2%, -1%, 0%, +1 %, +2%, +3%, and +4%, respectively.

11. Functional forms of electric dipole SHG for crystallographic 4mm and magnetic point-group m

Supplementary Figure 11 | Schematic diagram of the rotating-polarization-based RA-SHG setups.

The second-order nonlinear optical process can be expressed as: P2ω=χ2∶EωEω, where χ2 is the second-order nonlinear optical susceptibility tensor of the three-rank, and Eω is the incident optical electric field of the femtosecond laser with a frequency ω1,2. In general, the three-rank electric dipole (ED) term χED2ω plays a dominant role in the contribution of the SHG signal, and χED2ω can only be produced in non-centrosymmetric medium (such as ferroelectric materials, surfaces, and interfaces)3,4. For systems with broken spatial-inversion symmetry, information related to the crystal structure symmetry and phase transitions (such as crystal point groups and phase transition temperatures) can be analyzed from the results obtained from wide-temperature-range RA-SHG measurements5.

For a ferroelectric crystalline material with antiferromagnetic order (such as multiferroic BFO), χ2 can be expressed as: χED2=ε0χi+χc, where the time-invariant tensor χi and the time-noninvariant tensor χc represent the crystallographic (spatial-inversion symmetry breaking) and antiferromagnetic order structure (time-reversal symmetry breaking), respectively6,7. With an approximation that considers only the electric dipole, the SHG source term S2ω is related to the light-induced nonlinear polarization P2ω in the following way: S2ω=μ0∂2P2ω∂t2 , where P2ω=ε0χi+χc∶EωEω. The SHG signal measured experimentally is the intensity I2ωφ of the 2ω light, and its relationship with P is:

I2ωφ∝P2ω2∝ei'2ωχi'j'k'EDej'ωej'ω2.	(1)

To analyze SHG experimental data, the second-order nonlinear optical susceptibility tensor should be represented in the laboratory coordinate system (x, y, z). We generally try to make the laboratory coordinate system parallel to the crystal coordinate system. Here, the incident angle θ is 45°, as shown in the schematic diagram of Supplementary Fig. 12. By rotating the polarization angle φ of the incident light and fixing the polarization of the reflection light as p (ϕ = 0°, parallel to the plane of incidence) or s (ϕ = 90°, perpendicular to the plane of incidence), the variation of the SHG intensity can be obtained. For non-centrosymmetric crystal 4mm point groups, the time-invariant SHG susceptibility tensor χi is:

χi=0000χ15i0000χ15i00χ31iχ31iχ33i000,	(2)

for p-out configuration, so ϕ = 0°. Substituting the time-invariant SHG susceptibility tensor χi into P2ω, we have:

Pp-outi2ω=Acos2φ+Bsin2φ,	(3)

A=22Lyy2ωLyyωLzzωχ15i-2(Lyyω)2Lzz2ωχ31i-2(Lzzω)2Lzz2ωχ33i4,	(4)

B=-2(Lxxω)2Lzz2ωχ31i2,	(5)

in which Lxx, Lyy, and Lzz are the diagonal elements of the transmitted Fresnel factor L in fundamental and second harmonic optical materials. Considering I2ωφ∝P2ω2, we obtained:

Ip-outiφ∝Acos2φ+Bsin2φ2.	(6)

Below TN, the existence of the antiferromagnetic order in BFO films breaks the time-reversal symmetry. As the non-centrosymmetric magnetic order also breaks the spatial-inversion symmetry, the magnetization-induced ED-SHG is produced. With magnetic point-group m, the time-noninvariant SHG susceptibility tensor χc is7:

χc=χ11cχ12cχ13c0χ15c0000χ24c0χ12cχ15cχ24cχ33c0χ13c0.	(7)

Similarly, substituting the time-noninvariant SHG susceptibility tensor χc, we have:

Pp-outc2ω=Ccos2φ+Dsin2φ+Esin2φ,	(8)

C=22Lyy2ωLyyωLzzωχ24c-2(Lyyω)2Lzz2ωχ24c-2(Lzzω)2Lzz2ωχ33c4,	(9)

D=-2(Lxxω)2Lzz2ωχ15c2,	(10)

E=Lyy2ωLxxωLyyωχ12c-Lzz2ωLxxωLzzωχ13c2.	(11)

Considering I2ωφ∝P2ω2, we obtained:

Ip-outc2ω∝Ccos2φ+Dsin2φ+Esin2φ2.	(12)

References

1 Zhang, Y. et al. Doping-Induced Second-Harmonic Generation in Centrosymmetric Graphene from Quadrupole Response. Phys. Rev. Lett. 122, 047401 (2019). https://doi.org/10.1103/PhysRevLett.122.047401

2 Fiebig, M., Pavlov, V. V. & Pisarev, R. V. Second-harmonic generation as a tool for studying electronic and magnetic structures of crystals: review. Journal of the Optical Society of America B 22, 96-118 (2005). https://doi.org/10.1364/JOSAB.22.000096

3 Shen, Y.-R. The principles of nonlinear optics.  (1984).

4 Fiebig, M., Fröhlich, D., Krichevtsov, B. B. & Pisarev, R. V. Second Harmonic Generation and Magnetic-Dipole-Electric-Dipole Interference in Antiferromagnetic Cr2O3. Phys. Rev. Lett. 73, 2127-2130 (1994). https://doi.org/10.1103/PhysRevLett.73.2127

5 Xu, S. et al. Magnetoelectric coupling in multiferroics probed by optical second harmonic generation. Nature Communications 14, 2274 (2023). https://doi.org/10.1038/s41467-023-38055-x

6 Birss, R. R. Symmetry and magnetism. Vol. 3 (North-Holland Publishing Company, 1964).

7 Chauleau, J. Y., Haltz, E., Carrétéro, C., Fusil, S. & Viret, M. Multi-stimuli manipulation of antiferromagnetic domains assessed by second-harmonic imaging. Nat. Mater. 16, 803-807 (2017). https://doi.org/10.1038/nmat4899