Supporting information

Harmonizing Material Quantity and Terahertz Wave Interference Shielding Efficiency with Metallic Borophene Nanosheets

Haojian Lin†, Ximiao Wang†, Zhaolong Cao, Hongjia Zhu, Jiahao Wu, Runze Zhan, Ningsheng Xu, Shaozhi Deng*, Huanjun Chen*, and Fei Liu*

State Key Laboratory of Optoelectronic Materials and Technologies, Guangdong Province Key Laboratory of Display Material and Technology, and School of Electronics and Information Technology, Sun Yat-sen University, Guangzhou 510275, China

*Corresponding authors’ e-mail: liufei@mail.sysu.edu.cn; chenhj8@mail.sysu.edu.cn; stsdsz@mail.sysu.edu.cn.

Contents

S1. Thickness, Raman spectra and crystallographic characterization of β12-Br nanosheets	3

S2. The surface compositions and element distribution of a β12-Br nanosheet	4

S3. Electrical conductivity measurement of β12-Br nanosheet	5

S4. Measurement of the THz shielding performances of the composite film	6

S5. The complex conductivity and complex permittivity of β12-Br nanosheets	8

S6. Theoretical simulation to obtain the optimal structure parameters of β12-Br nanosheets with the most excellent THz absorption behaviors	10

S7. The comparable table of 2D nanomaterials used for THz shielding	11

S1. Thickness, Raman spectra and crystallographic characterization of β12-Br nanosheets

Supplementary Figure 1. A typical Raman spectrum of β12-Br nanosheets.

The XRD pattern of β12-Br nanosheets is presented in Supplementary Fig. 2, demonstrating a nice agreement between the characteristic peaks of the 2D nanosheets and the theoretical XRD peaks obtained from the DFT calculations. Furthermore, the narrower full width at half maximum (FWHM) and sharper diffraction peaks observed in the β12-Br nanosheets reveal their high-quality crystallinity.

Supplementary Figure 2. XRD pattern of β12-Br nanosheets.

Supplementary Figure 3. The layer-number and planar size distribution diagram of the as-grown β12-Br nanosheets.

S2. The surface compositions and element distribution of a β12-Br nanosheet

There is an obvious characteristic peak at 197.1 eV in the EELS spectrum (Supplementary Fig. 4) of the as-grown nanosheet, which should originate from the boron K-shell1. Also, the atomic ratio of element B in the nanosheet is over 98 at.%. So, it is suggested that the nanosheet can be indexed as 2D β12-Br with a planar sp2 bonding configuration resemble to graphene2.

Supplementary Figure 4. Representative EELS spectrum of a β12-Br nanosheet.

The XPS spectrum of the β12-Br nanosheets are presented in Supplementary Fig. 5a, in which three characteristic peaks of C 1s, O 1s, and B 1s are clearly found. From the high-resolution XPS spectra of Supplementary Fig. 5b, B 1s peak can be seen to be consisted of both B-O and B-B signal peaks and the molar ratio of B-B is over 90%.

Supplementary Figure 5. XPS spectra of β12-Br nanosheets. a, Full-scale survey spectrum. b, High-magnification XPS spectrum of B 1s.

To confirm the element distribution of the β12-Br nanosheet, EDX mapping technique is performed on the sample. It is clearly seen in Supplementary Fig. 6 that element B uniformly distribute over the nanosheet whereas element O only exists at the margin of the nanosheet. The above results suggest a slight oxidation of boron atoms occurrence at the edge of borophene nanosheets.

Supplementary Figure 6. a, Typical HAADF-STEM image of a β12-Br nanosheet. b, c, The corresponding EDX mapping images of elements boron and oxygen, respectively.

S3. Electrical conductivity measurement of β12-Br nanosheet

Sheet resistance of the β12-Br nanosheet film: By spin-coating technology, we have successfully achieved a uniform coating of β12-Br nanosheets on the interdigital electrodes, which were 4300 μm in width and 6300 μm in length. After that, a 200-nm- thickness β12-Br film was formed on the electrodes. Subsequently, the measurements of the I-V characteristics were conducted on the as-fabricated device. From Supplementary Fig. 7, the average electrical resistance was calculated to be about 82,000 Ω. Moreover, the sheet resistance of β12-Br nanosheet is as low as 5.6 × 104 Ω/sq, which is far smaller than that (109 Ω/sq) of the reported borophene film consisted of β12 and χ3 mixed phases3, fully showcasing their excellent conductivity.

Supplementary Figure 7. Representative I-V curve of β12-Br nanosheet film.

Electrical conductivity of individual β12-Br nanosheet: The electronic transportation properties of individual β12-Br nanosheet were investigated in our home-built in-situ microprobe measurement system. The electrical resistivity of a single β12-Br nanosheet can be obtained to be about 2.6 × 10–5 Ω∙m in Supplementary Fig. 8. The average electrical conductivity of the β12-Br nanosheet is about 3.8 × 104 S/m, which is two orders of magnitude higher than that of MoS2 (303.03 S/m) and WS2 (416.67 S/m)4 and close to that of graphene (~106 S/m)5, revealing their ultrahigh metallic conductivity.

Supplementary Figure 8. Typical I–V curve of a single β12–Br nanosheet.

S4. Measurement of the THz shielding performances of the composite film

Supplementary Figure 9 gives the THz-TDS spectra of the β12-Br/PDMS composite films with different weight fractions (wt.%) and film thicknesses. From Supplementary Fig. 9a, it can be observed that a 2-mm-thickness boron/PDMS composite film with 1.09 wt.% bulk boron powders only reduces the absolute THz voltage from 22.9 to 13.8 mV in comparison with a pure PDMS film with the same thickness. But when adding 0.13 wt.% β12-Br nanosheets into PDMS gel, the absolute THz voltage of the 2-mm-thickness composite film significantly decreases from 22.9 to 4.7 mV, unveiling that the β12-Br nanosheets exhibit more excellent performances in THz shielding than bare bulk boron powders.

Supplementary Figure 9. The THz-TDS spectra of the composite films with different weight fractions of boron fillers (a) and various film thicknesses (b).

Furthermore, as found in Supplementary Fig. 9a, the absolute THz voltage of β12-Br/PDMS composite film will decrease with increasing the weight fraction of β12-Br nanosheets when the thickness of composite film is kept at 2 mm. For instance, at weight fractions of 0.13, 0.41, 0.55, 1.09, and 2.10 wt.% respectively, the corresponding absolute THz voltages are about 4.7, 3.8, 2.9, 2.1 and 0.7 mV, suggesting that higher concentrations of β12-Br nanosheets will provide more effective shielding against THz waves.

Additionally, the effect of the composite film’s thickness on its THz shielding behaviors should not be ignored. TDS spectra for β12-Br/PDMS composite films with different thicknesses are shown in Supplementary Fig. 9b, where the weight fraction of β12-Br nanosheets remains at 0.50 wt.%. When reducing the thickness of the composite film from 4 to 0.20 mm, the absolute THz voltage is seen remarkably increase from 0.70 to 118 mV, revealing that the composite film’s thickness is a crucial factor for its THz shielding performance.

The absorptivity of the 1-mm-thickness β12-Br/PDMS composite film with a 0.5 wt.% β12-Br nanosheet is demonstrated in Supplementary Fig. 10, revealing its exceptional absorption ability across an ultrawide frequency range from 0.1 to 8 THz.

Supplementary Figure 10. The EMI SE curve of 1-mm-thickness 0.5 wt.% β12-Br/PDMS composite film in an ultrawide frequency range of 0.1 – 8 THz.

Supplementary Fig. 11 displays the curves of the EMI reflection effectiveness (SER), transmission effectiveness (SET) and absorption effectiveness (SEA) of a 2-mm-thickness β12-Br/PDMS composite film with 0.41 wt.% β12-Br nanosheet versus the irradiation wavelength ranging from 0.1 to 1.5 THz, respectively. The composite film is found to have a mean SER of about 5 dB and an average SET value of about 65 dB. Based on the equation of SEA = SET - SER, the average SEA of the composite film is calculated to be around 60 dB.

Supplementary Figure 11. The curves of transmission, reflection, and absorption shielding efficiencies of 0.41 wt.% β12-Br/PDMS composite film with a 2 mm thickness versus THz frequency, respectively.

S5. The complex conductivity and complex permittivity of β12-Br nanosheets

The relationship between the real and imaginary parts of the complex electrical conductivity of β12-Br nanosheet at different relaxation times (τ) and carrier densities (n) is presented in Supplementary Fig. 12, in which the measurement frequency ranges from 0.1 to 10 THz. In Supplementary Fig. 12a,b, τ ranges from 20 to 180 fs and n = 3 × 1019 m–2. With the increase of THz frequency, the real part of conductivity exhibits a decreasing trend whereas the imaginary part initially increases and then gradually decreases. The similar change tendency can be found in Supplementary Fig.12c,d, where n varies from 1 × 1019 to 6 × 1019 m−2 and τ = 100 fs. Furthermore, through comparative analysis, slight differences are observed between x and y directions for both real and imaginary parts of complex electrical conductivity due to their weak anisotropic nature6, 7. By modulating the values of τ and n, the real and imaginary parts of the film’s complex permittivity can be obtained in Supplementary Fig.13 by constructing a three-dimensional model of β12-Br nanosheet using FDTD software. One can clearly see that the real part of the complex permittivity occurs to a gradual decrease while the imaginary part exhibits a steady increase. The absolute values of both real and imaginary parts of the complex permittivity can respectively reach as high as 106 and 107, revealing that β12-Br nanosheet should have superior advantages over traditional metal materials for THz shielding8.

Supplementary Figure 12. Real and imaginary parts of the complex electrical conductivity (σx/y(S)) of β12-Br nanosheets. a,b, Frequency dependence of mean free time of electrons along x and y direction, where τ ranges from 20 to 180 fs and n is kept at 3 × 1019 m–2. c,d, Frequency dependence of complex conductivity along x and y direction, where n varies from 1 × 1019 to 6 × 1019 m−2 and τ remains at 100 fs.

Supplementary Figure 13. Real and imaginary parts of the complex permittivity (δx/y) of β12-Br nanosheets. a,b, Frequency dependence of the mean free time of electrons along x and y direction, where τ ranges from 20 to 180 fs and n is kept at 3 × 1019 m–2. c,d, Frequency dependence of the permittivity along x and y direction, where n ranges from 1 × 1019 to 6 × 1019 m−2 and τ remains at 100 fs.

S6. Theoretical simulation to obtain the optimal structure parameters of β12-Br nanosheets with the most excellent THz absorption behaviors

By tailoring the morphology and thickness of the β12-Br nanosheets, we endeavor to obtain the best THz absorption behaviors, as shown in Supplementary Fig. 14. Supplementary Fig. 14a gives the THz absorption spectra of circular, triangular, and square β12-Br nanosheets with the same thickness and surface area, respectively. The characteristic absorption peaks are observed to respectively locate at 1.86 THz, 1.75 THz and 1.82 THz for circular, square and triangular β12-Br nanosheets. Because the strongest absorption peak is situated at around 1 THz, the morphology of β12-Br nanosheets adopts the square shape with the closest absorption peak. Subsequently, The THz absorption spectra of square β12-Br nanosheets with various thicknesses are presented in Supplementary Fig. 14b, in which the thickness of β12-Br nanosheets is found to have a weak impact on their THz absorption behaviors. Considering there exists some limitations of simulation time and hardware conditions, monolayer (ML) β12-Br nanosheets were chosen for the following calculations.

Supplementary Figure 15. Optimized simulation of the absorptivity spectra by modifying the topography of ML β12-Br nanosheets. a, The absorptivity spectra of triangular, square and circular ML β12-Br nanosheets with the same surface area of 3.6 × 105 μm2. b, The absorptivity spectra of square β12-Br nanosheets with a thickness of 0.3, 400, 500, 600 and 700 nm, respectively. c, The absorptivity spectra of β12-Br/PDMS composite film and pure β12-Br nanosheets with the same planar size and thickness, respectively.

The comparison of THz absorption spectra between β12-Br/PDMS composite film and suspended β12-Br nanosheets in a vacuum chamber is demonstrated in Supplementary Fig.14c, where the β12-Br nanosheets uniformly dispersing in PDMS gel have a permittivity of 2.35(1+0.03i)4. It is obviously seen that the THz absorption spectra of β12-Br nanosheets exhibit a distinctive overlap with those of β12-Br/PDMS composite film. Based on the above results, both the morphology and thickness of ML β12-Br nanosheets only have little effect on their THz absorption behaviors. Therefore, it is reasonable that their effect can be negligible in their EMI SE experiments.

S7. The comparable table of 2D nanomaterials used for THz shielding

Table S1. Comparison of THz EMI SE performances for various 2D materials.

| Materials | Weight fraction (wt.%) |  | Thickness (mm) | Frequency range (THz) | EMI SE (dB) | EMI EESt (dB∙cm3/g) | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| MXene film |  | – | 0.0005 | 0.25–2.00 | 30 | – | 9 |
| MWCNTs film |  | – | ~0.02 | 0.40–2.20 | 30 | – | 10 |
| α-Br/PDMS |  | ~33.33 | 5 | 0.10–2.70 | ~42 | 0.125 | 11 |
| MXene/PAA/ACC |  | 8.5 | 0.13 | 0.20–2.00 | 45.3 | – | 12 |
| α-Br tablet |  | – | 1 | 0.10–2.70 | 50 | – | 11 |
| Graphene/Cu |  | – | 0.00016 | 0.10–1.00 | 60.95 | – | 13 |
| MXene film |  | – | 0.025 | 0.30–0.70 | 70 | – | 14 |
| rGO paper |  | – | ~0.37 | 0.10–1.00 | 72.1 | – | 15 |
| OLC/PMMA |  | 2 | 0.12 | 0.1–3 | 4 | 3.4 | 16 |
| SWCNT film on PET film |  | – | 0.00000005 | 0.1–1.2 | 4 | 3.6 | 17 |
| SWCNTs/PVA |  | 1.6 | 0.3 | 0.3–2.1 | 29 | 15.7 | 18 |
| MWCNTs/PMMA |  | ~2 | ~0.48 | 0.10–4.00 | 20 | 16.9 | 19 |
| CNF/PTFE/PVDF/PMMA |  | ~10 | ~0.05 | 0.57–0.63 | 32 | 27.1 | 20 |
| Graphene/PDMS |  | 10 | ~2 | 0.10–0.80 | ~32 | 30 | 21 |
| CNW/PMC |  | 50 | ~0.03 | 0.57–0.63 | ~40 | 36.4 | 22 |
| PAN/PU |  | 10 | 0.15 | 0.2–1.2 | 42 | 38.2 | 23 |
| Graphite/PMMA |  | 35.7 | 0.30 | 0.20–0.90 | ~50 | 42.4 | 24 |
| Kapton-derived carbon |  | – | 0.125 | 0.22–0.5 | ~70 | 54.5 | 25 |
| Zn2+/MXene/GO foams |  | – | 0.085 | 0.20–2.00 | ~51 | 451 | 26 |
| GO/Fe3O4 |  | 500 | 10 | 0.10–2.50 | – | 16000 | 27 |
| Graphene-1500/MWCNT |  | – | 3 | 0.10–1.60 | 40 | 21000 | 28 |
| MXene/GO foams |  | 20 | 4 | 0.20–2.00 | – | 46000 | 29 |
| Graphene foams-1500 |  | – | 3 | 0.10–1.60 | 50 | 110000 | 28 |
| Graphene/PMMA |  | – | 0.034 | 0.1–1.00 | 60 | 300000 | 30 |
| 3D graphene |  | – | – | 0.1–3 | 35 | 30000 | 31 |
| Graphene/TiCN @ Polyimide/MXene |  | – | 0.016 | 0.5–1.5 | 45 | 900 | 32 |
| Fe3O4/graphene |  | 27.3 | 10 | 0.1–2.5 | 42 | 16000 | 27 |
| Fe3O4/Polymer/CNFs |  | 40 | 0.54 | 0.1–1.2 | ~60 | – | 33 |
| MXene/CNT Janus |  | – | 0.00005 | 0.3–1.6 | 60 | 230756 | 34 |
| MXene/PGPDMS |  | 83.3 | 0.12 | 0.5–3 | 57.5 | 24000 | 35 |
| Aramid/MXene Janus |  | 80 | 0.9 | 0.2–2.4 | 60.49 | – | 36 |
| Polymer/Cellulose |  | 50 | 6.9 | 0.2–1.2 | ~58 | 66493.99 | 37 |
| 3D MXene/PI |  | 80 | 0.11 | 0.6–1.1 | 70.4 | – | 38 |
| CNFs/Polyme |  | 50 | ~0.6 | 0.1–1.2 | 43.9 | – | 39 |
| Graphene/Fe3GeTe2/FeTe2/Fe3Ge |  | – | 2.5 | 0.5–1.6 | 76 | – | 40 |
| Graphene-220/700 |  | 5 | 2 | 0.2–1.2 | 56.6 | – | 41 |
| PA/TS@IL-Ag-rGO |  | 3 | – | 0.2–2 | 36 | – | 42 |
| PUS-Ni/MXene |  | ~53 | 8 | 0.15–2.15 | 69.8 | 65.8 | 43 |
| MXene/PPy |  | 91 | 0.04 | 0.2–1.6 | 71.4 | 36983 | 44 |
| MXene/Graphene |  | 75 | 0.048 | 0.1–1 | 60 | – | 45 |
| CNF/SBC |  | 20 | 3 | 0.4–2 | 70 | – | 46 |
| OCF/GO |  | 100 | 4.34 | 0.3–1.5 | 34 | – | 47 |
| Mxene-PMMA /rGO-PVP |  | 16.7 | 0.148 | 0.37–2 | 57.7 | – | 48 |
| MS-Ni/CNT |  | 51.6 | 8 | 0.1–2.2 | 79.1 | 66.3 | 49 |
| β12-Br/PDMS |  | 0.13 | 2 | 0.10–2.00 | 68 | 480000 | This work |
|  |  | 0.50 | 4 |  | 83 | 250000 |  |

Note: MXene (Ti3C2Tx), GO (graphene oxide), PAA (﻿poly (acrylic acid)), ACC (﻿amorphous calcium carbonate), CNF (﻿carbon nano fiber), PTFE (﻿polytetrafluoroethylene), PVDF (﻿poly (vinylidene fluoride)), PMMA (poly (methyl methacrylate)), CNW (﻿carbon nano whiskers), PMC (﻿fluor acrylic copolymer), EBA (﻿ethylene co-butyl acrylate), MWCNTs (multiwalled carbon nanotubes), PVA (﻿polyvinyl alcohol), PDMS (﻿polydimethylsiloxane), OLC (onion-like carbon), PAN (polyaniline), PU (polyurethane), SBC (sustainable biocarbon), OCF (oxidized carbon fiber), MS (melamine sponge).

Table S2. Tensile properties of different 2D material-based composite film for THz shielding.

| Composite film | Tensile Stress (Pa) | Strain (%) | Ref. |
| --- | --- | --- | --- |
| MXene/PAA/ACC hydrogel | 20k | 1500 | 12 |
| MXene/PVA hydrogel | 100k | 50 | 50 |
| Graphene/PMMA | ~48M | ~8 | 30 |
| GO/PMMA | ~26M | ~2.2 | 51 |
| β12-Br/PDMS | ~32M | ~158 | This work |

References

1.	Stephan O., et al. Doping graphitic and carbon nanotube structures with boron and nitrogen. Science 266, 1683-1685 (1994).

2.	Nishino H., et al. Formation and characterization of hydrogen boride sheets derived from MgB2 by cation exchange. J. Am. Chem. Soc. 139, 13761-13769 (2017).

3.	Ranjan P., et al. Freestanding borophene and its hybrids. Adv. Mater. 31, 1900353 (2019).

4.	Wang Y., et al. Van der Waals contacts between three-dimensional metals and two-dimensional semiconductors. Nature 568, 70-74 (2019).

5.	Novoselov K. S., et al. Electric field effect in atomically thin carbon films. Science 306, 666-669 (2004).

6.	Huang Y., Shirodkar S. N., Yakobson B. I. Two-dimensional boron polymorphs for visible range plasmonics: a first-principles exploration. J. Am. Chem. Soc. 139, 17181-17185 (2017).

7.	Mannix A. J., Zhang Z., Guisinger N. P., Yakobson B. I., Hersam M. C. Borophene as a prototype for synthetic 2D materials development. Nat. Nanotechnol. 13, 444-450 (2018).

8.	Liu M., et al. Multi-controlled broadband terahertz absorber engineered with VO2-integrated borophene metamaterials. Opt. Mater. Express 11, 2627 (2021).

9.	Choi G., et al. Enhanced terahertz shielding of MXenes with nano-metamaterials. Adv. Opt. Mater. 6, 1701076 (2018).

10.	Polley D., Neeraj K., Barman A., Mitra R. K. Diameter-dependent shielding effectiveness and terahertz conductivity of multiwalled carbon nanotubes. J. Opt. Soc. Am. B 33, 2430-2436 (2016).

11.	Zhang Z., et al. Few-layer borophene prepared by mechanical resonance and its application in terahertz shielding. ACS Appl. Mater. Interfaces 12, 19746-19754 (2020).

12.	Zhu Y., et al. Multifunctional Ti3C2Tx MXene composite hydrogels with strain sensitivity toward absorption-dominated electromagnetic-interference shielding. ACS Nano 15, 1465-1474 (2021).

13.	Hou S., et al. Excellent terahertz shielding performance of ultrathin flexible Cu/graphene nanolayered composites with high stability. J. Mater. Sci. Technol. 52, 136-144 (2020).

14.	Zou Q., et al. MXene-based ultra-thin film for terahertz radiation shielding. Nanotechnology 31, 505710 (2020).

15.	Dong S., Shi Q., Huang W., Jiang L., Cai Y. Flexible reduced graphene oxide paper with excellent electromagnetic interference shielding for terahertz wave. J. Mater. Sci.: Mater. Electron. 29, 17245-17253 (2018).

16.	Macutkevic J., et al. Terahertz probing of onion-like carbon-PMMA composite films. Diam.  Relat. Mater. 17, 1608-1612 (2008).

17.	Seo M. A., et al. Terahertz electromagnetic interference shielding using single-walled carbon nanotube flexible films. Appl. Phys. Lett. 93, 231905 (2008).

18.	Polley D., Barman A., Mitra R. K. EMI shielding and conductivity of carbon nanotube-polymer composites at terahertz frequency. Opt. Lett. 39, 1541-1544 (2014).

19.	Macutkevic J., et al. Multi-walled carbon nanotubes/PMMA composites for THz applications. Diam. Relat. Mater. 25, 13-18 (2012).

20.	Das A., Megaridis C. M., Liu L., Wang T., Biswas A. Design and synthesis of superhydrophobic carbon nanofiber composite coatings for terahertz frequency shielding and attenuation. Appl. Phys. Lett. 98, 174101 (2011).

21.	Zdrojek M., et al. Graphene-based plastic absorber for total sub-terahertz radiation shielding. Nanoscale 10, 13426-13431 (2018).

22.	Das A., et al. Quasi-optical terahertz polarizers enabled by inkjet printing of carbon nanocomposites. Appl. Phys. Lett. 101, 910 (2012).

23.	Agnandji E. N., Vigneras V., Miane J. L., Mounaix P. Shielding effectiveness in terahertz domain of monolayer-doped polyaniline films. Electron. Lett. 43, 1271-1273 (2007).

24.	Seo M. A., Lee J. W., Kim D. S. Dielectric constant engineering with polymethylmethacrylate-graphite metastate composites in the terahertz region. J. Appl. Phys. 99, 066103 (2006).

25.	Venkatachalam S., Bertin D., Ducournau G., Lampin J. F., Hourlier D. Kapton-derived carbon as efficient terahertz absorbers. Carbon 100, 158-164 (2016).

26.	Lin Z., et al. Highly stable 3D Ti3C2Tx MXene-based foam architectures toward high-performance terahertz radiation shielding. ACS Nano 14, 2109-2117 (2020).

27.	Chen H., et al. Consecutively strong absorption from gigahertz to terahertz bands of a monolithic three-dimensional Fe3O4/graphene material. ACS Appl. Mater. Interfaces 11, 1274-1282 (2019).

28.	Huang Z., et al. Graphene-based composites combining both excellent terahertz shielding and stealth performance. Adv. Opt. Mater. 6, 1801165 (2018).

29.	Ma W., et al. Compressible highly stable 3D porous MXene/GO foam with a tunable high-performance stealth property in the terahertz band. ACS Appl. Mater. Interfaces 11, 25369-25377 (2019).

30.	Pavlou C., et al. Effective EMI shielding behaviour of thin graphene/PMMA nanolaminates in the THz range. Nat. Commun. 12, 4655 (2021).

31.	Kumar P., Šilhavík M., Parida M. R., Kužel P., Červenka J. 3D graphene straintronics for broadband terahertz modulation. Adv. Electron. Mater., 2300853 (2024).

32.	Ji J., Wang Y., Zhao W., Wang G. Laser-induced graphene/TiCN on a polyimide/MXene film as interference shielding materials for terahertz electromagnetic waves. ACS Appl. Nano Mater. 6, 23401-23409 (2023).

33.	Arooj N., et al. Polymeric Fe3O4 nanoparticle/carbon nanofiber hybrid nanocomposite coatings for improved terahertz shielding. ACS Appl. Nano Mater. 6, 5264-5273 (2023).

34.	Hong X., et al. High-permittivity solvents increase MXene stability and stacking order enabling ultraefficient terahertz shielding. Adv. Sci. 11, 2305099 (2024).

35.	Xie Q., et al. Lightweight MXene-based hybrid aerogels with ultrabroadband terahertz absorption and anisotropic strain sensitivity. ACS Appl. Mater. Interfaces 14, 57008-57015 (2022).

36.	Xu J., Fang J., Zuo P., Wang Y., Zhuang Q. Competitively assembled aramid-MXene janus aerogel film exhibiting concurrently robust shielding and effective anti-reflection performance. Adv. Funct. Mater., 2400732 (2024).

37.	Kuang C., et al. Switchable broadband terahertz absorbers based on conducting polymer-cellulose aerogels. Adv. Sci. 11, 2305898 (2024).

38.	Theja V. C. S., et al. 3D architectural MXene-based composite films for stealth terahertz electromagnetic interference shielding performance. Adv. Mater. Interfaces 10, 2300440 (2023).

39.	Arooj N., et al. Optimizing electromagnetic interference shielding of carbon nanofibers reinforced nylon 6, 6 nanocomposite films in terahertz range. J. Appl. Polym. Sci. 140, e53790 (2023).

40.	Li G., et al. Temperature-induced self-decomposition doping of Fe3GeTe2 to achieve ultra-high Tc of 496 K for multispectral compatible strong electromagnetic wave absorption. Adv. Funct. Mater. 33, 2210578 (2023).

41.	Zhou C., et al. Porous graphene produced by carbothermal shock for green electromagnetic interference shielding in both microwave and terahertz bands. Small Methods 7, 2201493 (2023).

42.	Xiang M., et al. Flexible composites by ionic liquid/silver/graphene in towel-gourd sponge fibers: Synergistic effect and dual-band electromagnetic interference shielding in X-band and terahertz-band. J. Appl. Polym. Sci. 139, e52511 (2022).

43.	Bai Y., Qin F., Lu Y. Flexible and lightweight Ni/MXene decorated polyurethane sponge composite with sensitive strain sensing performance for ultrahigh terahertz absorption. Adv. Optical Mater. 10, 2101868 (2022).

44.	Yang S., et al. Ultrathin, flexible, and high-strength polypyrrole/Ti3C2Tx film for wide-band gigahertz and terahertz electromagnetic interference shielding. J. Mater. Chem. A 10, 23570-23579 (2022).

45.	Danish M., et al. Spray deposited graphene@MXene on a flexible polymer substrate for terahertz shielding. Mater. Chem. Phys. 311, 128573 (2024).

46.	Pai A. R., et al. Ultra-broadband shielding of cellulose nanofiber commingled biocarbon functional constructs: A paradigm shift towards sustainable terahertz absorbers. Chem. Eng. J. 467, 143213 (2023).

47.	Cao Y., et al. Multifunctional graphene/carbon fiber aerogels toward compatible electromagnetic wave absorption and shielding in gigahertz and terahertz bands with optimized radar cross section. Carbon 199, 333-346 (2022).

48.	Li S., Xu S., Pan K., Du J., Qiu J. Ultra-thin broadband terahertz absorption and electromagnetic shielding properties of MXene/rGO composite film. Carbon 194, 127-139 (2022).

49.	Bai Y., Qin F., Lu Y. Lightweight Ni/CNT decorated melamine sponge with sensitive strain sensing performance for ultrahigh electromagnetic absorption in both GHz and THz bands. Chem. Eng. J. 429, 132393 (2022).

50.	Yang Y., et al. Biomimetic porous MXene-based hydrogel for high-performance and multifunctional electromagnetic interference shielding. ACS Materials Lett. 4, 2352-2361 (2022).

51.	Tripathi S. N., Saini P., Gupta D., Choudhary V. Electrical and mechanical properties of PMMA/reduced graphene oxide nanocomposites prepared via in situ polymerization. J. Mater. Sci. 48, 6223-6232 (2013).