Table 1. Median (Range) grade of adhesions, fibrosis and giant cell formation on postoperative day 14 in four groups

| Groups (n) | Greca adhesion score | Zühlke adhesion score | Fibrosis score | Giant cell formation |
| --- | --- | --- | --- | --- |
| Sham group (8) | 2 (1-2) * | 2 (0-3) *** | 1 (1-2) | 6 (0-12) |
| Polypropylene group (8) | 4 (3-6) | 3 (2-4) | 2 (1-3) | 1 (1-3) |
| Composite group (8) | 3 (2-6) | 2 (1-4) | 3 (3-3) | 11 (6-20) |
| Platelet rich fibrin group (8) | 3 (2-4) ** | 2 (2-3) | 3 (3-3)§ | 3.5 (2-16) §§ |

*p<0.001 compared to polypropylene and p=0.001 compared to composite group

**p=0.003 compared to polypropylene group

***p=0.004 compared to polypropylene group

§ p<0.001 compared to sham group and p=0.001 compared to polypropylene group

§§ p=0.001 compared to polypropylene group and p=0.007 compared to composite group

Table 2. Comparison of adhesion scores. The highest, lowest, and the IQR values are shown on the box plot. Blue box indicates Greca adhesion score and red box indicates Zühlke adhesion score.

P=0.001

P=0.003

P<0.001

P=0.004

Adhesion score