Supporting Information

Enhanced hydrothermal stability and propylene selectivity by e-beam irradiation-induced hierarchical HZSM-5 additives

Figure S1. Experimental procedure for synthesis of fresh H-ZSM-5 samples with different Si/Al molar ratios

Table S1. Properties of equilibrium catalyst (Ecat)

| Properties | Ecat |
| --- | --- |
| Physical analysis Zeolitic surface area, m2/g Matrix surface area, m2/g Pore volume, cc/g Average pore size, Å Unit cell size, Å Apparent bulk density, g/cc Average particle size (µm) 0-20 µm (wt.%) 0-40 µm (wt.%) 0-80 µm (wt.%) | 62.5 62.4 0.2 88.2 24.3 0.8 72.2 0.6 7.2 67.8 |
| Metals, ppm Ni V Na | 3503 327 0.13 |
| Chemical analysis, wt.% Rare-earth oxides Al2O3 | 1.1 55.3 |

Table S2. Properties of atmospheric residue (AR) feedstock

| Properties | Atmospheric residue (AR) |
| --- | --- |
| Density at 288 K, gm/cc Sulphur, wt.% Carbon residue, wt.% Viscosity at 373 K, cSt | 0.89 0.08 2.9 10.8 |
| ASTM-7169 Distillation, K Initial boiling point 5% 10% 30% 50% 60% | 579 624 646 696 734 759 |
| Metals, ppm Ni V Ca Fe | 8.8 0.4 3.9 10.9 |
| SARA, wt% Saturates Aromatics Asphaltenes Resin | 35.6 58.9 0.2 5.3 |

Table S3. Molar composition of the starting gels and the as-synthesized Na-ZSM-5 zeolites

| # Sample | # Initial gel composition |  |  |  |  | # Product composition* |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | # Molar composition | # Si/Al ratio |  | # Molar composition |  |  | # Si/Al ratio |
| # 20-NaZ | # 1SiO2 : 0.35TPABr : 0.054Na2O : 0.025Al2O3 : 40H2O | # 20.0 |  | # ((C3H7)4N)3.56Na0.99Al4.55Si91.45O192 |  |  | # 20.1 |
| # 30-NaZ | # 1SiO2 : 0.35TPABr : 0.054Na2O : 0.016Al2O3 : 40H2O | # 31.3 |  | # ((C3H7)4N)3.11Na0.14Al3.05Si92.95O192 |  |  | # 30.5 |

*: determined by TG/DSC and ICP/MS

Table S4. Elemental compositions of the fresh H-ZSM-5 and the deactivated H-ZSM-5

| # Sample | # Treatment | # Composition* (wt.%) |  |  |  |  | # Total Si, Al contents (mmol/g) |  | # Bulk Si/Al |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | # SiO2 | # Al2O3 | # Na2O | # H2O |  | # QTSi | # QTAl |  |
| # 20-HZ | # Activated (813K-3h) | # 89.0 | # 3.8 | # 0.07 | # 6.9 |  | # 14.81 | # 0.74 | # 20.0 |
| # 30-HZ |  | # 92.5 | # 2.6 | # 0.09 | # 4.7 |  | # 15.40 | # 0.51 | # 30.2 |
| # 20-HZ-Irra | # Irradiated (10kGy) + Activated (813K-3h) | # 89.9 | # 3.8 | # 0.08 | # 5.3 |  | # 14.96 | # 0.74 | # 20.2 |
| # 30-HZ-Irra |  | # 93.9 | # 2.6 | # 0.06 | # 3.3 |  | # 15.63 | # 0.51 | # 31.3 |
| # 20-HZ-St | # Activated (813K-3h) + Steamed 973K – 4h | # 94.6 | # 3.8 | # 0.09 | # 0.5 |  | # 15.74 | # 0.75 | # 21.0 |
| # 30-HZ-St |  | # 96.7 | # 2.6 | # 0.07 | # 0.5 |  | # 16.09 | # 0.52 | # 30.9 |
| # 20-HZ-Irra-St | # Irradiated (10kGy) + Activated (813K-3h) + Steamed (973K-4h) | # 92.8 | # 3.9 | # 0.09 | # 2.3 |  | # 15.44 | # 0.77 | # 20.1 |
| # 30-HZ-Irra-St |  | # 95.1 | # 2.6 | # 0.09 | # 1.4 |  | # 15.84 | # 0.51 | # 31.1 |

# *: determined by ICP/MS and TG/DSC