Supplementary Information to Towards a business case for CO2 mineralisation in the cement industry

Till Strunge1,2, Phil Renforth1, Mijndert Van der Spek1

1 Research Centre for Carbon Solutions, School of Engineering and Physical Sciences, Heriot-Watt University, Edinburgh EH14 4AS, UK.

2 Institute for Advanced Sustainability Studies e.V., Potsdam, Germany

Content

Supplementary notes	2

Note 1: Market analysis for CO2 mineralisation products	2

Note 2: Scope definition for the assessment	2

Note 3: SCMCCU product specification	2

Note 4: Improved process designs for SCM production	3

Supplementary figures	4

Figure 1: Current demands in Europe and the potential supply from CO2 carbonation	4

Figure 2: Flowsheets of proposed full-scale processes	5

Figure 3: Description of the techno-economic modelling sequence	6

Figure 4: Cost comparison of different process routes and mid scenario	7

Figure 5: Distribution of costs for the mid scenario	8

Figure 6: Material use for the mid scenario	9

Figure 7: Sensitivity analysis with the assumptions of the mid scenario	10

Figure 8: Probability density functions for the input parameters for the MonteCarlo simulations	11

Supplementary tables	12

Table 1: Literature review	12

Table 2: Review of carbonated material use in standardized cement products following EN 197-1	13

Table 3: Equations used for mass balance of feed recycling and separation in direct process.	13

Table 4: Used Equations for Density and viscosity	13

Table 5: Heat capacity calculation for different compounds	14

Table 6: Equations for electricity consumption	14

Table 7:  Used equations for deriving the total direct costs	15

Table 8: Process assumptions	17

Table 9: Major equipment design assumptions	18

Table 10: Assumptions carbon footprint reduction assessment	18

Table 11: Capital Cost factor assumptions	19

Table 12: Operational cost factor assumptions	19

Table 13: Probability density function for Monte Carlo Simulation and Scenario definition	20

References	21

# Supplementary notes

## Note 1: Market analysis for CO2 mineralisation products

The goal of implementing CO2 mineralisation in a cement production facility is to capture most of the plant’s emissions while creating revenue through utilizing mineralisation products.  Numerous small volume applications have been proposed to use carbonates (e.g., carbonates used as polymer additives or aggregate feedstock for land reclamation projects) 1,2. While at first these seem promising, niche markets offer only limited CO2 storage potential1,2 . Furthermore, these markets may not be located close to the cement production facilities3 or have stringent product specifications which can only be achieved at high costs1. Carbonating only the process-inherent emissions of cement would lead to a production of magnesite/calcite and silica 60x and 200x respectively greater than the current European market (Supporting Figure 1). Therefore, targeting niche markets such as selling high purity MgCO3 or CaCO3 and silica will not significantly lower emissions from cement production. Instead, we consider the use of these materials in cement products.

## Note 2: Scope definition for the assessment

A typical  European cement production facility has an annual capacity of 1.4 Mtcement/a emitting 850ktCO2/a4, and will be used as the baseline in this work. We propose retrofitting post-combustion capture onto this facility to obtain a pure CO2 gas with sufficient capacity to meet the demands of a mineralisation system that will be located on the same site. Suitable feedstock minerals  occur in distinct locations in south and northern Europe5-7, we assume a transport of 1200 km via a combination of train, ship and truck, which would allow to transport mineral from a site in Norway (Region of Steinsvik) to northern Germany (Region of Hamburg), where multiple cement plants are located8. On the cement site the carbonation products are used as SCM to create blended cement. The stoichiometry of the carbonation reaction produces inert material (carbonates) with  limited application in cementitious products2. Unused material is stored in the limestone quarry, which are assumed to be located within 10 km of the cement production facility.

## Note 3: SCMCCU product specification

The by-product silica (SiO2) from mineralisation reactions has been described of being of amorphous nature 6,9,10. Amorphous silica is a widely accepted pozzolanic additive in cement production. When added to cement, amorphous silica and calcium hydroxide react to produce additional binding products (e.g. calcium silicate hydrates), leading to a comparable or increased strength to using cement alone 11,12. Experimental work  suggests that  replacing 5-30wt% of cement using SiO2 increases the strength by 5-38wt%, with the strongest effect observed at 10-15wt% replacement11,13-15. Initial applicability studies by Benhelal, et al. 9 showed that a mixture of at least 5wt% carbonated material could be used as an SCM without significant workability (i.e. curing time, water demand) and strength changes of resulting mortars. As such, SCMs  must have high concentrations of small particles of silica as  the major drivers for the pozzolanic effect9,16.Fine particle silica increases the surface area of the cement, resulting in increased water requirements or the need for a superplasticizer to maintain workability11,16. Commonly, replacing cement with silica does not exceed 10wt%17. Some consider 25-35wt% replacement of ordinary Portland cement by carbonated material containing 30-50wt% silica to  be the upper limit 18,19. As cement is highly standardized we additionally reviewed the European standard for cement products EN-19712 showing that all cement types currently allow the usage of up to 5wt% of SCM via CO2 carbonation. Additionally, if carbonated minerals can be classified as natural pozzolanic material they could be used as SCM in certain blends (e.g. Portland pozzolana cement). That would allow displacements of up to 35wt% or 55wt% under current product specifications

## Note 4: Improved process designs for SCM production

Two pathways for mineral carbonation are typically distinguished5: a direct pathway where ground minerals are reacted with CO2 in a pressurized stirred tank using an aqueous slurry with additives such as NaCl and NaHCO3 10,20-23; and an indirect pathway where alkaline earth metal oxides are first extracted and in a later step reacted with CO2 to form carbonates. We selected one direct route and one indirect route to analyse and compare their technical and economic performance. We only selected processes that use natural minerals as feedstock: availability of some industrial wastes 24 might be limited in the future due to more sustainable production processes, and  heavy metal contents of some wastes  might limit their usability 25. Due to the availability of the mg-rich silicates in Europe5-7, we focused our assessment on olivine and serpentine-bearing feedstocks.

We compared multiple reaction conditions for the selection of a direct route which either use serpentine or olivine bearing rocks and differ in pressure, temperature, additive concentration as well as mechanical pre-treatment. Post-combustion CO2 capture (i.e., MEA capture) was used to capture the CO2 from the cement kiln flue gas20,22,26. The minerals are first mined, crushed and grinded. In the case of serpentine, thermal pre-treatment was added to activate the minerals. In a next step the water and the additives sodium bicarbonate (NaHCO3) and sodium chloride (NaCl) are added and the mixture is compressed to the desired reaction pressure (100-150 bar) and heated in a heat exchanger, recovering the heat from the reaction solution leaving the reactor. To create a process that resembles a large scale process as close as possible we implemented heat integration proposed by Ostovari, et al. 2 and developed a separation process based on initial findings from Kremer and Wotruba 27 that allows us to increase the efficiency of using mineral feedstock  and to produce a SCM with alterable silica concentrations. As the reaction of the direct process are not complete, when leaving the reactor, we here propose a post-processing train; first, cyclones are used to partially separate unreacted mineral via gravity separation (<10-75µm, depending on the grinding size)21,22 from the reaction products (3-5µm for magnesite and <1µm for silica)27. Unreacted mineral is cycled back into the process to increase the efficiency of utilizing the mineral feedstock. In a second step a share of the resulting product-rich slurry is fed into a classification centrifuge where magnesite and unreacted mineral are separated from the stream. Afterwards this silica-rich slurry is added to the residual slurry, producing a desired silica content. The SCMCCU is dewatered using solid bowl centrifuges, which have been reported to be suitable for this task28. The SCMCCU is assumed to be used with a residual humidity of 10%. We selected the conditions with the lowest costs (Supplementary Figure 4) leading to a design for a direct carbonation route based on Eikeland, et al. 22 (Olivine, 100bar, 190°C).

As one of the  most eminent indirect routes  we selected a liquid/liquid approach, also referred to as the Nottingham route 2,29. The Nottingham route uses serpentine as a feedstock, which is crushed, grinded and reacted in a three step aqueous process; First, an ammonium bisulphate solution (NH4HSO4aq) is used to extract magnesium oxide and impurities (e.g. iron oxide), leaving silica behind. Second, impurities are precipitated via pH adjustment. Third, the extracted magnesium reacts with ammonium bicarbonate (NH₄HCO₃aq) which acts as CO2 carrier and is recycled in an integrated post-combustion capture process, in which ammonia reacts with the flue gas-inherent CO2 to ammonium bicarbonate. After the separation of the carbonation products, the remainder of the ammonium sulphate–rich solution ((NH4)2SO4), is evaporated leading to a thermal treatment to recover NH3 and NH4HSO430-33. Here, a jacked mechanical scraped-surface crystallizer was selected to evaporate water from the additive (ammonium sulphate) and a indirect rotary drum dryer was selected for the thermal treatment. We selected this route for this study because it is possible to obtain high purity separated products2 so no purification step has to be designed. We implemented heat integration proposed by Ostovari, et al. 2 which also incorporates recompression of steam created during the additive regeneration. To produce the SCMCCU, silica is separated from the slurry after the first reaction and blended with separated carbonates from the third reaction. Solid bowl centrifuges are again used for dewatering. Simplified flowsheets are34 shown in Supplementary Figure 2.

# Supplementary figures

Figure 1: Current demands in Europe and the potential supply from CO2 carbonation

; Left, market sizes for cement, magnesite (MgCO3), calcium carbonate (CaCO3) and silica fume (SiO2)35-39. Right, supply from potential reaction of CO2 with Mg2SiO4; *Stoichiometric reaction yield assumed, only process CO2 emissions (60% of total emissions) taken into amount.

Figure 2: Flowsheets of proposed full-scale processes

. Panel a :direct process based on Eikeland, et al. 22 with heat treatment only being considered when serpentine is used as mineral feedstock. Panel b: indirect process

based on Wang and Maroto-Valer 30 and Ostovari, et al. 2.

Figure 3: Description of the techno-economic modelling sequence

used in this study.

Figure 4: Cost comparison of different process routes and mid scenario

. Process assumptions are shown in Supplementary Table 8. Note all mentioning in the main article of “direct process” refers to “Direct, Olivine, 10µm (X=0.6)” and “indirect process” refers to “Indirect, Serpentine 75µ (X = 0.87)”.

Figure 5: Distribution of costs for the mid scenario

: Panel a: Total capital required; Panel b: distribution of levelised costs of production.

Figure 6: Material use for the mid scenario

. Note, this figure displays the amount of material being used for the production of SCMCCU (In product) and how much material has to be stored (Stored). Inert material consists of unreacted mineral, carbonate and impurities.

Figure 7: Sensitivity analysis with the assumptions of the mid scenario

and changing input parameters: additive recovery (Recycling of Additives & Water), reaction constant (kreaction), reaction pressure (Preaction), reaction temperature (Treaction), reaction yield (Yield), solid-liquid ratio in reactor (XS/L), Number of plants to reach NOAK (No of plants), Learning rate on CAPEX (Learning rate), combined process and project contingencies (Contingencies), interest rate on capital (i), operation hours per year (toperating), electricity price (πelectricity), natural gas price (πnatural gas), mineral price (πmineral), Sodium bicarbonate price (πNaHCO3), Sodium chloride price (πNaCl), monoethanolamine price (πMEA), Ammonium sulphate price (π(NH4)2SO4) , content of SiO2 in product (Silica content in SCMCCU), distance of feedstock minerals (Transport distance), cement price (πcement), ETS price (πETS). Note that only one factor is changed at a time even when related (e.g. an increase in pressure does not change the yield). Hence, for the Monte Carlo Simulations only the reaction constant is used to cover the reaction conditions (see “Sensitive factors to lower costs” in the main article).

Figure 8: Probability density functions for the input parameters for the MonteCarlo simulations

using 10,000 runs: additive recovery (Additive Rec.), reaction constant (kreaction), solid-liquid ratio in reactor (XS/L), Number of plants to reach NOAK (No of plants), Learning rate on CAPEX (Learning rate), combined process and project contingencies (Contingencies), interest rate on capital (i), operation hours per year (toperating), electricity price (πelectricity), natural gas price (πnatural gas), mineral price (πmineral), Sodium bicarbonate price (πNaHCO3), Sodium chloride price (πNaCl), monoethanolamine price (πMEA), Ammonium sulphate price (π(NH4)2SO4).

# Supplementary tables

Table 1: Literature review

of existing economic assessments in the field of CO2 carbonation

| Author | Costs | Unit | Comment | Feedstock |
| --- | --- | --- | --- | --- |
| Sanna, et al. 5 | 44-264* | €/ tCO2, sequestered | / | mg -silicates |
| Hitch and Dipple 40 | 73*+ | €/ tCO2, sequestered | direct | mg -silicates |
| IEA GHG 2000 | 95* | €/ tCO2, avoided | direct | mg-silicate |
| IEA GHG 2000 | >150* | €/ tCO2, avoided | indirect | mg-silicate |
| Naraharisetti, et al. 41 | 410*# | €/ tCO2, avoided | direct | olivine |
| Naraharisetti, et al. 41 | 443*# | €/ tCO2, avoided | direct | olivine |
| W.K. O’Connor and L.R. Penner 21 | 65* | €/ tCO2, avoided | direct | olivine |
| Naraharisetti, et al. 41 | 302*# | €/ tCO2, avoided | direct | serpentine |
| W.K. O’Connor and L.R. Penner 21 | 258* | €/ tCO2, avoided | direct | serpentine |
| Sanna, et al. 1 | 16-75*+ | €/ tCO2, sequestered | post processing only | serpentine |
| Naraharisetti, et al. 41 | 349*# | €/ tCO2, avoided | direct | serpentine |
| Huijgen, et al. 42 | 77 | €/ tCO2, avoided | direct | steel slag |
| Katsuyama, et al. 43 | 128-284* | €/ tCaCO3 | / | waste cement |
| Iizuka, et al. 44 | 25*++ | €/ tCO2, avoided | indirect | waste cement |
| Naraharisetti, et al. 41 | 304*# | €/ tCO2, avoided | direct | wollastonite |
| W.K. O’Connor and L.R. Penner 21 | 93* | €/ tCO2, avoided | direct | wollastonite |
| Huijgen, et al. 42 | 102 | €/ tCO2, avoided | direct | wollastonite |
| Kakizawa et al 2001 | 57*++ | €/ tCO2, avoided | indirect | wollastonite |
| Pérez-Fortes, et al. 45 | M65.5§ | €/ tCO2, sequestered | direct | fly ash |
| Mehleri, et al. 46 | 228 | €/ tCO2, avoided | direct | fly ash |
| Pedraza, et al. 47 | 33-39* | €/ tCO2, sequestered | direct | Cement kiln dust |
| * Currency adapted to € # Cost of CO2 capture included + Only operational expenditures assessed § Only capital expenditures assessed ++ Only operational expenditures in the form of power generation assessed and revenue from CaCO3 included. |  |  |  |  |

Table 2: Review of carbonated material use in standardized cement products following EN 197-1

12.* Carbonated material has to be acknowledged as a natural pozzolan and must exhibit a silica content of at least 25 wt%.

| Description |  | Max SCMCCU allowance in current standard |
| --- | --- | --- |
| CEM I | Portland cement | 5% |
| CEM II | Portland-slag cement | 5% |
|  | Portland-silica fume cement | 5% |
|  | Portland pozzolana cement | 20-35%* |
|  | Portland-fly ash cement | 5% |
|  | Portland burnt shale cement | 5% |
|  | Portland limestone cement | 5% |
|  | Portland composite cement | 20-35%* |
| CEM III | Blast furnace cement | 5% |
| CEM IV | Pozzolanic cement | 35-55%* |
| CEM V | Composite cement | 30-50%* |

Table 3: Equations used for mass balance of feed recycling and separation in direct process.

| Use | Formula |  |
| --- | --- | --- |
| Recycling unreacted mineral, direct aqueous process | mMg2SiO4,theo= mCO2,reactedMCO2*νMg2SiO4νCO2*MMg2SiO4. mMg2SiO4,real=mMg2SiO42,theo*1Yield-mMg2SiO42,theo*1Yield*1-Yield*recovery factor. |  |
| Split of stream for classification centrifuge | z =1-1-xx*y1-y+1-yy-1-xx1+1-yy x = content of SiO2in final product y = content of SiO2in cyclone output z = split of stream fed to classification centrifuge; Eq. 1. |  |

Table 4: Used Equations for Density and viscosity

| Description | Equation | Reference |
| --- | --- | --- |
| Density slurry | ρslurry=100Xsolid, liquidρsolid*1000+100-Xsolid, liquidρH2O*1000 | Shashi 48 |
| Viscosity slurry | υslurry= υH2O*1+2.5*Vfraction+10.06*Vfraction2*0.00273*exp16.6*Vfraction | Shashi 48 |
| Density ABS(aq) | ρABSaq=0.99671 + 0.604706*10-1* cABS - 0.108981*10-2*cABS2+ 0.106394*10-4*cABS3 | Stelson and Seinfeld 49 |
| Density AS(aq) | ρABSaq= 0.0771*cABS0.8463+0.9945 | Adapted from The Engineering ToolBox 50 |
| Density MS(aq) | density = 0.9943 + -0.001323*cwt%, MS+ 0.003697*T | handymath.com 51 |

Table 5: Heat capacity calculation for different compounds

: The integral of the heat capacity is derived using the Shomate equation: T0=25°CTcp dT=a*T-T0+b*T2-T022+c*T3-T033+d*T4-T044-e*T-1-T0-1

| Description | a | b | c | d | e | Reference |
| --- | --- | --- | --- | --- | --- | --- |
| H2O(l) | -203.606 | 1523.29 | -3196.41 | 2474.455 | 3.855326 | Chase 52 |
| Fe2(SO4)3(s) | 85.69794 | 803.9765 | -695.757 | 215.6099 | -0.396145 | Chase 52 |
| CO2(g) | 24.99735 | 55.18696 | -33.6914 | 7.948387 | -0.136638 | Chase 52 |
| NH3(g) | 19.99563 | 49.77119 | -15.376 | 1.921168 | 0.189174 | Chase 52 |
| SiO2 | -6.076591 | 251.6755 | -324.796 | 168.5604 | 0.002548 | Chase 52 |
| Fe(OH)3 (s) | 56.70701 | 132.1357 | -83.5997 | 17.25465 | 0.711267 | Chase 52 |
| MgCO3 (s) | 44.937 | 149.7085 | -74.1827 | 11.9767 | -0.629261 | Chase 52 |
| H2O(g) | 30.092 | 6.832514 | 6.793435 | -2.53448 | 0.082139 | Chase 52 |
| MgO | 47.25995 | 5.681621 | -0.872665 | 0.1043 | -1.053955 | Chase 52 |
| Fe2O3 | 93.43834 | 108.3577 | -50.86447 | 25.58683 | -1.61133 | Chase 52 |
| NH4OH (l) | 9.8 | - | - | - | - | Southard and Green 53 |
| Mg3Si2O5.(OH)4(s) | 1.09 | - | - | - | - | Engineering Toolbox 50 |
| MgSO4 (l) | 111.713 | - | - | - | - | Southard and Green 53 |
| NH4HSO4 (l) | 1.423 | - | - | - | - | National Center for Biotechnology Information 54 |
| (NH4)2SO4 (l) | 1.419 | - | - | - | - | MatWeb 55 |
| NH4HCO3 (l) | 1.119 | - | - | - | - | Rademaekers, et al. 34 |

Table 6: Equations for electricity consumption

| Description | Equation | Reference |
| --- | --- | --- |
| Crushing | wcrushing=2* mmineral | Gerdemann, et al. 20 |
| Grinding | wgrinding,≤75µm=10*KBond*175-1dmineral,feed *mmineral | Schwister and Leven 56 |
|  | wgrinding,75µm to 37µm=70.31*mmineral | Gerdemann, et al. 20 |
|  | wgrinding,37µm to 10µm=150*mmineral | Hangx and Spiers 57 |
| Slurry Pumping | wpump= Vslurrytspace*3600*gearth*pumphead*ρslurryηpump1000*toperating | Costa, et al. 58 |
| Slurry stirring | wstirring=Vslurry*G2*toperating*νslurry1000 | Costa, et al. 58 |
| CO2 compression (5 stage) | wcomp=17.501*lnp+12.876*mCO2 | Aspen Plus Simulation |
| Steam compression | wcompression= 52.897*p- 52.668*msteam | Aspen Plus Simulation |
| Solid bowl centrifuge | wcentrifuge=Psolid+ Pwater+ Pempty*ηmotor*toperation Psolid= msolid*2*π*ubowl*rexit,solid 2 Pliquid= msolid*2*π*ubowl*rexit,water 2 Ploss= mshell*fdrag*gearth*2*π*ubowl*rshell | Adapted from Bell 59 |
| Disc centrifuge | wcentrifuge= 1.9339*exp0.0039*diameter | Regression from specification sheets |

Table 7:  Used equations for deriving the total direct costs

, derived from Aspen capital cost estimator.

| Equipment | Limits | Function | Coefficients | R2 |
| --- | --- | --- | --- | --- |
| Centr. Pump | V = 10-150L/s P= 10-150bar | TDC= a+ b*xn+ c*ym+ d*x*y | a = -5.534e+04 b = 3.169e+04 c = 9.356 d = 19.64 m = 2.306 n = 0.409 | 98.81% |
| Ball Mill | Power = 290-21540 kW | TDC= a*xn+b | a = 1.233e+05 b = -9.006e+05 n = 0.4977 | 99.89% |
| Furnace | V = 50-150L/s Duty = 100-1000MW | TDC= a+ b*xn+c*ym | a = 2.37e+05 b = 6686 c = 7.102 m = 1.988 n = 0.5224 | 99.91% |
| Cone Crusher | m = 75-300t/h | TDC= a*xn+b | a = 5040 b = 3.818e+04 n = 0.7435 | 99.83% |
| Agitator | Power = 10-75kW | TDC= a*xn+b | a = 909 b = 1.753e+04 n = 1.084 | 99.84% |
| Reactor | V = 50-200m3 P = 20-140bar | TDC= a+ b*xn+ c*ym+ d*x*y | a = 3.153e+05 b = 0.2124 c = 437.7 d = 90.18 m = 1.347 n = 2.698 | 99.85% |
| Heat exchanger max 10 bar | A = 25-75m2 | TDC= a*xn+b | a = 462 b = 7.943e+04 n = 1 | 90.05% |
|  | A = 100-200m2 | TDC= a*xn+b | a = 169.6 b = 1.261e+05 n = 1 | 99.24% |
|  | A = 225-500m2 | TDC= a*xn+b | a = 164.5 b = 1.577e+05 n = 1 | 98.64% |
|  | A = 550-900m2 | TDC= a*xn+b | a = 114.2 b = 2.074e+05 n = 1 | 98.71% |
|  | A = 950-1200m2 | TDC= a*xn+b | a = 115 b = 2.423e+05 n = 1 | 100.00% |
| Heat- exchanger 10-100 bar | A = 100-200m2 P = 10-100bar | TDC= a+b*xn+c*ym+d*x*y | a = 1.257e+05 b = 4.525 c = 0.02784 d = 1.000 m = 3.284 n = 1.705 | 99.42% |
|  | A = 225-500m2 P = 10-100bar | TDC= a+b*xn+c*ym+d*x*y | a = 1.441e+05 b = 44.82 c = 16.96 d = 1 .000 m = 1.999 n = 1.242 | 97.97% |
|  | A = 600-900m2 P = 10-100bar | TDC= a+b*xn+c*ym+d*x*y | a = 1.915e+05 b = 14.7 c = 23.76 d = 1 .000 m = 2 .000 n = 1.318 | 98.40% |
|  | A = 950-1200m2 P = 10-100bar | TDC= a+b*xn+c*ym+d*x*y | a = 9.173e+07 b = -9.052e+07 c = -2.057e+05 d = 6.274 m = 0.1789 n = 0.0009788 | 98.21% |
| Heat- exchanger 125-150bar | A = 100-200m2 P = 125-150bar | TDC= a+b*xn+c*ym+d*x*y | a = 2.474e+05 b = 14.09 c = 31.46 d = 4.678 m = -19.47 n = -5.865 | 99.03% |
|  | A = 225-500m2 P = 125-150bar | TDC= a+b*xn+c*ym+d*x*y | a = 2.417e+05 b = 999.2 c = 5.187 d = 2.141 m = 2.000 n = 0.8516 | 99.93% |
|  | A = 600-900m2 P = 125-150bar | TDC= a+b*xn+c*ym+d*x*y | a = -1.478e+05 b = 1081 c = 1.899e+05 d = 2.302 m = 0.2334 n = 0.7631 | 95.76% |
|  | A = 950-1200m2 P = 125-150bar | TDC= a+b*xn+c*ym+d*x*y | a = 4.067e+05 b = 308.1 c = 3.595e+04 d = 2.465 m = 0.3395 n = 0.9353 | 99.85% |
| Mechanical scraped-surface crystalliser | l = 8-150m | TDC= a+b*xn | a = 2238 b = 9615 n = 0.8106 | 100.00% |
| Indirect rotary dryer | A = 10-185m2 | TDC= a+b*xn | a = 69.7 b = 6513 n = 0.9392 | 100.00% |
| Hydro-cyclones | d = 100-290mm pcs per manifold = 10-100 | TDC= a+b*xn+c*ym | a = -0.4077 b = 27.36 c = 0.0003486 m = 1.616 n = -0.3809 | 99.80% |
|  | d=300-370mm pcs per manifold = 10-100 | TDC= a+b*xn+c*ym | a = 6.806 b = 1880 c = 0.0001596 m = 1.741 n = -2.428 | 99.72% |
|  | d=375-500mm pcs per manifold = 10-100 | TDC= a+b*xn+c*ym | a = -47.25 b = 77.37 c = 0.001123 m = 1.443 n = -0.06914 | 99.24% |
| Solid bowl centrifuge | d = 450-1250mm l = 750-3000mm | TDC= a+ b*x*y + c*ym | a = 4.192e+04 b = 0.1509 c = 13.29 m = 1.384 | 99.75% |
| Highspeed disc centrifuge | d = 37.5-125cm | TDC= a+b*x | a = 1.848e+05 b = 4.784e+05 | 99.98% |

Table 8: Process assumptions

| Description | Direct, Serpentine 37µm (X= 0.6)11 | Direct, Olivine 37µm (X= 0.3)11 | Direct, Olivine 37µm (X= 0.5)11 | Direct*, Olivine 10 µm (X= 0.6)13 | Direct, Olivine 10 µm (X= 0.8)13 | Indirect30,32,33* |
| --- | --- | --- | --- | --- | --- | --- |
| Yield | 0.6 | 0.3 | 0.5 | 0.6 | 0.8 | Overall: 0.87 Mineral diss.: 0.91 PH-Adjus.: 1.0 Carbonation: 0.95 |
| particle size [µm] | 37 | 37 | 37 | 10 | 10 | 75 |
| P [bar] | 115 | 150 | 150 | 100 | 100 | 1 |
| T [°C] | 155 | 185 | 185 | 190 | 190 | 80 |
| cNaHCO3 [mol/l] | 0.64 | 0.64 | 0.64 | 0.5 | 0.5 | / |
| cNaCl [mol/l] | 1 | 1 | 1 | 0.75 | 0.75 | / |
| c(NH4)2SO4 [mol/l] | / | / | / | / | / | 5.96 |
| Reaction constant | 0.1822** | 0.3022** | 0.3022** | 1.4717** | 1.4717** | Mineral diss.:1.2839** Carbonation: 4.186** |
| * Selected as routes for this study (referred to as “direct process” and “indirect process”). **derived regression of published lab data11130,32,33 |  |  |  |  |  |  |

Table 9: Major equipment design assumptions

| Equipment | Description | Reference |
| --- | --- | --- |
| Reactor | Max size 500 m3 (for p> 50 bar) Max size 1000 m3 (for p < 10 bar) Gas phase in reactor: 0.3 (direct), 0.05(indirect) Joint efficiency 1 Vessel security factor 0.1 | Own estimation, Towler and Sinnott 60 |
| Centrifugal Pump and compressor | Pump efficiency 0.80 Isentropic compressor efficiency 0.85 | Anantharaman, et al. 4 |
| Heat exchanger | Minimal Temp difference 10K Heat transfer coefficient liquid-liquid 675 W/m2K Heat transfer coefficient liquid-gas 40 W/m2K Heat transfer coefficient steam evaporation 1950 W/m2K Heat transfer coefficient indirect dryer 293 W/m2K | Njeng, et al. 61,The Engineering ToolBox 62 |
| Hydro Cyclone | Separation efficiency unreacted mineral 0.6 Max pressure drop 0.3 bar Max number per manifold 100 | Parametric study in Aspen Plus |
| Classification Centrifuge | Separation efficiency Silica 0.85 Purity of Silica stream 0.99 Speed 4000 rpm | Parametric study in Aspen Plus |
| Dewatering Centrifuge | Wall thickness 0.02m Speed 3000 rpm | Own estimation, Parametric study in Aspen Plus |

Table 10: Assumptions carbon footprint reduction assessment

: the assessment was adapted from Ostovari, et al. 2.

| Description | Name of data set | Database | Value |  |
| --- | --- | --- | --- | --- |
| Electricity grid emission | Electricity grid mix [EU-28] | GaBi ts | / |  |
| Natural gas emission | Thermal energy from natural gas [EU-28] | GaBi ts | / |  |
| Transport Train | Rail transport, average train, gross tonne weight 1000t / 726t payload capacity [EU-28] | GaBi ts | / |  |
| Transport Truck | Transport, small truck (up to 14 t total cap., 9.3t payload) [EU-28] | GaBi ts | / |  |
| Water | Process water [EU-28] | GaBi ts | / |  |
| NaHCO3 | Sodium bicarbonate | GaBi ts | / |  |
| NaCl | Sodium chloride (rock salt) [EU-28] | GaBi ts | / |  |
| (NH4)2SO4 | Ammonium sulfate production [RoW] | ecoinvent 3.3 |  | / |
| Construction | / | Ostovari, et al. 2 |  | 0.04 kgCOeq/tCO2stored |
| Mining Mineral | / | Ostovari, et al. 2 |  | 5.23 kWh/t |
| Cement production | / | Voldsund, et al. 63 | 850 kgCO2eq/tclinker |  |

Table 11: Capital Cost factor assumptions

| Description | Value | Basis | Reference |
| --- | --- | --- | --- |
| Indirect costs | 14% | TDC | Anantharaman, et al. 4 |
| Process contingencies | 40% | EPC | EPRI 64, AACE 65 |
| Project contingencies | 30% | EPC | EPRI 64 |
| Owner’s costs | 7% | TPC | Grande, et al. 66 |
| Learning rate | 10.55% | / | Rubin, et al. 67 |
| Number of plants for NOAK | 20 | / | Greig, et al. 68 |
| Lifetime of the plant | 30 years | / | / |

Table 12: Operational cost factor assumptions

| Description | Value | Basis | Reference |
| --- | --- | --- | --- |
| Insurance and local tax | 2% | TPC | Anantharaman, et al. 4 |
| Maintenance | 2.5% | TPC | Anantharaman, et al. 4 |
| Administration and support | 30% | Operating and Maintenance | Anantharaman, et al. 4 |

Table 13: Probability density function for Monte Carlo Simulation and Scenario definition

| Variable | Min | Max | Assumption in mid scenario#’ | Probability density function | Reference |
| --- | --- | --- | --- | --- | --- |
| Recycling of Additives & Water | 0.8 | 0.98 | 0.95 | Uniform | own estimations, Wang and Maroto-Valer 30,Eikeland, et al. 22 |
| Reaction constant§ | 0.5759* 0.6420** | 1.4717* 1.2839** | 1.4717* 1.2839** | Uniform | **Wang and Maroto-Valer 30,*Eikeland, et al. 22 |
| Solid content in Reactor* | 0.125 | 0.3 | 0.125* 0.3** | Uniform | Wang and Maroto-Valer 30,Eikeland, et al. 22 W.K. O’Connor and L.R. Penner 21 |
| Number of plants to reach NOAK | 5 | 30 | 20 | Uniform | own estimations, Greig, et al. 68 |
| Learning rate | 1.1% | 20% | 10.55% | Uniform | Rubin, et al. 67 |
| Process and project contingencies | 30%, 15% | 70%, 30% | 40% 30% | Uniform | EPRI 64, AACE 65 |
| Interest rate on debt | 1.40% | 3.72% | / | / | European Central Bank 69 |
| Return on equity | 5% | 20.20% | / | / | Gurufocus 70 |
| Debt/equity | 31.00% | 73.00% | / | / | Macrotrends 71,72 |
| Overall interest # | 4% | 17 % | 7.69% | Lognormal | / |
| Working hours | 4380 | 8688 | 8000 | Triangular | own estimations, Deolalkar 73 |
| Electricity price (in 2030) | 38 | 200 | 62 | Lognormal | European Commission 74 |
| Natural gas price (in 2030) | 16.18 | 40.94 | 32 | Normal | Duić, et al. 75 |
| Extraction Costs Mineral | 3.52 | 22.95 | 12 | Normal | Brown, et al. 76 , Béarat, et al. 77 Huijgen, et al. 42 et al. |
| Price NaHCO3* | 100* | 400* | 209 | Normal | Comparison of vendor prices78 |
| Price NaCl* | 20* | 300* | 61.6 | Lognormal | Comparison of vendor prices78 |
| Price MEA* | 600* | 2050* | 1320 | Normal | Comparison of vendor prices78 |
| Price (NH4)2SO4** | 90** | 740** | 140 | Lognormal | Comparison of vendor prices78 |
| Cement price§$ | 78 | 172 | 102 | Lognormal | de Vet, et al. 79, Statista 80 |
| ETS price (in 2030)§§ | 32 | 89 | 32 | Triangular | Schjølset 81, Watson 82, Carbon Tracker Initiative 83, Carbon Pulse 84, ArgusMedia 85 |
| * for direct process only ** for indirect process only § Note the reaction constant for the indirect process is taken from the slowest step, the mineral dissolution. # derived from Monte Carlo simulation on interest on debt, ROE and debt/equity ratio §§used for scenario definition. ## when multiple assumptions could be used (>5 references), the median was chosen. |  |  |  |  |  |

# References

1	Sanna, A., Hall, M. R. & Maroto-Valer, M. Post-processing pathways in carbon capture and storage by mineral carbonation (CCSM) towards the introduction of carbon neutral materials. Energy & Environmental Science 5, 7781, doi:10.1039/c2ee03455g (2012).

2	Ostovari, H., Sternberg, A. & Bardow, A. Rock ‘n’ use of CO2: carbon footprint of carbon capture and utilization by mineralization. Sustainable Energy & Fuels, doi:10.1039/D0SE00190B (2020).

3	Mario, M.-A., Vicente, N., José María del, C., José Santos, L.-G. & Esteban, M. D. Review of coastal Land Reclamation situation in the World. Journal of coastal research 75, 667-671, doi:10.2112/SI75-133.1 (2016).

4	Anantharaman, R. et al. CEMCAP Framework for Comparative Techno-economic Analysis of CO2 Capture From Cement Plants-D3. 2. (Zenodo, 2018).

5	Sanna, A., Uibu, M., Caramanna, G., Kuusik, R. & Maroto-Valer, M. M. A review of mineral carbonation technologies to sequester CO2. Chem Soc Rev 43, 8049-8080, doi:10.1039/c4cs00035h (2014).

6	Kremer, D. et al. Geological Mapping and Characterization of Possible Primary Input Materials for the Mineral Sequestration of Carbon Dioxide in Europe. Minerals 9, doi:10.3390/min9080485 (2019).

7	Park, A.-h. A., Kelemen, P., Matter, J. & Gadikota, G.

8	CemNet. The Global Cement Report - Online Database of Cement Plants, <https://www.cemnet.com/global-cement-report/> (2021).

9	Benhelal, E. et al. The utilisation of feed and byproducts of mineral carbonation processes as pozzolanic cement replacements. Journal of Cleaner Production 186, 499-513 (2018).

10	Stopic, S. et al. Synthesis of Nanosilica via Olivine Mineral Carbonation under High Pressure in an Autoclave. Metals 9, 708 (2019).

11	Wong, H. S. & Abdul Razak, H. Efficiency of calcined kaolin and silica fume as cement replacement material for strength performance. Cement and Concrete Research 35, 696-702, doi:https://doi.org/10.1016/j.cemconres.2004.05.051 (2005).

12	European standard.     (British Standards Institute, 2000).

13	Khedr, S. A. & Abou-Zeid, M. N. Characteristics of silica-fume concrete. Journal of Materials in Civil Engineering 6, 357-375 (1994).

14	Bhanja, S. & Sengupta, B. Investigations on the compressive strength of silica fume concrete using statistical methods. Cement and Concrete Research 32, 1391-1394, doi:https://doi.org/10.1016/S0008-8846(02)00787-1 (2002).

15	Hooton, R. D. Influence of Silica Fume Replacement of Cement on Physical Properties and Resistance to Sulfate Attack, Freezing and Thawing, and Alkali-Silica Reactivity. ACI Materials Journal 90, doi:10.14359/4009 (1993).

16	Lothenbach, B., Scrivener, K. & Hooton, R. Supplementary cementitious materials. Cement and concrete research 41, 1244-1256 (2011).

17	Mindess, S. in Developments in the Formulation and Reinforcement of Concrete (Second Edition)   (ed Sidney Mindess)  3-17 (Woodhead Publishing, 2019).

18	Blaum, P.    (ed Till Strunge) (Personal Communication).

19	Strunge, J.    (ed Till Strunge) (Personal Communication).

20	Gerdemann, S. J., O'Connor, W. K., Dahlin, D. C., Penner, L. R. & Rush, H. Ex situ aqueous mineral carbonation. Environmental science & technology 41, 2587-2593 (2007).

21	W.K. O’Connor, D. C. D., G.E. Rush, S.J. Gerdemann, & L.R. Penner, a. D. N. N. Aqueous Mineral Carbonation : Mineral Availability, Pretreatment, Reaction Parametrics, And Process Studies.  (National Energy Technology Laboratory, 2005).

22	Eikeland, E., Blichfeld, A. B., Tyrsted, C., Jensen, A. & Iversen, B. B. Optimized carbonation of magnesium silicate mineral for CO2 storage. ACS applied materials & interfaces 7, 5258-5264 (2015).

23	Huijgen, W. J. J. Carbon dioxide sequestration by mineral carbonation, S.n., (2007).

24	Wörtler, M. et al. Steel’s contribution to a low-carbon Europe 2050: Technical and economic analysis of the sector’s CO2 abatement potential. London: BCG. Retrieved April 20, 2015 (2013).

25	Yu, Q., Nagataki, S., Lin, J., Saeki, T. & Hisada, M. The leachability of heavy metals in hardened fly ash cement and cement-solidified fly ash. Cement and concrete research 35, 1056-1063, doi:10.1016/j.cemconres.2004.03.031 (2005).

26	Nduagu, E., Bergerson, J. & Zevenhoven, R. Life cycle assessment of CO2 sequestration in magnesium silicate rock – A comparative study. Energy Conversion and Management 55, 116-126, doi:10.1016/j.enconman.2011.10.026 (2012).

27	Kremer, D. & Wotruba, H. Separation of Products from Mineral Sequestration of CO2 with Primary and Secondary Raw Materials. Minerals 10, 1098 (2020).

28	Pinkerton, A. P. & Klima, M. S. Evaluation of a solid-bowl centrifuge for ultrafine size separations. Mining, Metallurgy & Exploration 18, 162-166 (2001).

29	Geerlings, H. & Zevenhoven, R. CO2 mineralization-bridge between storage and utilization of CO2. Annu Rev Chem Biomol Eng 4, 103-117, doi:10.1146/annurev-chembioeng-062011-080951 (2013).

30	Wang, X. & Maroto-Valer, M. M. Optimization of carbon dioxide capture and storage with mineralisation using recyclable ammonium salts. Energy 51, 431-438 (2013).

31	Sanna, A., Dri, M. & Maroto-Valer, M. Carbon dioxide capture and storage by pH swing aqueous mineralisation using a mixture of ammonium salts and antigorite source. Fuel 114, 153-161 (2013).

32	Wang, X. & Maroto-Valer, M. M. Dissolution of serpentine using recyclable ammonium salts for CO2 mineral carbonation. Fuel 90, 1229-1237 (2011).

33	Wang, X. & Maroto‐Valer, M. M. Integration of CO2 capture and mineral carbonation by using recyclable ammonium salts. ChemSusChem 4, 1291-1300 (2011).

34	Rademaekers, K. et al. Atmospheric Gas-Aerosol Equilibrium: IV. Thermodynamics of Carbonates. Aerosol Science and Technology 23, 131-154, doi:10.1080/02786829508965300 (1995).

35	European Association of Mining Industries Metal Ores & Industrial Minerals. The European Magnesite/Magnesia Industry: enabler in the transition to a low-carbon economy. (Brussels, 2020).

36	European Cement Association. Key Facts & Figures, <https://cembureau.eu/about-our-industry/key-facts-figures/> (2017).

37	Markets and Markets. Silica Fume Market by Application, by Geography  - Global Analysis and Forecast to 2020. (2015).

38	Industry ARC. Silica Fume Market - Forecast(2021 - 2026), <https://www.industryarc.com/Report/15138/silica-fume-market.html> (2020).

39	Markets and Markets. Calcium Carbonate Market by Type (GCC and PCC), End-Use Industry (Paper, Plastic, Paints & Coatings, Adhesive & Sealants), and Region (APAC, North America, Europe, South America, Middle East & Africa) - Global Forecast to 2024, <https://www.marketsandmarkets.com/Market-Reports/calcium-carbonate-market-86344547.html> (2018).

40	Hitch, M. & Dipple, G. Economic feasibility and sensitivity analysis of integrating industrial-scale mineral carbonation into mining operations. Minerals Engineering 39, 268-275 (2012).

41	Naraharisetti, P. K., Yeo, T. Y. & Bu, J. New classification of CO2 mineralization processes and economic evaluation. Renewable and Sustainable Energy Reviews 99, 220-233 (2019).

42	Huijgen, W. J., Comans, R. N. & Witkamp, G.-J. Cost evaluation of CO2 sequestration by aqueous mineral carbonation. Energy Conversion and Management 48, 1923-1935 (2007).

43	Katsuyama, Y. et al. Development of a process for producing high-purity calcium carbonate (CaCO3) from waste cement using pressurized CO2. Environmental Progress 24, 162-170, doi:10.1002/ep.10080 (2005).

44	Iizuka, A., Fujii, M., Yamasaki, A. & Yanagisawa, Y. Development of a new CO2 sequestration process utilizing the carbonation of waste cement. Industrial & Engineering Chemistry Research 43, 7880-7887 (2004).

45	Pérez-Fortes, M., Bocin-Dumitriu, A. & Tzimas, E. Techno-economic assessment of carbon utilisation potential in Europe. Chemical Engineering Transactions (2014).

46	Mehleri, E., Bhave, A., Shah, N., Fennell, P. & MacDowell, N. in Fifth International Conference on Accelerated Carbonation for Environmental and Material Engineering (ACEME 2015), New York.

47	Pedraza, J., Zimmermann, A., Tobon, J., Schomäcker, R. & Rojas, N. On the road to net zero-emission cement: Integrated assessment of mineral carbonation of cement kiln dust. Chemical engineering journal (Lausanne, Switzerland : 1996) 408, doi:10.1016/j.cej.2020.127346 (2021).

48	Shashi, E. Piping calculations manual.  (McGraw-Hill, 2005).

49	Stelson, A. W. & Seinfeld, J. H. Prediction of the density of ammonium bisulfate solutions. The Journal of Physical Chemistry 85, 3730-3733, doi:10.1021/j150624a042 (1981).

50	The Engineering ToolBox. Density of aqueous solutions of some inorganic substances, <https://www.engineeringtoolbox.com/density-aqueous-solution-inorganic-salt-acid-concentration-d_1958.html> (n. d.).

51	handymath.com. The Complete Aqueous Magnesium Sulfate Solutions Density-Concentration Calculator, <https://www.handymath.com/cgi-bin/mgsulftble.cgi?submit=Entry> (n. d.).

52	Chase, M. W. J. NIST-JANAF Themochemical Tables. J. Phys. Chem. Ref. Data, Monograph 9, 1-1951 (1998).

53	Southard, M. Z. & Green, D. W. Perry's chemical engineers' handbook.  (McGraw-Hill, 2018).

54	National Center for Biotechnology Information. PubChem Compound Summary for CID 6097028, Ammonium sulfate., <https://pubchem.ncbi.nlm.nih.gov/compound/Ammonium-sulfate> (2004).

55	MatWeb. Material Property data, <http://www.matweb.com/search/datasheet.aspx?matguid=71feb59d7edd41e798c032c1d63de8dd&ckck=1> (n. d.).

56	Schwister, K. & Leven, V. Verfahrenstechnik für Ingenieure: Ein Lehr-und Übungsbuch (mit umfangreichem Zusatzmaterial).  (Carl Hanser Verlag GmbH Co KG, 2020).

57	Hangx, S. J. & Spiers, C. J. Coastal spreading of olivine to control atmospheric CO2 concentrations: A critical analysis of viability. International Journal of Greenhouse Gas Control 3, 757-767 (2009).

58	Costa, G., Polettini, A., Pomi, R., Stramazzo, A. & Zingaretti, D. Energetic assessment of CO2 sequestration through slurry carbonation of steel slag: a factorial study. Greenhouse Gases: Science and Technology 7, 530-541 (2017).

59	Bell, G. R. A. Analysis and Development of a Decanter Centrifuge

60	Towler, G. & Sinnott, R. Chemical engineering design: principles, practice and economics of plant and process design.  (Elsevier, 2012).

61	Njeng, A. S. B., Vitu, S., Clausse, M., Dirion, J.-L. & Debacq, M. Wall-to-solid heat transfer coefficient in flighted rotary kilns: Experimental determination and modeling. Experimental Thermal and Fluid Science 91, 197-213 (2018).

62	The Engineering ToolBox. Heat Exchanger Heat Transfer Coefficients, <https://www.engineeringtoolbox.com/heat-transfer-coefficients-exchangers-d_450.html> (2003).

63	Voldsund, M. et al. D4. 6: CEMCAP Comparative Techno-Economic Analysis of CO2 Capture in Cement Plants. H2020 Project: CO2 Capture from Cement Production (2018).

64	EPRI. Technical Assessment Guide Volume 1:  Electricity Supply—1993, TR-102276-V1R1. Electric Power Research Institute, Palo Alto, California (1993).

65	AACE. Cost estimate classification system – as applied in engineering, procurement, and construction for the process industries, AACE International Recommended Practice No. 18R-97 (Rev. November 29, 2011).  (2011).

66	Grande, C., Roussanaly, S., Anantharaman, R. & Lindqvist, K. CO2 Capture in Natural Gas Production by Adsorption Processes for CO2 Storage, EOR and EGR. IEAGHG, editor (2016).

67	Rubin, E. S., Azevedo, I. M., Jaramillo, P. & Yeh, S. A review of learning rates for electricity supply technologies. Energy Policy 86, 198-218 (2015).

68	Greig, C., Garnett, A., Oesch, J. & Smart, S. Guidelines for scoping and estimating early mover ccs projects. Univ. Queensl., Brisbane (2014).

69	European Central Bank. Cost of borrowing for corporations - Euro area, <https://sdw.ecb.europa.eu/browseSelection.do?type=series&q=MIR.M.U2.B.L22.A.R.A.2240.EUR.N+MIR.M.U2.B.A2I.AM.R.A.2240.EUR.N&node=SEARCHRESULTS> (2021).

70	Gurufocus. ROE % Sector Distribution, <https://www.gurufocus.com/term/ROE/OTCPK:HDELY/ROE-Percentage/HeidelbergCement%20AG> (2020).

71	Macrotrends. Holcim Debt to Equity Ratio 2010-2020, <https://www.macrotrends.net/stocks/charts/HCMLY/holcim/debt-equity-ratio> (2020).

72	Macrotrends. HeidelbergCement AG Debt to Equity Ratio 2008-2020, <https://www.macrotrends.net/stocks/charts/HDELY/heidelbergcement-ag/debt-equity-ratio> (2020).

73	Deolalkar, S. P. in Designing Green Cement Plants   (ed S. P. Deolalkar)  83-86 (Butterworth-Heinemann, 2016).

74	European Commission. Communication from the commission to the European Parliament, the Council, the European Economic and Social Committee and the Committee of the regions - Energy prices and costs in Europe (COM (2019) 1 final). (Brussels, 2019).

75	Duić, N. et al. Heat Roadmap Europe: EU28 fuel prices for 2015, 2030 and 2050 - Deliverable 6.1: Future fuel price review. (University of Zagreb, Zagreb, 2017).

76	Brown, T. J. et al. Underground mining of aggregates. Main report.  (2010).

77	Béarat, H. et al. Carbon sequestration via aqueous olivine mineral carbonation: role of passivating layer formation. Environmental science & technology 40, 4802-4808 (2006).

78	Alibaba. Product search at Alibaba.com, <https://www.alibaba.com/> (2020).

79	de Vet, J.-M. et al. Competitiveness of the European Cement and Lime Sectors. (2018).

80	Statista. Forecast in percentage change in cement prices worldwide from 2013 to 2016 with a forecast from 2017 to 2020, <https://www.statista.com/statistics/248359/change-in-global-cement-prices/> (2017).

81	Schjølset, S. The MSR: Impact on market balance and prices. (Thomson Reuters,, 2014).

82	Watson, F. Analysts see EU carbon prices at Eur56-Eur89/mt by 2030, <https://www.spglobal.com/platts/en/market-insights/latest-news/coal/120320-analysts-see-eu-carbon-prices-at-eur56-eur89mt-by-2030> (2020).

83	Carbon Tracker Initiative. EU carbon prices could double by 2021 and quadruple by 2030, <https://carbontracker.org/eu-carbon-prices-could-double-by-2021-and-quadruple-by-2030/> (2018).

84	Carbon Pulse. EU carbon prices to double on raised 2030 climate target, over €100 possible from other reforms -analysts, <https://carbon-pulse.com/109931/> (2020).

85	ArgusMedia. EU ETS price €32-65/t under 2030 scenarios, <https://www.argusmedia.com/en/news/2142240-eu-ets-price-3265t-under-2030-scenarios> (2020).