Investigation of influence of physicochemical parameters on the bismuth(III) extraction with N-n-heptylaniline from hydrochloric acid media: separation of bismuth(III) from polymetallic mixtures

Rupali R. Pawara, Vishal J. Suryavanshia,b*, Makrand M. Patila,c, Sushant R. Kadamd, Ajinkya D. Mandakee, Ganesh S. Kambalef Ganpatrao N. Mulika*

aP.G. Department of Chemistry, Balwant College, Vita - 415 311, Maharashtra, India

bGeneral Engineering Department, D. Y. Patil Technical Campus, Talsande-416112,Kolhapur, Maharashtra, India

c Department of Chemistry, Raje Ramrao College Jath – 416404, Maharashtra, India

dDepartment of Chemistry, Deogiri College, Aurangabad-431005, Maharashtra, India

eDepartment of Chemistry,Yashwantrao Mohite College of Arts Science and Commerce, Pune -411038, Maharashtra, India

f Department of Engineering Chemistry, Kolhapur Institute of Technology’s College of Engineering, Kolhapur – 416234, Maharashtra, India

*E-mail address of the corresponding author: ganpatraomulik@rediffmail.com;

vishal.suryavanshi16@rediffmail.com

Table 1. Influence of diluents on bismuth(III) extraction

| Sr. No. | Diluents used | Percentage extraction of Bi(III), (%E) | Distribution ratio, (D) |
| --- | --- | --- | --- |
| 1 | Xylene* | 100.0 | ∞ |
| 2 | Benzene | 100.0 | ∞ |
| 3 | Toluene | 100.0 | ∞ |
| 4 | Carbon-tetrachloride | 100.0 | ∞ |
| 5 | Chloroform | 55.0 | 1.8 |
| 6 | Nitrobenzene | 85.0 | 8.5 |
| 7 | Amyl acetate | 100.0 | ∞ |
| 8 | Methyl isobutyl ketone | 100.0 | ∞ |
| 9 | n-butanol | 14.0 | 0.24 |
| 10 | Diethyl ether | 100.0 | ∞ |

Conditions: Bismuth(III) = 1 mg, N-n-heptylaniline = 4 % in xylene, HCl = 1.5 M, aq: org. = 1.5 : 1, equilibrium time = 2 min, stripping agent = Acetate buffer (pH 4.63)

Table 2.Influence of equilibrium time on bismuth(III) extraction

| Sr. No. | Equilibration time, min. | Percentage extraction, (% E) | Distribution ratio, (D) |
| --- | --- | --- | --- |
| 1 | 0.08 | 90.0 | 13.5 |
| 2 | 0.17 | 92.0 | 17.3 |
| 3 | 0.25 | 95.0 | 28.5 |
| 4 | 0.33 | 100.0 | ∞ |
| 5 | 0.5 | 100.0 | ∞ |
| 6 | 0.75 | 100.0 | ∞ |
| 7 | 1.0 | 100.0 | ∞ |
| 8 | 2.0 | 100.0 | ∞ |
| 9 | 3.0 | 100.0 | ∞ |

Bismuth(III) = 1 mg, N-n-heptylaniline = 4 % in xylene, HCl = 1.5 M, aq: org. = 1.5 : 1, stripping agent = Acetate buffer (pH 4.63)

Table 3.Influence of aqueous to organic volume ratio on extraction of bismuth(III)

| Sr. No. | Aqueous to organic phase ratio | Percentage extraction, (% E) | Distribution ratio, (D) |
| --- | --- | --- | --- |
| 1 | 1:1 | 98.1 | 77.4 |
| 2 | 1.5:1* | 100.0 | ∞ |
| 3 | 2:1 | 100.0 | ∞ |
| 4 | 3:1 | 81.0 | 6.4 |
| 5 | 4:1 | 26.0 | 0.52 |
| 6 | 5:1 | 16.0 | 0.29 |
| 7 | 6:1 | 10.0 | 0.16 |
| 8 | 10:1 | 6.0 | 0.1 |
| 9 | 15:1 | 0.0 | - |

Condition: Bismuth(III) = 1 mg, N-n-heptylaniline = 4 % in xylene, HCl = 1.5 M, equilibrium time = 2 min, stripping agent = Acetate buffer (pH 4.63)

Table 4.Influence of loading capacity of bismuth(III) on 4 %  N-n-heptylaniline

| Sr. No. | Bi(III), (mg) | Percentage extraction, (% E) | Distribution ratio, (D) |
| --- | --- | --- | --- |
| 1 | 0.5 | 100.0 | ∞ |
| 2 | 1.0* | 100.0 | ∞ |
| 3 | 2.0 | 100.0 | ∞ |
| 4 | 3.0 | 100.0 | ∞ |
| 5 | 4.0 | 100.0 | ∞ |
| 6 | 5.0 | 100.0 | ∞ |
| 7 | 6.0 | 94.8 | 27.34 |
| 8 | 7.0 | 81.9 | 6.79 |
| 9 | 8.0 | 76.4 | 4.86 |
| 10 | 9.0 | 64.6 | 2.74 |
| 11 | 10.0 | 50.2 | 1.51 |

Conditions: N-n-heptylaniline = 4 % in xylene, HCl = 1.5 M, aq: org. = 1.5 : 1, equilibrium time = 2 min, stripping agent = Acetate buffer (pH 4.63)

Table 5.Influence of stripping agents

| Sr. No. | Strippant, (M) | H2SO4 |  | HNO3 |  | HClO4 |  | CH3COOH |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | % Ra | Db | % Ra | Db | % Ra | Db | % Ra | Db |
| 1 | 0.1 | 32.0 | 0.71 | 22.0 | 0.42 | 46.0 | 1.28 | 12.0 | 0.20 |
| 2 | 0.3 | 34.0 | 0.77 | 28.0 | 0.58 | 52.0 | 1.63 | 26.0 | 0.53 |
| 3 | 0.5 | 38.0 | 0.91 | 46.0 | 1.28 | 68.0 | 3.19 | 38.0 | 0.92 |
| 4 | 0.7 | 0.0 | - | 58.0 | 2.07 | 76.0 | 4.75 | 42.0 | 1.09 |
| 5 | 0.9 | 0.0 | - | 76.0 | 4.75 | 78.0 | 5.32 | 48.0 | 1.38 |
| 6 | 1.0 | 0.0 | - | 88.0 | 11.0 | 78.0 | 5.32 | 56.0 | 1.91 |
| 7 | 2.0 | 0.0 | - | 86.0 | 9.21 | 72.0 | 3.86 | 60.0 | 2.25 |
| 8 | 3.0 | 0.0 | - | 82.0 | 6.83 | 64.0 | 2.67 | 60.0 | 2.25 |
| 9 | 4.0 | 0.0 | - | 78.0 | 5.32 | 62.0 | 2.45 | 54.0 | 1.76 |
| 10 | 5.0 | 0.0 | - | 72.0 | 3.86 | 54.0 | 1.76 | 52.0 | 1.63 |

Conditions: Bismuth(III) = 1 mg, N-n-heptylaniline = 4 % in xylene, HCl = 1.5 M, aq: org. = 1.5 : 1, equilibrium time = 2 min

% Ra = Percentage recovery		Db = Distribution ratio

Stripping agent						% Recovery

- Acetate buffer (pH 4.63) (2 × 25 mL)				100*

* Recommended for further extraction study

Table 6. Influence of foreign ions on extraction of bismuth(III)

| Foreign ion | Added as | Tolerance limit, (mg) |
| --- | --- | --- |
| Sn(II) | SnCl2.2H2O | 0.5 |
| Sb(III) | Sb2O3 | 1.0 |
| In(III) | InCl3.4H2O | 1.0 |
| Al(III) | AlCl3.6H2O | 2.5 |
| Ni(II) | NiCl2.6H2O | 5 |
| Zn(II) | ZnSO4.7H2O | 5 |
| Cd(II)a | CdCl2 | 5 |
| Mn(II) | MnCl2.6H2O | 5 |
| Cu(II) | CuCl2.5H2O | 5 |
| Pb(II) | Pb(NO3)2 | 5 |
| Co(II)b | CoCl2.6H2O | 5 |
| Fe(III) | FeCl3 | 5 |
| Cr(III) | CrCl3 | 5 |
| Fe(II) | FeSO4 | 5 |
| Ag(I) | AgNO3 | 5 |
| Hg(II) | HgCl2 | 10 |
| Th(IV) | Th(NO3)4.5H2O | 10 |
| Ca(II) | CaCl2.6H2O | 30 |
| Mg(II) | MgSO4.7H2O | 30 |
| Ba(II) | Ba(NO3)2.4H2O | 30 |
| Tartrate | Sodium tartrate | 2.0 |
| Fluoride | Sodium fluoride | 5.0 |
| Malonate | Sodium malonate | 10 |
| Bromide | Potassium bromide | 25 |
| Salicylate | Sodium salicylate | 25 |
| EDTA | EDTA | 50 |
| Oxalate | Oxalic acid | 100 |
| Acetate | Sodium acetate | 100 |
| Ascorbate | Ascorbic acid | 100 |
| Thiosulphate | Sodium thiosulphate | 100 |
| Thiourea | Thiourea | 100 |
| Nitrite | Sodium nitrite | 100 |
| Nitrate | Sodium nitrate | 100 |

a. Masked by 100 mg I-, 		b Masked by 10 mg thiosulphate,

Table 7. Separation of Bismuth(III) from associated metal ions

| Metal ion | Concentration, mg | Average % Recovery* | Reagent | Ref. |
| --- | --- | --- | --- | --- |
| Bi(III) Mg(II) | 1 1 | 98.4 98.2 | EDTA | 44 |
| Bi(III) Pb(II) | 1 1 | 98.6 97.8 | PAR | 50 |
| Bi(III) Cd(II)a | 1 1 | 98.4 97.8 | PAR | 50 |
| Bi(III) Zn(II) | 1 1 | 97.8 98.8 | PAR | 50 |
| Bi(III) Cu(II) | 1 1 | 98.2 98.6 | 4-Chloro PTPT | 51 |
| Bi(III) Co(II) | 1 1 | 98.2 97.8 | 2,4-dinitro APTPT | 52 |
| Bi(III) Ba(II) | 1 1 | 98.4 99.2 | EBT | 45 |
| Bi(III) Ni(II) | 1 1 | 98.4 97.8 | DMG | 54 |
| Bi(III) Mn(II) | 1 1 | 97.6 97.8 | KI | 54 |
| Bi(III) Al(III) | 1 1 | 98.6 97.6 | Eriochrome cyanine R | 54 |
| Bi(III) Sn(IV)b | 1 1 | 98.8 99.2 | Pyrocatechol Violet | 54 |

* Average of six determinations

a masked by 50 mg I-

b masked by 5 mg F-

EBT- Eriochrome Black T, KI- Potassium Iodide, DMG-Dimethylglyoxime, PAR-4-(2′-Pyridylazo) resorcinol, 4-Chloro PTPT- 4-chlorophenyl-4,4,6-trimethyl-1,4-dihydropyrimidine-2-thiol, 2,4-dinitro APTPT- 1-(2’,4’-dinitro aminophenyl)-4,4,6-trimethyl-1,4-dihydropyrimidine-2-thiol

Table 8. Analysis of synthetic mixtures corresponding to the composition of ore samples

| Synthetic mixture composition, (mg) | Bismuth(III) found, (mg) | % Recovery* |
| --- | --- | --- |
| Zn(II), 5; Ni(II), 5; Bi(III), 1.0 | 0.99 | 99.0 |
| Fe(II), 5; Mn(II), 5; Bi(III), 1.0 | 0.98 | 98.0 |
| Fe(III), 5; Pb(II), 5; Bi(III), 1.0 | 0.99 | 99.0 |
| Ba(II), 5; Ca(II), 5; Zn(II), 5; Bi(III), 0.5 | 0.49 | 98.0 |
| Kusachite ore: Cu(II) 1, Bi(III) 1 | 0.99 | 99.0 |
| Pekoite ore: Cu(II) 1, Bi(III) 1, Pb(II) 1 | 0.98 | 98.0 |
| Kitaibelite ore: Bi(III) 1, Pb(II) 1, Ag(I) 1 | 0.99 | 99.0 |

* Average of 4 determinations

Table 9.Analysis of alloys

| Sample alloy composition, (%) | Bismuth(III) present, (mg) | Bismuth (III) found, (mg) | Recovery*, (%) | Relative error, (%) |
| --- | --- | --- | --- | --- |
| Lead-bismuth alloy (Bi 15.4, Pb 84.6) | 1.0 | 0.99 1.00 0.98 | 99.5 | 0.5 |
| Tin-bismuth alloy (Bi 25, Sn 75) | 1.0 | 0.98 0.99 0.99 | 99.5 | 0.5 |
| Bismuth solder alloy (Bi 27.5, Pb 27.5, Sn 45) | 1.0 | 1.00 0.99 0.98 | 99.5 | 0.5 |
| Wood metal alloy (Bi 50, Pb 26.7, Sn 13.3, Cd 10) | 1.0 | 1.00 1.00 0.99 | 100.0 | 0.0 |

* Average of six determinations

Table 10.Analysis of pharmaceutical samples

| Sample | Manufacturer | Composition | Amount of Bismuth certified | Amount of Bismuth found by proposed method * |
| --- | --- | --- | --- | --- |
| Trymo Tablet | ReptakosBreet Ltd.(India) | Colloidal Bismuth subcitrate calculated as Bi2O3 | 120 mg (per tablet) | 119.5 mg (per tablet) |

* Average of six determinations