Supporting Information

Elucidating the Roles of Redox and Structure for Grain Growth in Mn-doped UO2

Murphy et al.

Corresponding authors:

Gabriel L. Murphy (g.murphy@fz-juelich.de)

Supplementary Information Note 1. Synchrotron X-ray Powder Diffraction

Supplementary Figure 1 displays Rietveld refinement profiles for Mn-doped UO2 (0, 500, 1000 and 2000 ppm Mn addition) made against synchrotron X-ray diffraction (S-XRD) data at ambient temperature obtained at BM20 ROBL ESRF. Measured samples are single phase fluorite structures in space group Fm3m.

Supplementary Figure 1. Rietveld fit of the S-XRD data at ambient temperature for UO2 with 0 (a), 500 (b), 1000 (c) and 2000 (d) ppm Mn addition. The black crosses, upper red line, lower red line and vertical black markers respectively represent observed data, calculated profile, difference profile and allowed reflections for UO2 according to the space group Fm3m. Respective wRp/R values are 6.66%/5.23%, 6.53%/5.08%, 5.34%/4.35%, and 8.55%/6.19%, all for λ  =  0.7749 Å.

Supplementary Information Note 2. Single Crystal X-ray Diffraction

Supplementary Table 1 provides the structural solution for the Mn-doped UO2 single crystal (SC1) shown in Figure 1 of the manuscript and measured with SEM-EDS and HERFD-XANES, indicating the occurrence of the Mn doped-UO2 fluorite structure in space group Fm3m. No attempts were made to refine the Mn position. Supplementary Table 2 provides the structural solution for additional Mn-doped UO2 single crystal also extracted and subject to SEM-EDS analysis but not HERFD-XANES measurements.

Supplementary Table 1. Crystallographic data for a Mn doped UO2 single crystal grain (SC1).

| Compound | Mn-doped UO2 |
| --- | --- |
| Formula weight (g mol−1) | 270.03 |
| Crystal system | Cubic |
| Space group | Fm3m |
| a (Å) | 5.4653(2) |
| b (Å) | 5.4653(2) |
| c (Å) | 5.4653(2) |
| α (o) | 90 |
| β (o) | 90 |
| γ (o) | 90 |
| Volume (Å3) | 163.246(18) |
| Z | 4 |
| F(000) | 432.0 |
| dcalcd (g cm−3) | 10.987 |
| GOF | 1.455 |
| Final R1 a [I > 2σ(I)] | 0.0136 |
| Final wR2 b [I > 2σ(I)] | 0.0295 |

a R1 = Fo -Fc/Fo,

b wR2 = {w[(Fo)2 - (Fc)2 ] 2/w [(Fo)2] 2}½

Supplementary Table 2. Crystallographic data for a Mn-doped UO2 single crystal grain (SC2).

| Compound | Mn-doped UO2 |
| --- | --- |
| Formula weight (g mol−1) | 270.03 |
| Crystal system | Cubic |
| Space group | Fm3m |
| a (Å) | 5.4881(3) |
| b (Å) | 5.4881(3) |
| c (Å) | 5.4881(3) |
| α (o) | 90 |
| β (o) | 90 |
| γ (o) | 90 |
| Volume (Å3) | 165.30(3) |
| Z / μ (mm−1) | 4 |
| F(000) | 432 |
| dcalcd (g cm−3) | 10.851 |
| GOF | 1.225 |
| Final R1 a [I > 2σ(I)] | 0.0196 |
| Final wR2 b [I > 2σ(I)] | 0.0416 |

a R1 = Fo -Fc/Fo,

b wR2 = {w[(Fo)2 - (Fc)2 ] 2/w [(Fo)2] 2}½

Supplementary Information Note 3. High Energy Resolution Fluorescence Detection X-ray Absorption Near Edge Structure (HERFD-XANES) Analysis

HERFD-XANES measurements were performed on the Mn K-edge for the Mn-doped UO2 single crystal and powder using the standards metallic Mn (Mn0), Mn+2Cl2·4H2O, Mn+3F3, Mn+2O, Mn+32O3 and Mn+4O2. The results of these are presented in Supplementary Figure 2.

Supplementary Figure 2. Normalised Mn K-edge HERFD XANES spectra for UO2 and Mn-doped UO2 powder with 2000 ppm addition as Mn with Mn standards as listed in the inset. The increased noise in the single crystal grain line spectra is due to its significantly smaller size. Note a.u. denotes arbitrary units.

Supplementary Information Note 4. Extended X-ray Absorption Fine Structure (EXAFS) Analysis

Supplementary Figure 3. k3-weighted Mn K–edge EXAFS spectra (left) and corresponding Fourier transforms (FT) in the spectral range from 2.0 to 8.8 Å-1 (right) of the Mn-doped UO2 powder using two Mn-O shells (bottom) and only one Mn-O shell (top). Phase shifts (Δ) are not corrected in the FTs.

Supplementary Table 3. EXAFS structural parameters for the Mn K-edge spectrum of Mn-doped UO2 bulk material with 2000 ppm doped Mn. The parameters are determined from analysis with (top) and without (bottom) the first Mn-O shell split.

| Path | CN | R/Å | σ2/Å² | dE0/eV |
| --- | --- | --- | --- | --- |
| First shell Mn-O interaction split in two shells |  |  |  |  |
| Mn-O | 3.0(8) | 2.14(2) | 0.009(8) | 8.95(9) |
| Mn-O | 3.0+ | 2.32(3) | 0.009/ | 8.95/ |
| Mn-Mn | 3(1) | 3.100(7) | 0.002(4) | 8.95/ |
| Mn-O | 4(1) | 3.73(6) | 0.008f | 8.95/ |
| Mn-Mn | 5.7(8) | 4.10(1) | 0.008f | 8.95/ |
| Mn-O | 5(3) | 4.97(7) | 0.008f | 8.95/ |
| Mn-Mn | 15(2) | 5.45(1) | 0.008f | 8.95/ |
| Mn-U | 13(4) | 5.70(2) | 0.008f | 8.95/ |
| Mn-U | 12(4) | 6.00(3) | 0.008f | 8.95/ |
| Mn-Mn | 21(4) | 7.05(2) | 0.008f | 8.95/ |
| Mn-U | 18(4) | 7.34(2) | 0.008f | 8.95/ |
| First shell Mn-O interaction not split in two shells |  |  |  |  |
| Mn-O | 6.9(8) | 2.215(9) | 0.023(3) | 8.95(9) |
| Mn-Mn | 2.7(1) | 3.100(7) | 0.002(4) | 8.95/ |
| Mn-O | 4(1) | 3.73(6) | 0.008f | 8.95/ |
| Mn-Mn | 5.6(8) | 4.10(1) | 0.008f | 8.95/ |
| Mn-O | 5(3) | 4.98(7) | 0.008f | 8.95/ |
| Mn-Mn | 15(2) | 5.45(1) | 0.008f | 8.95/ |
| Mn-U | 13(3) | 5.70(2) | 0.008f | 8.95/ |
| Mn-U | 12(4) | 6.00(3) | 0.008f | 8.95/ |
| Mn-Mn | 21(4) | 7.05(2) | 0.008f | 8.95/ |
| Mn-U | 18(4) | 7.35(2) | 0.008f | 8.95/ |

CN - coordination number, R - radial distance, σ2 – squared Debye-Waller factor, dE0 - shift in energy threshold, f  - fixed parameter, / - linked parameter, + - constant sum. Estimated standard deviations of the variable parameter as calculated by EXAFSPAK [1].

Supplementary Information Note 5. References

[1] G.N. George, I.J. Pickering, EXAFSPAK: A Suite Of Computer Programs For Analysis Of X-Ray Absorption Spectra, Stanford Synchrotron Radiation Laboratory, Stanford, CA, USA, 1995.