Supporting Information

Temperature-dependent cytokine neutralization induced by magnetoelectric nanoparticles: an in silico study

Alessandra Marrella1*, Paolo Giannoni2, Martina Lenzuni1, Giulia Suarato1, Serena Fiocchi1, Emma Chiaramello1, Paolo Ravazzani1

1 Cnr-Istituto di Elettronica e di Ingegneria dell’Informazione e delle Telecomunicazioni, Milan, 20133, Italy

2 Department of Experimental Medicine, Biology Section, University of Genoa, Genoa, 16132, Italy

*e-mail: alessandra.marrella@cnr.it

Table S1. MENPs core properties

|  | Symbol | Value | Reference |
| --- | --- | --- | --- |
| Magnetic Saturation [A/m] | MS | 3.69*105 | Chinnasamy et al. 1 |
| Saturation magnetostriction [ppm] | λS | -200 | Betal et al. 2, Zhao et al. 3 |
| Density [kg/m3] | ρ | 5200 | Kurian et al. 4, COMSOL Library |
| Initial magnetic susceptibility | χ0 | 3 | Betal et al. 2, Fiocchi et al. 5 |
| Electrical conductivity [S/m] | σ | 5.2*106 | COMSOL Library |
| Poisson ratio | ν | 0.48 | Zhao et al. 3 |
| Young’s modulus [GPa] | E | 230 | Zhao et al. 3 |
| Relative permeability | μr | 1 | COMSOL Library |
| Thermal conductivity [W/mK] | K | 400 | He et al. 6 |
| Tissue-specific heat capacity [J/(kgK)] | Cp | 2.61 | He et al. 6 |

Table S2. MENPs shell properties (from COMSOL library)

|  | Symbol | Value |
| --- | --- | --- |
| Density [kg/m3] | ρ | 5700 |
| Thermal conductivity [W/mK] | k | 2.4 |
| Tissue-specific heat capacity [J/(kgK)] | Cp | 400 |
| Relative permittivity | {εr11; εr22; εr33} | {1115.1; 1115.1; 1251.3} |
| Electrical conductivity [Sm-1] | σ | 178.5 |
| Elasticity matrix, Voigt notation [GPa] | {cE11; cE12; cE22; cE13; cE23; cE33; cE14; cE24; cE34; cE44; cE15; cE25; cE35; cE45; cE55; cE16; cE26; cE36; cE46; cE56; cE66} | {150.4; 65.6; 150.4;65.; 65.9; 145.5; 0; 0;0;43.9;0; 0; 0; 0;43.9; 0; 0; 0; 0; 0; 42.4} |
| Piezoelectric coupling matrix, Voigt notation [C/m2] | {eES11; eES21; eES31; eES12; eES22; eES32; eES12; eES23; eES33; eES14; eES24; eES34; eES15; eES25; eES35; eES16; eES26; eES36} | {0; 0; -4.32; 0; 0; -4.32; 0; 0; 17.4; 0; 11.4; 0; 11.4; 0; 0; 0; 0; 0} |

References

1.	Chinnasamy, C. N. et al. Synthesis of size-controlled cobalt ferrite particles with high coercivity and squareness ratio. J. Colloid Interface Sci. 263, 80–83 (2003).

2.	Betal, S. et al. Magneto-elasto-electroporation (MEEP): in-vitro visualization and numerical characteristics. Sci Rep 6, (2016).

3.	Zhao, X. et al. Electric-field tuning of magnetic anisotropy in the artificial multiferroic Fe3O4/PMN–PT heterostructure. Mater. Res. Lett. 6, 592–597 (2018).

4.	Kurian, M. et al. Structural, magnetic, and acidic properties of cobalt ferrite nanoparticles synthesised by wet chemical methods. J. Adv. Ceram. 4, 199–205 (2015).

5.	Fiocchi, S. et al. Modeling of core-shell magneto-electric nanoparticles for biomedical applications: Effect of composition, dimension, and magnetic field features on magnetoelectric response. PLOS ONE 17, e0274676 (2022).

6.	He, Y. Heat capacity, thermal conductivity, and thermal expansion of barium titanate-based ceramics. Thermochim. Acta 419, 135–141 (2004).